Supplementary Information

Sustainability Cost of Defect Engineering in Color Centers for Quantum Communications

Sahar Shataa and Julie M. Schoenunga,b,*

a Department of Materials Science & Engineering, Texas A&M University, College Station, TX, USA

b J. Mike Walker ’66 Department of Mechanical Engineering, Texas A&M University, College Station, TX, USA

* Corresponding author email: schoenung@tamu.edu

The supplementary information contains the following sections and inventories:

NITROGEN VACANCY CENTERS IN DIAMOND

Table S1: Fabrication inventory calculations for nitrogen vacancy (NV) centers in diamond chip via ion implantation defect engineering technique.

Table S2: Fabrication inventory calculations for nitrogen vacancy (NV) centers in diamond chip via e-beam irradiation defect engineering technique.

Table S3: Fabrication inventory calculations for nitrogen vacancy (NV) centers in diamond chip via Laser writing defect engineering technique.

Table S4: Fabrication inventory calculations for nitrogen vacancy (NV) centers in diamond chip via heteroepitaxial growth and in-situ doping defect engineering technique.

DIVACANCY CENTERS IN SILICON CARBIDE

Table S5: Fabrication inventory calculations for divacancy (VV) centers in SiC chip via ion implantation defect engineering technique.

Table S6: Fabrication inventory calculations for divacancy (VV) centers in SiC chip via e-beam irradiation defect engineering technique.

Table S7: Fabrication inventory calculations for divacancy (VV) centers in SiC chip via laser writing defect engineering technique.

Table S8: Fabrication inventory calculations for divacancy (VV) centers in SiC chip via heteroepitaxial growth defect engineering technique.

BORON VACANCY CENTERS IN HEXAGONAL BORON NITRIDE

Table S9: Fabrication inventory calculations for boron vacancy (VB) centers in hexagonal boron nitride (h-BN) chip via ion implantation defect engineering technique.

Table S10: Fabrication inventory calculations for boron vacancy (VB) centers in hexagonal boron nitride (h-BN) chip via e-beam irradiation defect engineering technique.

Table S11: Fabrication inventory calculations for boron vacancy (VB) centers in hexagonal boron nitride (h-BN) chip via laser writing defect engineering technique.

Table S12: Fabrication inventory calculations for boron vacancy (VB) centers in hexagonal boron nitride (h-BN) chip via heteroepitaxial growth defect engineering technique.

ALUMINUM VACANCY CENTERS IN GALLIUM NITRIDE

Table S13: Fabrication inventory calculations for aluminum vacancy (VAl centers in GaN chip via ion implantation defect engineering technique.

Table S14: Fabrication inventory calculations for aluminum vacancy (VAl) centers in GaN chip via e-beam irradiation defect engineering technique.

Table S15: Fabrication inventory calculations for aluminum vacancy (VAl) color centers in GaN chip via laser writing defect engineering technique.

Table S16: Fabrication inventory calculations for aluminum vacancy (VAl) centers in GaN chip via heteroepitaxial growth defect engineering technique.

ZINC VACANCY CENTERS IN ZINC OXIDE

Table S17: Fabrication inventory calculations for zinc vacancy (VZn centers in ZnO chip via ion implantation defect engineering technique.

Table S18: Fabrication inventory calculations for zinc vacancy (VZn) centers in ZnO chip via e-beam irradiation defect engineering technique.

Table S19: Fabrication inventory calculations for zinc vacancy (VZn) centers in ZnO chip via laser writing defect engineering technique.

Table S20: Fabrication inventory calculations for zinc vacancy (VZn) centers in ZnO chip via heteroepitaxial growth defect engineering technique.

NITROGEN VACANCY CENTERS IN DIAMOND

Table S1: Fabrication inventory calculations for nitrogen vacancy (NV) centers in diamond chip via ion implantation defect engineering technique.1, 2, 3, 4, 5, 6

| Category | Inventory |  |
| --- | --- | --- |
|  | Description/value | Calculation/estimation |
| Substrate | Diamond | Chip dimensions 10 mm x 10 mm x 0.75 mm |
| Defect engineering | Ion Implantation | Ion source, ion implanter, and accelerator |
| Substrate growth | MPCVD* (150 m/h), 900 oC, 100 Torr, CH4/H2 | Microwave generation = 4 kW x 5 h = 20 kWh Plasma source = 1 kW x 5 h = 5 kWh CVD chamber = 0.5 kW x 5 h = 2.5 kWh Furnace = 2 kW x 5 h = 10 kWh Vacuum pumping = 0.1 kW x 1 h = 0.1 kWh CH4 = 2% (500 sccm x 5 h) = 3 L = 2.15 g H2 = 98% (500 sccm x 5 h) = 147 L = 13.22 g |
| Ion implantation | N+ ions, 1013 ions/cm2 | N2+ = 1013 ions/cm2 x 1 cm2 = 1013 ions 0.5 ng Implanter = 80 kW x 1 h = 80 kWh |
| Post-defect processing | Thermal annealing (1200 oC, Ar) | Furnace = 5 kW x 3 h = 15 kWh Ar = 25 sccm x 3 h = L = 8 g |
|  | Reactive ion etching (Ar/Cl2 plasma) | Ar = 25 sccm x 10 min 0.5 g Cl2 = 25 sccm x 10 min 0.8 g RF source = 200 W x 10 min = 0.033 kWh |
|  | Chemical etching (HNO3/H2SO4 acids) | HNO3 = 100 mL = 141 g H2SO4 = 100 mL = 184 g |
|  | Atomic layer deposition (Al2O3/HfO2 layers) | Al2O3 (5 nm) = 3.97 g/cm3 x 5 x 10-7 cm3 1.985 g HfO2 (5 nm) = 9.68 g/cm3 x 5 x 10-7 cm3 4.84 g Furnace = 2 kW x 5 min = 0.17 kWh |
|  | E-beam evaporation (Ti/Au gates) | Ti (5 nm) 0.0025 mg Au (150 nm) 0.29 mg Furnace = 5 kW x 3.3 h 16.5 kWh. |

* MPCVD = Microwave Plasma Chemical Vapor Deposition

Table S2: Fabrication inventory calculations for nitrogen vacancy (NV) centers in diamond chip via e-beam irradiation defect engineering technique.7, 8, 9, 10, 11

| Category | Inventory |  |
| --- | --- | --- |
|  | Description/value | Calculation/estimation |
| Substrate | Diamond | Chip dimensions 10 mm x 10 mm x 0.75 mm |
| Defect engineering | E-beam irradiation | Electron gun, accelerator, vacuum system |
| Substrate growth | MPCVD* (150 m/h), 900 oC, 100 Torr, CH4/H2 | Microwave generation = 4 kW x 5 h = 20 kWh Plasma source = 1 kW x 5 h = 5 kWh CVD chamber = 0.5 kW x 5 h = 2.5 kWh Furnace = 2 kW x 5 h = 10 kWh Vacuum pumping = 0.1 kW x 1 h = 0.1 kWh CH4 = 2% (500 sccm x 5 h) = 3 L = 2.15 g H2 = 98% (500 sccm x 5 h) = 147 L = 13.22 g |
| E-beam irradiation | Electrons, 1013 e/cm2 | Accelerator = 20 kW x 1 h = 20 kWh |
| Post-defect processing | Thermal annealing (1200 oC, Ar) | Furnace = 5 kW x 3 h = 15 kWh Ar = 25 sccm x 3 h = L = 8 g |
|  | Reactive ion etching (Ar/Cl2 plasma) | Ar = 25 sccm x 10 min 0.5 g Cl2 = 25 sccm x 10 min 0.8 g RF source = 200 W x 10 min = 0.033 kWh |
|  | Chemical etching (HNO3/H2SO4 acids) | HNO3 = 100 mL = 141 g H2SO4 = 100 mL = 184 g |
|  | Atomic layer deposition (Al2O3/HfO2 layers) | Al2O3 (5 nm) = 3.97 g/cm3 x 5 x 10-7 cm3 1.985 g HfO2 (5 nm) = 9.68 g/cm3 x 5 x 10-7 cm3 4.84 g Furnace = 2 kW x 5 min = 0.17 kWh |
|  | E-beam evaporation (Ti/Au gates) | Ti (5 nm) 0.0025 m g Au (150 nm) 0.29 mg Furnace = 5 kW x 3.3 h 16.5 kWh. |

* MPCVD = Microwave Plasma Chemical Vapor Deposition

Table S3: Fabrication inventory calculations for nitrogen vacancy (NV) centers in diamond chip via Laser writing defect engineering technique.12, 13, 14, 15, 16

| Category | Inventory |  |
| --- | --- | --- |
|  | Description/value | Calculation/estimation |
| Substrate | Diamond | Chip dimensions 10 mm x 10 mm x 0.75 mm |
| Defect engineering | Laser writing | Laser source, chillers, chamber |
| Substrate growth | MPCVD* (150 m/h), 900 oC, 100 Torr, CH4/H2 | Microwave generation = 4 kW x 5 h = 20 kWh Plasma source = 1 kW x 5 h = 5 kWh CVD chamber = 0.5 kW x 5 h = 2.5 kWh Furnace = 2 kW x 5 h = 10 kWh Vacuum pumping = 0.1 kW x 1 h = 0.1 kWh CH4 = 2% (500 sccm x 5 h) = 3 L = 2.15 g H2 = 98% (500 sccm x 5 h) = 147 L = 13.22 g |
| Laser writing | Femtosecond laser, 800 nm | Laser source = 4 kW x 1 h = 4 kWh Chillers = 0.2 kW x 1 h = 0.2 kWh Chillers (cooling water) = 6 L |
| Post-defect processing | Thermal annealing (1200 oC, Ar) | Furnace = 5 kW x 3 h = 15 kWh Ar = 25 sccm x 3 h = L = 8 g |
|  | Reactive ion etching (Ar/Cl2 plasma) | Ar = 25 sccm x 10 min 0.5 g Cl2 = 25 sccm x 10 min 0.8 g RF source = 200 W x 10 min = 0.033 kWh |
|  | Chemical etching (HNO3/H2SO4 acids) | HNO3 = 100 mL = 141 g H2SO4 = 100 mL = 184 g |

* MPCVD = Microwave Plasma Chemical Vapor Deposition

Table S4: Fabrication inventory calculations for nitrogen vacancy (NV) centers in diamond chip via heteroepitaxial growth and in-situ doping defect engineering technique.17, 18, 19, 20

| Category | Inventory |  |
| --- | --- | --- |
|  | Description/value | Calculation/estimation |
| Substrate | Diamond | Chip dimensions 10 mm x 10 mm x 0.70 mm Thin film doped diamond 50 m |
| Defect engineering | Heteroepitaxial growth and in-situ doping | MPCVD, in-situ doping of N |
| Substrate growth | MPCVD* (150 m/h), 900 oC, 100 Torr, CH4/H2 | Microwave generation = 4 kW x 4.67 h = 18.68 kWh Plasma source = 1 kW x 4.67 h = 4.67 kWh CVD chamber = 0.5 kW x 4.67 h = 2.34 kWh Furnace = 2 kW x 4.67 h = 9.34 kWh Vacuum pumping = 0.1 kW x 1 h = 0.1 kWh CH4 = 2% (500 sccm x 4.67 h) 2.01 g H2 = 98% (500 sccm x 4.67 h) 12.34 g |
| Heteroepitaxial growth and in-situ doping | MPCVD (5 m/h), 900 oC, 100 Torr, CH4/H2/N2 | Microwave generation = 4 kW x 10 h = 40 kWh Plasma source = 1 kW x 10 h = 10 kWh CVD chamber = 0.5 kW x 10 h = 5 kWh Furnace = 2 kW x 10 h = 20 kWh Vacuum pumping = 0.1 kW x 1 h = 0.1 kWh CH4 = 2% (500 sccm x 10 h) 4.3 g H2 = 98% (500 sccm x 4.67 h) 26.8 g N2 = 5 sccm x 10 h 0.13 g |
| Post-defect processing | Reactive ion etching (Ar/Cl2 plasma) | Ar = 25 sccm x 10 min 0.5 g Cl2 = 25 sccm x 10 min 0.8 g RF source = 200 W x 10 min = 0.033 kWh |
|  | Chemical etching (HNO3/H2SO4 acids) | HNO3 = 100 mL = 141 g H2SO4 = 100 mL = 184 g |
|  | Atomic layer deposition (Al2O3/HfO2 layers) | Al2O3 (5 nm) = 3.97 g/cm3 x 5 x 10-7 cm3 1.985 g HfO2 (5 nm) = 9.68 g/cm3 x 5 x 10-7 cm3 4.84 g Furnace = 2 kW x 5 min = 0.17 kWh |
|  | E-beam evaporation (Ti/Au gates) | Ti (5 nm) 0.0025 mg Au (150 nm) 0.29 mg Furnace = 5 kW x 3.3 h 16.5 kWh. |

* MPCVD = Microwave Plasma Chemical Vapor Deposition

DIVACANCY CENTERS IN SILICON CARBIDE

Table S5: Fabrication inventory calculations for divacancy (VV) centers in SiC chip via ion implantation defect engineering technique.21, 22, 23

| Category | Inventory |  |
| --- | --- | --- |
|  | Description/value | Calculation/estimation |
| Substrate | Silicon carbide (4H-SiC) | Chip dimensions 10 mm x 10 mm x 0.75 mm |
| Defect engineering | Ion Implantation | Ion source, ion implanter, and accelerator |
| Substrate growth | PVT* (37.5 m/h), 2500 oC | Furnace = 10 kW x 20 h = 200 kWh Vacuum pumping = 0.5 kW x 20 h = 10 kWh Ar = 500 sccm x 20 h 1070.4 g SiC (seed) = 0.24 g |
| Ion implantation | He+ ions, 1013 ions/cm2 | He+ = 1013 ions/cm2 x 1 cm2 = 1013 ions 0.07 ng Implanter = 80 kW x 1 h = 80 kWh |
| Post-defect processing | Thermal annealing (1300 oC, Ar) | Furnace = 5 kW x 0.5 h = 2.5 kWh Ar = 100 sccm x 0.5 h 4.8 g |
|  | Reactive ion etching (O2 plasma) | O2 = 25 sccm x 10 min 0.5 g RF source = 200 W x 10 min = 0.033 kWh |
|  | Chemical etching (HF/H2O2 acid) | HF = 50 mL = 57.5 g H2O2 = 50 mL = 15 g |
|  | Atomic layer deposition (Al2O3 layer) | Al2O3 (5 nm) = 3.97 g/cm3 x 5 x 10-7 cm3 1.985 g Furnace = 2 kW x 5 min = 0.17 kWh |
|  | E-beam evaporation (Cr/Au gates) | Cr (5 nm) 0.003 mg Au (150 nm) 0.29 mg Furnace = 5 kW x 3.3 h 16.5 kWh. |

* PVT = Physical Vapor Transport

Table S6: Fabrication inventory calculations for divacancy (VV) centers in SiC chip via e-beam irradiation defect engineering technique.24, 25, 26, 27

| Category | Inventory |  |
| --- | --- | --- |
|  | Description/value | Calculation/estimation |
| Substrate | Silicon carbide (4H-SiC) | Chip dimensions 10 mm x 10 mm x 0.75 mm |
| Defect engineering | E-beam irradiation | Electron gun, accelerator, vacuum system |
| Substrate growth | PVT* (37.5 m/h), 2500 oC | Furnace = 10 kW x 20 h = 200 kWh Vacuum pumping = 0.5 kW x 20 h = 10 kWh Ar = 500 sccm x 20 h 1070.4 g SiC (seed) = 0.24 g |
| E-beam irradiation | Electrons, 1013 e/cm2 | Accelerator = 20 kW x 1 h = 20 kWh |
| Post-defect processing | Thermal annealing (1300 oC, Ar) | Furnace = 5 kW x 0.5 h = 2.5 kWh Ar = 100 sccm x 0.5 h 4.8 g |
|  | Reactive ion etching (O2 plasma) | O2 = 25 sccm x 10 min 0.5 g RF source = 200 W x 10 min = 0.033 kWh |
|  | Chemical etching (HF/H2O2 acid) | HF = 50 mL = 57.5 g H2O2 = 50 mL = 15 g |
|  | Atomic layer deposition (Al2O3 layer) | Al2O3 (5 nm) = 3.97 g/cm3 x 5 x 10-7 cm3 1.985 g Furnace = 2 kW x 5 min = 0.17 kWh |
|  | E-beam evaporation (Cr/Au gates) | Cr (5 nm) 0.003 mg Au (150 nm) 0.29 mg Furnace = 5 kW x 3.3 h 16.5 kWh. |

* PVT = Physical Vapor Transport

Table S7: Fabrication inventory calculations for divacancy (VV) centers in SiC chip via laser writing defect engineering technique.28, 29, 30, 31, 32

| Category | Inventory |  |
| --- | --- | --- |
|  | Description/value | Calculation/estimation |
| Substrate | Silicon carbide (4H-SiC) | Chip dimensions 10 mm x 10 mm x 0.75 mm |
| Defect engineering | Laser writing | Laser source, chillers, chamber |
| Substrate growth | PVT* (37.5 m/h), 2500 oC | Furnace = 10 kW x 20 h = 200 kWh Vacuum pumping = 0.5 kW x 20 h = 10 kWh Ar = 500 sccm x 20 h 1070.4 g SiC (seed) = 0.24 g |
| Laser writing | Femtosecond laser, 1030 nm | Laser source = 5 kW x 1 h = 5 kWh Chillers = 0.2 kW x 1 h = 0.2 kWh Chillers (cooling water) = 6 L |
| Post-defect processing | Thermal annealing (1300 oC, Ar) | Furnace = 5 kW x 0.5 h = 2.5 kWh Ar = 100 sccm x 0.5 h 4.8 g |
|  | Reactive ion etching (O2 plasma) | O2 = 25 sccm x 10 min 0.5 g RF source = 200 W x 10 min = 0.033 kWh |
|  | Chemical etching (HF/H2O2 acid) | HF = 50 mL = 57.5 g H2O2 = 50 mL = 15 g |
|  | Atomic layer deposition (Al2O3 layer) | Al2O3 (5 nm) = 3.97 g/cm3 x 5 x 10-7 cm3 1.985 g Furnace = 2 kW x 5 min = 0.17 kWh |
|  | E-beam evaporation (Cr/Au gates) | Cr (5 nm) 0.003 mg Au (150 nm) 0.29 mg Furnace = 5 kW x 3.3 h 16.5 kWh. |

* PVT = Physical Vapor Transport

Table S8: Fabrication inventory calculations for divacancy (VV) centers in SiC chip via heteroepitaxial growth defect engineering technique.33, 34, 35

| Category | Inventory |  |
| --- | --- | --- |
|  | Description/value | Calculation/estimation |
| Substrate | Silicon carbide (4H-SiC) | Chip dimensions 10 mm x 10 mm x 0.70 mm Thin film 50 m with divacancies |
| Defect engineering | Heteroepitaxial growth | PVT, no in-situ doping |
| Substrate growth | PVT* (37.5 m/h), 2500 oC | Furnace = 10 kW x 18.7 h = 187 kWh Vacuum pumping = 0.5 kW x 18.7 h = 9.35 kWh Ar = 500 sccm x 18.7 h 1001.4 g SiC (seed) = 0.21 g |
| Heteroepitaxial growth | PVT (5 m/h), 2500 oC | Furnace = 10 kW x 10 h = 100 kWh Vacuum pumping = 0.5 kW x 10 h = 5 kWh Ar = 500 sccm x 10 h 267.6 g SiC (seed) = 0.015 g |
| Post-defect processing | Reactive ion etching (O2 plasma) | O2 = 25 sccm x 10 min 0.5 g RF source = 200 W x 10 min = 0.033 kWh |
|  | Chemical etching (HF/H2O2 acid) | HF = 50 mL = 57.5 g H2O2 = 50 mL = 15 g |
|  | Atomic layer deposition (Al2O3 layer) | Al2O3 (5 nm) = 3.97 g/cm3 x 5 x 10-7 cm3 1.985 g Furnace = 2 kW x 5 min = 0.17 kWh |
|  | E-beam evaporation (Cr/Au gates) | Cr (5 nm) 0.003 mg Au (150 nm) 0.29 mg Furnace = 5 kW x 3.3 h 16.5 kWh. |

* PVT = Physical Vapor Transport

BORON VACANCY CENTERS IN HEXAGONAL BORON NITRIDE

Table S9: Fabrication inventory calculations for boron vacancy (VB) centers in hexagonal boron nitride (h-BN) chip via ion implantation defect engineering technique.36, 37, 38, 39

| Category | Inventory |  |
| --- | --- | --- |
|  | Description/value | Calculation/estimation |
| Substrate | Hexagonal boron nitride (h-BN) | Chip dimensions 10 mm x 10 mm x 0.75 mm |
| Defect engineering | Ion Implantation | Ion source, ion implanter, and accelerator |
| Substrate growth | LPCVD* (150 m/h), 1000 oC | Furnace = 2.5 kW x 5 h = 12.5 kWh Vacuum pumping = 0.1 kW x 5 h = 0.5 kWh H2 = 500 sccm x 5 h 13.47 g Ammonia borane (NH3BH3) = 500 sccm x 5 h = 0.81 g |
| Ion implantation | He+ ions, 1013 ions/cm2 | He+ = 1013 ions/cm2 x 1 cm2 = 1013 ions 0.07 ng Implanter = 80 kW x 0.3 h = 24 kWh |
| Post-defect processing | Thermal annealing (1100 oC, N2) | Furnace = 5 kW x 1 h = 5 kWh N2 = 100 sccm x 1 h 7.5 g |
|  | Reactive ion etching (O2 plasma) | O2 = 25 sccm x 10 min 0.36 g RF source = 200 W x 10 min = 0.033 kWh |
|  | Chemical etching (HF acid) | HF = 100 mL = 115 g |
|  | Atomic layer deposition (Al2O3 layer) | Al2O3 (5 nm) = 3.97 g/cm3 x 5 x 10-7 cm3 1.985 g Furnace = 2 kW x 5 min = 0.17 kWh |
|  | Electrostatic gating (graphene gates) | Graphene 0.77 g Acetone = 50 mL = 39.2 g Isopropanol = 50 mL = 39.3 g |

* LPCVD = Low-Pressure Chemical Vapor Deposition

Table S10: Fabrication inventory calculations for boron vacancy (VB) centers in hexagonal boron nitride (h-BN) chip via e-beam irradiation defect engineering technique.38, 40, 41

| Category | Inventory |  |
| --- | --- | --- |
|  | Description/value | Calculation/estimation |
| Substrate | Hexagonal boron nitride (h-BN) | Chip dimensions 10 mm x 10 mm x 0.75 mm |
| Defect engineering | E-beam irradiation | Electron gun, accelerator, vacuum system |
| Substrate growth | LPCVD* (150 m/h), 1000 oC | Furnace = 2.5 kW x 5 h = 12.5 kWh Vacuum pumping = 0.1 kW x 5 h = 0.5 kWh H2 = 500 sccm x 5 h 13.47 g Ammonia borane (NH3BH3) = 500 sccm x 5 h = 0.81 g |
| E-beam irradiation | Electrons, 1013 e/cm2 | Accelerator = 20 kW x 0.5 h = 10 kWh |
| Post-defect processing | Thermal annealing (1100 oC, N2) | Furnace = 5 kW x 1 h = 5 kWh N2 = 100 sccm x 1 h 7.5 g |
|  | Reactive ion etching (O2 plasma) | O2 = 25 sccm x 10 min 0.36 g RF source = 200 W x 10 min = 0.033 kWh |
|  | Chemical etching (HF acid) | HF = 100 mL = 115 g |
|  | Atomic layer deposition (Al2O3 layer) | Al2O3 (5 nm) = 3.97 g/cm3 x 5 x 10-7 cm3 1.985 g Furnace = 2 kW x 5 min = 0.17 kWh |
|  | Electrostatic gating (graphene gates) | Graphene 0.77 g Acetone = 50 mL = 39.2 g Isopropanol = 50 mL = 39.3 g |

* LPCVD = Low-Pressure Chemical Vapor Deposition

Table S11: Fabrication inventory calculations for boron vacancy (VB) centers in hexagonal boron nitride (h-BN) chip via laser writing defect engineering technique.42, 43, 44, 45, 46

| Category | Inventory |  |
| --- | --- | --- |
|  | Description/value | Calculation/estimation |
| Substrate | Hexagonal boron nitride (h-BN) | Chip dimensions 10 mm x 10 mm x 0.75 mm |
| Defect engineering | Laser writing | Laser source, chillers, chamber |
| Substrate growth | LPCVD* (150 m/h), 1000 oC | Furnace = 2.5 kW x 5 h = 12.5 kWh Vacuum pumping = 0.1 kW x 5 h = 0.5 kWh H2 = 500 sccm x 5 h 13.47 g Ammonia borane (NH3BH3) = 500 sccm x 5 h = 0.81 g |
| Laser writing | Femtosecond laser, 515 nm | Laser source = 4 kW x 1 h = 4 kWh Chillers = 0.2 kW x 1 h = 0.2 kWh Chillers (cooling water) = 6 L |

* LPCVD = Low-Pressure Chemical Vapor Deposition

Table S12: Fabrication inventory calculations for boron vacancy (VB) centers in hexagonal boron nitride (h-BN) chip via heteroepitaxial growth defect engineering technique.47, 48

| Category | Inventory |  |
| --- | --- | --- |
|  | Description/value | Calculation/estimation |
| Substrate | Hexagonal boron nitride (h-BN) | Chip dimensions 10 mm x 10 mm x 0.745 mm Thin film 5 m, VB centers |
| Defect engineering | Heteroepitaxial growth | LPCVD, no in-situ doping |
| Substrate growth | LPCVD* (150 m/h), 1000 oC | Furnace = 2.5 kW x 4.97 h = 12.42 kWh Vacuum pumping = 0.1 kW x 4.97 h = 0.5 kWh H2 = 500 sccm x 4.97 h 13.4 g Ammonia borane (NH3BH3) = 500 sccm x 4.97 h = 0.81 g |
| Heteroepitaxial growth | LPCVD (5 m/h), 1000 oC | Furnace = 2.5 kW x 1 h = 2.5 kWh Vacuum pumping = 0.1 kW x 1 h = 0.1 kWh H2 = 500 sccm x 1 h 2.7 g Ammonia borane (NH3BH3) = 500 sccm x 1 h = 0.38 g |
| Post-defect processing | Thermal annealing (1100 oC, N2) | Furnace = 5 kW x 1 h = 5 kWh N2 = 100 sccm x 1 h 7.5 g |
|  | Reactive ion etching (O2 plasma) | O2 = 25 sccm x 10 min 0.36 g RF source = 200 W x 10 min = 0.033 kWh |
|  | Chemical etching (HF acid) | HF = 100 mL = 115 g |
|  | Atomic layer deposition (Al2O3 layer) | Al2O3 (5 nm) = 3.97 g/cm3 x 5 x 10-7 cm3 1.985 g Furnace = 2 kW x 5 min = 0.17 kWh |
|  | Electrostatic gating (graphene gates) | Graphene 0.77 g Acetone = 50 mL = 39.2 g Isopropanol = 50 mL = 39.3 g |

* LPCVD = Low-Pressure Chemical Vapor Deposition

ALUMINUM VACANCY CENTERS IN GALLIUM NITRIDE

Table S13: Fabrication inventory calculations for aluminum vacancy (VAl centers in GaN chip via ion implantation defect engineering technique.49, 50

| Category | Inventory |  |
| --- | --- | --- |
|  | Description/value | Calculation/estimation |
| Substrate | Gallium nitride (GaN) | Chip dimensions 10 mm x 10 mm x 0.75 mm |
| Defect engineering | Ion Implantation | Ion source, ion implanter, and accelerator |
| Substrate growth | MOCVD* (150 m/h), 1050 oC | Furnace = 2.5 kW x 5 h = 12.5 kWh Vacuum pumping = 0.1 kW x 5 h = 0.5 kWh H2 = 500 sccm x 5 h 13.47 g Trimethylgallium (Ga (CH3)3) = 10 sccm x 5 h = 5.43 g Ammonia (NH3) = 5000 sccm x 5 h = 915 g |
| Ion implantation | N+ ions, 1013 ions/cm2 | He+ = 1013 ions/cm2 x 1 cm2 = 1013 ions 0.07 ng Implanter = 80 kW x 0.3 h = 24 kWh |
| Post-defect processing | Thermal annealing (1200 oC, N2) | Furnace = 5 kW x 3 h = 15 kWh N2 = 25 sccm x 3 h 5.6 g |
|  | Reactive ion etching (Cl2 plasma) | Cl2 = 25 sccm x 10 min 0.8 g RF source = 200 W x 10 min = 0.033 kWh |
|  | Chemical etching (HF acid) | HF = 100 mL = 115 g |
|  | Atomic layer deposition (HfO2 /SiNx layers) | HfO2 (5 nm) = 9.68 g/cm3 x 5 x 10-7 cm3 4.84 g SiNx (5 nm) = 3.1 g/cm3 x 5 x 10-7 cm3 1.55 g Furnace = 2 kW x 5 min = 0.17 kWh |

* MOCVD = Metal Organic Chemical Vapor Deposition

Table S14: Fabrication inventory calculations for aluminum vacancy (VAl) centers in GaN chip via e-beam irradiation defect engineering technique.51, 52

| Category | Inventory |  |
| --- | --- | --- |
|  | Description/value | Calculation/estimation |
| Substrate | Gallium nitride (GaN) | Chip dimensions 10 mm x 10 mm x 0.75 mm |
| Defect engineering | E-beam irradiation | Electron gun, accelerator, vacuum system |
| Substrate growth | MOCVD* (150 m/h), 1050 oC | Furnace = 2.5 kW x 5 h = 12.5 kWh Vacuum pumping = 0.1 kW x 5 h = 0.5 kWh H2 = 500 sccm x 5 h 13.47 g Trimethylgallium (Ga (CH3)3) = 10 sccm x 5 h = 5.43 g Ammonia (NH3) = 5000 sccm x 5 h = 915 g |
| E-beam irradiation | Electrons, 1013 e/cm2 | Accelerator = 20 kW x 0.5 h = 10 kWh |
| Post-defect processing | Thermal annealing (1200 oC, N2) | Furnace = 5 kW x 3 h = 15 kWh N2 = 25 sccm x 3 h 5.6 g |
|  | Reactive ion etching (Cl2 plasma) | Cl2 = 25 sccm x 10 min 0.8 g RF source = 200 W x 10 min = 0.033 kWh |
|  | Chemical etching (HF acid) | HF = 100 mL = 115 g |
|  | Atomic layer deposition (HfO2 /SiNx layers) | HfO2 (5 nm) = 9.68 g/cm3 x 5 x 10-7 cm3 4.84 g SiNx (5 nm) = 3.1 g/cm3 x 5 x 10-7 cm3 1.55 g Furnace = 2 kW x 5 min = 0.17 kWh |

* MOCVD = Metal Organic Chemical Vapor Deposition

Table S15: Fabrication inventory calculations for aluminum vacancy (VAl) color centers in GaN chip via laser writing defect engineering technique.32, 53, 54

| Category | Inventory |  |
| --- | --- | --- |
|  | Description/value | Calculation/estimation |
| Substrate | Gallium nitride (GaN) | Chip dimensions 10 mm x 10 mm x 0.75 mm |
| Defect engineering | Laser writing | Laser source, chillers, chamber |
| Substrate growth | MOCVD* (150 m/h), 1050 oC | Furnace = 2.5 kW x 5 h = 12.5 kWh Vacuum pumping = 0.1 kW x 5 h = 0.5 kWh H2 = 500 sccm x 5 h 13.47 g Trimethylgallium (Ga (CH3)3) = 10 sccm x 5 h = 5.43 g Ammonia (NH3) = 5000 sccm x 5 h = 915 g |
| Laser writing | Femtosecond laser, 515 nm | Laser source = 4 kW x 1 h = 4 kWh Chillers = 0.2 kW x 1 h = 0.2 kWh Chillers (cooling water) = 6 L |

* MOCVD = Metal Organic Chemical Vapor Deposition

Table S16: Fabrication inventory calculations for aluminum vacancy (VAl) centers in GaN chip via heteroepitaxial growth defect engineering technique.52, 55, 56

| Category | Inventory |  |
| --- | --- | --- |
|  | Description/value | Calculation/estimation |
| Substrate | Gallium nitride (GaN) | Chip dimensions 10 mm x 10 mm x 0.7 mm Thin film 50 m, VAl centers |
| Defect engineering | Heteroepitaxial growth | MOCVD, no in-situ doping |
| Substrate growth | MOCVD* (150 m/h), 1050 oC | Furnace = 2.5 kW x 4.67 h = 11.68 kWh Vacuum pumping = 0.1 kW x 4.67 h = 0.47 kWh H2 = 500 sccm x 4.67 h 12.57 g Trimethylgallium (Ga (CH3)3) = 10 sccm x 4.67 h = 5.07 g Ammonia (NH3) = 5000 sccm x 4.67 h = 854 g |
| Heteroepitaxial growth | MOCVD (5 m/h), 1050 oC | Furnace = 2.5 kW x 10 h = 25 kWh Vacuum pumping = 0.1 kW x 10 h = 1 kWh H2 = 500 sccm x 10 h 27 g Trimethylgallium (Ga (CH3)3) = 10 sccm x 10 h = 11.4 g Ammonia (NH3) = 5000 sccm x 10 h = 1830 g |
| Post-defect processing | Thermal annealing (1200 oC, N2) | Furnace = 5 kW x 3 h = 15 kWh N2 = 25 sccm x 3 h 5.6 g |
|  | Reactive ion etching (Cl2 plasma) | Cl2 = 25 sccm x 10 min 0.8 g RF source = 200 W x 10 min = 0.033 kWh |
|  | Chemical etching (HF acid) | HF = 100 mL = 115 g |
|  | Atomic layer deposition (HfO2 /SiNx layers) | HfO2 (5 nm) = 9.68 g/cm3 x 5 x 10-7 cm3 4.84 g SiNx (5 nm) = 3.1 g/cm3 x 5 x 10-7 cm3 1.55 g Furnace = 2 kW x 5 min = 0.17 kWh |

* MOCVD = Metal Organic Chemical Vapor Deposition

ZINC VACANCY CENTERS IN ZINC OXIDE

Table S17: Fabrication inventory calculations for zinc vacancy (VZn centers in ZnO chip via ion implantation defect engineering technique.57, 58

| Category | Inventory |  |
| --- | --- | --- |
|  | Description/value | Calculation/estimation |
| Substrate | Zinc oxide (ZnO) | Chip dimensions 10 mm x 10 mm x 0.75 mm |
| Defect engineering | Ion Implantation | Ion source, ion implanter, and accelerator |
| Substrate growth | MOCVD (150 m/h), 600 oC | Furnace = 2.5 kW x 5 h = 12.5 kWh Vacuum pumping = 0.1 kW x 5 h = 0.5 kWh Ar = 500 sccm x 5 h 267 g diethylzinc (C4H10Zn) = 10 sccm x 5 h = 7.2 g O2 = 500 sccm x 5 h = 214 g |
| Ion implantation | He+ ions, 1013 ions/cm2 | He+ = 1013 ions/cm2 x 1 cm2 = 1013 ions 0.07 ng Implanter = 80 kW x 0.3 h = 24 kWh |
| Post-defect processing | Thermal annealing (800 oC, N2) | Furnace = 5 kW x 3 h = 15 kWh N2 = 25 sccm x 3 h 5.6 g |
|  | Chemical etching (HF/HCl acid) | HF = 50 mL = 57.5 g HCl = 50 mL = 59.5 g |
|  | Atomic layer deposition (Al2O3 / ZnO layers) | Al2O3 (5 nm) = 3.97 g/cm3 x 5 x 10-7 cm3 1.985 g ZnO (5 nm) = 5.61 g/cm3 x 5 x 10-7 cm3 2.8 g Furnace = 2 kW x 5 min = 0.17 kWh |

Table S18: Fabrication inventory calculations for zinc vacancy (VZn) centers in ZnO chip via e-beam irradiation defect engineering technique.59, 60, 61

| Category | Inventory |  |
| --- | --- | --- |
|  | Description/value | Calculation/estimation |
| Substrate | Zinc oxide (ZnO) | Chip dimensions 10 mm x 10 mm x 0.75 mm |
| Defect engineering | E-beam irradiation | Electron gun, accelerator, vacuum system |
| Substrate growth | MOCVD (150 m/h), 600 oC | Furnace = 2.5 kW x 5 h = 12.5 kWh Vacuum pumping = 0.1 kW x 5 h = 0.5 kWh Ar = 500 sccm x 5 h 267 g diethylzinc (C4H10Zn) = 10 sccm x 5 h = 7.2 g O2 = 500 sccm x 5 h = 214 g |
| E-beam irradiation | Electrons, 1013 e/cm2 | Accelerator = 20 kW x 0.5 h = 10 kWh |
| Post-defect processing | Thermal annealing (800 oC, N2) | Furnace = 5 kW x 3 h = 15 kWh N2 = 25 sccm x 3 h 5.6 g |
|  | Chemical etching (HF/HCl acid) | HF = 50 mL = 57.5 g HCl = 50 mL = 59.5 g |
|  | Atomic layer deposition (Al2O3 / ZnO layers) | Al2O3 (5 nm) = 3.97 g/cm3 x 5 x 10-7 cm3 1.985 g ZnO (5 nm) = 5.61 g/cm3 x 5 x 10-7 cm3 2.8 g Furnace = 2 kW x 5 min = 0.17 kWh |

Table S19: Fabrication inventory calculations for zinc vacancy (VZn) centers in ZnO chip via laser writing defect engineering technique.62, 63, 64, 65

| Category | Inventory |  |
| --- | --- | --- |
|  | Description/value | Calculation/estimation |
| Substrate | Zinc oxide (ZnO) | Chip dimensions 10 mm x 10 mm x 0.75 mm |
| Defect engineering | Laser writing | Laser source, chillers, chamber |
| Substrate growth | MOCVD (150 m/h), 600 oC | Furnace = 2.5 kW x 5 h = 12.5 kWh Vacuum pumping = 0.1 kW x 5 h = 0.5 kWh Ar = 500 sccm x 5 h 267 g diethylzinc (C4H10Zn) = 10 sccm x 5 h = 7.2 g O2 = 500 sccm x 5 h = 214 g |
| Laser writing | Femtosecond laser, 800 nm | Laser source = 5 kW x 1 h = 5 kWh Chillers = 0.2 kW x 1 h = 0.2 kWh Chillers (cooling water) = 6 L |

Table S20: Fabrication inventory calculations for zinc vacancy (VZn) centers in ZnO chip via heteroepitaxial growth defect engineering technique.66, 67, 68

| Category | Inventory |  |
| --- | --- | --- |
|  | Description/value | Calculation/estimation |
| Substrate | Zinc oxide (ZnO) | Chip dimensions 10 mm x 10 mm x 0.7 mm Thin film 50 m, VZn centers |
| Defect engineering | Heteroepitaxial growth | MOCVD, no in-situ doping |
| Substrate growth | MOCVD (150 m/h), 600 oC | Furnace = 2.5 kW x 4.67 h = 11.68 kWh Vacuum pumping = 0.1 kW x 4.67 h = 0.47 kWh Ar = 500 sccm x 4.67 h 249 g diethylzinc (C4H10Zn) = 10 sccm x 4.67 h = 6.7 g O2 = 500 sccm x 4.67 h = 200 g |
| Heteroepitaxial growth | MOCVD (5 m/h), 600 oC | Furnace = 2.5 kW x 10 h = 25 kWh Vacuum pumping = 0.1 kW x 10 h = 1 kWh Ar = 500 sccm x 10 h 534 g diethylzinc (C4H10Zn) = 10 sccm x 10 h = 14.4 g O2 = 500 sccm x 10 h = 429 g |
| Post-defect processing | Thermal annealing (800 oC, N2) | Furnace = 5 kW x 3 h = 15 kWh N2 = 25 sccm x 3 h 5.6 g |
|  | Chemical etching (HF/HCl acid) | HF = 50 mL = 57.5 g HCl = 50 mL = 59.5 g |
|  | Atomic layer deposition (Al2O3 / ZnO layers) | Al2O3 (5 nm) = 3.97 g/cm3 x 5 x 10-7 cm3 1.985 g ZnO (5 nm) = 5.61 g/cm3 x 5 x 10-7 cm3 2.8 g Furnace = 2 kW x 5 min = 0.17 kWh |

References

1.	Haque A, Sumaiya S. An Overview on the Formation and Processing of Nitrogen-Vacancy Photonic Centers in Diamond by Ion Implantation. Journal of Manufacturing and Materials Processing 1, 6 (2017).

2.	Toyli DM, Weis CD, Fuchs GD, Schenkel T, Awschalom DD. Chip-scale nanofabrication of single spins and spin arrays in diamond. Nano letters 10, 3168-3172 (2010).

3.	Sangtawesin S, Brundage T, Atkins Z, Petta JR. Highly tunable formation of nitrogen-vacancy centers via ion implantation. Applied Physics Letters 105,  (2014).

4.	Naydenov B, et al. Increasing the coherence time of single electron spins in diamond by high temperature annealing. Applied Physics Letters 97,  (2010).

5.	Santori C, Barclay PE, Fu K-MC, Beausoleil RG. Vertical distribution of nitrogen-vacancy centers in diamond formed by ion implantation and annealing. Physical Review B—Condensed Matter and Materials Physics 79, 125313 (2009).

6.	Lang N, et al. Controlled lateral positioning of NV centres in diamond by CVD overgrowth. Physica Scripta 99, 105408 (2024).

7.	Ishii S, Saiki S, Onoda S, Masuyama Y, Abe H, Ohshima T. Ensemble negatively-charged nitrogen-vacancy centers in type-Ib diamond created by high fluence electron beam irradiation. Quantum Beam Science 6, 2 (2021).

8.	Losero E, et al. Creation of NV centers in diamond under 155 MeV electron irradiation. Advanced Physics Research 3, 2300071 (2024).

9.	Schwartz J, Aloni S, Ogletree DF, Schenkel T. Effects of low-energy electron irradiation on formation of nitrogen–vacancy centers in single-crystal diamond. New Journal of Physics 14, 043024 (2012).

10.	McLellan CA, Myers BA, Kraemer S, Ohno K, Awschalom DD, Bleszynski Jayich AC. Patterned formation of highly coherent nitrogen-vacancy centers using a focused electron irradiation technique. Nano letters 16, 2450-2454 (2016).

11.	Solà-Garcia M, Meuret S, Coenen T, Polman A. Electron-induced state conversion in diamond NV centers measured with pump–probe cathodoluminescence spectroscopy. ACS photonics 7, 232-240 (2019).

12.	Chen Y-C, et al. Laser writing of coherent colour centres in diamond. Nature Photonics 11, 77-80 (2017).

13.	Gao S, et al. Laser-induced color centers in crystals. Optics & Laser Technology 146, 107527 (2022).

14.	Addhya A, et al. Photonic-Cavity-Enhanced Laser Writing of Color Centers in Diamond. Nano Letters 24, 11224-11231 (2024).

15.	Szunerits S, Boukherroub R. Different strategies for functionalization of diamond surfaces. Journal of Solid State Electrochemistry 12, 1205-1218 (2008).

16.	Smith JM, Meynell SA, Bleszynski Jayich AC, Meijer J. Colour centre generation in diamond for quantum technologies. Nanophotonics 8, 1889-1906 (2019).

17.	Eichhorn TR, McLellan CA, Bleszynski Jayich AC. Optimizing the formation of depth-confined nitrogen vacancy center spin ensembles in diamond for quantum sensing. Physical Review Materials 3, 113802 (2019).

18.	Bogdanov S, et al. Optical investigation of as-grown NV centers in heavily nitrogen doped delta layers in CVD diamond. Materials Today Communications 24, 101019 (2020).

19.	Weippert J, et al. NV-doped microstructures with preferential orientation by growth on heteroepitaxial diamond. Journal of Applied Physics 133,  (2023).

20.	Schreck M, Gsell S, Brescia R, Fischer M. Ion bombardment induced buried lateral growth: the key mechanism for the synthesis of single crystal diamond wafers. Scientific reports 7, 44462 (2017).

21.	Lin W-X, et al. Room temperature coherent control of a single solid-state spin under anti-Stokes excitation. Physical Review B 108, 235312 (2023).

22.	Lin W-X, et al. Temperature dependence of divacancy spin coherence in implanted silicon carbide. Physical Review B 104, 125305 (2021).

23.	Sun T, et al. Divacancy and silicon vacancy color centers in 4H-SiC fabricated by hydrogen and dual ions implantation and annealing. Ceramics International 49, 7452-7465 (2023).

24.	Son N, Shafizadeh D, Ohshima T, Ivanov I. Modified divacancies in 4H-SiC. Journal of Applied Physics 132,  (2022).

25.	Kimura T, et al. Computationally guided experimental validation of divacancy defect formation in 4H-SiC. Applied Physics Letters 126,  (2025).

26.	Xiong H, et al. Defects evolution in n-type 4H-SiC induced by electron irradiation and annealing. Journal of Semiconductors 45, 072502 (2024).

27.	Son N, et al. Electron-paramagnetic-resonance studies of defects in electron-irradiated p-type 4H and 6H SiC. Physica B: Condensed Matter 273, 655-658 (1999).

28.	Almutairi AFM, Partridge J, Xu C, Cole I, Holland A. Direct writing of divacancy centers in silicon carbide by femtosecond laser irradiation and subsequent thermal annealing. Applied Physics Letters 120,  (2022).

29.	Castelletto S, et al. Photoluminescence in hexagonal silicon carbide by direct femtosecond laser writing. Optics letters 43, 6077-6080 (2018).

30.	Chen Y-C, et al. Laser writing of scalable single color centers in silicon carbide. Nano letters 19, 2377-2383 (2019).

31.	Wang J, et al. Femtosecond laser controllable annealing for color centers based on ion-implanted silicon carbide substrate. Ceramics International 50, 46566-46578 (2024).

32.	Castelletto S, Maksimovic J, Katkus T, Ohshima T, Johnson BC, Juodkazis S. Color centers enabled by direct femto-second laser writing in wide bandgap semiconductors. Nanomaterials 11, 72 (2020).

33.	Zhang S, Fan G, Li T, Zhao L. Optimization of thermal field of 150 mm SiC crystal growth by PVT method. RSC advances 12, 19936-19945 (2022).

34.	Magnusson B, et al. Excitation properties of the divacancy in 4 H-SiC. Physical Review B 98, 195202 (2018).

35.	Ji Y, et al. Optimization of temperature field and crystal growth in the PVT method for high-quality 8-inch silicon carbide single crystal growth. Journal of Crystal Growth 664, 128181 (2025).

36.	Guo N-J, et al. Generation of spin defects by ion implantation in hexagonal boron nitride. ACS omega 7, 1733-1739 (2022).

37.	Zabelotsky T, et al. Creation of boron vacancies in hexagonal boron nitride exfoliated from bulk crystals for quantum sensing. ACS Applied Nano Materials 6, 21671-21678 (2023).

38.	Murzakhanov FF, et al. Creation of negatively charged boron vacancies in hexagonal boron nitride crystal by electron irradiation and mechanism of inhomogeneous broadening of boron vacancy-related spin resonance lines. Nanomaterials 11, 1373 (2021).

39.	Qian P, et al. Investigation of spin defects in hexagonal boron nitride generated via ion implantation. Optics Express 32, 46489-46499 (2024).

40.	Healey AJ, et al. Optimisation of electron irradiation for creating spin ensembles in hexagonal boron nitride. Materials for Quantum Technology 4, 035701 (2024).

41.	Bianco F, Corte E, Ditalia Tchernij S, Forneris J, Fabbri F. Engineering multicolor radiative centers in hBN flakes by varying the electron beam irradiation parameters. Nanomaterials 13, 739 (2023).

42.	Gan L, et al. Large-scale, high-yield laser fabrication of bright and pure single-photon emitters at room temperature in hexagonal boron nitride. ACS nano 16, 14254-14261 (2022).

43.	Vaidya S, Gao X, Dikshit S, Aharonovich I, Li T. Quantum sensing and imaging with spin defects in hexagonal boron nitride. Advances in Physics: X 8, 2206049 (2023).

44.	Hou S, et al. Localized emission from laser-irradiated defects in 2D hexagonal boron nitride. 2D Materials 5, 015010 (2017).

45.	Yang Y-Z, et al. Laser direct writing of visible spin defects in hexagonal boron nitride for applications in spin-based technologies. ACS Applied Nano Materials 6, 6407-6414 (2023).

46.	Gao X, et al. Femtosecond laser writing of spin defects in hexagonal boron nitride. ACS Photonics 8, 994-1000 (2021).

47.	Li Z, et al. Research progress on the epitaxial growth of hexagonal boron nitride on different substrates by the CVD method. Nanoscale Advances 7, 2395-2417 (2025).

48.	Singhal R, Echeverria E, McIlroy DN, Singh RN. Post-growth enhancement of CVD-grown hexagonal boron nitride films on sapphire. Results in Materials 16, 100339 (2022).

49.	Uedono A, et al. Annealing properties of vacancy-type defects in ion-implanted GaN studied by monoenergetic positron beams. Journal of Applied Physics 102,  (2007).

50.	Shi Y-T, et al. Realization of p-type gallium nitride by magnesium ion implantation for vertical power devices. Scientific Reports 9, 8796 (2019).

51.	Saarinen K, Suski T, Grzegory I, Look DC. Ga vacancies in electron irradiated GaN: introduction, stability and temperature dependence of positron trapping. Physica B: Condensed Matter 308-310, 77-80 (2001).

52.	Watkins GD, et al. Intrinsic defects in GaN: what we are learning from magnetic resonance studies. Physica B: Condensed Matter 340-342, 25-31 (2003).

53.	Pearton SJ, Zolper JC, Shul RJ, Ren F. GaN: Processing, defects, and devices. Journal of Applied Physics 86, 1-78 (1999).

54.	Hua R, Xu Z, Tao Z, Dong B, Wang H, Yang L. Fabrication of high-quality surface microtextures on GaN by femtosecond laser direct writing. Nanotechnology and Precision Engineering 8,  (2024).

55.	Mansor M, et al. Enhancement of gallium nitride on silicon (111) using pulse atomic-layer epitaxy (PALE) AlN with composition-graded AlGaN buffer. Scientific Reports 13, 8793 (2023).

56.	Rabiee Golgir H, et al. Fast growth of GaN epilayers via laser-assisted metal–organic chemical vapor deposition for ultraviolet photodetector applications. ACS applied materials & interfaces 9, 21539-21547 (2017).

57.	Selim FA, Weber MH, Solodovnikov D, Lynn KG. Nature of Native Defects in ZnO. Physical Review Letters 99, 085502 (2007).

58.	Pan M, et al. Metal-organic chemical vapor deposition of ZnO. Journal of crystal growth 287, 688-693 (2006).

59.	Evans SM, Giles NC, Halliburton LE, Kappers LA. Further characterization of oxygen vacancies and zinc vacancies in electron-irradiated ZnO. Journal of Applied Physics 103,  (2008).

60.	Knutsen KE, et al. Zinc vacancy and oxygen interstitial in ZnO revealed by sequential annealing and electron irradiation. Physical Review B 86, 121203 (2012).

61.	Tuomisto F, Saarinen K, Look DC, Farlow GC. Introduction and recovery of point defects in electron-irradiated ZnO. Physical Review B 72, 085206 (2005).

62.	Shen Y, et al. Femtosecond laser writing of waveguides in zinc oxide crystals: fabrication and mode modulation. Optics Express 30, 27694-27703 (2022).

63.	Museur L, Manousaki A, Anglos D, Kanaev AV. Surface modification of monocrystalline zinc oxide induced by high-density electronic excitation. Journal of Applied Physics 110,  (2011).

64.	Nie M, Zhao Y, Zeng Y. Effects of annealing and laser irradiation on optical and electrical properties of ZnO thin films. Journal of Laser Applications 26,  (2014).

65.	Khudiar AI, Mohsen MK, Oufi AM. Laser-induced oxygen vacancies for enhanced gas sensing in zinc oxide thick films. Radiation Physics and Chemistry 238, 113187 (2026).

66.	Kashiwaba Y, Katahira F, Haga K, Sekiguchi T, Watanabe H. Hetero-epitaxial growth of ZnO thin films by atmospheric pressure CVD method. Journal of Crystal Growth 221, 431-434 (2000).

67.	Zubiaga A, et al. Zinc vacancies in the heteroepitaxy of ZnO on sapphire: Influence of the substrate orientation and layer thickness. Applied Physics Letters 86,  (2005).

68.	Koida T, et al. Correlation between the photoluminescence lifetime and defect density in bulk and epitaxial ZnO. Applied Physics Letters 82, 532-534 (2003).