Effective alternative host-guest separation strategies for mixed pyridine/methylpyridines with thioxanthenyl- and xanthenyl-derived host molecules

Danica B. Trollip,*a Benita Barton,*a Mino R. Caira*b and Eric C. Hostena

aDepartment of Chemistry, PO Box 77000, Nelson Mandela University, Gqeberha (Port Elizabeth), 6031, South Africa. E-mail:  s217468225@mandela.ac.za and benita.barton@mandela.ac.za.

bDepartment of Chemistry, University of Cape Town, Rondebosch 7701, South Africa. E-mail: mino.caira@uct.ac.za

| a) |  | b) |  |  |
| --- | --- | --- | --- | --- |
| c) |  | d) |  |  |
| Figure S1 1H NMR for complexes a) H1·PYR, b) H1·2MP, c) H1·3MP and d) H1·4MP |  |  |  |  |  |
| a) |  | b) |  |  |
| c) |  | d) |  |  |
| Figure S2 1H NMR for complexes a) H2·4(PYR), b) H2·2(2MP), c) H2·3MP and d) H2·4MP |  |  |  |  |  |
| a) |  | b) |  |  |
| c) |  | d) |  |  |
| e) |  | f) |  |  |
| g) |  | h) |  |  |
| i) |  | j) |  |  |
| k) |  |  |  |  |
| Figure S3 Host compound H1 1H NMR for equimolar mixtures a) PYR/2MP, b) PYR/3MP, c) PYR/4MP, d) 2MP/3MP, e) 2MP/4MP, f) 3MP/4MP, g) PYR/2MP/3MP, h) PYR/2MP/4MP, i) PYR/3MP/4MP, j) 2MP/3MP/4MP and k) PYR/2MP/3MP/4MP. |  |  |  |  |  |
| a) |  | b) |  |  |
| c) |  | d) |  |  |
| e) |  | f) |  |  |
| g) |  | h) |  |  |
| i) |  | j) |  |  |
| k) |  |  |  |  |
| Figure S4 Host compound H2 1H NMR for equimolar mixtures a) PYR/2MP, b) PYR/3MP, c) PYR/4MP, d) 2MP/3MP, e) 2MP/4MP, f) 3MP/4MP, g) PYR/2MP/3MP, h) PYR/2MP/4MP, i) PYR/3MP/4MP, j) 2MP/3MP/4MP and k) PYR/2MP/3MP/4MP. |  |  |  |  |  |
| a) |  |  | b) |  |  |  |
| c) |  |  | d) |  |  |  |
| e) |  |  | f) |  |  |  |
| g) |  |  | h) |  |  |  |
| i) |  |  | j) |  |  |  |
| k) |  |  | l) |  |  |  |
| Figure S5 Host compounds H1 with the duplicate crystal data for the binary mixtures PYR/2MP in a) and b), for PYR/3MP in c) and d), for PYR/4MP in e) and f), for 2MP/3MP in g) and h), for 2MP/4MP in i) and j), and for 3MP/4MP in k) and l). |  |  |  |  |  |  |  |
| a) |  |  | b) |  |  |  |
| c) |  |  | d) |  |  |  |
| e) |  |  | f) |  |  |  |
| g) |  |  | h) |  |  |  |
| Figure S6 Host compounds H1 with the duplicate crystal data for the ternary mixtures PYR/2MP/3MP in a) and b), for PYR/2MP/4MP in c) and d), for PYR/3MP/4MP in e) and f), and for 2MP/3MP/4MP in g) and h). |  |  |  |  |  |  |  |
| a) |  |  | b) |  |  |  |
| Figure S7 Host compounds H1 with the duplicate crystal data for the quaternary mixtures PYR/2MP/3MP/4MP in a) and b). |  |  |  |  |  |  |  |
| a) |  |  | b) |  |  |  |
| c) |  |  | d) |  |  |  |
| Figure S8 Host compounds H1 for the selectivity profile PYR/2MP for the crystals with a) 80/20, b) 60/40, c) 40/60, and d) 20/80 concentrations. |  |  |  |  |  |  |  |
| a) |  |  | b) |  |  |  |
| c) |  |  | d) |  |  |  |
| Figure S9 Host compounds H1 for the selectivity profile PYR/3MP for the crystals with a) 80/20, b) 60/40, c) 40/60, and d) 20/80 concentrations. |  |  |  |  |  |  |  |
| a) |  |  | b) |  |  |  |
| c) |  |  | d) |  |  |  |
| Figure S10 Host compounds H1 for the selectivity profile PYR/4MP for the crystals with a) 80/20, b) 60/40, c) 40/60, and d) 20/80 concentrations. |  |  |  |  |  |  |  |
| a) |  |  | b) |  |  |  |
| c) |  |  | d) |  |  |  |
| Figure S11 Host compounds H1 for the selectivity profile 2MP/3MP for the crystals with a) 80/20, b) 60/40, c) 40/60, and d) 20/80 concentrations. |  |  |  |  |  |  |  |
| a) |  |  | b) |  |  |  |
| c) |  |  | d) |  |  |  |
| Figure S12 Host compounds H1 for the selectivity profile 2MP/4MP for the crystals with a) 80/20, b) 60/40, c) 40/60, and d) 20/80 concentrations. |  |  |  |  |  |  |  |
| a) |  |  | b) |  |  |  |
| c) |  |  | d) |  |  |  |
| Figure S13 Host compounds H1 for the selectivity profile 3MP/4MP for the crystals with a) 80/20, b) 60/40, c) 40/60, and d) 20/80 concentrations. |  |  |  |  |  |  |  |
| a) |  |  | b) |  |  |  |
| c) |  |  | d) |  |  |  |
| e) |  |  | f) |  |  |  |
| g) |  |  | h) |  |  |  |
| i) |  |  | j) |  |  |  |
| k) |  |  | l) |  |  |  |
| Figure S14 Host compounds H2 with the duplicate crystal data for the binary mixtures PYR/2MP in a) and b), for PYR/3MP in c) and d), for PYR/4MP in e) and f), for 2MP/3MP in g) and h), for 2MP/4MP in i) and j), and for 3MP/4MP in k) and l). |  |  |  |  |  |  |  |
| a) |  |  | b) |  |  |  |
| c) |  |  | d) |  |  |  |
| e) |  |  | f) |  |  |  |
| g) |  |  | h) |  |  |  |
| Figure S15 Host compounds H2 with the duplicate crystal data for the ternary mixtures PYR/2MP/3MP in a) and b), for PYR/2MP/4MP in c) and d), for PYR/3MP/4MP in e) and f), and for 2MP/3MP/4MP in g) and h). |  |  |  |  |  |  |  |
| a) |  |  | b) |  |  |  |
| Figure S16 Host compounds H2 with the duplicate crystal data for the quaternary mixtures PYR/2MP/3MP/4MP in a) and b). |  |  |  |  |  |  |  |
| a) |  |  | b) |  |  |  |
| c) |  |  | d) |  |  |  |
| Figure S17 Host compounds H2 for the selectivity profile PYR/2MP for the crystals with a) 80/20, b) 60/40, c) 40/60, and d) 20/80 concentrations. |  |  |  |  |  |  |  |
| a) |  |  | b) |  |  |  |
| c) |  |  | d) |  |  |  |
| Figure S18 Host compounds H2 for the selectivity profile PYR/3MP for the crystals with a) 80/20, b) 60/40, c) 40/60, and d) 20/80 concentrations. |  |  |  |  |  |  |  |
| a) |  |  | b) |  |  |  |
| c) |  |  | d) |  |  |  |
| Figure S19 Host compounds H2 for the selectivity profile PYR/4MP for the crystals with a) 80/20, b) 60/40, c) 40/60, and d) 20/80 concentrations. |  |  |  |  |  |  |  |
| a) |  |  | b) |  |  |  |
| c) |  |  | d) |  |  |  |
| Figure S20 Host compounds H2 for the selectivity profile 2MP/3MP for the crystals with a) 80/20, b) 60/40, c) 40/60, and d) 20/80 concentrations. |  |  |  |  |  |  |  |
| a) |  |  | b) |  |  |  |
| c) |  |  | d) |  |  |  |
| Figure S21 Host compounds H2 for the selectivity profile 2MP/4MP for the crystals with a) 80/20, b) 60/40, c) 40/60, and d) 20/80 concentrations. |  |  |  |  |  |  |  |
| a) |  |  | b) |  |  |  |
| c) |  |  | d) |  |  |  |
| Figure S22 Host compounds H2 for the selectivity profile 3MP/4MP for the crystals with a) 80/20, b) 60/40, c) 40/60, and d) 20/80 concentrations. |  |  |  |  |  |  |  |

Table S1 C─H···π interactions present in the eight complexes.

|  | Interaction | H···π/Å | C─H···π/° | C···π/Å |  | Interaction | H···π/Å | C─H···π/° | C···π/Å |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| H1·PYR | (host)N─H···π(host) (host)C─H···π(host) (host)C─H···π(host) (host)C─H···π(host) | 2.98(5) 2.92 2.99 3.00 | 155(4) 150 140 132 | 3.824(3) 3.774(4) 3.769(5) 3.703(6) | H2·4(PYR) | (host)C─H···π(host) (host)C─H···π(guest) (host)C─H···π(host) (host)C─H···π(guest) (host)C─H···π(guest) (guest)C─H···π(host) (host)C─H···π(host) (guest)C─H···π(host) (guest)C─H···π(host) (guest)C─H···π(host) (guest)C─H···π(host) | 2.80 3.00 2.92 2.66 2.68 2.96 2.76 2.95 2.98 2.95 2.90 | 152 129 148 169 168 140 157 129 141 147 128 | 3.6600(15) 3.669(8) 3.7602(14) 3.595(7) 3.610(7) 3.741(14) 3.654(9) 3.623(17) 3.773(15) 3.780(12) 3.565(17) |
| H1·2MP | (host)C─H···π(host) (host)C─H···π(host) (guest)C─H···π(host) (guest)C─H···π(host) (guest)C─H···π(host) | 2.71 3.00 2.92 2.42 2.95 | 170 144 155 171 134 | 3.646(2) 3.805(2) 3.795(3) 3.364(14) 3.682(18) | H2·2(2MP) | (host)C─H···π(host) (host)C─H···π(guest) (guest)C─H···π(host) | 2.77 2.94 2.76 | 172 152 158 | 3.7132(14) 3.7998(14) 3.6895(15) |
| H1·3MP | (host)C─H···π(host) (host)C─H···π(guest) (host)C─H···π(host) (host)C─H···π(host) (guest)C─H···π(host) | 2.80 2.92 2.87 2.94 2.80 | 151 142 172 144 166 | 3.6535(18) 3.714(2) 3.8102(14) 3.778(2) 3.758(3) | H2·3MP | (host)C─H···π(host) (guest)C─H···π(host) (guest)C─H···π(host) (guest)C─H···π(host) (guest)C─H···π(host) | 2.72 2.83 2.93 2.92 2.89 | 172 166 159 143 160 | 3.6612(17) 3.790(5) 3.863(5) 3.725(4) 3.833(6) |
| H1·4MP | (guest)C─H···π(host) | 2.72 | 169 | 3.6563(15) | H2·4MP | (host)C─H···π(guest) (host)C─H···π(host) (guest)C─H···π(host) (guest)C─H···π(host) | 2.89 2.71 2.82 2.78 | 157 168 156 174 | 3.782(5) 3.6465(18) 3.711(2) 3.753(16) |

Table S2 Inter- and intramolecular hydrogen bonding identified in the eight complexes.

| Interaction | H···A/Å | D···A/Å | D─H···A/° | Interaction | H···A/Å | D···A/Å | D─H···A/° |
| --- | --- | --- | --- | --- | --- | --- | --- |
| H1·PYR (host)N─H···N(guest)a,c (host)C─H···F(host)a,d (host)C─H···S(host)a,d (host)C─H···N(host)b,d (host)C─H···N(host)b,d (host)C─H···F(host)a,d (guest)C─H···F(host)a,,d | 2.49(3) 2.52 2.87 2.45 2.43 2.61 2.57 | 3.377(4) 3.373(5) 3.752(3) 2.789(4) 2.783(4) 3.214(4) 3.425(6) | 169(3) 150 155 101 102 132 149 | H2·4(PYR) (host)N─H···N(guest)a,c (host)N─H···N(guest)a,c (host)C─H···N(host)b,d | 2.61 2.31 2.43 | 3.489(11) 3.271(13) 2.798(2) | 178 173 103 |
| H1·2MP (host)C─H···N(guest)a,d (host)C─H···N(host)b,d (host)C─H···N(host)b,d (host)C─H···F(host)a,d | 2.60 2.42 2.44 2.56 | 3.403(5) 2.784(3) 2.787(3) 3.349(3) | 142 102 102 140 | H2·2(2MP) (host)N─H···N(guest)a,c (host)C─H···N(guest)a,d (host)C─H···N(host)b,d | 2.500(2) 2.51 2.48 | 3.403(2) 3.463(2) 2.805(2) | 173.8(13) 176 100 |
| H1·3MP (host)N─H···N(guest)a,c (host)C─H···N(host)b,d (host)C─H···N(host)b,d | 2.524(17) 2.42 2.42 | 3.385(2) 2.774(2) 2.779(2) | 174.5(14) 102 102 | H2·3MP (host)N─H···N(guest)a,c (host)N─H···N(guest)a,c (host)C─H···N(host)b,d (host)C─H···N(host)b,d (guest)C─H···O(host)a,d | 2.371(18) 2.45(2) 2.42 2.41 2.67 | 3.280(8) 3.356(10) 2.774(2) 2.770(2) 3.490(2) | 175.6(15) 174.2(14) 102 102 142 |
| H1·4MP (host)N─H···N(guest)a,c (host)C─H···F(host)a,d (host)C─H···N(host)b,d (host)C─H···N(host)b,d | 2.599(17) 2.52 2.44 2.43 | 3.466(2) 3.305(2) 2.784(2) 2.788(2) | 172.8(15) 140 101 102 | H2·4MP (host)N─H···N(guest)a,c (host)C─H···N(host)b,d (host)C─H···N(host)b,d (host)C─H···F(host)a,d | 2.44(2) 2.41 2.44 2.63 | 3.308(3) 2.774(2) 2.780(2) 3.263(2) | 171.7(19) 102 101 124 |

a Intermolecular hydrogen bonding

b Intramolecular hydrogen bonding

c Classical hydrogen bonding

d Non-classical hydrogen bonding

Table S3 Other short contacts present between host molecules, guest molecules, and host and guest molecules.a

|  | Interaction | Note | D(I···J)/Å | X─I···J/° |  | Interaction | Note | D(I···J)/Å | X─I···J/° |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| H1·PYR | (host)C─H···C─N(guest) (host)C─H···C─C(host) | < < | 2.85 2.80 | 134 159 | H2·4(PYR) | (host)C─H···C─N(guest) (host)C─H···C─C(host) (host)C─H···C─N(guest) (guest)C─H···C─C(host) (guest)C─H···C─C(host) | < < < < < | 2.83 2.89 2.88 2.87 2.79 | 155 155 141 131 151 |
| H1·2MP | (host)C─H···C─C(guest) (host)C─H···C─C(host) (host)C─C···H─C(guest) (host)C─H···C─C(host) (guest)C─H···C─C(host) (guest)C─H···C─C(host) | < < << < << << | 2.80 2.84 2.54 2.83 2.46 2.54 | 169 142 111 133 169 140 | H2·2(2MP) | None | None | None | None |
| H1·3MP | (host)C─H···C─C(host) (host)C─H···C─S(host) (host)C─H···C─C(host) (guest)C─H···C─F(host) | < < < < | 2.83 2.82 2.87 2.87 | 135 152 176 139 | H2·3MP | (host)C─H···C─C(host) (host)C─H···C─C(host) (host)C─H···C─C(host) (guest)C─H···C─F(host) (guest)C─C···H─C(host) (guest)C─H···C─C(host) | < < < < < < | 2.86 2.76 2.76 2.81 2.82 2.49 | 147 138 175 139 127 155 |
| H1·4MP | (host)C─H···C─S(host) (host)C─H···C─C(host) (host)C─H···C─C(host) (guest)C─H···C─C(host) | < < < << | 2.86 2.80 2.85 2.69 | 145 135 163 144 | H2·4MP | (host)C─H···C─C(host) (host)C─H···C─C(host) (guest)C─H···C─C(host) | < < < | 2.78 2.84 2.76 | 138 173 135 |

a where I···J is the bond distance between atom 1 and atom 2, and X─I···J is the bond angle.