| Supplementary Table 7.Py-GC/MS calibration curves of polymers |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Polymer | Characteristic compound | Retention time(min) | Calibration curve equation | R2 | LOD(μg) | LOQ(μg) |
| PET | benzoic acd | 9.954 | Y=43653 * x + 19734.8 | 0.996004 | 0.02 | 0.06 |
| PE | n-monoene | 14.398 | Y=90663.9x + -422837 | 0.997293 | 0.5 | 0.15 |
| PVC | naphthalene | 3.938 | Y=187227 * x + -966404 | 0.996353 | 0.02 | 0.06 |
| PA-66 | cyclopentanone | 9.954 | Y=25151.9 * x + -13826.2 | 0.994654 | 0.02 | 0.06 |

Abbreviations: LOD, limit of detection: LOQ, limit of quantitation; PA, polyamide;

PE, polyethylene; PET,polyethylene terephthalate; PVC, polyvinyl chloride: Py-GC/Ms, pyrolysis gas chromatography/mass spectrometry.