SUPPLEMENTARY MATERIALS

Designing a Molecularly Imprinted Polymer Sensor for Sensitive and Selective Detection of the Prostate Cancer Drug Abiraterone Acetate

Abdullah Al Faysal1, Taner Erdoğan2, and Ayşegül Gölcü1*

1Istanbul Technical University, Faculty of Sciences and Letters, Department of Chemistry, Maslak, Istanbul, Türkiye.

2Kocaeli University, Kocaeli Vocational School, Department of Chemistry and Chemical Processing Technologies, Kocaeli, Türkiye

Figure S1. The plots of ΔIp1 values versus (A) monomer ratio, (B) drop volume, (C) photopolymerization time, (D) removal solution, (E) removal time, and ΔIp2 values versus (F) rebinding time. Conditions: potential scan range, −0.2 V to +0.6 V; scan rate, 0.001587 V/s; step potential 8 mV; modulation amplitude 50 mV; modulation time 0.05 s, interval time 0.5 s.

Figure S2.  Results of the PP-MIP(AA)/GCE sensor imprinting factor analysis (5 mM [Fe(CN)6]3−/4− solution was used for all studies).

Figure S3. The findings of the PP-MIP(AA)/GCE sensor with 5 ×10-12 M AA in the presence of interfering substances (5 mM [Fe(CN)6]3−/4− solution was used for all studies).

Figure S4. Template-monomer interactions in AA-AMPS (1:2) complex.

Table S1. The developed sensor's specificity for AA detection.

|  | PP-MIP(AA)/GCE |  | NIP |  |  |
| --- | --- | --- | --- | --- | --- |
|  | ΔІ2/μА | k(MIP) | ΔІ2/μА | k(NIP) | k'(MIP/NIP) |
| AA | 67.67 | - | 23.14 | - | - |
| Enzalutamide | 30.74 | 2.20 | 25.83 | 0.90 | 2.46 |
| Darolutamide | 28.61 | 2.37 | 26.63 | 0.87 | 2.72 |
| Olaparib | 35.11 | 1.93 | 26.91 | 0.86 | 2.24 |
| Niraparib | 32.04 | 2.11 | 26.47 | 0.87 | 2.42 |

Table S2.  The designed sensor's selectivity for AA detection.

| Interferent | Recovery of AA (%) | RSD (%)* |
| --- | --- | --- |
| KNO3 | 98.72 | 0.76 |
| Na2SO4 | 102.09 | 0.50 |
| MgCl2 | 99.88 | 0.76 |
| Dopamine | 98.05 | 0.37 |
| Paracetamol | 101.06 | 0.96 |
| Uric acid | 100.06 | 0.81 |
| Ascorbic acid | 99.15 | 0.69 |

*Each value is the mean of three experiments.

Table S3. The calculated binding energies.

| AA-AMPS Ratio | Binding Energy (kJ/mol) |
| --- | --- |
| 1:1 | -24.03 |
| 1:2 | -42.32 |
| 1:3 | -34.62 |
| 1:4 | -71.07 |
| 1:5 | -512.08 |