Supplementary Information

Ultrathick MoS2 Films with Exceptionally High Volumetric Capacitance

Zheng Bo1,2,★, Xiangnan Cheng1,2, Huachao Yang1,2, Xinzheng Guo1,2, Jianhua Yan1,2, Kefa Cen1,2, Zhaojun Han3,4,5, Liming Dai5

1State Key Laboratory of Clean Energy Utilization, College of Energy Engineering, Zhejiang University, Hangzhou, Zhejiang 310027, China.

2ZJU-Hangzhou Global Scientific and Technological Innovation Center, Hangzhou, Zhejiang 311200, China.

3School of Chemical Engineering, University of New South Wales, Sydney, NSW 2052, Australia.

4CSIRO Manufacturing, 36 Bradfield Road, Lindfield, NSW 2070, Australia.

5Australian Carbon Materials Centre (A-CMC), University of New South Wales, Sydney, NSW 2052, Australia.

★Correspondence and requests for materials should be addressed to Z.B. (e-mail: bozh@zju.edu.cn)

Supplementary Figure 1. Raman measurements of MoS2 nanosheets prepared by the traditional hydrothermal method and the solvated-ion-intercalated method with different Li+ concentrations. In comparison, 2H MoS2 only shows two Raman peaks at 378 and 401 cm-1.

Supplementary Figure 2. The 1T phase stability of MoS2 aqueous dispersion from traditional hydrothermal method. Inset shows the obvious particle precipitation after 24 hours.

Supplementary Figure 3. (a) Image of the 1.45-μm-thick Li+-intercalated MoS2 film. (b-c) GCD and (d) CV curves of the 1.45-μm-thick MoS2 film. Surface capacitive and diffusion-limited contributions of the 1.45-μm-thick MoS2 film at the CV scan rates of (e) 5 mV s-1, (f) 10 mV s-1, (g) 50 mV s-1 and (h) 100 mV s-1, along with (i) their normalized contribution ratios.

Supplementary Figure 4. (a) SEM images and (b) CV curves of the 1.60-μm-thick MoS2 film from the traditional hydrothermal method, which shows a volumetric capacitance of 763.9 F cm-3 at 5 mV s-1. Surface capacitive and diffusion-limited contributions of the 1.60-μm-thick MoS2 film at the CV scan rates of (c) 5 mV s-1, (d) 10 mV s-1, (e) 50 mV s-1 and (f) 100 mV s-1, along with (f) their normalized contribution ratios.

Supplementary Figure 5. (a) Schematic of the equivalent circuit model. In the model, the combined resistance of electrode and electrolyte is represented by reduced equivalent series resistance (Rs). Charge-transfer resistance (Rct) is calculated from the semicircle of the Nyquist plot. CPEdl and CPEpseudo represent electric double layer capacitance and possibly-existed pseudocapacitance, respectively. The low-frequency region of the Nyquist plot is related to the diffusion-controlled processes (CPEw). (b) The fitting curves (red line for this work; blue line for the traditional method) and the calculated equivalent series resistance (Rs) and charge transfer resistance (Rct) based on the equivalent circuit model.

Supplementary Figure 6. (a) CV curves and (b) EIS test of the 94.2-μm-thick MoS2 film.

Supplementary Figure 7. CV curves and EIS test of the asymmetric MoS2||activated carbon supercapacitor.