Supporting Information File

Chemicals and Instruments

The chemicals and reagents used in this study including diethylenetriamine pentaacetic acid dianhydride (cDTPA), N, N-Disiopropyl ethylamine (DIPEA; Hunig’s base), triethylamine (TEA), trifluoroacetic acid (TFA), O-(7-azabenzotriazol-1-yl)-N,N,N',N'-tetramethyluron hexafluorophosphate (HATU; coupling agent), dimethyl sulfoxide (DMSO), dimethylformamide (DMF), and sodium borate were purchased from Sigma-Aldrich (Germany). Cyanine 5.5 N-Hydroxysuccinimide ester (Cy5.5 NHS: ≥ 95% purity; ex/em: 650 nm/ 700 nm) was purchased from Biocone Biotechnology Co. Ltd. Chengdu, China. Head-to-tail cyclic heptapeptide having Arg-Gly-Asp-Lys(Boc)-Leu-Ala-Lys [RGDK(Boc)LAK; Mr = 869.41 g/ mole] sequence was obtained from KareBay Biochem, Inc. New Jersey, USA. Other chemicals including acetic acid (CH3COOH), sodium hydroxide (NaOH), hydrochloric acid (HCl), deionized water, deuterated dimethyl sulfoxide (d6-DMSO), stannous chloride dihydrate (SnCl2.2H2O), sodium borohydride (NaBH4), acetonitrile (HPLC Grade), Milli-Q ultrapure water (Millipore), and Phosphate buffer saline (PBS; pH 7.4) were purchased from Sigma-Aldrich, Germany. All the reagents used in the experiments were of analytical grade and used without further purification. Thin-layer chromatography coated with silica-gel (TLC-SG; 60 F254 20 × 20 cm), Whatman paper no. 3 (3MM), and pH paper were bought from Merck, Germany. The locally produced 99Mo/99mTc generator (PAKGEN) was purchased from PINSTECH, Nilore, Islamabad-Pakistan, and radioactivity (99mTc; Half-life 6.0 h, energy 140 keV, ≥ 98% purity) was eluted from a generator using elution solvent (0.9% saline; sterilized vials) in the form of sodium pertechnetate (Na99mTcO4).

The qualitative measurements of Cy5.5 NHS, cDTPA, and cyclic peptide were carried out before and after modifications using High-Performance Liquid Chromatography (HPLC) Primaide ORG, Hitachi interconnected with 1410 UV detector and NaI(Tl) detector (for radioactive measurements) along with C-18 column (4.6 × 250 mm ID; 5 µm particle size) as stationary phase as well as isocratic mobile phase (acetonitrile: water with 0.1% TFA) system was used for all analysis. High-resolution mass spectrometer (HRMS; Thermo Scientific, Orbitrap ELITE) and Fourier-transform infrared spectrometer-attenuated total reflectance (FTIR-ATR; Thermo Scientific) was used for quantitative measurements after modification of peptide analogs. Fluorescence intensity measurements were performed on Fluorescence Spectrophotometer (RF-5301PC; SHIMADZU, USA). Particle size, shape, and morphology of nanoparticles were determined using Dynamic laser light scattering (DLS, BI-200SM, USA), and Transmission electron microscope (TEM, Tecnai G2 TF30, USA). A cell viability study was carried out using Microplate reader SPARK 10M (TECAN, Switzerland). Cell imaging studies were performed using a confocal fluorescence microscope connected with Imager.Z2 Axiocam 506 color/mono ZEISS camera and functionalized with ZEN V2.3 pro software. Apoptosis assay was performed using the BD FACSCantoTM flow cytometer instrument (BD Biosciences, USA). For the animal imaging study, a Dual-headed SPECT/CT camera (Discovery NM/CT 670 Pro, GE Healthcare USA) interconnected with DICOM V3.0 software was used for acquiring static images.

Characterizations

Fluorescence

The final product Cy5.5@SAPD nanoparticles were diluted with sodium phosphate buffer (Na-PB; pH 7.4) with a concentration of 0.5 µM/ mL, filled in a quartz cuvette (1 cm path length), and subjected to measure the emission spectra. The excitation wavelength was set at 650 nm and emission wavelength set from 675 – 750 nm with slit width 5/5 nm and intensity 500 mV. The same protocol was used to measure the spectra after dilution with deionized water (DW).

Dynamic light scattering (Particle size)

The diluted solution of Cy5.5@SAPD nanoparticles (0.5 mg/ mL DW) was analyzed using a dynamic laser light scattering device. The measurements were carried out at 25°C with a detection angle of 90° on Delsa Nano C Particle Analyzer (Beckman coulter) interconnected with 25 mW He-Ne solid-state laser (660 nm). The size of hydrophilic samples was obtained by calculating mean values from three to five measurements.

Ultra-centrifugation

The increasing concentrations of the radiotracer Cy5.5@SAPDN-99mTc(CO)3 (0 – 100 µL) were added in saline up to the total volume of 1 mL and vortex for 30 sec followed by sonication for 30 min at room temperature. After that, the suspension was centrifuged at 13000 rpm for 5 min and the supernatant was separated from the pellet. The radioactivity of pellet and supernatant was measured using NaI(Tl) well-type gamma-counter to observe the unbound activity present in the supernatant.

Transmission electron microscopy (TEM)

The sample solutions of Cy5.5@SAPD nanoparticles and Cy5.5@SAPDN-99mTc(CO)3 were prepared in deionized water with a concentration of 0.5 mg/ mL. About 50 µL sample solution was placed on carbon-coated copper grids separately for each sample and dried at room temperature under normal atmospheric pressure before the TEM study. The images were acquired on TEM operating at 200 kV accelerating voltage.

Supplementary Figures

Figure S1: High-Pressure Liquid Chromatography (HPLC) analysis of cyclic peptide-DTPA (cPD) complex indicating single peak at retention time Rt = 3.780 min.

Figure S2: High resolution mass spectrometry (HR-MS) analysis of cyclic peptide-DTPA (cPD) complex showing molar mass in addition with proton [M+H+] = 1143 a.m.u

Figure S3: Fourier-Transform Infrared Spectroscopy with Attenuated Total Reflection (FTIR-ATR) analysis of cDTPA (black line), cyclic peptide (red line), and cyclic peptide-DTPA (cPD) complex (blue line) indicates superimposed spectrum

Figure S4: Ultra-High Performance Liquid Chromatography (UHPLC) analysis of fac-[99mTc-(CO)3(H2O)3]+ core complex (99mTc-Tricarbonyl precursor) indicating ≥ 97% purity, inset figure shows TLC-SG analysis of 99mTc-Tricarbonyl precursor (left) and Cy5.5-SAPD-99mTc nanoparticles (right).

Figure S5: Dynamic Light Scattering (DLS) analysis of Cy5.5 coupled self-assembled cyclic peptide-DTPA (Cy5.5@SAPD) nanoparticles shows the hydrodynamic size of nanoparticles