- DSC results

Fig. 1 Sample A

Fig. 2 Sample B

Fig. 3 Sample B (magnification of the low temperature peak)

Fig. 4 Sample D

Fig. 5 Sample E

Fig. 6 Sample F

Fig. 7 Sample G

Fig. 8 Sample H

Fig. 9 Sample J

- SEM results

Fig. 10 Drop of mixture (Al) + Al11La3 in the microstructure of sample A

Table 1. EDS analysis of the Spectrum 1 in figure 10

|  | at.% |  |  |
| --- | --- | --- | --- |
| Spectrum | Al | Cr | La |
| 1 | 90.8 | 1.7 | 7.5 |

Fig. 11 Microstructure of sample G (just to prove that ternary LaCr2Al20 phase (Spectrum 1) is present in the microstructure)

Table 2. EDS analysis of the Spectrum 1 and 2 in figure 11

|  | at.% |  |  |
| --- | --- | --- | --- |
| Spectrum | Al | Cr | La |
| 1 | 87.4 | 8.0 | 4.6 |
| 2 | 99.8 | 0.2 | / |

Microstructure of samples H to J (to prove that the proportion of the ternary phase LaCr2Al20 increases from H to J). Sharp-edged dark grey phases are ternary LaCr2Al20 phases.

Fig. 12 Microstructure of sample H

Fig. 13 Microstructure of sample I

Fig. 14 Microstructure of sample J