Supporting Information

Activating Free Volume of Polymeric Aggregates toward Advanced Hard Carbon for Sodium Storage

Jianhao Lin1, Zhishan Liao1, Yike Liu2, Bote Zhao1, Jiexi Wang3 and Xunhui Xiong1, *

1 School of Environment and Energy, Guangdong Provincial Key Laboratory of Advanced Energy Storage Mater., South China University of Technology, Guangzhou 510006, China

2 School of Materials and Energy Engineering, Guizhou Institute of Technology, Guiyang 550003, China

3 Engineering Research Center of the Ministry of Education for Advanced Battery Materials, Hunan Provincial Key Laboratory of Nonferrous Value-Added Metallurgy, School of Metallurgy and Environment, Central South University, Changsha 410083, China

E-mail: esxxiong@scut.edu.cn

1. Correlated Calculations

Swelling ratio (ΔS/S0): the change in the upper area (ΔS) with the respect to the original upper area (S0).

ΔS/S0 (%) = (S1- S0)/S0                      Equation S1

in which S0 is upper area before swelling and S1 is upper area after swelling calculated by Photoshop software.

Interlayer spacing (d002): d002 is calculated using Bragg’s equation:

d= nλ2sin (θ)                          Equation S2

in which n=1(order of diffraction)

is the XRD wavelength (Cu Kα radiation,1.54056 Å)

θ is the scattering angle (002) peak

Tensile stress (σ, Pa), Tensile strain (ɛ, %) and Tensile Modulus (E, Pa) was calculated using the following equation:

σ = F/S                              Equation S3

ɛ=Δl/l0                              Equation S4

E=σ/ɛ                               Equation S5

where S is the cross-sectional area of PPR or PR samples (m2), F is load (N), Δl is the change in the length (m) and l0 is the gauge length of PPR or PR samples (m).

Shrinkage ratio (Δl/l0) of PPR and PR during the carbonization process:

Δl/l0 (%) = (l1-l0)/ l0                              Equation S6

where l1 is the side length after carbonization and l0 is the original side length.

Closed pore volume (Vclosed pore, cm3 g-1) was calculated from true density (ρtrue) according to the following equation:

Vclosed pore = 1/ρtrue-1/2.26                           Equation S7

Na+ diffusion coefficients were calculated using Fick’s second law:

D=4πτmBVMMBS2∆Es∆Eτ2                        Equation S8

where τ (s) is the pulse duration

mB (g) is active mass of the electrode

VM (cm3 mol-1) is molar volume

MB (g mol-1) is active mass of the el molecular weight

S (m2 g-1) is active surface area of the electrode

∆Es and ∆Eτ are obtained from the GITT curves.

The average distance between adjacent crystalline domains was calculated by Bragg equation:

d=2π/qmax                              Equation S9

in which qmax is the scattering vector at the peak position in SAXS curve.

Falling steel ball test: the PPR-S or PPR-W pieces was covered on a glass substrate, and the impact process was mimicked by dropping a 50 g steel ball above the samples from the same height of about 1 m.

2. Additional Figures and Tables

Supplementary Fig. 1 Scheme of reaction mechanism of PPR aggregates.

Supplementary Fig. 2 The digital photographs of synthesis process of PPR and PR aggregates with different reaction time.

Supplementary Fig. 3 The photographs of the transparency and flexibility of PPR and PR aggregates.

Supplementary Fig. 4 The storage modulus (E’), loss modulus (E”) for PR and PPR aggregates at 25~120 °C by DMA in compression mode (frequency:1 Hz).

Supplementary Fig. 5 Swelling ratio of PPR and PR aggregates in ethanol solvent.

Supplementary Fig. 6 Photos of the immersion process of PR aggregates in ethanol and water solvents.

Supplementary Fig. 7 Photographs of the PPR and PPR-A aggregates during falling-ball test.

Supplementary Fig. 8 Fitted PALS spectra of (a) PPR-S and (b) PPR-W aggregates.

Supplementary Fig. 9 The mercury porosimetry intrusion and retraction curves of PPR-S and PPR-W aggregates.

Supplementary Fig. 10 Photographs of the PPR-S and PPR-W aggregates before and after carbonization process.

Supplementary Fig. 11 FTIR spectrums of PPR-S and PPR-W aggregates at (a) 300 °C and (b) 400 °C.

Supplementary Fig. 12 (a) N2 adsorption/desorption isotherms and (b) pore size distribution of PPR-S-1400 and PPR-W-1400 anodes.

Supplementary Fig. 13 Fitted SAXS curves of (a) PPR-W-1400 and (b) PPR-S-1400 anodes.

Supplementary Fig. 14 Fitted XRD curves of PPR-W-1400 and PPR-S-1400 anodes.

Supplementary Fig. 15 Fitted Raman curves of (a) PPR-W-1400 and (b) PPR-S-1400 anodes.

Supplementary Fig. 16 (a) XPS full spectra and (b) High-resolution C 1s XPS spectra of PPR-W-1400 and PPR-S-1400 anodes.

Supplementary Fig. 17 Photographs of the PR-EG and PR-PEG400 aggregates with the dual-solvent uptake and carbonization process.

Supplementary Fig. 18 The initial discharge/charge curves of HC samples derived from strongly and weakly aggregated state in PR, PR-EG and PR-PEG400 systems.

Supplementary Fig. 19 SAXS patterns of PR aggregates after only ethanol or ethanol/water dual-solvent immersion.

Supplementary Fig. 20 XRD patterns of PR aggregates after only ethanol or ethanol/water dual-solvent immersion.

Supplementary Fig. 21 In-situ XRD spectra of PPR-S-1400 anode.

Supplementary Fig. 22 (a) GITT curves and (b) Na+ diffusion coefficients at de-sodiation process estimated from GITT curves of PPR-W-1400 and PPR-S-1400 anodes.

Supplementary Fig. 23 Electrochemical performance of NVP cathode. (a) Initial charge/discharge curve at 0.1 C; (b) Rate performance; (c) Charge/discharge curves at different rate; (d) Cycling performance at 1 C.

Supplementary Table S1. Positron lifetime distributions in PPR-S and PPR-W precursor

| Samples | Lifetimes (ns) |  |  | Intensities (%) |  |  | Free volume radius (Å) | Free volume size (Å3) | Fractional free volume |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | τ1 | τ2 | τ3 | I1 | I2 | I3 |  |  |  |
| PPR-W | 0.17 | 0.36 | 1.48 | 10.2 | 72.0 | 19.6 | 2.311 | 51.698 | 0.015 |
| PPR-S | 0.32 | 0.45 | 1.29 | 61.7 | 31.9 | 8.5 | 2.091 | 38.295 | 0.005 |