LIST OF TABLES

Table 1:  Stratigraphic Succession of the Lower Benue Trough (Fatoye et al.,2013)

Table 2:  Coordinate Readings and details of the Sample Location

Table 3:   Result of the Grain Size Distribution Analysis

Table 4:   Result of the Liquid Limit Test at Different Temperatures

Table 5:   Result of the Plastic Limit Test at Different Temperatures

Table 6:   Result of the Plasticity Index at Different Temperatures

Table 7:   Results Classified According to AASHTO

Table 8:    Results Classified According to USCS

Table 9:    Group Names

Table 10: Result of the Liquid Limit Test at Different Time Intervals

Table 11: Result of the Plastic Limit Test at Different Time Intervals

Table 12: Result of the Plasticity Index at Different Time Intervals

Table 13: Results Classified According to AASHTO

Table 14: Results Classified According to USCS

Table 15: Group Names

Table 16. Summary of Correlation Coefficients (R²) for Different Temperature values at Constant Heating Duration of 24 hours

Table 17. Summary of Correlation Coefficients (R²) for Different Time Intervals at Constant Heat of 105℃

Table 1

Table 2

| Location | Test hole no. | Coordinate reading |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  | Northing | Easting | Elevation(m) |  |
| Kpiri Kpiri | L1 | 6.323902 | 8.122773 | 82 |  |
| Azu Ugwu | L2 | 6.334697 | 8.103549 | 97 |  |
| Ntezi Abba | L3 | 6.307898 | 8.117659 | 84 |  |
| Nkaliki | L4 | 6.293883 | 8.090386 | 86 |  |
| Azuiyiokwu | L5 | 6.305909 | 8.101371 | 76 |  |

Table 3

| Sample No. | Grain size (%) |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Gravel | Sand | Clay | 4.75 mm | 0.075mm |
| L1 | 13 | 18 | 16 | 11 | 15 |
| L2 | 28 | 27 | 26 | 28 | 28 |
| L3 | 59 | 55 | 58 | 61 | 57 |
| L4 | 87 | 82 | 84 | 89 | 85 |
| L5 | 59 | 55 | 58 | 61 | 57 |

Table 4

| Sample No. | Liquid Limit Test |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | 85°C | 95°C | 105°C | 115°C | 125°C |
| 1 | 47 | 49 | 49 | 48 | 46 |
| 2 | 46 | 40 | 45 | 47 | 46 |
| 3 | 47 | 45 | 44 | 47 | 46 |
| 4 | 47 | 46 | 46 | 46 | 47 |
| 5 | 46 | 45 | 46 | 46 | 46 |
| Average | 46.6 | 45 | 46 | 46.8 | 46.2 |

Table 5

| Sample No. | Plastic Limit Test |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | 85°C | 95°C | 105°C | 115°C | 125°C |
| 1 | 33.86 | 34.41 | 35.23 | 34.11 | 34.45 |
| 2 | 30.49 | 33.25 | 33.46 | 33.59 | 34.97 |
| 3 | 31.23 | 35.25 | 30.62 | 32.93 | 32.13 |
| 4 | 34.86 | 32.37 | 32.71 | 33.39 | 34.64 |
| 5 | 28.63 | 31.80 | 32.45 | 32.18 | 38.16 |
| Average | 31.814 | 33.416 | 32.894 | 33.24 | 34.87 |

Table 6

| Sample No. | Plasticity Index |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | 85°C | 95°C | 105°C | 115°C | 125°C |
| 1 | 13 | 15 | 14 | 14 | 12 |
| 2 | 16 | 65 | 11 | 13 | 11 |
| 3 | 16 | 10 | 13 | 14 | 14 |
| 4 | 12 | 14 | 13 | 13 | 12 |
| 5 | 17 | 14 | 14 | 14 | 8 |
| Average | 14.8 | 23.6 | 13 | 13.6 | 11.4 |

Table 7

| Sample No. | USCS |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | 85°C | 95°C | 105°C | 115°C | 125°C |
| L1 | ML | ML | ML | ML | ML |
| L2 | ML | ML | ML | ML | ML |
| L3 | ML | ML | ML | ML | ML |
| L4 | ML | ML | ML | ML | ML |
| L5 | ML | ML | ML | ML | ML |

Table 8

| Sample No. | USCS |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | 85°C | 95°C | 105°C | 115°C | 125°C |
| 1 | ML | ML | ML | ML | ML |
| 2 | ML | ML | ML | ML | ML |
| 3 | ML | ML | ML | ML | ML |
| 4 | ML | ML | ML | ML | ML |
| 5 | ML | ML | ML | ML | ML |

Table 9

| Sample No. | Soil Group Name |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | 85°C | 95°C | 105°C | 115°C | 125°C |
| 1A | Sandy silt with gravel | Sandy silt with gravel | Sandy silt with gravel | Sandy silt with gravel | Sandy silt with gravel |
| 1B | Sandy silt with gravel | Sandy silt with gravel | Sandy silt with gravel | Sandy silt with gravel | Sandy silt with gravel |
| 1C | Sandy silt with gravel | Sandy silt with gravel | Sandy silt with gravel | Sandy silt with gravel | Sandy silt with gravel |
| 1D | Sandy silt with gravel | Sandy silt with gravel | Sandy silt with gravel | Sandy silt with gravel | Sandy silt with gravel |
| 1E | Sandy silt with gravel | Sandy silt with gravel | Sandy silt with gravel | Sandy silt with gravel | Sandy silt with gravel |

Table 10

| Sample No. | Liquid Limit Test |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | 20hrs | 22hrs | 24hrs | 26hrs | 28hrs |
| L1 | 43 | 43 | 44 | 45 | 43 |
| L2 | 44 | 42 | 45 | 46 | 42 |
| L3 | 45 | 43 | 43 | 45 | 43 |
| L4 | 42 | 44 | 44 | 45 | 45 |
| L5 | 43 | 43 | 43 | 44 | 41 |
| Average | 43.4 | 43 | 43.8 | 45 | 42.8 |

Table 11

| Sample No. | Plastic Limit Test |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | 20hrs | 22hrs | 24hrs | 26hrs | 28hrs |
| L1 | 29.74 | 29.32 | 30.62 | 13.32 | 32.86 |
| L2 | 30.44 | 28.01 | 29.51 | 12.55 | 31.43 |
| L3 | 28.63 | 30.03 | 31.97 | 14.41 | 33.47 |
| L4 | 29.43 | 29.11 | 30.46 | 13.83 | 32.35 |
| L5 | 30.26 | 31.45 | 30.73 | 12.89 | 32.79 |
| Average | 29.7 | 29.584 | 30.658 | 13.4 | 32.58 |

Table 12

| Sample No. | Plasticity Index |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | 20hrs | 22hrs | 24hrs | 26hrs | 28hrs |
| L1 | 13 | 14 | 13 | 32 | 10 |
| L2 | 14 | 14 | 15 | 33 | 11 |
| L3 | 16 | 13 | 11 | 31 | 9 |
| L4 | 13 | 16 | 14 | 31 | 13 |
| L5 | 13 | 12 | 12 | 31 | 8 |
| Average | 13.8 | 13.8 | 13 | 31.6 | 10.2 |

Table 13

| Sample No. | AASHTO |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | 20hrs | 22hrs | 24hrs | 26hrs | 28hrs |
| L1 | A-7-6(6) | A-7-6(6) | A-7-5(6) | A-7-5(6) | A-7-5(6) |
| L2 | A-7-6(6) | A-7-6(6) | A-7-6(6) | A-7-5(6) | A-7-6(6) |
| L3 | A-7-6(6) | A-7-6(6) | A-7-6(6) | A-7-6(6) | A-7-6(6) |
| L4 | A-7-5(6) | A-7-5(6) | A-7-6(6) | A-7-5(6) | A-7-5(6) |
| L5 | A-7-6(6) | A-7-5(6) | A-7-5(6) | A-7-6(6) | A-7-6(6) |

Table 14

| Sample No. | USCS |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | 20hrs | 22hrs | 24hrs | 26hrs | 28hrs |
| L1 | ML | ML | ML | ML | ML |
| L2 | ML | ML | ML | ML | ML |
| L3 | ML | ML | ML | ML | ML |
| L4 | ML | ML | ML | ML | ML |
| L5 | ML | ML | ML | ML | ML |

Table 15

| Sample No. | USCS |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | 20 hrs | 22 hrs | 24 hrs | 26 hrs | 28 hrs |
| L1 | Sandy silt with gravel | Sandy silt with gravel | Sandy silt with gravel | Sandy silt with gravel | Sandy silt with gravel |
| L2 | Sandy silt with gravel | Sandy silt with gravel | Sandy silt with gravel | Sandy silt with gravel | Sandy silt with gravel |
| L3 | Sandy silt with gravel | Sandy silt with gravel | Sandy silt with gravel | Sandy silt with gravel | Sandy silt with gravel |
| L4 | Sandy silt with gravel | Sandy silt with gravel | Sandy silt with gravel | Sandy silt with gravel | Sandy silt with gravel |
| L5 | Sandy silt with gravel | Sandy silt with gravel | Sandy silt with gravel | Sandy silt with gravel | Sandy silt with gravel |

Table 16

| Equations | LL | PL | PI |
| --- | --- | --- | --- |
| Linear | 0.0508 | 0.7279 | 0.305 |
| Exponential | 0.0516 | 0.7294 | 0.3718 |
| Logarithm | 0.0084 | 0.6958 | 0.1887 |
| Polynomial | 0.1684 | 0.7405 | 0.3951 |

Table 17

| Equations | LL | PL | PI |
| --- | --- | --- | --- |
| Linear | 0.0211 | 0.0447 | 0.0381 |
| Exponential | 0.0197 | 0.0667 | 0.0068 |
| Logarithm | 0.0425 | 0.0622 | 0.0562 |
| Polynomial | 0.2617 | 0.1652 | 0.1709 |