Supplementary Information for

Carbonate-Anion Engineering Enables Humidity-Resistant Halide Solid Electrolytes with Superionic Conductivity

Jiacong Li1,2,3,4†, Yuge Cao1,2†, Pushun Lu9,10 Kehao Tao6,7, Wujie Dong3,4,5, Junchao Chen8, Weiping Tang8, Zhan Yu11, Hong Zhu11 and Fuqiang Huang3,4,5*

1 Shanghai Institute of Ceramics, Chinese Academy of Sciences, Shanghai 200050, China.

2 Center of Materials Science and Optoelectronics Engineering, University of Chinese Academy of Sciences, Beijing, 100049, China.

3 Key laboratory of Artificial Intelligent Creation Extreme Energy Materials, School of Materials Science and Engineering, Shanghai Jiao Tong University, Shanghai, 200240, China.

4 School of Materials Science and Engineering and Zhang jiang Institute for Advanced Study (ZIAS), Shanghai Jiao Tong University, Shanghai, 200240, China.

5 Inner Mongolia Research Institute, Shanghai Jiao Tong University, Hohhot 010010.

6 National Key Laboratory of Advanced Micro and Nano Manufacture Technology, Shanghai Jiao Tong University, Shanghai, 200240, China.

7 Department of Micro/Nano Electronics, School of Electronic Information and Electrical Engineering, Shanghai Jiao Tong University, Shanghai, 200240, China.

8 School of Chemistry and Chemical Engineering, Shanghai Jiao Tong University, Shanghai 200240, China.

9 Eastern Institute for Advanced Study, Ningbo Institute of Digital Twin, Eastern Institute of Technology, Ningbo, 315200, China.

10 Zhejiang Key Laboratory of All-Solid-State Battery, Ningbo Key Laboratory of All-Solid-State Battery, Ningbo, 315200, China.

11 Global College, Shanghai Jiao Tong University, Shanghai, 200240, China

†These authors contributed equally to this work

* Corresponding author: Fuqiang Huang, e-mail: huangfq@sjtu.edu.cn

Supplementary Fig. 1 Lab-based XRD patterns for xLi2CO3-ZrCl4. The large peak between 10-22° is the diffraction peak of the Kapton film used to seal the tested powders to avoid any air exposure.

Supplementary Fig. 2 Lab-based XRD patterns for xLi2CO3-HfCl4. The large peak between 10-22° is the diffraction peak of the Kapton film used to seal the tested powders to avoid any air exposure.

Supplementary Fig. 3 EXAFS for xLi2CO3-TaCl5 amorphous SEs, as well as Ta2O5 and TaCl5 at Ta L3-edge.

Supplementary Fig. 4 Wavelet-transformed (WT) EXAFS spectra of 0.8Li2CO3-TaCl5 (a), 0.9Li2CO3-TaCl5 (b), 1.1Li2CO3-TaCl5 (c) at Ta L3-edge with a k2 weighting. R + ΔR represents the radial distance, and ΔR indicates the distance correction due to phase shifts.

Supplementary Fig. 5 Fourier-transform (FT) EXAFS fitting for the Ta L3-edge spectrum of 0.8Li2CO3-TaCl5 (a), 0.9Li2CO3-TaCl5 (b), and 1.1Li2CO3-TaCl5 (c).

Supplementary Fig. 6 Computed structure of amorphous LTCCO (a) and LZCCO (b) at 1200 K generated from melt-and-quench AIMD simulations.

Supplementary Fig. 7 High-resolution transmission electron microscopy (HRTEM) images of LTCCO. Bright-field image (a), energy-dispersive X-ray spectroscopy (EDS) mapping (b) and selected-area electron diffraction (SAED) image (c) of LTCCO.

Supplementary Fig. 8 Fourier transform infrared spectroscopy (FT-IR) of LTCCO (a), and LZCCO (b).

Supplementary Fig. 9 Normalized Nyquist plots for the xLi2CO3-TaCl5 cold-pressed pellets at various temperatures.

Supplementary Fig. 10 Normalized Nyquist plots for the xLi2CO3-ZrCl4 cold-pressed pellets at various temperatures.

Supplementary Fig. 11 Normalized Nyquist plots for the xLi2CO3-HfCl4 cold-pressed pellets at various temperatures.

Supplementary Fig. 12 Normalized Nyquist plots for the Li2ZrCl6 (a), and Li2HfCl6 (b) cold-pressed pellets.

Supplementary Fig. 13 Normalized Nyquist plots for the Li2CO3-AlCl3 (a), Li2CO3-InCl3 (b), Li2CO3-SrCl2 (c), and Li2CO3-CaCl2 (d) cold-pressed pellets.

Supplementary Fig. 14 Lab-based XRD patterns for LTCCO under different ball-milling durations. The large peak between 10-22°is the diffraction peak of the Kapton film used to seal the tested powders to avoid any air exposure.

Supplementary Fig. 15 Normalized Nyquist plots for the LTCCO cold-pressed pellets under different ball-milling durations.

Supplementary Fig. 16 Arrhenius plots for xLi2CO3-ZrCl4 (a), and xLi2CO3-HfCl4(b) SEs.

Supplementary Fig. 17 The variation of ionic conductivity of LTCCO (a), and normalized Nyquist plots for the LTCCO (b) cold-pressed pellets at different exposure time.

Supplementary Fig. 18 The XRD patterns of LZCCO cold-pressed pellets exposed to air with 20% humidity for different periods of time.

Supplementary Fig. 19 The XRD patterns and sample images of LZC cold-pressed pellets exposed to air with 20% humidity for different periods of time.

Supplementary Fig. 20 Scanning electron microscope (SEM) images of the LTCCO (a), LZCCO (b), and LHCCO (c) cold-pressed pellets.

Supplementary Fig. 21 Scanning electron microscope (SEM) images of the Li3InCl6 (a), and Li2ZrCl6 (b) cold-pressed pellets.

Supplementary Fig. 22 Electronic conductivity of LTCCO (a), LZCCO (b), and LHCCO (c) determination by DC measurements at room temperature.

Supplementary Fig. 23 Linear cyclic voltammetry (LSV) profiles of LTCCO (a), LZCCO (b), and LHCCO (c).

Supplementary Fig. 24 Long cycle performance of LCO (a), and NCM88 (b) ASSBs using LTCCO at room temperature.

Supplementary Fig. 25 Rate performance of LCO (a), and NCM88 (b) ASSBs using LTCCO at −10°C.

Supplementary Table 1 Summary of the ionic conductivities of the representative SEs

| Inorganic SSE category | Materials | Ionic conductivity at 25oC (S cm-1) | Ref. |  |
| --- | --- | --- | --- | --- |
| Sulfide | Li9.54Si1.74P1.44S11.7Cl0.3 | 2.5 × 10-2 | Nat. Energy 2016, 1 (4),16030. |  |
|  | Li10GeP2S12 | 1.2 × 10-2 | Nat. Mater. 2011, 10 (9), 682-686. |  |
|  | Li6.6Si0.6Sb0.4S5I | 1.5 × 10-3 | J. Am. Chem. Soc. 2019, 141(48), 19002-19013. |  |
|  | Li6PS5X (X = Cl, Br) | 5.4 × 10-3 | J. Am. Chem. Soc. 2018, 140(47), 16330-16339 |  |
|  |  | 1.0 × 10-3 | Angew. Chem. Int. Ed. 2008, 47 (4), 755-758. |  |
|  | Li5.5PS4.5Cl1.5 | 9.4 × 10-3 | Angew. Chem. Int. Ed. 2019, 58 (26), 8681-8686 |  |
|  | Glass-ceramic Li7P3S11 | 3.2 × 10-3 | Adv. Mater. 2005, 17 (7), 918-921. |  |
| Oxide | Li7La3Zr2O12 system | 10-4 ~10-3 | Angew. Chem. Int. Ed. 2007, 46,7778–7781; Chem. Mater. 2014,26, 3610–3617; Chem. Mater.2016, 28, 2384–2392; ACS Appl. Mater. Interfaces 2017, 9, 1542–1552; Chem. Mater. 2017, 29,1769–1778; |  |
|  | LiTi2(PO4)3 system | ~10-4 | J. Electrochem. Soc. 1990, 137, 1023-1027; Acc. Chem Res. 1994, 27, 265–270. |  |
|  | LiGe2(PO4)3 system | ~10-3 | J. Electrochem. Soc. 2008, 155, A915–A920; Solid State Ionics 2016, 289, 180–187. |  |
|  | Li3xLa2/3 − xTiO3 | ~10-4 | Solid State Commun. 1993, 86,10, 689-693 |  |
|  | 100[Li1.5Cr0.5Ti1.5(PO4)3]- 5SiO2 | 2.14 × 10−2 | J. Non-Cryst. Solids 2015, 409,120–125 |  |
| Halide | Li2ZrCl6 | 8.1 × 10-4 | Nat. Commun. 2021, 12(1), 1- 11 |
|  | Li3YCl6 | 5.1 × 10-4 | Adv. Mater. 2018, 30 (44), 1803075 |
|  | Li3YBr6 | 1.7 × 10-3 | Adv. Mater. 2018, 30 (44), 1803075 |
|  | Li3InCl6 | 2.0 × 10-3 | Angew. Chem. Int. Ed. 2019, 58 (46), 16427-16432 |
|  | Li3ScCl6 | 3.0 × 10-3 | J. Am. Chem. Soc. 2020, 142 (15), 7012-7022 |
|  | Li2Sc2/3Cl4 | 1.5 × 10-3 | Energy Environ. Sci. 2020, 13 (7), 2056-2063 |
| Dual-anion amorphous SEs | 1.6Li2O-TaCl5 | 6.6× 10-3 | Nat Commun.2023,14, 3780 |
|  | 1.5Li2O-HfCl4 | 1.97× 10-3 | Nat Commun.2023,14, 3780 |
|  | 1.5Li2O-ZrCl4 | 1.3× 10-3 | J. Am. Chem. Soc. 2024, 146, 2977−2985 |
|  | Li1.75ZrCl4.75O0.5 | 2.42× 10-3 | Nat Commun.2023,14, 3807 |
|  | Li3N-TaCl5 | 7.34× 10-3 (30℃) | Angew. Chem. Int. Ed. 2024, e202415847 |
|  | 0.4125Li3N-TaCl5 | 5.91× 10-3 | Nat Commun. 2025,16, 143. |
|  | Li1.5Zr0.5Ta0.5Cl5.0O0.5 | 3.88× 10-3 | J. Am. Chem. Soc. 2025, 147, 23170−23179 |

Supplementary Table 2. Structural parameters of xLi2CO3-TaCl5 (x = 0.8, 0.9, 1.0 and 1.1) amorphous SEs extracted from Ta L3-edge EXAFS fittings.

|  |  | 0.8Li2CO3-TaCl5 | 0.9Li2CO3-TaCl5 | 1.0Li2CO3-TaCl5 | 1.1Li2CO3-TaCl5 |
| --- | --- | --- | --- | --- | --- |
| Ta-O path | CN | 4.537 | 4.094 | 4.345 | 5.864 |
|  | d (Å) | 1.862 | 1.872 | 1.877 | 1.910 |
|  | σ2(Å2) | 0.003 | 0.018 | 0.004 | 0.004 |
| Ta-Cl path | CN | 3.996 | 4.171 | 3.898 | 4.05 |
|  | d (Å) | 2.518 | 2.557 | 2.453 | 2.305 |
|  | σ2 (Å2) | 0.016 | 0.003 | 0.018 | 0.009 |

*CN, coordination number; d (Å), bonding distance; σ2, Debye-Waller factor; Ta-O path is from the crystal structures of Ta2O5 (mp-10390). Ta-Cl path from the crystal structure of TaCl5 (mp-29831). The fitted k range was set to be 2–12 Å−1, and the fitted R range was set to be 1−2.6 Å. A k2 weighting was used.

Supplementary Table 3. Summary of the electrochemical performances of ASSBs operating at low temperature

| Battery | Lowest working temperature ( °C) | Capacity retention vs. RT (%) | Current density (mA/cm2) | Ref. |
| --- | --- | --- | --- | --- |
| In¦Li6PS5Cl¦NCM622 | −30 | 60 | 0.053 | Chem. Commun., 2018,54, 14116-14119 |
| Li-In¦65Li2S-30P2S5 5Li2O ¦Li3InCl6¦NCM622 | −20 | 45.7 | 0.08 | Rare Met. 41, 106–114. |
| Li-In¦Li5.6PS4.6Br1.4¦NCM622 | −20 | 67.7 | 0.0064 | Materialia 26, 101603. |
| Li-In¦Li5.5PS4.5Cl1.5¦NCM622 | −20 | 26.6 | 0.8 | Chem. Eng. J. 430, 132896. |
| Li-In¦Li6PS5I¦NCM712 | −20 | 23.4 | 0.024 | Rare Met. 41, 798–805. |
| Li-In¦Li5.5PS4.5Cl1.5¦LNO@NCM712 | −20 | 50.4 | 0.044 | Energy Storage Mater. 43, 53–61. |
| Li-In¦Li5.5PS4.5Cl1.5¦LNO@NCM712 | −20 | 50.0 | 0.016 | Energy Environ. Mater. 6, 12308. |
| Li-In¦Li5.5PS4.5Cl1.5¦NCM811 | −20 | 60.8 | 0.0063 | J. Power Sources 520, 230890. |
| Li-In¦Li5.5PS4.425O0.075Cl1.5¦NCM811 | −20 | 59.2 | 0.016 | ACS Appl. Mater. Interfaces 14, 4179–4185. |
| μSi¦Li6PS5Cl¦NCM811 | −20 (discharge) | 36.7 | 0.3 | Science 373, 1494–1499. |
| Ag-C¦Li6PS5Cl¦Li2O-ZrO2 @NCM90(LiNi0.90Co0.05Mn0.05O2) | −10 (discharge) | 47 | 0.68 | Nat. Energy 5, 299–308. |
| Li-In¦Li6PS5Cl¦ Li3InCl6¦NCM (LiNi0.90Co0.06Mn0.04O2) | −20 | 54.7 | 0.1 | Energy Environ. Sci. 16, 4453–4463. |

| Li4Ti5O12¦LGPS¦LNO@LCO | −30 (discharge) | 92.6 ( 68.1) | 0.06 (0.6) | Nat. Energy 1, 1–7. |
| --- | --- | --- | --- | --- |
| Li-In¦Li9.54 [Si0.6Ge0.4]1.74 P1.44 S11.1Br0.3O0.6¦LNO@LCO | −10 (discharge) | 75 | 0.587 | Science 381, 50–53. |
| Li-In¦Li10SnP1.84Sb0.16S11.6O0.4 ¦LNO@LCO | −20 | 75 | 0.069 | Chem Electro Chem 9, e202200156. |
| Li-In¦Li6PS5Cl¦Li3InCl6¦LCO | −30(−10) | 53.8 (74.9) | 0.06 (0.48) | Adv. Funct. Mater. 32, 2205594. |
| Li-In¦Li6PS5Cl¦Li3InCl6¦LCO¦GLC@Al | −10 | 75.2 | 0.03 | Adv. Funct. Mater. 32, 2200767. |
| Li-In¦Li6PS5Cl¦1.6Li2O-TaCl5¦LCO | −10 | 74.5 | 0.125 | Nat. Commun. 14, 3780. |
| Li¦Li6.5La3Zr1.5Ta0.5O12¦LCO | 10 (discharge) | 20 | 0.0567 | Small 19, e2301904. |