Fig. S1. Schematic representation of the 2D and 3D indirect co-culture for individual cells. (A) C2C12, MEF, and HECs were individually seeded at a density of in a 4-well confocal dish and allowed to attach for 1 h. Following attachment, the central wall of the dish was perforated using a heat-treated 18-gauge needle tip, creating interconnected compartments between the wells. (B) Schematic of the five-chamber co-culture system. Using a stainless-steel mold in a 10 cm dish, Fu/Algi or Bw/Algi hydrogels containing C2C12, MEF, or HECs were arranged in five chambers. The chambers were arranged from the border toward the center as follows: (1)  6 mL Fu/Algi hydrogel mixed with 2.5×10⁵ C2C12 cells;  (2)  6 mL Bw/Algi hydrogel; (3)  4 mL Fu/Algi hydrogel mixed with 2.5×10⁵ MEF cells; (4) 6 mL Bw/Algi hydrogel; and (5)  2 mL Fu/Algi hydrogel mixed with 2.5×10⁵ HECs.

Fig. S2. The microscopic analysis reveals differentiated myotubes in both 2D co-culture times after 7 days of differentiation. Scale bar 100 µm. Control represented the C2C12 cell culture.

Fig. S3. The cytotoxic effect of high fucoidan (Fu) concentrations on C2C12 cell growth through fucoidan/alginate hydrogel (Fu/Algi).  (A) Live & Dead staining of C2C12 cells, presenting live cells in green and dead cells in red. Scale bar 500 µm.  (B-C) C2C12 viability was assessed using the CCK-8 assay for up to 7 days at high and low concentrations of Fu (n=4).

Table S1. Comparison of C2C12 protein content through indirect co-culture at different co-culture times.

| Co-culture through proliferation and differentiation phase | Average Protein content µg/ml |
| --- | --- |
| C2C12 | 417.25 |
| C2C12 ( co-with MEF) | 1196 |
| C2C12 ( co-with HECs) | 226 |
| C2C12 ( co-with MEF+HECs) | 832.875 |
| C2C12 ( co-with MEF +HECs +Bw.A) | 1111.625 |
| Co-culture through differentiation phase | Average Protein content µg/ml |
| C2C12 | 202.875 |
| C2C12 ( co-with MEF) | 584.125 |
| C2C12 ( co-with HECs) | 246 |
| C2C12 ( co-with MEF+HECs) | 206 |
| C2C12 ( co-with MEF +HECs +Bw.A) | 867.25 |