Chemical, Electrochemical and Surface Studies of New Metal-organic Networks as Corrosion Inhibitors for Carbon Steel in Sulfuric Acid Environment

Abd El-Aziz S. Fouda1*, Safaa Eldin H. Etaiw 2, Gannat S. Hassan 2

1Department of Chemistry, Faculty of Science, Mansoura University, Mansoura-35516, Egypt, email: asfouda@hotmail.com;  Fax: +2 050 2202264 Tel: +2 050 2365730

2Department of Chemistry, Faculty of Science, Tanta University, Tanta-31527, Egypt

Supplementary Materials

Figure S1 1D-chain of SC1 connected by H-bonds along the b-axis

Figure S2 Perspective view of 3D-framework of SC1 along (a) a-axis and (b) b-axis

Figure S3 Visualization of the corrugated 1D-chain of the SCP2 down the projection of the ac -plane showing the distribution of the methyl groups at both sides of the chain

Figure S4 Visualization of the 3D-network structure of the SCP2 down the projection of b -axis showing the methyl groups and (qox) molecules located in the space of the network

Figure S5 View showing the distorted ring structure in the network of SCP2

Table S1 Crystal data and structure refinement parameters of SC 1

| Chemical formula | C16 H40 Co2 N12 O7 S4 |
| --- | --- |
| Formula weight | 774.70 |
| Crystal system | Triclinic |
| Space group | P -1 |
| a (Å) | 7.8696(16) |
| b (Å) | 8.9388(18) |
| c (Å) | 12.827(3) |
| α (°) | 94.07(3) |
| β (°) | 96.94(3) |
| γ (°) | 114.85(3) |
| V (Å3) | 805.3(4) |
| Z, wavelength | 1, 0.7 Å |
| Dcalcd (g/cm3) | 1.597 |
| Absorption coefficient, mm–1 | 1.348 |
| F(000) | 402.0 |
| θ range, deg | 1.590°– 29.996° |
| Index range h, k, l | 11,12,18 |
| Rint | 0.023 |
| Data/restraint/parameters | 4761/16/ 226 |
| Goodness of fit on F 2 | 1.1158 |
| Final R1, wR2 (I > 2σ(I)) | 0.0279, 0.0843 |
| Δρmax, eÅ−3 , Δρmin, eÅ−3 | 0.58,-0.77 |
| CCDC NO | 1991081 |

| Co2—N1 | 2.100 | N1—C1 | 1.166 |
| --- | --- | --- | --- |
| Co2—O2 | 2.065 |  |  |
| Co2—O3 | 2.106 |  |  |
| N2—C2 | 1.166 | N3—C3 | 1.488 |
| C2—S2 | 1.645 | N3—C4 | 1.493 |
|  |  | N3—C5 | 1.490 |
|  |  | C7—N4 | 1.479 |
|  |  | C4—N5 | 1.474 |
|  |  | C5—N6 | 1.478 |
| CO2—C2 N2—S2 CO1—O1 CO1—N1 CO1—N3 N2— C2— S2 Co2— N2— C2 N1— CO1— O1 | 3.265 2.811 2.088 2.051 2.305 178.37 177.28 90.16 | C7—N6 C5—N6 H83—O4—H84 N1—C1—S1 CO1—N1—C1 C3— N3— C5 | 1.474 1.478 104.45 179.27 163.39 107.40 |

Table S2 needs to be tabulated correctly

Table S2 Bond lengths (Å) and bond angles (deg.) of SC1

Table S3 Crystal data and structure refinement parameters of the SCP 2

| Chemical formula | C23H35N8OSn3Co |
| --- | --- |
| Formula weight | 854.65 |
| Crystal system | Monoclinic |
| Space group | C2/c |
| a (Å) | 16.837(3), |
| b (Å) | 12.542(3), |
| c (Å) | 33.116(7) |
| α (°) | 90 |
| β (°) | 93.29(3) |
| γ (°) | 90 |
| V (Å3) | 6982(2) |
| Z | 8 |
| Dcalcd (g/cm3) | 1.626 |
| Absorption coefficient, mm–1 | 2.614 |
| F(000) | 3312.0 |
| Crystal size, mm | 0.040 x 0.070 x 0.090 |
| θ range, deg | 1.213°– 29.763° |
| Index range h, k, l | -23 / 23, 0/ 17, 0/ 46 |
| Rint | 0.0572 |
| Data/restraint/parameters | 9198/4/ 333 |
| Goodness of fit on F 2 | 0.9458 |
| Final R1, wR2 (I > 2σ(I)) | 0.0609, 0.1588 |
| Δρmax, eÅ−3 , Δρmin, eÅ−3 | 1.61, -0.49 |
| CCDC NO | 1948888 |

Table S4 Bond lengths (Å) and bond angles (deg.) of the SCP 2

| Co1—C1 | 1.877 (5) | Sn1—C7 | 2.112 (9) |
| --- | --- | --- | --- |
| Co1—C2 | 1.884 (6) | Sn1—C8 | 2.127 (7) |
| Co1—C3 | 1.879 (6) | Sn1—C9 | 2.091 (9) |
| Co1—C4 | 1.872 (5) | Sn1—C10 | 2.132 (7) |
| Co1—C5 | 1.881 (6) | Sn1—C11 | 2.114 (7) |
| Co1—C6 | 1.881 (6) | Sn1—C12 | 2.118 (7) |
| C1—N1 | 1.152 (7) | Sn1—N1 | 2.291 (5) |
| C2—N2 | 1.141 (8) | Sn1—N4 | 2.314 (5) |
| C3—N3 | 1.146 (7) | Sn2—N2 | 2.309 (5) |
| C4—N4 C5—N5 C6—N6 N7—C16 N7—C23 N8—C21 N8—C22 O1— Sn3— N3 Co1— C1— N1 Co1— C2— N2 Co1— C3— N3 | 1.146 (7) 1.155 (8) 1.132 (8) 1.383 (8) 1.300 (8) 1.373 (8) 1.304 (9) 177.17 (8) 178.6 (5) 178.5 (5) 178.6 (5) | Sn3—N3 Sn2—N6 O2— Sn3 Sn1—N1—C1 Sn2—N2—C2 Sn3—N3—C3 Sn1—N4—C4 Sn2—N6—C6 Co1— C4— N4 Co1— C5— N5 Co1— C6— N6 | 2.310 (5) 2.320 (6) 2.251 (4) 159.4 (5) 158.0 (5) 156.5 (5) 162.17 (2) 150.1 (6) 176.8 (7) 178.0 (6) 176.6 (6) |