Table 3: Concentrations of chemical elements in the lateritic gravels obtained by EDS

|  |  | Mean values of concentrations of major chemical elements obtained by EDS |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Element |  | Gneiss |  | Metasyenite |  | Micaschists |  | Quartzites |  |
| Si |  | 15.42 |  | 10.93 |  | 18.80 |  | 15.28 |  |
| O |  | 44.88 |  | 47.70 |  | 46.43 |  | 47.43 |  |
| Fe |  | 15.22 |  | 27.79 |  | 22.60 |  | 24.30 |  |
| Al |  | 7.24 |  | 12.90 |  | 10.57 |  | 12.15 |  |