Sustainable Synthesis and Enhanced Photocatalytic Activity of Titanium Oxide-Clay Nanocomposite Toward Persistent Polychlorinated Biphenyl Degradation in Real Samples

Jasem Chanani, Foad Buazar*, Yadollah Nikpour

Department of Marine Chemistry, Khorramshahr University of Marine Science and Technology, P.O. Box 669, Khorramshahr, Iran

*Corresponding author, Tel: +98-916115084, Email: fb@kmsu.ac.ir

| Element | Weight% | Atomic% |  |
| --- | --- | --- | --- |
| O K | 57.76 | 73.62 |  |
| Na K | 0.13 | 0.12 |  |
| Mg K | 1.61 | 1.36 |  |
| Al K | 8.46 | 6.39 |  |
| Si K | 16.77 | 12.18 |  |
| K K | 0.03 | 0.02 |  |
| Ca K | 0.33 | 0.17 |  |
| Ti K | 11.7 | 4.98 |  |
| Fe K | 3.21 | 1.16 |  |
| Totals | 100.00 |  |  |

Table 1S. the elemental composition of TiO2-clay nanocomposite using SEM-EDX analyzer

Table 1S. elemental composition of TiO2-clay nanocomposite as determined by EDX analyzer.

| Element | Weight% | Atomic% |
| --- | --- | --- |
| O K | 57.76 | 73.62 |
| Na K | 0.13 | 0.12 |
| Mg K | 1.61 | 1.36 |
| Al K | 8.46 | 6.39 |
| Si K | 16.77 | 12.18 |
| K K | 0.03 | 0.02 |
| Ca K | 0.33 | 0.17 |
| Ti K | 11.7 | 4.98 |
| Fe K | 3.21 | 1.16 |
| Totals | 100.00 |  |

Figure 1S. Effect of solution temperature on the degradation efficiency of TiO2-clay toward PBC-52 pollutant

Figure 2S. Effect of solution contact time on the degradation efficiency of TiO2-clay toward PBC-52 pollutant

Figure 3S. Effect of TiO2-clay nanocomposite amount on the degradation rate toward PBC-52 pollutant

Figure 4S. The correlation between photodegradation of green TiO2-clay nanocomposite and varying PBC-52 concentration