Table 1. Summary of the effects of reaction parameters and conditions on the reaction efficiency[a]

| Entry | Deviation from standard conditions | Yield 3a [%] |
| --- | --- | --- |
| 1 | None | 98 (92) |
| 2 | LCFOCN-1 instead of LCFOCN-2 | 46 |
| 3 | LCFOCN-3 instead of LCFOCN-2 | 53 |
| 4 | LCFOCN-4 instead of LCFOCN-2 | 42 |
| 5 | LCFOCN-5 instead of LCFOCN-2 | 30 |
| 6 | g-C3N4 instead of LCFOCN-2 | 22 |
| 7 | 4-CzlPN instead of LCFOCN-2 | 35 |
| 8 | LCFO-1,2,3,4,5 instead of LCFOCN-2 | Trace |
| 9 | no light | 0 |
| 10 | no photocatalyst | 0 |
| 11 | no NiCl2 and no ligand | 0 |
| 12 | no ligand | 0 |
| 13 | no TEOA | 0 |

[a] Reaction condition:1a (0.3 mmol), 2a (0.3 mmol), NiCl2 (5 mol%), 1,10-Phenanthroline (5 mol%), DMSO (3.8 mL), triethanolamine (TEOA 5 eq.), blue LED light irradiation, 24h. Conversion was measured by GC using naphthalene as an internal standard.