Appendix I

One of the common methods in multivariate analysis is the multiple linear regression technique. In multiple linear regression, the parameters of a linear model are estimated using an objective function and the values of the variables. In this method, model is a linear relation in terms of parameters. Therefore, the strain relationship in terms of printing parameters can be written as follows:

| (I- 1) | εi=xviv*+xhih*+xTiT*+yi i=1,2 |
| --- | --- |

Which is estimated by the following relation:

| (I- 2) | εi= Xviv*+Xhih*+XTiT*+Yi i=1,2 |
| --- | --- |

Now the sum of squared errors must be minimized:

| (I- 3) | SSE=(εi-εi)2=(εi- Xviv*+Xhih*+XTiT*+Yi)2 |
| --- | --- |

That is:

| (I- 4) | ∂SSE∂Y=-2(εi- Xviv*-Xhih*-XTiT*-Yi)=0 ∂SSE∂Xv=-2Xvi(εi- Xviv*-Xhih*-XTiT*-Yi)=0 ∂SSE∂Xh=-2Xhi(εi- Xviv*-Xhih*-XTiT*-Yi)=0 ∂SSE∂XT=-2XTi(εi- Xviv*-Xhih*-XTiT*-Yi)=0 |
| --- | --- |

To obtain the values of the coefficients, 64 samples with a printing pattern of [0]n and dimensions of 40mm×10mm×1mm were printed using a full factorial design of experiment and their strain was measured. The parameter values and the strain of each sample are given in Table I-1. By solving the system of equations, the values of the coefficients are obtained as follows:

| (I- 5) | X=Xv1Xh1XT1Xv2Xh2XT2Xv12Xh12XT12=-0.150.0750.30.015-0.0075-0.03000 Y=Y1Y2Y12=-0.750.0750 |
| --- | --- |

Table I- 1. Printing parameters values and their measured strains

| S No. | v* | h* | T* | ε1 | ε2 |
| --- | --- | --- | --- | --- | --- |
| 1 | 0.2 | 0.1 | 1.15 | -0.35 | 0.038 |
| 2 | 0.2 | 0.2 | 1.15 | -0.276 | 0.025 |
| 3 | 0.2 | 0.3 | 1.15 | -0.205 | 0.022 |
| 4 | 0.2 | 0.4 | 1.15 | -0.145 | 0.014 |
| 5 | 0.4 | 0.1 | 1.15 | -0.398 | 0.040 |
| 6 | 0.4 | 0.2 | 1.15 | -0.331 | 0.032 |
| 7 | 0.4 | 0.3 | 1.15 | -0.222 | 0.021 |
| 8 | 0.4 | 0.4 | 1.15 | -0.161 | 0.016 |
| 9 | 0.6 | 0.1 | 1.15 | -0.431 | 0.041 |
| 10 | 0.6 | 0.2 | 1.15 | -0.371 | 0.039 |
| 11 | 0.6 | 0.3 | 1.15 | -0.26 | 0.024 |
| 12 | 0.6 | 0.4 | 1.15 | -0.218 | 0.020 |
| 13 | 0.8 | 0.1 | 1.15 | -0.451 | 0.046 |
| 14 | 0.8 | 0.2 | 1.15 | -0.39 | 0.035 |
| 15 | 0.8 | 0.3 | 1.15 | -0.282 | 0.027 |
| 16 | 0.8 | 0.4 | 1.15 | -0.221 | 0.024 |
| 17 | 0.2 | 0.1 | 1.25 | -0.335 | 0.036 |
| 18 | 0.2 | 0.2 | 1.25 | -0.254 | 0.028 |
| 19 | 0.2 | 0.3 | 1.25 | -0.171 | 0.016 |
| 20 | 0.2 | 0.4 | 1.25 | -0.121 | 0.011 |
| 21 | 0.4 | 0.1 | 1.25 | -0.372 | 0.035 |
| 22 | 0.4 | 0.2 | 1.25 | -0.306 | 0.028 |
| 23 | 0.4 | 0.3 | 1.25 | -0.198 | 0.020 |
| 24 | 0.4 | 0.4 | 1.25 | -0.157 | 0.017 |
| 25 | 0.6 | 0.1 | 1.25 | -0.418 | 0.043 |
| 26 | 0.6 | 0.2 | 1.25 | -0.33 | 0.036 |
| 27 | 0.6 | 0.3 | 1.25 | -0.226 | 0.024 |
| 28 | 0.6 | 0.4 | 1.25 | -0.179 | 0.019 |
| 29 | 0.8 | 0.1 | 1.25 | -0.439 | 0.043 |
| 30 | 0.8 | 0.2 | 1.25 | -0.349 | 0.036 |
| 31 | 0.8 | 0.3 | 1.25 | -0.26 | 0.028 |
| 32 | 0.8 | 0.4 | 1.25 | -0.223 | 0.021 |
| 33 | 0.2 | 0.1 | 1.45 | -0.261 | 0.024 |
| 34 | 0.2 | 0.2 | 1.45 | -0.178 | 0.017 |
| 35 | 0.2 | 0.3 | 1.45 | -0.122 | 0.013 |
| 36 | 0.2 | 0.4 | 1.45 | 0.068 | 0.007 |
| 37 | 0.4 | 0.1 | 1.45 | -0.312 | 0.033 |
| 38 | 0.4 | 0.2 | 1.45 | -0.218 | 0.022 |
| 39 | 0.4 | 0.3 | 1.45 | -0.116 | 0.012 |
| 40 | 0.4 | 0.4 | 1.45 | -0.081 | 0.008 |
| 41 | 0.6 | 0.1 | 1.45 | -0.336 | 0.032 |
| 42 | 0.6 | 0.2 | 1.45 | -0.247 | 0.026 |
| 43 | 0.6 | 0.3 | 1.45 | -0.166 | 0.016 |
| 44 | 0.6 | 0.4 | 1.45 | -0.1 | 0.010 |
| 45 | 0.8 | 0.1 | 1.45 | -0.377 | 0.036 |
| 46 | 0.8 | 0.2 | 1.45 | -0.268 | 0.028 |
| 47 | 0.8 | 0.3 | 1.45 | -0.195 | 0.019 |
| 48 | 0.8 | 0.4 | 1.45 | -0.143 | 0.014 |
| 49 | 0.2 | 0.1 | 1.65 | -0.22 | 0.020 |
| 50 | 0.2 | 0.2 | 1.65 | -0.14 | 0.013 |
| 51 | 0.2 | 0.3 | 1.65 | -0.066 | 0.007 |
| 52 | 0.2 | 0.4 | 1.65 | -0.03 | 0.003 |
| 53 | 0.4 | 0.1 | 1.65 | -0.252 | 0.026 |
| 54 | 0.4 | 0.2 | 1.65 | -0.154 | 0.014 |
| 55 | 0.4 | 0.3 | 1.65 | -0.088 | 0.008 |
| 56 | 0.4 | 0.4 | 1.65 | -0.041 | 0.004 |
| 57 | 0.6 | 0.1 | 1.65 | -0.285 | 0.031 |
| 58 | 0.6 | 0.2 | 1.65 | -0.186 | 0.018 |
| 59 | 0.6 | 0.3 | 1.65 | -0.114 | 0.011 |
| 60 | 0.6 | 0.4 | 1.65 | -0.071 | 0.007 |
| 61 | 0.8 | 0.1 | 1.65 | -0.322 | 0.035 |
| 62 | 0.8 | 0.2 | 1.65 | -0.218 | 0.022 |
| 63 | 0.8 | 0.3 | 1.65 | -0.146 | 0.016 |
| 64 | 0.8 | 0.4 | 1.65 | -0.095 | 0.009 |