SUPPLEMENTARY MATERIALS

Phenoxazinone Synthase Functional Mimic Activity of Mixed-ligand Copper(II) Complexes of L-proline and Diimine Ligands Conjugated with Chitosan

Liji Muthirakalayil Abraham,a Manikandan Varadhan,a  Kugan Mahalingam,a  Thangaraja Chinnathangavel,b and Venugopal Rajendiran,*a

aDepartment of Chemistry, School of Basic and Applied Sciences, Central University of Tamil Nadu, Thiruvarur 610101, India

bDepartment of Chemistry, Anna University Regional Campus, Madurai 625019, India

*Corresponding Author:   Venugopal Rajendiran, Email: rajendiran@cutn.ac.in

| Sl.No. | Content | Page No. |
| --- | --- | --- |
| 1 | Figure S1. 1H NMR spectra of (a) and (b) correspond to Boc-Proline-chitosan and chito-pro, respectively. (c) and (d) correspond to 13C NMR spectrum of Boc-Proline-chitosan and chito-pro, respectively, in D2O. | S3 |
| 2 | Figure S2. FT-IR Spectrum of Ligand(L) | S5 |
| 3 | Figure S3. FT-IR Spectrum of Complex 1 | S5 |
| 4 | Figure S4. FT-IR Spectrum of Complex 2 | S6 |
| 5 | Figure S5. 1H NMR of APX | S6 |
| 6 | Figure S6. HR-MS spectrum of APX | S7 |
| 7 | Table S1. Comparison of FT-IR Data | S8 |

(a)

(b)

(c)

(d)

Figure S1. 1H NMR spectra of (a) and (b) correspond to Boc-Proline-chitosan and chito-pro, respectively. (c) and (d) correspond to 13C NMR spectrum of Boc-Proline-chitosan and chito-pro, respectively, in D2O.

Figure S2. FT-IR Spectrum of Ligand(L)

Figure S3. FT-IR Spectrum of Complex 1

Figure S4. FT-IR Spectrum of Complex 2

Figure S5. 1H NMR of APX

Figure S6. HR-MS spectrum of APX

Table S1. Comparison of FT-IR Data

| Functional groups | L (cm-1) | 1 (cm-1) | 2 (cm-1) |
| --- | --- | --- | --- |
| ν(N-H) | 3268 | 3081 | 2897 |
| ν(C=N) | - | 1566 | 1598 |
| ν(-OH)bend | 1406 | 1425 | 1449 |
| ν(C-H)S | 2935 | 3081 | 2897 |
| ν(C=O) | 1699 | 1610 | 1601 |
| ν(Cu-N) | - | 430 | 413 |
| ν(O-C-O) | 1092 | 1082 | 1092 |
| ν(C-H)out of plane | 612 | 619 | 618 |