Fig. S1 The experimental and simulated XRD patterns of [Ce2(2,6-dipic)4Ni(H2O)8]·8H2O

Fig. S2 The experimental and simulated XRD patterns of [Pr2(2,6-dipic)4Ni(H2O)8]·8H2O

Fig. S3 The experimental and simulated XRD patterns of [Nd2(2,6-dipic)4Ni(H2O)8]·8H2O

Fig. S4 The experimental and simulated XRD patterns of [Sm2(2,6-dipic)4Ni(H2O)8]·8H2O

Table S1  Selected bond lengths [Ã] and angles [°] of [Ce2(2,6-dipic)4Ni(H2O)8]·8H2O

| [Ce2Ni(2,6-dipic)4 (H2O)8]·4H2O |  |  |  |
| --- | --- | --- | --- |
| Ce1-O7 Ce1-O4 Ce1-O9 Ce1-O5 Ce1-O2 Ce1-O2i O7-Ce1-O4 O7-Ce1-O9 O4-Ce1-O9 O7-Ce1-O5 O4-Ce1-O5 O9-Ce1-O5 O7-Ce1-O2 O4-Ce1-O2 O9-Ce1-O2 O5-Ce1-O2 O7- Ce1-O2i O4- Ce1-O2i O9- Ce1-O2i | 2.489(4) 2.513(5) 2.517(5) 2.518(5) 2.531(4) 2.552(4) 78.14 (15) 82.62 (15) 73.78 (16) 123.79 (16) 81.98 (15) 139.49 (16) 154.07 (16) 123.59 (15) 89.99 (15) 76.89 (15) 101.70 (15) 154.43 (15) 131.77 (15) | Ce1-O10 Ce1-N2 Ce1-N1 O1-C1 N1-O11ii Ni1-O8 O5- Ce1-O2i O2- Ce1-O2i O7- Ce1-O10 C4- Ce1-O10 O9- Ce1-O10 O5- Ce1-O10 O2- Ce1-O10 O2i - Ce1-O10 O7- Ce1-N2 O4- Ce1-N2 O9- Ce1-N2 O5-Ce1-N2 O2- Ce1-N2 | 2.594(5) 2.611(5) 2.618(5) 1.224(9) 2.055(5) 2.059(5) 76.99 (15) 65.33 (17) 74.67 (16) 134.39 (16) 67.02 (16) 143.62 (16) 79.55 (15) 68.08 (15) 61.91 (15) 70.25 (16) 133.38 (16) 61.91 (15) 134.81 (15) |

Note: i Represents the position (1/2-X, 1/2-Y, 1-Z); ii Represents the position (1-X, +Y, 3/2-Z).

Table S2  Selected bond lengths [Ã] and angles [°] of [Nd2(2,6-dipic)4Ni(H2O)8]·8H2O

| [Nd2Ni(2,6-dipic)4 (H2O)8]·4H2O |  |  |  |
| --- | --- | --- | --- |
| Nd1-N1 Nd1-O2i Nd1-O2 Nd1-N2 Nd1-O5 Nd1-O4 O2-Nd1-N1 O2i -Nd1-N1 O2-Nd1-O2i O2i -Nd1-N2 O2-Nd1-N2 O2-Nd1-O10 O2i -Nd1-O10 N2-Nd1-N1 O5-Nd1-N1 O5-Nd1-O2 O5-Nd1-O2i O5-Nd1-N2 O5-Nd1-O10 O4-Nd1-N1 O4-Nd1-O2i O4-Nd1-O2 O4-Nd1-N2 O4-Nd1-O5 | 2.579(5) 2.532(4) 2.509(4) 2.577(5) 2.488(4) 2.481(4) 62.24(13) 122.83(14) 65.40(15) 85.93(13) 134.94(14) 79.36(14) 68.50(14) 116.48(14) 70.98(14) 77.10(13) 76.70(14) 62.34(14) 143.72(14) 62.94(14) 153.64(13) 125.05(13) 70.13(14) 82.33(14) | Nd1-O9 Nd1-O7 Nd1-O10 C1-O1 C1-O2 Ni1-O8ii O4-Nd1-O9 O4-Nd1-O10 O9-Nd1-N1 O9-Nd1-O2 O9-Nd1-O2i O9-Nd1-N2 O9-Nd1-O5 O9-Nd1-O10 O7-Nd1-N1 O7-Nd1-O2i O7-Nd1-O2 O7-Nd1-N2 O7-Nd1-O5 O7-Nd1-O4 O7-Nd1-O9 O7-Nd1-O10 O10-Nd1-N1 O10-Nd1-N2 | 2.485(4) 2.464(4) 2.547(4) 1.228(8) 1.275(8) 1.506(8) 73.55(14) 133.95(14) 69.23(14) 90.65(14) 132.71(13) 132.92(14) 139.56(14) 67.27(14) 135.78(14) 101.39(13) 152.55(13) 62.76(14) 125.06(13) 77.81(14) 81.24(14) 73.30(14) 120.27(15) 122.99(15) |

Note: i Represents the position (1/2-X, 1/2-Y, 1-Z); ii Represents the position (1-X, +Y, 3/2-Z).

Table S3 Selected bond lengths [Ã] and angles [°] of [Sm2(2,6-dipic)4Ni(H2O)8]·8H2O

| [Sm2Ni(2,6-dipic)4 (H2O)8]·4H2O |  |  |  |
| --- | --- | --- | --- |
| Sm1-N1 Sm1-O2 Sm1-O2i Sm1-N2 Sm1-O5 Sm1-O3 O2-Sm1-N1 O2i -Sm1-N1 O2-Sm1-O2i O2i -Sm1-N2 O2-Sm1-N2 O2-Sm1-O10 O2i -Sm1-O10 N2-Sm1-N1 O5-Sm1-N1 O5-Sm1-O2i O5-Sm1-O2 O5-Sm1-N2 O5-Sm1-O9 O5-Sm1-O10 O3-Sm1-N1 O3-Sm1-O2 O3-Sm1-O2i O10-Sm1-N1 | 2.539(9) 2.493(7) 2.504(7) 2.532(9) 2.460(8) 2.458(7) 62.6(3) 123.4(3) 65.7(3) 85.0(3) 135.1(3) 79.3(3) 68.4(3) 117.2(3) 70.7(3) 77.0(3) 77.3(2) 62.9(3) 139.9(3) 143.9(3) 64.1(3) 126.7(3) 153.4(3) 120.6(3) | Sm1-O7 Sm1-O9 Sm1-O10 C1-O1 N1-C2 Ni1-O8ii O3-Sm1-N2 O3-Sm1-O5 O3-Sm1-O9 O3-Sm1-O10 O7-Sm1-N1 O7-Sm1-O2i O7-Sm1-O2 O7-Sm1-N2 O7-Sm1-O5 O7-Sm1-O3 O7-Sm1-O9 O7-Sm1-O10 O9-Sm1-N1 O9-Sm1-O2 O9-Sm1-O2i O9-Sm1-N2 O9-Sm1-O10 O10-Sm1-N2 | 2.448(7) 2.463(8) 2.524(8) 1.239(14) 1.344(14) 1.355(14) 70.2(3) 83.0(3) 73.3(3) 133.1(3) 136.1(3) 100.5(3) 151.1(3) 63.3(3) 126.2(3) 77.3(3) 79.9(3) 71.9(3) 70.0(3) 91.3(2) 132.9(3) 132.5(3) 67.1(3) 122.0(3) |

Note: i Represents the position (1/2-X, 1/2-Y, 1-Z); ii Represents the position (1-X, +Y, 3/2-Z).

Fig. S5 The experimental IR spectrum of the pure ligand

Fig. S6 The standard IR spectrum of the pure ligand from http://www.basechem.org/