Synthesis and Characterization of Biocompatible Cryogels Based on Chitosan, Poly(ethylene glycol) Diacrylate, and Graphene with a Controlled Porous Structure

A.S. Buinov1*, E.R. Gafarova2, K.N. Bardakova2,3, B.Ch. Kholkhoev1, V.M. Poglazova2, N.B. Serezhnikova2, Y.M. Efremov2, I.A. Farion1, D.I. Gapich4,5, V.A. Kuznetsov4,5, P.S. Timashev2,6,7, V.F. Burdukovskii1

1 Baikal Institute of Nature Management
Siberian branch of the Russian Academy of Sciences,

Russian Federation, 670047 Ulan-Ude, 6 Sakhyanovoy str.

2 Institute for Regenerative Medicine, Sechenov First Moscow State Medical University (Sechenov University), Russian Federation, 119991 Moscow, 8-2 Trubetskaya str.

3 National Research Centre “Kurchatov Institute”, Russian Federation, 123182 Moscow, 1 Akademika Kurchatova Square

4 Nikolaev Institute of Inorganic Chemistry
Siberian Branch of Russian Academy of Sciences, Russian Federation, 630090 Novosibirsk, 3 Acad. Lavrentiev Ave.

5 Novosibirsk State Technical University, Russian Federation, 630073 Novosibirsk, 20 K. Marx ave.

6 Semenov Institute of Chemical Physics, Russian Academy of Sciences, Russian Federation, 119991 Moscow, 4 Kosygina str.

7 Chemistry Department, Lomonosov Moscow State University, Russian Federation, 119991 Moscow, 1-3 Leninskiye Gory

*Corresponding author

E-mail: buinov.aleksandr.96@mail.ru

Figure S1. Experimental design of subcutaneous implantation in rats.

Figure S2. Macrophotographs of porous chitosan-based scaffolds crosslinked with PEGDA: (a) CS-PEGDA 9.8, (b) CS-PEGDA 9.8 G1, (c) CS-PEGDA 9.8 G2, (d) CS-PEGDA 21.3 G2, (e) CS-PEGDA 35.1 G2.

Table S1. Criteria for semi-quantitative evaluations of morphological parameters of skin samples with implanted material according to a five-point scale

| Parameter | Evaluation criteria | Grade |
| --- | --- | --- |
| Inflammatory reaction in the dermis (infiltration of lymphocytes, macrophages, neutrophils) | Absent | 0 |
|  | Single immune cells | 1 |
|  | Several clusters of immune cells | 2 |
|  | Multiple clusters of immune cells | 3 |
|  | Significant diffuse infiltration of immune cells | 4 |
| Exudative inflammation in the implant (neutrophil infiltration) | Absent | 0 |
|  | Single neutrophils on the implant surface | 1 |
|  | Individual small clusters of neutrophils in the pores of the implant, occupying ~ 1/3 of the implant area | 2 |
|  | Numerous clusters of neutrophils in the pores of the implant, occupying ~ 1/2 of the implant area | 3 |
|  | All pores of the implant are filled with neutrophilic detritus and fibrin | 4 |
| Infiltration of the implant by macrophages and giant multinucleated cells | Absent | 0 |
|  | Single immune cells | 1 |
|  | Several clusters of immune cells | 2 |
|  | Multiple clusters of immune cells | 3 |
|  | Significant diffuse infiltration by immune cells | 4 |
| Implant resorption | Absent | 0 |
|  | Single fibers of the implant material are loosened and undergo cellular resorption | 1 |
|  | Several clusters of resorptions of the implant material along the periphery | 2 |
|  | Multiple clusters of resorptions of the material over the entire area of ​​the implant | 3 |
|  | Significant resorptions of the entire implant material | 4 |
| Implant ingrowth by connective tissue | Absent | 0 |
|  | Single strands of connective tissue penetrating the surface layer of the implant | 1 |
|  | Few strands of connective tissue penetrating 1/3 of the implant thickness | 2 |
|  | Numerous strands of connective tissue penetrating 1/2 of the implant thickness | 3 |
|  | Numerous strands of connective tissue penetrating the entire implant | 4 |
| Connective tissue capsule around the implant | Absent | 0 |
|  | Very thin (10-50 µm) with minimal inflammatory infiltration and vascularization | 1 |
|  | Thin (50-200 µm) with weak inflammatory infiltration and vascularization | 2 |
|  | Fairly thick (200-400 µm) with moderate inflammatory infiltration and vascularization | 3 |
|  | Significant thickness (more than 400 µm) with pronounced inflammatory infiltration and vascularization | 4 |