Supporting Information

Hierarchical Porous Aero-Cryogels for Wind Energy Enhanced Solar Vapor Generation

Shuai Lia, Xiaochun Yanga, Yingying Hea, Yanan Wanga, Daogui Liaoa, Yunhua Chen*b, Huihong Xie*a, Hongxia Liu*a, Li Zhoua

a Guangxi Key Laboratory of Optical and Electronic Materials and Devices, and College of Material Science & Engineering, Guilin University of Technology, Guilin 541004, China

b School of Materials Science and Engineering, South China University of Technology, Guangzhou 510640, China

*Corresponding author

E-mail: yhchen0723@gmail.com (Y. Chen), huihong0917@foxmail.com (H. Xie), hliu28551@gmail.com (H. Liu)

1. Characterization

1.1. Measurement of equivalent evaporation enthalpy of water in SVGs

According to a previous study (Zhou, Zhao, Guo, Rosenberger, & Yu, 2019), a control experiment was designed to estimate the actual vaporization enthalpy. Water and A-CGs were simultaneously placed within the same evaporation area in a closed and insulated container. The humidity of the closed environment was kept constant by using silica gel. The actual evaporation enthalpy (Eaee) of the water in the A-CGs can be estimated as follows:

|  | Uin=E0m0=Eaeemg | (S1) |
| --- | --- | --- |

where Uin is the energy input; E0 and m0 are the evaporation enthalpy under atmospheric pressure (2260 J g-1) and the mass change of water, respectively; mg is the mass change of the A-CGs.

1.2. Measurement of thermal conductivity

The thermal conductivity was measured at room temperature using an IR imaging method (Tao et al., 2018). A sample piece with a thickness of 3.0 mm was sandwiched between two 3.0-mm glasses. The sandwich structure was placed between a heating source and a cooling source, and the temperature at the three interfaces was monitored. The heat transfer rate (q) permeating the sample and the thermal conductivity of sample (k) were calculated using the Fourier Equation, as follows:

|  | q=-k1T2-T1d1=-kT3-T2d2 | (S2) |
| --- | --- | --- |

where k1 is the thermal conductivity of glass (1.05 W m-1 K-1); T1, T2, T3 are the average temperature at the interface between the heating source and the hot glass, the hot glass and the sample, and the cold glass and the sample, respectively; d1 and d2 (3.0 mm) are the thickness of the glass and sample, respectively.

1.3. Energy balance analysis during evaporation

Solar energy was used as the energy source in the evaporation process, and the input energy flux was 1 kw m-2 when irradiated by 1 Sun of sunlight. There are five main strategies for energy consumption, as follows (Chen et al., 2019; Li et al., 2020; Xu et al., 2017): (1) water evaporation (ηth), (2) reflection energy loss (ηref), (3) radiation (ηrad) heat loss from the SVG to the environment, (4) convection (ηconv) heat loss to the environment and (5) conductive (ηcond) heat loss to the water.

1) The value of ηth can be determined by Equation 2, as has been discussed in detail in this paper. The ηth of A-CG and A-CG/F is 82.1% and 93.6%, respectively.

2) The ηref can be obtained using an ultraviolet-visible near-infrared spectrophotometer, and the refection loss is approximately 2%.

3) The ηrad was analyzed using the Stefan-Boltzmann Equation, as follows:

|  | Qrad=εAσ(T14-T24) | （S3） |
| --- | --- | --- |

where Qrad represents the heat flux, ε is the emissive rate (the evaporator has a emissivity of 0.95, as determined by an IR camera), A is the evaporation surface area (approximately 10.17 cm2 for A-CG, approximately 8 cm2 for the A-CG/F top area, and approximately 10 cm2 for the A-CG/F side area), σ is the Stefan-Boltzmann constant (5.670373×10-8 W m-2 K-4), T1 is the surface temperature of the SVG (308.25 K for the A-CG, 307.65 K for the A-CG/F top area, 302.15 K for the A-CG/F side area), and T2 is the ambient temperature (299.15 K) in this experiment.

|  | ηrad=QradPin | （S4） |
| --- | --- | --- |

Therefore, based on Equation S3 and S4, the ηrad of A-CG is approximately 5.5%. The ηrad of A-CG/F is approximately 5.8%, including the top surface loss of approximately 4.1% and the side surface loss of approximately 1.7%.

4) The value of ηconv can be calculated based on Newton’s law of cooling.

|  | Qconv=hA∆T | （S5） |
| --- | --- | --- |

where Qconv is the heat energy, h denotes the convection heat transfer coefficient (approximately 5 W m−2 K−1) (Li et al., 2020); A represents the surface area; ∆T is the difference between the ambient temperature around the evaporator and the surface temperature of the evaporator. Therefore, based on Equation S5, the ηconv value of A-CG is approximately 4.5%. The ηconv of A-CG/F is approximately 5.7%, including the top surface loss of approximately 4.2% and the side surface loss of approximately 1.5%.

5) The heat flux of conduction Qcond can be calculated as follows:

|  | Qcond=cm∆T | （S6） |
| --- | --- | --- |

where Qcond denotes the heat energy, c is the specific heat capacity of pure water (4.2 kJ °C-1 kg-1), m represents the weight of bulk water (40 g), and ∆T is the increased temperature of the bulk water after stable steam generation (2.5 °C for A-CG, 0.1 °C for A-CG/F). Therefore, the conduction heat loss of A-CG is approximately 11.4%, and the conduction heat loss of A-CG/F is approximately 0.5%.

2. Supplementary Table

Table S1. Cryogel formulation

| Sample code | CMC aqueous dispersion (ml) | PANI solution (ml) | Water (ml) | GA (ml) |
| --- | --- | --- | --- | --- |
| CG-0 | 12 | 0 | 1.15 | 0.3 |
| CG-2 | 12 | 0.29 | 0.86 | 0.3 |
| CG-5 | 12 | 0.72 | 0.43 | 0.3 |
| CG-8 | 12 | 1.15 | 0 | 0.3 |

Table S2. Photothermal materials, substrate, working mechanism, energy source and evaporation rate of between our work and other reported SVGs

| Photothermal materials | Substrate | SVG above the water surface | Supplemented energy | E. R.* | Ref |
| --- | --- | --- | --- | --- | --- |
| CNT* | CNF aerogel | No | No | 1.11 | (Jiang et al., 2018) |
| CNT | Carbon aerogel | No | No | 1.44 | (Mu et al., 2019) |
| PHS* | PVA* hydrogel* | No | No | 1.83 | (Tan, Wang, Song, Fang, & Zhang, 2019) |
| PANI | PEGDA* hydrogel | No | No | 1.40 | (Yin et al., 2018) |
| rGO* | PVA hydrogel | No | No | 2.50 | (Zhou, Zhao, Guo, Zhang, & Yu, 2018) |
| PPy | PVA/chitosan hydrogel | No | No | 3.6 | (Zhou et al., 2019) |
| PPy | PVDF* membrane | No | No | 0.92 | (Wang et al., 2018) |
|  |  | Yes |  | 1.70 |  |
| PPy | Cotton fabric | No | No | 1.54 | (Xiao et al., 2019) |
|  |  | Yes |  | 3.37 |  |
| CB* | PAN aerogel | No | No | 0.83 | (Chen et al., 2020) |
|  |  | Yes |  | 1.31 |  |
| CB | Cotton core | Yes | Heat | 1.62 | (Li et al., 2018) |
| CB | Bacterial Cellulose Aerogel | No | No | 0.84 | (Li et al., 2020) |
|  |  | Yes | No | 1.82 |  |
|  |  | Yes | Wind (4 m/s) | 4.32 |  |
| PANI | CMC hydrogel | No | No | 1.84 | This work |
|  |  | Yes | No | 2.16 |  |
|  |  | Yes | Wind (3 m/s) Heat | 5.67 |  |

*Evaporation rate (E. R.), carbon nanotube (CNT), polymer hollow spheres (PHS), polyvinyl alcohol (PVA), hydrogel (cryogel completely swollen with water), poly(ethylene glycol) diacrylate (PEGDA), reduced graphene oxide (RGO), polyvinylidene fluoride (PVDF).

4. Supplementary figures

Fig. S1. Cryogel sinking after complete swelling

Fig. S2. The water contact angle of CNF aerogel, CNF/PLA aerogel, CNF/PLA aerogel cross-linked by GA and digital photos of aerogels soaked in water for different time

Fig. S3. Compressive stress-strain curves of aerogels

Fig. S4. Aerogels prepared by different molds

Fig. S5. The aerogel lifts the swollen cryogel and petri dish through strong interface bonding force.

Fig. S6. Aero-cryogels in harsh conditions

Fig. S7. Water diffusion in GA-crosslinked CNF/PLA aerogel

Fig. S8. The water contact angle of CGs

Fig. S9. Thermal conductivities of aerogel filled with water and swollen cryogels

Fig. S10. A-CG/F with salt crystals and the salts were extracted to the 3.5 wt% NaCl solution

Fig. S11. A schematic diagram of an artificial optical device that simulates water evaporation measurement in a windy environment

Fig. S12. Infrared thermal images showing temperature distribution of A-CG/F under irradiation of 1 Sun at different wind speeds for 900 s

References

Chen, G., Li, N., He, J., Qiao, L., Li, F., Wang, S., & Xu, X. (2020). Design of self-righting steam generators for solar-driven interfacial evaporation and self-powered water wave detection. Journal of Materials Chemistry A, 8(46), 24664-24674.

Chen, Y., Shi, Y., Kou, H., Liu, D., Huang, Y., Chen, Z., & Zhang, B. (2019). Self-Floating Carbonized Tissue Membrane Derived from Commercial Facial Tissue for Highly Efficient Solar Steam Generation. ACS Sustainable Chemistry & Engineering, 7(3), 2911-2915.

Jiang, F., Liu, H., Li, Y., Kuang, Y., Xu, X., Chen, C., & Hu, L. (2018). Lightweight, Mesoporous, and Highly Absorptive All-Nanofiber Aerogel for Efficient Solar Steam Generation. ACS Applied Materials & Interfaces, 10(1), 1104-1112.

Li, N., Qiao, L., He, J., Wang, S., Yu, L., Murto, P., & Xu, X. (2020). Solar‐Driven Interfacial Evaporation and Self‐Powered Water Wave Detection Based on an All‐Cellulose Monolithic Design. Advanced Functional Materials, 31(7), 2008681.

Li, X., Li, J., Lu, J., Xu, N., Chen, C., Min, X., & Zhu, J. (2018). Enhancement of Interfacial Solar Vapor Generation by Environmental Energy. Joule, 2(7), 1331-1338.

Mu, P., Zhang, Z., Bai, W., He, J., Sun, H., Zhu, Z., & Li, A. (2019). Superwetting Monolithic Hollow-Carbon-Nanotubes Aerogels with Hierarchically Nanoporous Structure for Efficient Solar Steam Generation. Advanced Energy Materials, 9(1), 1802158.

Tan, M., Wang, J., Song, W., Fang, J., & Zhang, X. (2019). Self-floating hybrid hydrogels assembled with conducting polymer hollow spheres and silica aerogel microparticles for solar steam generation. Journal of Materials Chemistry A, 7(3), 1244-1251.

Tao, P., Ni, G., Song, C., Shang, W., Wu, J., Zhu, J., & Deng, T. (2018). Solar-driven interfacial evaporation. Nature Energy, 3(12), 1031-1041.

Wang, Y., Wang, C., Song, X., Huang, M., Megarajan, S. K., Shaukat, S. F., & Jiang, H. (2018). Improved light-harvesting and thermal management for efficient solar-driven water evaporation using 3D photothermal cones. Journal of Materials Chemistry A, 6(21), 9874-9881.

Xiao, P., Gu, J., Zhang, C., Ni, F., Liang, Y., He, J., & Chen, T. (2019). A scalable, low-cost and robust photo-thermal fabric with tunable and programmable 2D/3D structures towards environmentally adaptable liquid/solid-medium water extraction. Nano Energy, 65, 104002.

Xu, N., Hu, X., Xu, W., Li, X., Zhou, L., Zhu, S., & Zhu, J. (2017). Mushrooms as Efficient Solar Steam-Generation Devices. Advanced Materials, 29 (28), 1606762.

Yin, X., Zhang, Y., Guo, Q., Cai, X., Xiao, J., Ding, Z., & Yang, J. (2018). Macroporous Double-Network Hydrogel for High-Efficiency Solar Steam Generation Under 1 sun Illumination. ACS Applied Materials & Interfaces, 10(13), 10998-11007.

Zhou, X., Zhao, F., Guo, Y., Rosenberger, B., & Yu, G. (2019). Architecting highly hydratable polymer networks to tune the water state for solar water purification. Science Advances, 5(6), eaaw5484.

Zhou, X., Zhao, F., Guo, Y., Zhang, Y., & Yu, G. (2018). A hydrogel-based antifouling solar evaporator for highly efficient water desalination. Energy & Environmental Science, 11(8), 1985-1992.