USE OF MORINGA OLEIFERA SEEDS AS A BIOSORBENT AND ANTIMICROBIAL AGENT IN ACIDIC MINERAL EFFLUENTS

ENVIRONMENTAL PROCESSES

*PAULINE NCUBE, FREEMAN NTULI, THABO FALAYI

DEPARTMENT OF CHEMICAL ENGINEERING, UNIVERSITY OF JOHANNESBURG

P.O BOX 17011, DOORNFONTEIN 2028, JOHANNESBURG

SOUTH AFRICA

ppncube01@gmail.com

ANOVA ANALYSIS for the effect of pH, temperature, time, and solid loading on biosorption (S1) and antimicrobial activity of MO seed extract (S2)

Effect of solid loading

Table S1 Anova, Single Factor- Ni

| SUMMARY |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Groups | Count | Sum | Average | Variance |  |  |
| 0.08 | 3 | 280.3744 | 93.45813 | 0.242686 |  |  |
| 0.1 | 3 | 294.2287 | 98.07623 | 0.101948 |  |  |
| ANOVA |  |  |  |  |  |  |
| Source of Variation | SS | df | MS | F | P-value | F crit |
| Between Groups | 31.99028 | 1 | 31.99028 | 185.6481 | 0.000168 | 7.708647 |
| Within Groups | 0.689267 | 4 | 0.172317 |  |  |  |
| Total | 32.67954 | 5 |  |  |  |  |

| Table S1.1 Anova, Single Factor- Cu |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SUMMARY |  |  |  |  |  |  |  |  |
| Groups | Count | Sum | Average | Variance |  |  |  |
| 0.08 | 3 | 265.8786 | 88.62621 | 0.385244 |  |  |  |
| 0.1 | 3 | 285.2595 | 95.08649 | 0.080356 |  |  |  |
| ANOVA |  |  |  |  |  |  |  |
| Source of Variation | SS | df | MS | F | P-value |  | F crit |
| Between Groups | 62.60275 | 1 | 62.60275 | 268.9123 | 8.1E-05 |  | 7.708647 |
| Within Groups | 0.9312 | 4 | 0.2328 |  |  |  |  |
| Total | 63.53395 | 5 |  |  |  |  |  |

Table S1.2 Anova, Single Factor-Mn

Summary

| Groups | Count | Sum | Average | Variance |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| 0.08 | 3 | 24.13982 | 8.046608 | 0.00989 |  |  |
| 0.1 | 3 | 24.85377 | 8.284589 | 0.018341 |  |  |
| ANOVA |  |  |  |  |  |  |
| Source of Variation | SS | df | MS | F | P-value | F crit |
| Between Groups | 0.084952 | 1 | 0.084952 | 6.018326 | 0.070201 | 7.708647 |
| Within Groups | 0.056463 | 4 | 0.014116 |  |  |  |
| Total | 0.141415 | 5 |  |  |  |  |

| Effect of pH Table S1.3 Anova, Single Factor-Ni |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| SUMMARY |  |  |  |  |  |  |
| Groups | Count | Sum | Average | Variance |  |  |
| pH2 | 3 | 173.6259 | 57.8753 | 0.272443 |  |  |
| pH3 | 3 | 292.8004 | 97.60015 | 0.418392 |  |  |
| ANOVA |  |  |  |  |  |  |
| Source of Variation | SS | df | MS | F | P-value | F crit |
| Between Groups | 2367.095 | 1 | 2367.095 | 6852.849 | 1.28E-07 | 7.708647 |
| Within Groups | 1.381671 | 4 | 0.345418 |  |  |  |
| Total | 2368.477 | 5 |  |  |  |  |

| Table S1.4 Anova, Single Factor-Cu |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| SUMMARY |  |  |  |  |  |  |
| Groups | Count | Sum | Average | Variance |  |  |
| pH2 | 3 | 160.4421 | 53.48069 | 0.203447 |  |  |
| pH3 | 3 | 272.064 | 90.688 | 0.42732 |  |  |
| ANOVA |  |  |  |  |  |  |
| Source of Variation | SS | df | MS | F | P-value | F crit |
| Between Groups | 2076.576 | 1 | 2076.576 | 6584.296 | 1.38E-07 | 7.708647 |
| Within Groups | 1.261533 | 4 | 0.315383 |  |  |  |
| Total | 2077.838 | 5 |  |  |  |  |

| Table S1.5 Anova, Single Factor-Fe |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| SUMMARY |  |  |  |  |  |  |
| Groups | Count | Sum | Average | Variance |  |  |
| pH2 | 3 | 120.4556 | 40.15187 | 0.430004 |  |  |
| pH3 | 3 | 189.1218 | 63.04059 | 0.009489 |  |  |
| ANOVA |  |  |  |  |  |  |
| Source of Variation | SS | df | MS | F | P-value | F crit |
| Between Groups | 785.8401 | 1 | 785.8401 | 3576.124 | 4.68E-07 | 7.708647 |
| Within Groups | 0.878985 | 4 | 0.219746 |  |  |  |
| Total | 786.719 | 5 |  |  |  |  |

| Table S1.6 Anova, Single Factor-Mn |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| SUMMARY |  |  |  |  |  |  |
| Groups | Count | Sum | Average | Variance |  |  |
| pH2 | 3 | 87.92469 | 29.30823 | 0.028587 |  |  |
| pH3 | 3 | 107.6351 | 35.87837 | 0.038914 |  |  |
| ANOVA |  |  |  |  |  |  |
| Source of Variation | SS | df | MS | F | P-value | F crit |
| Between Groups | 64.7501 | 1 | 64.7501 | 1918.515 | 1.62E-06 | 7.708647 |
| Within Groups | 0.135 | 4 | 0.03375 |  |  |  |
| Total | 64.8851 | 5 |  |  |  |  |

Effect of contact time

Table S1.7 Anova, Single Factor- Ni

| SUMMARY |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Groups | Count | Sum | Average | Variance |  |  |
| 30mins | 3 | 204.1592 | 68.05305 | 0.024889 |  |  |
| 60mins | 3 | 264.0077 | 88.00256 | 0.006693 |  |  |
| 90mins | 3 | 266.9598 | 88.98659 | 0.020167 |  |  |
| ANOVA |  |  |  |  |  |  |
| Source of Variation | SS | df | MS | F | P-value | F crit |
| Between Groups | 837.1642 | 2 | 418.5821 | 24265.87 | 1.89E-12 | 5.143253 |
| Within Groups | 0.103499 | 6 | 0.01725 |  |  |  |
| Total | 837.2677 | 8 |  |  |  |  |

| Table S1.8 Anova, Single Factor- Cu |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| SUMMARY |  |  |  |  |  |  |
| Groups | Count | Sum | Average | Variance |  |  |
| 30mins | 3 | 192.4529 | 64.15097 | 0.109183 |  |  |
| 60mins | 3 | 209.6785 | 69.89282 | 0.154283 |  |  |
| 90mins | 3 | 243.5315 | 81.17715 | 0.068595 |  |  |
| ANOVA |  |  |  |  |  |  |
| Source of Variation | SS | df | MS | F | P-value | F crit |
| Between Groups | 450.1958 | 2 | 225.0979 | 2033.638 | 3.2E-09 | 5.143253 |
| Within Groups | 0.664124 | 6 | 0.110687 |  |  |  |
| Total | 450.8599 | 8 |  |  |  |  |

| Table S1.9 Anova: Single Factor- Fe |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| SUMMARY |  |  |  |  |  |  |
| Groups | Count | Sum | Average | Variance |  |  |
| 30mins | 3 | 117.9466 | 39.31552 | 5.53E-05 |  |  |
| 60mins | 3 | 138.0033 | 46.00111 | 0.010088 |  |  |
| 90mins | 3 | 177.6942 | 59.23141 | 9.64E-05 |  |  |
| ANOVA |  |  |  |  |  |  |
| Source of Variation | SS | df | MS | F | P-value | F crit |
| Between Groups | 616.3803 | 2 | 308.1901 | 90291.95 | 3.67E-14 | 5.143253 |
| Within Groups | 0.02048 | 6 | 0.003413 |  |  |  |
| Total | 616.4008 | 8 |  |  |  |  |

| Effect of temperature Table S1.10 Anova, Single Factor-Ni |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| SUMMARY |  |  |  |  |  |  |  |
| Groups | Count | Sum | Average | Variance |  |  |  |
| 298K | 3 | 231.3506 | 77.11686 | 4.3E-05 |  |  |  |
| 308K | 3 | 297.3137 | 99.10455 | 2.68E-05 |  |  |  |
| 318K | 3 | 278.6848 | 92.89494 | 3E-05 |  |  |  |
| ANOVA |  |  |  |  |  |  |  |
| Source of Variation | SS | df | MS | F |  | P-value | F crit |
| Between Groups | 770.9658 | 2 | 385.4829 | 11577504 |  | 1.74E-20 | 5.143253 |
| Within Groups | 0.0002 | 6 | 3.33E-05 |  |  |  |  |
| Total | 770.966 | 8 |  |  |  |  |  |

| Table S1.11 Anova, Single Factor-Cu |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| SUMMARY |  |  |  |  |  |  |
| Groups | Count | Sum | Average | Variance |  |  |
| 298K | 3 | 243.825 | 81.27501 | 0.012139 |  |  |
| 308K | 3 | 294.1867 | 98.06222 | 0.003762 |  |  |
| 318K | 3 | 272.1838 | 90.72792 | 4.36E-05 |  |  |
| ANOVA |  |  |  |  |  |  |
| Source of Variation | SS | df | MS | F | P-value | F crit |
| Between Groups | 424.9595 | 2 | 212.4798 | 39976.61 | 4.23E-13 | 5.143253 |
| Within Groups | 0.031891 | 6 | 0.005315 |  |  |  |
| Total | 424.9914 | 8 |  |  |  |  |

| Table S1.12 Anova, Single Factor-Fe |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SUMMARY |  |  |  |  |  |  |  |  |  |
| Groups | Count | Sum | Average | Variance |  |  |  |  |  |
| 298K | 3 | 209.8591 | 69.95304 | 3.36E-08 |  |  |  |  |  |
| 308K | 3 | 285.3757 | 95.12522 | 9.23E-05 |  |  |  |  |  |
| 318K | 3 | 250.2418 | 83.41392 | 1.52E-05 |  |  |  |  |  |
| ANOVA |  |  |  |  |  |  |  |  |  |
| Source of Variation | SS | df | MS | F |  | P-value |  | F crit |  |
| Between Groups | 951.9885 | 2 | 475.9942 | 13273678 |  | 1.15E-20 |  | 5.143253 |  |
| Within Groups | 0.000215 | 6 | 3.59E-05 |  |  |  |  |  |  |
| Total | 951.9887 | 8 |  |  |  |  |  |  |  |
| Table S1.13 Anova, Single Factor- Mn |  |  |  |  |  |  |  |  |
| SUMMARY |  |  |  |  |  |  |  |  |
| Groups | Count | Sum | Average | Variance |  |  |  |  |
| 298K | 3 | 83.77101 | 27.92367 | 7.31E-05 |  |  |  |  |
| 308K | 3 | 90.22867 | 30.07622 | 0.002908 |  |  |  |  |
| 318K | 3 | 60.27962 | 20.09321 | 0.00096 |  |  |  |  |
| ANOVA |  |  |  |  |  |  |  |  |
| Source of Variation | SS | df | MS | F | P-value |  | F crit |  |
| Between Groups | 165.6103 | 2 | 82.80514 | 63022.03 | 1.08E-13 |  | 5.143253 |  |
| Within Groups | 0.007883 | 6 | 0.001314 |  |  |  |  |  |
| Total | 165.6182 | 8 |  |  |  |  |  |  |

Antimicrobial activity of MO seed extract

Table S2 Anova, Two-Factor without Replication

| SUMMARY | Count | Sum | Average | Variance |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| 50 | 2 | 39 | 19.5 | 144.5 |  |  |
| 100 | 2 | 18 | 9 | 98 |  |  |
| 150 | 2 | 8 | 4 | 32 |  |  |
| Crude | 3 | 52 | 17.33333 | 101.3333 |  |  |
| Aqueous | 3 | 13 | 4.333333 | 34.33333 |  |  |
| ANOVA |  |  |  |  |  |  |
| Source of Variation | SS | df | MS | F | P-value | F crit |
| Rows | 250.3333 | 2 | 125.1667 | 11.92063 | 0.077396 | 19 |
| Columns | 253.5 | 1 | 253.5 | 24.14286 | 0.039012 | 18.51282 |
| Error | 21 | 2 | 10.5 |  |  |  |
| Total | 524.8333 | 5 |  |  |  |  |