Extended Data Table 1 | Comparison of swelling characterization techniques.

| Type | In-situ detection | Dynamic detection | Detection parameters | Temporal resolution | Spatial resolution | Detection range | Ref |
| --- | --- | --- | --- | --- | --- | --- | --- |
| EQCM-D | No | Yes | Film quality | ~5 ms | No | sub-ng ~ μg | 8,15,18,53-58 |
| GIWAXS | Yes | No | Crystal lattice | No | ~mm | / | 15,18,19,59 |
| 4D-STEM | No | No | Crystal lattice | No | ~10 nm | / | 17 |
| AFM | Yes | No | Film thickness | No | ~0.1 nm (X/Y axis) ~10 pm (Z axis) | pm ~ μm | 16,18 |
| ESM | Yes | No | Film thickness | No | ~0.1 nm (X/Y axis) ~10 pm (Z axis) | pm ~ μm | 16,18 |
| LDV-M | Yes | Yes | Film thickness | ~10 ns | ~1 μm (X/Y axis) ~600 pm (Z axis) | nm ~ mm | This work |

Extended Data Fig. 1 | Representative transfer curves of vOECTs with different OMIECs. (a)BBL; (b) Homo-gDPP:GDA; (c) Homo-gDPP:DA; (d) p(g2T-T):GDA; (e) p(g2T-T):DA; (f) gDPP-g2T:GDA; (g) gDPP-g2T:DA.

Extended Data Fig. 2 | Single-point swelling behavior of OECT channels based on various polymers. Swelling behavior of vOECT channels based on (a) Homo-gDPP:GDA, (b) Homo-gDPP:DA, (c) p(g2T-T):GDA, (d) p(g2T-T):DA, (e) gDPP-g2T:GDA, and (f) gDPP-g2T:DA, respectively, under switching frequencies of 3.3 Hz, 11.1 Hz, and 111.1 Hz. g, Illustration of the planar OECT. h, Laser spot position of LDV-M on a planar OECT based on BBL and single point swelling behaviors. i, Laser spot position of LDV-M on a planar OECT based on p(g2T-T):GDA and single point swelling behaviors. 3.3Hz VG switching frequency is applied. Note that the active swelling magnitudes in planar OECTs are obviously larger than those in vOECTs (Figs. 2c and Extended Data Fig. 2c), indicating that vertical architecture can effectively suppress the swelling of the channel39.

Extended Data Fig. 3 | Laser spot position during mapping. 3D swell mapping is performed by subsequently monitoring the swelling of each point. Specifically, starting from the lower left corner (1,1), the system collects the swelling data step-by-step from (1,1) to (6,1), then moves to (2,1), continuing to collect the data from (2,y). Following this sequence, swelling of the whole vOECT channel is measured point-by-point until reaching point (6,4). Note, the displacement process is controlled by the planar electrical positioning stage, which enables displacement regulation with 1 μm precision. Note, faster mapping can be enabled with a laser equipped with a micro mirror, where the mirror controls the laser spot on the channel, instead of by moving the stage holding the OECT.

Extended Data Fig. 4 | 3D swell mapping of BBL channel under different switching frequencies and different cycles. a-b, 3D swell mapping under 3.3 Hz and 111.1 Hz switching frequencies, along with an ID switching cycle and corresponding 3D swell mapping frames for each. c, 3D swell mapping of BBL-based vOECT during indicated cycling numbers (111.1 Hz switching frequency).

Extended Data Fig. 5 | 3D swell mappings of vOECTs based on different polymers. a, p(g2T-T):GDA, (b) p(g2T-T):DA, (c) Homo-gDPP:GDA, (d) Homo-gDPP:DA, (e) gDPP-g2T:GDA, (f) gDPP-g2T:DA-based vOECTs. Note, the doping and dedoping frames are all from a 3.3 Hz switching frequency upon a relatively stable ID after 15 switching cycles.

Extended Data Fig. 6 | Effect of vertical Coulombic forces on swelling. (a) BBL, (b) p(g2T-T):GDA, (c) Homo-gDPP:GDA, and (d) gDPP-g2T:GDA-based vOECTs demonstrating the optical microscope images of the channels with a laser spot positioned at location (3,1), along with the channel swelling behaviors with two different bias situations (VD = 0.1 V, VS = 0 V; or VD = VS = 0 V).

Extended Data Fig. 7 | Transfer characteristics of vOECTs with conventional or optimized encapsulations after indicated switching cycles, along with their ID switching transient times. Transfer characteristic curves of vOECTs based on different materials (BBL, Homo-gDPP:DA, Homo-gDPP:GDA, p(g2T-T):DA, p(g2T-T):GDA, gDPP-g2T:DA, and gDPP-g2T:GDA) under (a) optimized encapsulations and (b) conventional encapsulations at different switching cycles. c, Their transient response times under different encapsulation methods (Standard deviations are based on the performance of at least 3 devices).

Extended Data Fig. 8 | Cycling stability of vOECTs. During cyclic stability measurements: ID current decay trends, transconductance curves, and gm_max decay trends for (a) p(g2T-T):DA and (b) Homo-gDPP:DA-based vOECTs; and for (c) BBL-based vOECT, these parameters plus ID current curves.

Extended Data Fig. 9 | vOECNs spiking characteristics. (a–c) Spiking patterns under different input currents at Cmem = 500 pF and VDD = 0.6, 0.7, 0.8 V. (d, e) spiking patterns at VDD = 0.7 V with IIN = 0.5, 1, 5, 10, 50 μA and Cmem = 10, 50 nF. The vOECN circuit operates as follows: the IIN is integrated through the Cmem, causing the membrane voltage (Vmem) to gradually increase. When Vmem reaches a specific threshold, the output terminal generates neuron-like pulses (Vfire). Specifically, the amplification module exhibits a steep increase in gain when Vmem exceeds the transition voltage (VT), driving the rise of Vfire. When Vfire reaches a sufficient level, Treset is conducted, discharging Cmem and decreasing Vmem. Once Vmem drops back to VT, the feedback loop activates, causing Vfire to decrease in response to minor changes in Vmem rapidly. Eventually, Vfire returns to its initial state, Treset turns off, terminating the pulse and initiating the next cycle.

References

53	Maria, I. P. et al. The Effect of Alkyl Spacers on the Mixed Ionic‐Electronic Conduction Properties of N‐Type Polymers. Adv. Funct. Mater. 31, 2008718 (2021). https://doi.org/10.1002/adfm.202008718

54	Nicolini, T. et al. A Low‐Swelling Polymeric Mixed Conductor Operating in Aqueous Electrolytes. Adv. Mater. 33, 2005723 (2020). https://doi.org/10.1002/adma.202005723

55	Sun, Z. et al. Controlling Ion Uptake in Carboxylated Mixed Conductors. Adv. Mater. 37, 2414963 (2024). https://doi.org/10.1002/adma.202414963

56	Ohayon, D., Druet, V. & Inal, S. A guide for the characterization of organic electrochemical transistors and channel materials. Chem. Soc. Rev. 52, 1001-1023 (2023). https://doi.org/10.1039/d2cs00920j

57	Jackson, S. R., Kingsford, R. L., Collins, G. W. & Bischak, C. G. Crystallinity Determines Ion Injection Kinetics and Local Ion Density in Organic Mixed Conductors. Chem. Mater. 35, 5392-5400 (2023). https://doi.org/10.1021/acs.chemmater.3c00657

58	Wu, R., Paulsen, B. D., Ma, Q. & Rivnay, J. Mass and Charge Transport Kinetics in an Organic Mixed Ionic–Electronic Conductor. Chem. Mater. 34, 9699-9710 (2022). https://doi.org/10.1021/acs.chemmater.2c02476

59	Paulsen, B. D. et al. Time-Resolved Structural Kinetics of an Organic Mixed Ionic–Electronic Conductor. Adv. Mater. 32, 2003404 (2020). https://doi.org/https://doi.org/10.1002/adma.202003404