Assessing strong consistency of symmetrical solid-state supercapacitors based on three-dimensional porous carbon material

P.A. Le1, Van Qui Le2,3, Thi Viet Bac Phung1*, Nghia Trong Nguyen4*

1 Institute of Sustainability Science, Vietnam-Japan University, Vietnam National University-Hanoi, Hanoi, Vietnam.

2 Laboratory of Advanced Materials Chemistry, Advanced Institute of Materials Science,

Ton Duc Thang University, Ho Chi Minh, Vietnam.

3 Faculty of Applied Sciences, Ton Duc Thang University, Ho Chi Minh, Vietnam.

4 School of Chemical Engineering, Hanoi University of Science and Technology, Hanoi, Vietnam.

*Corresponding author:

Nghia Trong Nguyen; E-mail: nghia.nguyentrong@hust.edu.vn

Thi Viet Bac Phung; E-mail: ptv.bac@vju.ac.vn

1 Powder characterization

1.1 BET data in this report

1.1.1 Commercial activated carbon

Summary Report

Surface Area

Single point surface area at P/Po = 0.202185304:    889.2957 m²/g

BET Surface Area:    885.5030 m²/g

Langmuir Surface Area:    1158.6500 m²/g

t-Plot Micropore Area:    552.2905 m²/g

t-Plot External Surface Area:    333.2126 m²/g

BJH Adsorption cumulative surface area of pores

between 1.7000 nm and 300.0000 nm diameter:    245.682 m²/g

BJH Desorption cumulative surface area of pores

between 1.7000 nm and 300.0000 nm diameter:    263.6999 m²/g

Pore Volume

Single point adsorption total pore volume of pores

less than 196.3680 nm diameter at P/Po = 0.990058070:    0.602542 cm³/g

t-Plot micropore volume:    0.249866 cm³/g

BJH Adsorption cumulative volume of pores

between 1.7000 nm and 300.0000 nm diameter:    0.319187 cm³/g

BJH Desorption cumulative volume of pores

between 1.7000 nm and 300.0000 nm diameter:    0.321838 cm³/g

Pore Size

Adsorption average pore width (4V/A by BET):    2.72181 nm

BJH Adsorption average pore diameter (4V/A):    5.1967 nm

BJH Desorption average pore diameter (4V/A):    4.8819 nm

1.1.2 Commercial black carbon

Summary Report

Surface Area

Single point surface area at P/Po = 0.200128086:    51.9548 m²/g

BET Surface Area:    49.6578 m²/g

Langmuir Surface Area:    64.5366 m²/g

t-Plot Micropore Area:    49.0396 m²/g

t-Plot External Surface Area:    0.6183 m²/g

BJH Adsorption cumulative surface area of pores

between 1.7000 nm and 300.0000 nm diameter:    17.463 m²/g

BJH Desorption cumulative surface area of pores

between 1.7000 nm and 300.0000 nm diameter:    21.2019 m²/g

Pore Volume

Single point adsorption total pore volume of pores

less than 354.6759 nm diameter at P/Po = 0.994535210:    0.148730 cm³/g

t-Plot micropore volume:    0.022863 cm³/g

BJH Adsorption cumulative volume of pores

between 1.7000 nm and 300.0000 nm diameter:    0.134164 cm³/g

BJH Desorption cumulative volume of pores

between 1.7000 nm and 300.0000 nm diameter:    0.135393 cm³/g

Pore Size

Adsorption average pore width (4V/A by BET):    11.98043 nm

BJH Adsorption average pore diameter (4V/A):    30.7307 nm

BJH Desorption average pore diameter (4V/A):    25.5436 nm

1.1.3 Carbon P

Summary Report

Surface Area

Single point surface area at P/Po = 0.204014519:    1335.4627 m²/g

BET Surface Area:    1348.1072 m²/g

Langmuir Surface Area:    1783.4169 m²/g

t-Plot Micropore Area:    765.8650 m²/g

t-Plot External Surface Area:    582.2422 m²/g

BJH Adsorption cumulative surface area of pores

between 1.7000 nm and 300.0000 nm diameter:    289.409 m²/g

BJH Desorption cumulative surface area of pores

between 1.7000 nm and 300.0000 nm diameter:    289.0496 m²/g

Pore Volume

Single point adsorption total pore volume of pores

less than 314.5005 nm diameter at P/Po = 0.993829229:    0.655554 cm³/g

t-Plot micropore volume:    0.339081 cm³/g

BJH Adsorption cumulative volume of pores

between 1.7000 nm and 300.0000 nm diameter:    0.193942 cm³/g

BJH Desorption cumulative volume of pores

between 1.7000 nm and 300.0000 nm diameter:    0.190626 cm³/g

Pore Size

Adsorption average pore width (4V/A by BET):    1.94511 nm

BJH Adsorption average pore diameter (4V/A):    2.6805 nm

BJH Desorption average pore diameter (4V/A):    2.6380 nm

1.2 Carbon P

Figure S1 SEM imagine of highly porous carbon P at various magnification.

1.3 Electrochemical characterization

Figure S2 Images of working electrode: carbon P (12), activated carbon (11), and black carbon (10), respectively.

Figure S3 Electrochemical properties of activated carbon and black carbon: (a, b) CV curves and (c, d) GCD curves, respectively.

Electronic Supplementary Video 1

Electronic Supplementary Video 2