Supplementary data

A stepwise-targeting strategy for the treatment of cerebral ischemic stroke

Jingbo Hu1*,#, Xueying Tan2#, Dongwei Wang1, Hongze Liang1, Jiejun Peng3*, Fengyan Li2, Quan Zhou4, Peiwu Geng4, Shuanghu Wang4, Yue Yu5, Jin Liu4*

1 Faculty of Materials Science and Chemical Engineering, Ningbo University, Ningbo 315211, China.

2 College of pharmacy, Zhejiang Pharmaceutical College, Ningbo 315100, China.

3 State Key Laboratory for Managing Biotic and Chemical Threats to the Quality and Safety of Agroproducts, Institute of Plant Virology, Ningbo University, Ningbo 315211, Zhejiang, China.

4 Department of Neurosurgery, The People’s Hospital of Lishui, The Sixth Affiliated Hospital of Wenzhou Medical University, Lishui 323000, China.

5 Department of pharmacy, Ningbo women and children’s hospital, Ningbo 315012, China.

# These authors contributed equally to this paper

Fig. S1 Semi-quantitative fluorescent analysis of live and dead cells.

Fig. S2 1H NMR spectrum of TGN-PEG-PLGA (500 MHz, DMSO-d6).

Fig. S3 1H NMR spectrum of SHp-PEG-PLGA (500 MHz, DMSO-d6).

Fig. S4 Intracellular fluorescence intensity, measured by flow cytometry, of bEnd.3 cells ncubated with TGN/SHp/cy3 micelles for for 0.5 and 2.0 h, TGN/cy3 micelles, SHp/cy3 micelles, cy3 micelles and free cy3 as control (n = 6, P>0.05).

Fig. S5 The transport ratios (%) of HRP across BBB model during 24 h (n = 6).

Fig. S6 Intracellular fluorescence intensity, measured by flow cytometry, of PC-12 cells ncubated with TGN/SHp/cy3 micelles for for 0.5 and 2.0 h, TGN/cy3 micelles, SHp/cy3 micelles, cy3 micelles and free cy3 as control (n = 6, P>0.05).

Table S1 Characterization of TGN/SHp/TPP-MLT micelles (n = 6)

| Feeding ratio (%) | Particle size (nm) | PDI | Zeta potential (mV) | TPP-MLT |  |
| --- | --- | --- | --- | --- | --- |
|  |  |  |  | EE (%) | DL (%) |
| 0 5 10 20 30 40 | 88.6 ± 5.3 84.2 ± 4.8 97.5 ± 4.9 100.4 ± 4.3 102.2 ± 5.1 105.9 ± 5.4 | 0.13 ± 0.09 0.19 ± 0.05 0.18 ± 0.06 0.16 ± 0.04 0.19 ± 0.05 0.17 ± 0.04 | -8.1 ± 0.9 -8.5 ± 0.7 -8.3 ± 0.9 -8.6 ± 0.5 -8.3 ± 0.8 -8.3 ± 1.4 | 90.52 ± 1.23 88.24 ± 1.34 80.45 ± 1.04 74.82 ± 1.22 70.88 ± 1.13 | 4.29 ± 0.55 8.94 ± 0.89 9.11 ± 0.95 9.62 ± 0.84 10.06 ± 0.96 |

PDI, polydispersity index; EE, encapsulation efficiency; DL, drug loading