Gel Permeation Chromatography Process for Highly Oriented Cs3Cu2I5 Nanocrystal Film

Yu-Hong Cheng1, Rikuo Suzuki1, Narumi Shinotsuka1, Hinako Ebe1, Naoaki Oshita2, Ryohei Yamakado1, Takayuki Chiba1 *, Akito Masuhara2, and Junji Kido1 *

1 Graduate School of Organic Materials Science, Yamagata University, 4-3-16 Jonan, Yonezawa, Yamagata 992-8510, Japan
2 Graduate School of Science and Engineering, Yamagata University, 4-3-16 Jonan, Yonezawa, Yamagata 992-8510, Japan
*Corresponding authors
Takayuki Chiba: T-chiba@yz.yamagata-u.ac.jp and Junji Kido: kid@yz.yamagata-u.ac.jp

DFT calculation:

The crystal structure of Cs3Cu2I5 was obtained from SXRD spectra by Rietveld refinement. For slab systems, surface reconstruction and single-point calculations were performed, whereas for the bulk systems, single point calculations were performed at the ZORA-GGA-PBE/DZP theoretical level using the ADF BAND package. In the slab and bulk system, the cif files listed in a separate file were used. For the slab system, two layers of the bulk system were used in the (020) direction, where the surfaces are (020) and (040).

The surface energy was calculated from the following equation:

σ=1A(Eslab-nEbulk)	(1)

where σ is the surface energy, A is the surface area of the slab on both sides, Eslab is the model of the slab system, n is a factor to match the number of atoms in the bulk system with the number of atoms in the slab system, and Ebulk is the energy of the bulk system. The calculation was based on the exact crystal model with infinite boundary of a-axis and c-axis shown in Figure S4 1.

Figure S1 (a) Schematic of hot-injection and typical purification process by adding anti-solvent to the Cs3Cu2I5 dispersion. (b) the SEM of the precipitate of anti-solvent treated dispersion

Figure S2 (a) the TEM image of Cs3Cu2I5 NCs before processing GPC and its (b) size distribution

Figure S3 The XPS spectra of Cs3Cu2I5 film prepared by the dispersion with or without GPC process: (a)Cs 3d, (b) Cu 3p, and (c) I 3p

Figure S4 the calculation is based on the model on a slab of (a) (020) phase and (b) (040) phase

Figure S5 the PL decay of Cs3Cu2I5 film

Figure S6 (a) the photo of dispersion, dried cell, and re-dispersed solution in toluene, (b) the PL spectra, and the (c) PL decay spectra

Table S1 The XPS composition from before and after GPC NCs prepared by spin coating

|  | Cs | Cu | I |
| --- | --- | --- | --- |
| Before GPC | 24.49 | 17.88 | 57.63 |
|  | 26.30 | 20.05 | 53.64 |
|  | 23.82 | 17.59 | 58.57 |
| average | 24.87 | 18.51 | 56.61 |
| After GPC | 26.38 | 17.32 | 56.29 |
|  | 27.99 | 17.04 | 54.98 |
|  | 26.61 | 18.24 | 55.15 |
| average | 26.99 | 17.53 | 55.47 |

Table S2 Single crystal X-ray diffraction data for Cs3Cu2I5 NCs

| Empirical formula | Cs3Cu2I5 |
| --- | --- |
| Temperature | 292(2) K |
| Source | Mo-Ka |
| Crystal system | Orthorhombic |
| Space group | Pnma |
| Unit cell dimensions | a = 10.1824(8) Å, alpha = 90 deg. |
|  | b = 11.6655(11) Å, beta = 90 deg. |
|  | c = 14.3687(12) Å, gamma = 90 deg. |
| Volume | 1706.8(3) Å3 |
| Crystal size | 0.500 × 0.460 × 0.310 mm |
| Z | 4 |
| R1 | 0.0434 |
| wR2 | 0.1120 |
| GOF | 1.126 |

Table S3 The thin film XRD peak information and the comparison of calculated data

| No. | Miller index | Calculated data 2 (deg.) | Thin film 2 (deg.) | d (Å) | FWHM (deg.) |
| --- | --- | --- | --- | --- | --- |
| 1 | (020) | 15.178 | 15.320 | 5.779 | 0.396 |
| 2 | (040) | 30.630 | 30.799 | 2.9008 | 0.401 |
| 3 | (060) | 46.681 | 46.896 | 1.9358 | 0.454 |

Table S4 The optical properties of each Cs3Cu2I5 in different forms.

| Samples | PL (nm) | FWHM (nm) | PLQY (%) | 𝛕avg (µs) |
| --- | --- | --- | --- | --- |
| NCs colloid (Before GPC) | 444 | 73.1 | ~100 | 1.237 |
| NCs colloid (After GPC) | 443 | 73.5 | ~100 | 1.236 |
| NCs re-dispersion | 442 | 72.4 | 98.3 | 1.175 |
| NCs film (GPC purified) | 443 | 74.3 | 79.7 | 1.284 |
| NCs + PMMA | 443 | 74.9 | nd(a) | 1.141 |

a) no data

1. K. Momma, F. Izumi, "VESTA 3 for three-dimensional visualization of crystal, volumetric and morphology data" J. Appl. Crystallogr. 44, 1272 (2011).