Supplementary Information

Sustained CO2-photoreduction activity and high selectivity over C, Mn-codoped ZnO core-triple shell hollow spheres

Sayed et al.

Supplementary Figure S1 FTIR spectra of salicylic acid, Zn acetate and Zn, Mn-CPSs.

Supplementary Figure S2 Morphology of the prepared samples. FESEM of Mn, Zn CPSs precursors a before calcination, after calcination for b 1 h, c 2 h and d 3 h, the inset in d shows the core-triple shell morphology. e FESEM image shows the porosity of  C, Mn-ZnO CTSHSs sample.

Supplementary Figure S3 N2 adsorption-desorption isotherms of Mn, Zn-CPSs precursors, and the precursor after calcination for 1, 2 and 3 h. The inset represents the pore size distribution of the samples.

Supplementary Figure S4 XRD patterns of the prepared samples together with commercial ZnO.

Supplementary Figure S5 Chemical analysis of samples. XPS spectra of C-ZnO and 2%Mn,C-ZnO CTSHSs samples (left panel) and 2%Mn, C-ZnO sample loaded with CO2 under both dark and irradiation conditions (right panel). a, a* The survey spectra of samples and high resolution XPS of b, b* C 1s, c, c* O 1s and d, d* Zn 2p.

Supplementary Figure S6 EDS elemental signals, the inset table represents the weight percentage of each element in the sample.

Supplementary Figure S7 Bandgap estimation of the prepared samples. Tauc plots of prepared C-ZnO and C, Mn-ZnO samples together with comm. ZnO. The results indicate a progressive narrowing of the ZnO-band gap after C and Mn doping.

Supplementary Figure S8 CO2 PR pathway over Mn, C-codoped ZnO photocatalyst. In-situ DRIFTS spectra of photocatalytic CO2 reduction using 2%Mn, C-ZnO CTSHSs sample under dark condition after a 0 min , b 30 min and c 60 min. And under 365 nm LED light irradiation after d 30 min and e 60 min.

Supplementart Table S1 BET surface area (S BET), pore volume (Vpore) and average pore size (Vpore) of the starting Mn, Zn-CPSs and the calcined intermediate products.

| Sample | S BET (m2 g-1) | Vpore (cm3 g-1) | Average pore size (nm) |
| --- | --- | --- | --- |
| Zn-Mn-CPSs | 5.4 | 0.03 | 28 |
| After calcination for 1 h | 9.2 | 0.05 | 29 |
| After calcination for 2 h | 11 | 0.07 | 19 |
| After calcination for 3 h (2% Mn,C-ZnO CTSHSs) | 14 | 0.11 | 28 |
| C-ZnO CTSHSs | 14 | 0.08 | 23 |
| Comm. ZnO | 14 | 0.02 | 7.5 |

Supplementary Table S2 XRD parameters of C, Mn-ZnO CTSHSs with different content of Mn together with Comm. ZnO.

| Sample | Calculated* “a” ( ᵒA) | Calculated “c” ( ᵒA) | Diffraction from “100” plane |  | Diffraction from “101” plane |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  | 2 Theta | d ( ᵒA) | 2 Theta | d ( ᵒA) |
| Comm. ZnO | 3.2588 | 5.2518 | 31.6480 | 2.8222 | 36.0992 | 2.4862 |
| C-ZnO | 3.2529 | 5.1024 | 31.7633 | 2.8152 | 36.3545 | 2.4692 |
| 1% Mn,C-ZnO | 3.2502 | 5.0932 | 31.7802 | 2.8130 | 36.1134 | 2.4852 |
| 2% Mn,C-ZnO | 3.2526 | 5.2360 | 31.7407 | 2.8171 | 36.1991 | 2.4794 |
| 5% Mn,C-ZnO | 3.2466 | 5.2703 | 31.8209 | 2.8099 | 36.2408 | 2.4768 |

Supplementary Table S3 Comparison of CO2 photocatalytic reduction activity of Mn,C-codoped ZnO CTSHSs with some reported systems.

| Catalyst | Irradiation source | Main product | Evolution rate (μmol g-1h-1) | Reference |
| --- | --- | --- | --- | --- |
| TiO2/MXene Ti3C2 composite | 300 W Xe arc lamp | CH4 | 0.22 | 1 |
| g-C3N4/Bi2WO6 composite | 300 W Xe arc lamp | CO | 5.19 | 2 |
| Cu2O/TiO2 composite | 1 kW high-pressure Hg (Xe) arc lamp | CO | 2.11 | 3 |
| MOF-derived ZnO/NiO porous hollow spheres | 300 W Xe arc lamp | CH3OH | 1.57 | 4 |
| Reduced graphene oxide-CdS nanorod composite | 300 W Xe lamp | CH4 | 2.51 | 5 |
| C, Mn-ZnO core-triple shell hollow spheres | 300 W Xe lamp | CH3OH | 11.64 | This work |

Supplementary Table S4 TRPL fitting parameters for the analyzed samples; comm. ZnO, C-ZnO and Mn, C-ZnO CTSHSs.

| Sample | τ1 (ns) (percentage) | τ2 (ns) (percentage) | B1 | B2 | τ(ns) (average)* |
| --- | --- | --- | --- | --- | --- |
| Comm. ZnO | 0.25 (75%) | 2.64 (25 %) | 9113 | 282 | 0.8 |
| C-ZnO | 0.170 (73%) | 2.75 (27 %) | 7251 | 164 | 0.9 |
| 2%Mn,C-ZnO | 0.24 (68%) | 2.83 (32 %) | 8372 | 328 | 1.1 |

Supplementary Note 1

XRD analysis. in Supplementary Figure S4, we can notice (i) the absence of secondary phases arising from the doping process even with 5% Mn loading, (ii) dramatic change of the characteristic diffraction peaks and the apparent contraction on the cell parameters (Supplementary Table S2) of the prepared samples compared to those of typical hexagonal ZnO sample manifests that C and Mn were successfully doped to the ZnO lattice structure rather than attached to the surface. Mn could replace some Zn2+ within the ZnO lattice and may be introduced as Mn (II) or higher oxidation states. After the doping process, prepared ZnO CTSHSs samples exhibit almost lattice contraction ((Supplementary Table S2, as indicated from the lattice constants) which could be attributed to the extremely small ionic radius of C ions replaced the O ions within the lattice (ionic radii= 0.66, 0.58, 0.53, 0.46, 0.6, 0.29 and 1.24 ᵒA for Mn2+, Mn3+ , Mn4+, Mn7+, Zn2+, C4- and  O2-, respectively).6  Based on this fact, it is reasonable to notice such a change in the lattice constants. Furthermore, crystal distortion and surface defects generated within the prepared samples upon C and Mn doping (further confirmed from XPS and DRS results) is very crucial for altering the surface energy of the photocatalysts and providing more active sites for targeted application thus enhance the photocatalytic activity.7

The calculation of the lattice constants “a” and “c” is based on the following equation: 8

1d2=43h2+hk+k2a2+l2c2

where h, k, and l are Miller’s indices. The values of “a” and “c” were derived from this equation by applying the values of the d-spacing of the (100) and (101) planes, respectively, (see Supplementary Table S2).

Supplementary Note 2

XPS interpretation. The XPS survey spectra of C-ZnO and 2%Mn, C-ZnO CTSHSs (untreated and CO2-treated one under both dark and illumination conditions) samples are presented in Supplementary Figure S5a, a*, which show the characteristic peaks for Zn, O, C and Mn. The high resolution XPS of Zn 2p3/2 at ~ 1022 eV assuming Zn2+ state of ZnO in all samples (Supplementary Figure5d).9 The slight chemical shift of this peak to lower binding energies (BEs) after Mn insertion and CO2 loading ascertain the finite Mn substitution of Zn2+ in the lattice of ZnO and an added Zn-Mn binding energy and possible emergence of new Zn-CO2 bond, respectively, which also confirmed from C 1s peak fitting.10,11

The XPS for the O 1s in all samples shows two different oxygen states. That (i) at higher BE is typically associated with loosely bound oxygen (OH) on the surface such as OH groups and O2- ions in oxygen-deficient regions. That (ii) at lower BE is due to lattice oxygen (OL) from ZnO.12–16 Obviously, the intensity of OH peak increases upon Mn incorporation, indicating more surface oxygen-containing groups. Oxygen-containing groups are believed to not only facilitate the adsorption and activation of reactant molecules at the photocatalyst surface but also suppress the charge carrier recombination.17 Therefore, it is reasonable to predict a higher photocatalytic activity of Mn,C-ZnO TSHSs samples over C-ZnO one. Additionally, the OL peak has been shifted to higher BE after Mn doping revealing Mn-O-Zn bond.12

The core level C 1s XPS for all samples are fitted into four peaks and presented in Fig.S5c. The peaks around 288.9, 286.0, 284.8 and 283.0 eV are ascribed to C=C, C-O-C, C-C and M-C, respectively. Those were originated from hydrocarbon residues of the decomposed carbon skeleton and successful carbon doping.1,18 After CO2 treatment, a new tiny peak at ~ 293 eV is evolved, which could be ascribed to M-CO2 binding upon the interaction between metallic centers and loaded CO2 molecules.

Supplementary Note 3

CO2 reduction mechanism. Once activated at the preferential Mn active sites on the surface of the catalyst, the obtained CO2˙ˉ radical anions are highly reactive. They underwent several proton-coupled multiple-electron-transfer reactions, almost instantaneously, culminated in a variety of valuable products.7,19,20 To elucidate the photoreduction (PR) mechanism of CO2 and explore the intermediate products of such process over 2%Mn,C-ZnO CTSHSs sample, in-situ DRIFTS spectrum of the sample was analyzed during the reaction under dark and light conditions (Supplementary Figure S8).

Markedly, CO2 molecules underwent recognizable adsorption and activation over the photocatalyst as indicated by the distinctive carbonate peaks (at 1380, 1445,1495 and 1541 cm-1) arising from CO2 adsorption onto surface-active Mn-species of the Mn, C-ZnO CTSHSs sample under dark conditions.21 No detectable products were observed without light irradiation (Supplementary Figure S8b,c) suggesting that CO2 is indeed photocatalytically reduced to valuable product. Upon light illumination, distinctive formaldehyde (HCHO) and formate (HCOO-) peaks (at 1403, 1583, 1784 and 1530, 1808, 1858, 1934 cm-1, respectively)1,4 emerged on the DRIFTS spectra as intermediate products. Moreover, a time-enhanced peak for the predominant product (i.e. methanol, CH3OH) appeared at 1060, 1211, 1350, 1481 and  1725 cm-1.4,21 Based on these findings, the photocatalytic CO2 reduction paradigm can be drawn. Firstly, reliable adsorption of CO2 molecules onto Mn5+ species (with AOS~5), is attained, followed by successful activation steps will culminate in the active radical anion intermediates i.e. CO2˙ˉ formation (see original manuscript, Fig.7). Furthermore, this active intermediate will take a proton from water to yield HCOO˙ or ˙COOH, according to its binding mode to the photocatalyst, which could experience subsequent reduction steps by the photoexcited electrons from the photocatalyst resulting in HCOO-, CO and CH3OH, respectively (Supplementary Equations 1-7):22

CO2ads+Mn5+S CO2˙ˉads+Mn6+(S)                    (1)                                                                         CO2˙-ads+H+ads→HCOO∙ads                                  2

HCOO∙ads+e-→HCOO-ads                                         (3)

CO2˙-ads+H+ads→˙COOHads                                   4

˙COOHads+e-→COads+OH-                                    (5)

COads+4H+ads+4e-→CH3OH                                  (6)

Mn6+S+e-→ Mn5+S                                                        (7)

The regeneration of the Mn5+ species is very critical to maintain sustainable and stable activity observed for the Mn-doped ZnO photocatalyst. Moreover, the charge trapping action manifested to restore the active Mn5+ species is of great essence for charge carrier’s separation.

Supplementary Note 4

Fitting of TRPL. *: τ(average) represents the average lifetime for charge carriers generated on the photocatalyst upon light illumination, and such value is calculated based on the following equation23 via substitution with the fitting parameters deduced from the TRPL results:

τaverage=B1τ12+B2τ22B1τ1+B2τ1

where τ1 and τ2 are the lifetimes of radiative and non-radiative actions that occurred after the excitation process, respectively, and B1 and B2 are the pre-exponential factors.

Supplementary References

1.	Low, J., Zhang, L., Tong, T., Shen, B. & Yu, J. TiO2/MXene Ti3C2composite with excellent photocatalytic CO2 reduction activity. J. Catal. 361, 255–266 (2018).

2.	Li, M. et al. Highly selective CO2 photoreduction to CO over g-C3N4/Bi 2WO6 composites under visible light. J. Mater. Chem. A 3, 5189–5196 (2015).

3.	Aguirre, M. E., Zhou, R., Eugene, A. J., Guzman, M. I. & Grela, M. A. Cu2O/TiO2 heterostructures for CO2 reduction through a direct Z-scheme: Protecting Cu2O from photocorrosion. Appl. Catal. B Environ. 217, 485–493 (2017).

4.	Chen, S., Yu, J. & Zhang, J. Enhanced photocatalytic CO2 reduction activity of MOF-derived ZnO/NiO porous hollow spheres. J. CO2 Util. 24, 548–554 (2018).

5.	Yu, J., Jin, J., Cheng, B. & Jaroniec, M. A noble metal-free reduced graphene oxide-cds nanorod composite for the enhanced visible-light photocatalytic reduction of CO2 to solar fuel. J. Mater. Chem. A 2, 3407–3416 (2014).

6.	Shannon, R. D. & Prewitt, C. T. Effective ionic radii in oxides and fluorides. Acta Crystallogr. Sect. B 25, 925–946 (1969).

7.	Li, W. Advances in CO2 Conversion and Utilization. in Advances in CO2 Conversion and Utilization 5–55 (American Chemical Society, 2010). doi:10.1021/bk-2010-1056.ch005

8.	Sharma, D. & Jha, R. Analysis of structural, optical and magnetic properties of Fe/Co co-doped ZnO nanocrystals. Ceram. Int. 43, 8488–8496 (2017).

9.	Wang, T. et al. A Co3O4 -embedded porous ZnO rhombic dodecahedron prepared using zeolitic imidazolate frameworks as precursors for CO2 photoreduction. Nanoscale 8, 6712–6720 (2016).

10.	Etacheri, V., Roshan, R. & Kumar, V. Mg-doped ZnO nanoparticles for efficient sunlight-driven photocatalysis. ACS Appl. Mater. Interfaces 4, 2717–2725 (2012).

11.	Guo, Y. et al. Solution-based doping of manganese into colloidal ZnO nanorods. J. Phys. Chem. C 112, 8832–8838 (2008).

12.	Ajrina, N. et al. Mn-doping-induced photocatalytic activity enhancement of ZnO nanorods prepared on glass substrates. Appl. Surf. Sci. 439, 285–297 (2018).

13.	Sambandam, B., Michael, R. J. V. & Manoharan, P. T. Oxygen vacancies and intense luminescence in manganese loaded Zno microflowers for visible light water splitting. Nanoscale 7, 13935–13942 (2015).

14.	Wang, Y. et al. Synergistic effect of N-decorated and Mn2+ doped ZnO nanofibers with enhanced photocatalytic activity. Sci. Rep. 6, 32711 (2016).

15.	Gallegos, M. V., Peluso, M. A., Thomas, H., Damonte, L. C. & Sambeth, J. E. Structural and optical properties of ZnO and manganese-doped ZnO. J. Alloys Compd. 689, 416–424 (2016).

16.	Santos, V. P. et al. Structural and chemical disorder of cryptomelane promoted by alkali doping: Influence on catalytic properties. J. Catal. 293, 165–174 (2012).

17.	Liu, D. et al. Defect-related photoluminescence and photocatalytic properties of porous ZnO nanosheets. J. Mater. Chem. A 2, 15377 (2014).

18.	Wang, S. et al. C-doped ZnO ball-in-ball hollow microspheres for efficient photocatalytic and photoelectrochemical applications. J. Hazard. Mater. 331, 235–245 (2017).

19.	Aylmer-Kelly, A. W. B., Bewick, A., Cantrill, P. R. & Tuxford, A. M. Studies of electrochemically generated reaction intermediates using modulated specular reflectance spectroscopy. Faraday Discuss. Chem. Soc. 56, 96–107 (1973).

20.	Zhu, D. D., Liu, J. L. & Qiao, S. Z. Recent Advances in Inorganic Heterogeneous Electrocatalysts for Reduction of Carbon Dioxide. Adv. Mater. 28, 3423–3452 (2016).

21.	Xia, P., Zhu, B., Yu, J., Cao, S. & Jaroniec, M. Ultra-thin nanosheet assemblies of graphitic carbon nitride for enhanced photocatalytic CO2 reduction. J. Mater. Chem. A 5, 3230–3238 (2017).

22.	Yu, J., Xiang, Q. & Zhou, M. Preparation, characterization and visible-light-driven photocatalytic activity of Fe-doped titania nanorods and first-principles study for electronic structures. Appl. Catal. B Environ. 90, 595–602 (2009).

23.	Xia, P., Liu, M., Cheng, B., Yu, J. & Zhang, L. Dopamine Modified g-C3N4 and Its Enhanced Visible-Light Photocatalytic H2-Production Activity. ACS Sustain. Chem. Eng. 6, 8945–8953 (2018).