Supporting Information

Biomimetic non-classical crystallization induced hierarchically structured efficient circularly polarized phosphors

Li-Zhe Feng1,2, Jing-Jing Wang1,2, Tao Ma3, Yi-Chen Yin1,2, Kuang-Huang Song1,2, Zi-Du Li4,5,6, Man-Man Zhou7, Shan Jin7, Tao-Tao Zhuang1,3, Feng-Jia Fan4,5,6, Man-Zhou Zhu7, Hong-Bin Yao1,2,*

1Hefei National Laboratory for Physical Sciences at the Microscale, University of Science and Technology of China, Hefei, Anhui 230026, China

2Department of Applied Chemistry, Hefei Science Center of Chinese Academy of Sciences, University of Science and Technology of China, Hefei, Anhui 230026, China

3Department of Chemistry, Hefei Science Center of Chinese Academy of Sciences, University of Science and Technology of China, Hefei, Anhui 230026, China

4Department of Physics, Hefei Science Center of Chinese Academy of Sciences, University of Science and Technology of China, Hefei, Anhui 230026, China

5CAS Key Laboratory of Microscale Magnetic Resonance, University of Science and Technology of China, Hefei, Anhui 230026, China

6Synergetic Innovation Center of Quantum Information and Quantum Physics, University of Science and Technology of China, Hefei, Anhui 230026, China

7Key Laboratory of Structure and Functional Regulation of Hybrid Materials, Anhui University, Ministry of Education, Hefei, Anhui 230601, China

*Correspondence and requests for materials should be addressed to H.-B.Y. (yhb@ustc.edu.cn)

Supplementary Fig. 1. 1H NMR spectrum of (S)-1-iodo-2-methylbutane in CDCl3.

Supplementary Fig. 2. 1H NMR spectrum of L1 in DMSO-d6.

Supplementary Fig. 3. 1H NMR spectrum of (R)-2-iodobutane in CDCl3.

Supplementary Fig. 4. 1H NMR spectrum of L2 in DMSO-d6.

Supplementary Fig. 5. 1H NMR spectrum of (R)-2-iodoheptane in CDCl3.

Supplementary Fig. 6. 1H NMR spectrum of L3 in DMSO-d6.

Supplementary Fig. 7. 1H NMR spectrum of (S)-1-iodo-4-methylhexane in CDCl3.

Supplementary Fig. 8. 1H NMR spectrum of L4 in DMSO-d6.

Supplementary Fig. 9. Fluorescence microscopy images of Cu4I4(L1)44+ Cu8I124- (a), Cu5I7(L2)2 (b), Cu5I7(L3)2 (c) and Cu5I7(L4)2 (d) single crystals.

Supplementary Fig. 10. Experimental and simulated PXRD patterns of Cu4I4(L1)44+ Cu8I124-, Cu5I7(L2)2, Cu5I7(L3)2 and Cu5I7(L4)2.

Supplementary Fig. 11. Helical arrangement of Cu4I4(L1)44+ Cu8I124- hybrid clusters in crystal lattices along the b axis. The Cu-I inorganic chains were omitted in the helical arrangement structure of Cu4I4(L1)44+ Cu8I124- for clarity. Color scheme: Cu, red; I, yellow; N, blue; C, Gray.

Supplementary Fig. 12. Helical arrangement of Cu5I7(L2)2 hybrid clusters in crystal lattices along the c axis. Color scheme: Cu, red; I, yellow; N, blue; C, Gray.

Supplementary Fig. 13. Helical arrangement of Cu5I7(L3)2 hybrid clusters in crystal lattices along the c axis. Color scheme: Cu, red; I, yellow; N, blue; C, Gray.

Supplementary Fig. 14. Helical arrangement of Cu5I7(L4)2 hybrid clusters in crystal lattices along the c axis. Color scheme: Cu, red; I, yellow; N, blue; C, Gray.

Supplementary Fig. 15. CD spectra of Cu4I4(L1)44+ Cu8I124-, Cu5I7(L2)2, Cu5I7(L3)2 and Cu5I7(L4)2 single crystal powders.

Supplementary Fig. 16. CPL (a) and glum (b) spectra of Cu4I4(L1)44+ Cu8I124-, Cu5I7(L2)2, Cu5I7(L3)2 and Cu5I7(L4)2 single crystal powders.

Supplementary Fig. 17. a, PXRD patterns of Cu4I4(L1)44+ Cu8I124- polycrystals with different reaction time ([L1] = 6 mM). b, PXRD patterns of Cu5I7(L2)2 polycrystals with different reaction time ([L2] = 20 mM). c, PXRD patterns of Cu5I7(L3)2 polycrystals with different reaction time ([L3] = 25 mM). d, PXRD patterns of Cu5I7(L4)2 polycrystals with different reaction time ([L4] = 20 mM).

Supplementary Fig. 18. a-d, SEM images of different stages of crystallization for Cu5I7(L2)2 polycrystals with reaction time of 3 min (a), 2 h (b), 3 h (c), 6 h (d), respectively ([L2] = 20 mM). e-h, SEM images of different stages of crystallization for Cu5I7(L4)2 polycrystals with reaction time as 3 min (e), 1 h (f), 7 h (g), 12 h (h), respectively ([L4] = 20 mM).

Supplementary Fig. 19. TEM images of Cu5I7(L4)2 helical nanobelts.

Supplementary Fig. 20. Schematic diagram of repulsive forces between assembly units caused by long (left) and short (right) chains of ligands absorbed on the surfaces, respectively. Blue cuboids represent the assembly units, and the wavy lines attached to the surfaces of cuboids represent ligands.

Supplementary Fig. 21. CD spectra of Cu4I4(L1)44+ Cu8I124-, Cu5I7(L2)2, Cu5I7(L3)2 and Cu5I7(L4)2 hierarchically structured polycrystals with the concentrations of L1-L4 as 6 mM, 20 mM, 25 mM, 20 mM, respectively.

Supplementary Fig. 22. a, SEM images of (rac)-Cu4I4(L1)44+ Cu8I124- hierarchically structured polycrystals synthesized by racemic L1 ligands. b-d, CD (b), CPL (c), and glum (d) spectra of hierarchically structured polycrystals synthesized by racemic and chiral L1 ligands, respectively. Other conditions: [racemic L1] = [L1] = 6 mM.

Supplementary Fig. 23. PXRD patterns of Cu4I4(L1)44+ Cu8I124- (a), Cu5I7(L2)2 (b), Cu5I7(L3)2 (c) and Cu5I7(L4)2 (d) polycrystals with different concentration of ligands.

Supplementary Fig. 24. a-d, SEM images of Cu4I4(L1)44+ Cu8I124- polycrystals with the concentrations of L1 as 4 mM (a), 5 mM (b), 6 mM (c), 10 mM (d), respectively. e-h, SEM images of Cu5I7(L2)2 polycrystals with concentrations of L2 as 5 mM (e), 10 mM (f), 20 mM (g), 30 mM (h), respectively. i-l, SEM images of Cu5I7(L3)2 polycrystals with concentrations of L3 as 10 mM (i), 20 mM (j), 25 mM (k), 40 mM (l), respectively. m-p, SEM images of Cu5I7(L4)2 polycrystals with concentration of L4 as 3 mM (m), 5 mM (n), 10 mM (o), 20 mM (p), respectively.

Supplementary Fig. 25. CD (a), CPL (b), and glum (c) spectra of Cu4I4(L1)44+ Cu8I124- polycrystals with different concentration of L1, respectively.

Supplementary Fig. 26. CD (a), CPL (b), and glum (c) spectra of Cu5I7(L2)2 polycrystals with different concentration of L2, respectively.

Supplementary Fig. 27. CD (a), CPL (b), and glum (c) spectra of Cu5I7(L3)2 polycrystals with different concentration of L3, respectively.

Supplementary Fig. 28. CD (a), CPL (b), and glum (c) spectra of Cu5I7(L4)2 polycrystals with different concentration of L4, respectively.

Supplementary Fig. 29. TGA curves of Cu4I4(L1)44+ Cu8I124-, Cu5I7(L2)2, Cu5I7(L3)2 and Cu5I7(L4)2 hierarchically structured polycrystals.

Supplementary Fig. 30. Schematic illustration of LED polarization measurement system. We measured the circularly polarized light emitted by the fabricated LED device by dividing the emitted light into left- and right-handed portions, respectively, using a quarter-wave plate and a linear polarizer to eliminate the influence of linear polarized light.

Supplementary Fig. 31. CPL spectra (a) and the polarized degree (b) of the fabricated LED device based on racemic Cu4I4(L1)44+ Cu8I124- polycrystals powered by 2.4 V electric source.

Supplementary text 1: The crystallization process of Cu5I7(L4)2 polycrystals. As shown in Supplementary Fig. 18e and f, at the beginning, Cu5I7(L4)2 clusters aggregated into conglobate particles, and then grew into nanosheets. PXRD patterns of nanoparticles and nanosheets show wide width of diffraction peaks, indicating low crystallinity of Cu5I7(L4)2 at this stage (Supplementary Fig. 17d). Additionally, strong diffraction peak at 5° does not belong to the phase of Cu5I7(L4)2. According to the Bragg’s law, we speculate that it is owing to the two dimensional layered structure with large distance between two layers due to the long alkyl chain length of L4, which give rise to the peak at small degree of 5°. But, as the reaction time prolonged, nanosheets were avulsed, restructured and twisted into M-helical nanobelts (Supplementary Fig. 18g, h). And the helicity of nanobelts can also be verified by transmission electron microscopy (TEM) images (Supplementary Fig. 19). Correspondingly, diffraction peak at 5° in PXRD pattern is disappeared at this time, indicating the disappearance of two dimensional structures and the transformation of nanosheets to nanobelts (Supplementary Fig. 17d).

Supplementary Table 1. Crystallography parameters of Cu4I4(L1)44+ Cu8I124-, Cu5I7(L2)2, Cu5I7(L3)2 and Cu5I7(L4)2 single crystals.

| Compounds | Cu4I4(L1)44+ Cu8I124- | Cu5I7(L2)2 | Cu5I7(L3)2 | Cu5I7(L4)2 |
| --- | --- | --- | --- | --- |
| Empirical formula | C22H45Cu6I8N4 | C24H48Cu5I7N6 | C22H46Cu5I7N4 | C26H54Cu5I7N4 |
| Formula weight | 1762.06 | 1626.68 | 1572.63 | 1628.73 |
| Temperature/K | 100.15 | 100.00(10) | 100.00(10) | 100.00(10) |
| Crystal system | tetragonal | triclinic | trigonal | triclinic |
| Space group | P42 | P1 | P3221 | P1 |
| a/Å | 22.0722(2) | 8.69065(18) | 12.1489(5) | 11.5081(2) |
| b/Å | 22.0722(2) | 13.3957(3) | 12.1489(5) | 11.6450(3) |
| c/Å | 8.55280(10) | 18.0042(5) | 22.9488(9) | 16.9677(4) |
| α/° | 90 | 89.407(2) | 90 | 109.679(2) |
| β/° | 90 | 89.889(2) | 90 | 95.9038(16) |
| γ/° | 90 | 79.2342(19) | 120 | 98.0117(19) |
| Volume/Å3 | 4166.77(9) | 2059.01(9) | 2933.4(3) | 2092.61(9) |
| Z | 4 | 2 | 3 | 2 |
| ρcalcg/cm3 | 2.809 | 2.624 | 2.671 | 2.585 |
| μ/mm-1 | 50.026 | 7.813 | 8.220 | 7.686 |
| F(000) | 3212.0 | 1500.0 | 2166.0 | 1508.0 |
| Final R indexes [I>=2σ (I)] | R1 = 0.0615 wR2 = 0.1539 | R1 = 0.0355 wR2 = 0.0806 | R1 = 0.0346 wR2 = 0.0637 | R1 = 0.0307 wR2 = 0.0719 |
| Final R indexes [all data] | R1 = 0.0679 wR2 = 0.1607 | R1 = 0.0392 wR2 = 0.0834 | R1 = 0.0362 wR2 = 0.0647 | R1 = 0.0315 wR2 = 0.0724 |
| Flack parameter | 0.05(2) | 0.00(3) | 0.04(3) | 0.056(12) |

Supplementary Table 2. Summary of the photoluminescence quantum yields (PLQYs) and luminescence dissymmetry factor (glum) of previously reported CPL materials.

| Material types |  | CPL Material | Peak Wavelength (nm) | PLQY (%) | ¦glum¦ | Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| Clusters | (R-MBA)4Cu4I4 |  | 630 | 52.8 | 1.0 × 10-2 | 1 |
|  | (S-MBA)4Cu4I4 |  | 630 | 59.7 | 6 × 10-3 |  |
|  | [Cu3(R-BINAP)3CO3](tBuSO3) |  | 605 | 1.2 | 2 × 10-2 | 2 |
|  | [Cu3(S-BINAP)3CO3](tBuSO3) |  | 605 | 1.2 | 2 × 10-2 |  |
|  | Ag6PD6 |  | 575 | 95 | 4.42 × 10-3 | 3 |
|  | Ag6PL6 |  | 575 | 95 | 4.42 × 10-3 |  |
|  | [D-valinol(18-crown-6)]+[Cu5(StBu)6]- |  | 660 | 47.4 | 9.77 × 10-3 | 4 |
|  | [L-valinol(18-crown-6)]+[Cu5(StBu)6]- |  | 660 | 46.5 | 9.77 × 10-3 |  |
| Coordination compounds | L-Cysteine capped CaAl2O4:Eu,Nd |  | 440 | - | 2.1 × 10-2 | 5 |
|  | D-Cysteine capped CaAl2O4:Eu,Nd |  | 440 | - | 1.9 × 10-2 |  |
|  | [Au(NHC)2][Au(CN)2] (RC-A) |  | 500 | 65 | 1.6 × 10-3 | 6 |
|  | [Au(NHC)2][Au(CN)2] (SC-A) |  | 500 | 65 | 1.45 × 10-3 |  |
|  | CsEu(hfbc)4 |  | 595 | 3 | 1.38 | 7 |
| Organic molecules | P-2-aza[4]helicene |  | 402 | - | 8.7 × 10-3 | 8 |
|  | M-2-aza[4]helicene |  | 402 | - | 9.5 × 10-3 |  |
|  | Helical carbazole-based BODIPY analogues |  | 411~532 | 20.0~36.4 | 7 × 10-4~1.9 × 10-3 | 9 |
|  | g-BNMe2-Cp |  | 525 | 53 | 4.24 × 10-3 | 10 |
|  | m-BNMe2-Cp |  | 487 | 33 | - |  |
| Nanocrystals | R-α-octylamine modified CsPbBr3 NCs |  | 520 | 60-70 | 7 × 10-3 | 11 |
|  | S-α-octylamine modified CsPbBr3 NCs |  | 520 | 60-70 | 6.5 × 10-3 |  |
|  | LGAM capped CsPbBr3 NCs |  | 511 | 47.4 | 7.3 × 10-3 | 12 |
|  | DGAM capped CsPbBr3 NCs |  | 511 | 47.4 | 7.3 × 10-3 |  |
|  | D-cysteine-CdSe/CdS NCs |  | 614 | 20 | 5.17 × 10-4 | 13 |
| Assemblies | LPF/DPF-2An co-gel |  | 500 | 18.5 | 4.2 × 10-3 | 14 |
|  | R-Py/TCNB |  | 508 | 5.2 | 1.7 × 10-2 | 15 |
|  | L/D-NDI-GE π-nanotube |  | 546 | - | 7× 10-2 | 16 |
|  | Au-L-Cys twisted ribbons |  | 620 | - | 2 × 10-3 | 17 |
|  | Au-D-Cys twisted ribbons |  | 620 | - | 2 × 10-3 |  |
|  | NDI•− radical anion gels |  | 560-700 | - | 0.26-0.20 | 18 |
| This work | Cu4I4(L1)44+ Cu8I124- polycrystals |  | 544 | 32 | 1.5 × 10-2 |  |
|  | Cu5I7(L2)2 polycrystals |  | 580 | 50 | 4.0 × 10-3 |  |
|  | Cu5I7(L3)2 polycrystals |  | 590 | 7 | 3.7 × 10-3 |  |
|  | Cu5I7(L4)2 polycrystals |  | 620 | 6 | 6.0 × 10-3 |  |

References.

1.	Yao, L. et al. Circularly polarized luminescence from chiral tetranuclear copper(I) iodide clusters. J. Phys. Chem. Lett. 11, 1255-1260 (2020).

2.	Kong, Y.-J. et al. Photoresponsive Propeller-like Chiral AIE Copper(I) Clusters. Angew. Chem. Int. Ed. 59, 5336-5340 (2020).

3.	Han, Z. et al. Ultrastable atomically precise chiral silver clusters with more than 95% quantum efficiency. Sci. Adv. 6, eaay0107 (2020).

4.	Jin, Y. et al. Cations controlling the chiral assembly of luminescent atomically precise copper (I) clusters. Angew. Chem. Int. Ed. 131, 12271-12276 (2019).

5.	Hao, W., Li, Y. & Liu, M. Endowing phosphor materials with long-afterglow circularly polarized phosphorescence via ball milling. Adv. Opt. Mater., 2100452 (2021).

6.	Yang, J. G. et al. Controlling metallophilic interactions in chiral gold (I) double salts towards excitation wavelength-tunable circularly polarized luminescence. Angew. Chem. Int. Ed. 59, 6915-6922 (2020).

7.	Zinna, F., Giovanella, U. & Bari, L. D. Highly circularly polarized electroluminescence from a chiral europium complex. Adv. Mater. 27, 1791-1795 (2015).

8.	Wang, F., Gan, F., Shen, C. & Qiu, H. Amplifiable symmetry breaking in aggregates of vibrating helical molecules. J. Am. Chem. Soc. 142, 16167-16172 (2020).

9.	Wade, J. et al. 500-Fold amplification of small molecule circularly polarised luminescence through circularly polarised FRET. Angew. Chem. Int. Ed. 60, 222-227 (2021).

10.	Zhang, M.-Y. et al. Solid-state emissive triarylborane-based [2.2] paracyclophanes displaying circularly polarized luminescence and thermally activated delayed fluorescence. Org. Lett. 20, 6868-6871 (2018).

11.	Chen, W. et al. Two-photon absorption-based upconverted circularly polarized luminescence generated in chiral perovskite nanocrystals. J. Phys. Chem. Lett. 10, 3290-3295 (2019).

12.	Shi, Y., Duan, P., Huo, S., Li, Y. & Liu, M. Endowing perovskite nanocrystals with circularly polarized luminescence. Adv. Mater. 30, 1705011 (2018).

13.	Hao, J. et al. Ligand-induced chirality in asymmetric CdSe/CdS nanostructures: a close look at chiral tadpoles. ACS Nano 14, 10346-10358 (2020).

14.	Yang, L. et al. Highly efficient full-color and white circularly polarized luminescent nanoassemblies and their performance in light emitting devices. Nanoscale 12, 6233-6238 (2020).

15.	Han, J. et al. Enhanced circularly polarized luminescence in emissive charge-transfer complexes. Angew. Chem. Int. Ed. 131, 7087-7093 (2019).

16.	Wang, Y. et al. Bamboo-like π-nanotube with tunable helicity and circularly polarized luminescence. Angew. Chem. Int. Ed. 133, 16751-16757 (2021).

17.	Jiang, W. et al. Emergence of complexity inhierarchically organized chiral particles. Science 368, 642-648 (2020).

18.	Wang, Y., Jiang, Y. Q., Zhu, X. F. & Liu, M. H. Significantly boosted and inversed circularly polarized luminescence from photogenerated radical anions in dipeptide naphthalenediimide assemblies. J. Phys. Chem. Lett. 10, 5861-5867 (2019).