Preparation of Room-temperature Self-healing Recyclable Polyurethane Elastomers Based on

Multiple Hydrogen/Nitrogen Coordination Boro-oxygen Bonds System

Yuchen Jiaoa.c, Ming Zhoua.b.c.g*, Bo Pud, Xiaoling Yanga.c, Chenyiting Lia.c, Liangliang Xiaa.c, Guilin Denga.c, Yunyao Weia.c, Jing Zhonga.c, Zheng Wua.c, Shi Chena.c, Jian Wangb.e*, Yujun Zhouf

a School of New Energy and Materials, Southwest Petroleum University, Chengdu, Sichuan 610500, People’s Republic of China

b National Key Laboratory of Oil and Gas Reservoir Geology and Exploitation, School of New Energy and Materials, Southwest Petroleum University, Chengdu, Sichuan 610500, People’s Republic of China

c Research Center of Energy Polymer Materials, Southwest Petroleum University, Chengdu, Sichuan 610500, People’s Republic of China

d CNPC Chuanqing Drilling Engineering Company Limited Safety, Environment, Quality Supervision and Testing Research Institute

e College of Food and Biological Engineering, Chengdu University, Chengdu, 610106, China

f College of Chemistry and Chemical Engineering, China West Normal University, Chengdu, 637002, China

g Sichuan Provincial Engineering Research Center of Advanced Materials Manufacturing Technology for Shale Gas High-efficient Exploitation

*Corresponding author Ming Zhou (E-mail: mr.zhouming@163.com) and Jian Wang (E-mail: wangjian@cdu.edu.cn).

Table S1. PUPIPMB series polyurethane elastomer production composition monomer

| Elastomers | PTMEG-2000/mmol | IPDI/mmol | PDM/mmol | MOCA/mmol | FBA/mmol |
| --- | --- | --- | --- | --- | --- |
| PUHB-90/10 | 10.00 | 37.80 | 26.97 | 3.00 | 4.56 |
| PUHB-80/20 | 10.00 | 37.80 | 24.46 | 5.96 | 5.45 |
| PUHB-70/30 | 10.00 | 37.80 | 21.15 | 8.95 | 5.10 |
| PUHB-60/40 | 10.00 | 37.80 | 17.98 | 11.91 | 4.70 |
| PUHB-50/50 | 10.00 | 37.80 | 15.15 | 14.88 | 4.38 |
| PUHB-30/70 | 10.00 | 37.80 | 8.63 | 120.97 | 4.03 |
| PUHB-10/90 | 10.00 | 37.80 | 2.97 | 26.96 | 4.02 |

Figure S1. FTIR spectra of PUHB-60/40

Table S2. FTIR data of PUHB-60/40

| Characteristic | Wavenumber(cm-1) |
| --- | --- |
| H-bonded (N-H) | 3351 |
| a (CH2) | 2935 |
| s (CH2) | 2858 |
| H-bonded (C=O) amide | 1704 |
| H-bonded (C-N) + (N-H) amide | 1527 |
| H-bonded (C-N) + (N-H) amide | 1241 |
| (C-O-C) | 1106 |
| (B-O) | 1367 |
| δ (B3O3) | 675 |
| δ (-C7H) | 775 |

Figure. S2. 1HNMR spectra of PUHB-60/40

Figure S3. DSC map of PUPIPMB series of room temperature self-healing polyurethane elastomers

Figure S4. WXAD diagram of PUPIPMB series of room temperature self-healing polyurethane elastomers

Table S3. GPC test of PUPIPMB series of room temperature self-healing polyurethane elastomers

| Sample | Mn(g/mol) | Mw(g/mol) | PDI |
| --- | --- | --- | --- |
| PUHB-90/10 | 35434 | 59464 | 1.678 |
| PUHB-80/20 | 32212 | 54642 | 1.696 |
| PUHB-70/30 | 64231 | 118295 | 1.842 |
| PUHB-60/40 | 65631 | 145637 | 2.219 |
| PUHB-50/50 | 27654 | 48825 | 1.765 |
| PUHB-30/70 | 113950 | 228669 | 2.006 |
| PUHB-10/90 | 33813 | 57618 | 1.704 |

Table S4. Glass Transition temperature (Tg) of PUPIPMB series of room temperature

self-healing polyurethane elastomers

| Sample | Tg(°C) |
| --- | --- |
| PUHB-90/10 | ﹣40.2 |
| PUHB-80/20 | ﹣41.0 |
| PUHB-70/30 | ﹣44.8 |
| PUHB-60/40 | ﹣41.4 |
| PUHB-50/50 | ﹣56.1 |
| PUHB-30/70 | ﹣48.2 |
| PUHB-10/90 | ﹣52.6 |

(a)

(b)

Figure S3. AFM image of PUHB-60/40: (a) Height map of AFM of PUHB-60/40; (b) AFM 3D images of PUHB-60/40

Table S5. Mechanical properties data of PUPIPMB series of room temperature

self-healing polyurethane elastomers

| Sample | Tensile Strength/MPa | Elongation at Break/% | Toughness/MJ·m-3 |
| --- | --- | --- | --- |
| PUHB-90/10 | 6.1 | 2490 | 61.6 |
| PUHB-80/20 | 2.7 | 2472 | 33.1 |
| PUHB-70/30 | 11 | 2475 | 104.6 |
| PUHB-60/40 | 18.8 | 2132 | 117 |
| PUHB-50/50 | 1.8 | 2479 | 25.1 |
| PUHB-30/70 | 17.1 | 2025 | 108.9 |
| PUHB-10/90 | 11.6 | 1689 | 67.3 |

Table S6. Comparison of mechanical properties between PUHB-60/40 and recently reported relevant materials

| Sample | Tensile strength/MPa | Elongation at break/% | Toughness/MJ.m-3 |
| --- | --- | --- | --- |
| This study | 18.8 | 2132 | 117.0 |
| Ref.35 | 1.1 | 229 | 6.5 |
| Ref.36 | 5.72 | 1726 | 24.45 |
| Ref.37 | 4.83 | 2010 | 65.49 |
| Ref.38 | 1.3 | 2100 | --- |
| Ref.39 | 6.31 | 710 | --- |
| Ref.40 | 3.9 | 348.57 | --- |
| Ref.41 | 11 | 725.5 | 52.1 |
| Ref.42 | 11.91 | 723.57 | 30.07 |
| Ref.43 | 16.1 | 771 | --- |

Table S7. Self-healing results of mechanical properties of polyurethane elastomers at 25°C±2°C for 48h (relative humidity 60%±2%)

| Sample | Tensile strength (SE)/% | Elongation (SE)/% | Toughness (SE)/% |
| --- | --- | --- | --- |
| PUHB-90/10 | 77.0 | 99.2 | 86.0 |
| PUHB-80/20 | 98.9 | 98.4 | 96.5 |
| PUHB-70/30 | 87.7 | 84.0 | 83.1 |
| PUHB-60/40 | 94.7 | 91.7 | 86.7 |
| PUHB-50/50 | 90.3 | 99.8 | 95.7 |
| PUHB-30/70 | 98.4 | 80.7 | 79.0 |
| PUHB-10/90 | 72.9 | 92 | 80.7 |

Table S8. Trend of self-healing efficiency of mechanical properties of PUHB-60/40 over time

| PUHB-60/40 | Tensile strength (SE)/% | Elongation (SE)/% | Toughness (SE)/% |
| --- | --- | --- | --- |
| 12h | 28.7 | 55.4 | 24.6 |
| 24h | 41.4 | 63.6 | 37.1 |
| 36h | 78.1 | 90.2 | 74.6 |
| 48h | 94.7 | 91.7 | 86.7 |

Table S9. 48h self-healing efficiency of PUHB-60/40 at room temperature under different relative humidity

| Relative humidity | Tensile strength (SE)/% | Elongation (SE)/% | Toughness (SE)/% |
| --- | --- | --- | --- |
| 60% | 94.7 | 91.7 | 86.7 |
| 70% | 81.5 | 97.8 | 83.0 |
| 80% | 74.5 | 100.0 | 83.0 |
| 90% | 70.3 | 87.5 | 67.8 |

Table S10. 48h efficiency of self-healing at room temperature after PUHB-60/40 immersion

and conventional treatment

| PUHB-60/40 | Tensile strength (SE)/% | Elongation (SE)/% | Toughness (SE)/% |
| --- | --- | --- | --- |
| Healed for 48h at 25℃ (Water) | 90.8 | 92.3 | 84.5 |
| Healed for 48h at 25℃ | 95.6 | 91.7 | 87.5 |

Table S11. Mechanical properties data of PUHB-60/40 cyclic preparation

| Sample | Tensile strength/MPa | Elongation/% | Toughness/MJ·m-3 |
| --- | --- | --- | --- |
| Original | 18.8 | 2132 | 117 |
| 1st recycle | 18.1 | 2130 | 115 |
| 3rd recycle | 17.1 | 2255 | 108 |
| 5th recycle | 17.3 | 2154 | 108 |