Novel Azo-benzoyl acetone metal complexes for inhibition of atmospheric steel corrosion

Yusif S. El-Sayeda, Nadia El-Wakiela*, Kamal El-Baradiea, Basma M. Salema*

aChemistry Department, Faculty of Science, Tanta University, 31527 Tanta, Egypt

2.1. Chemicals and Instrumentations

## 5-aminoindazole (97%), benzoyl acetone (99%), Cobalt (II) chloride hexahydrate (98%), Nickel (II) chloride hexahydrate (99.9%), and Copper (II) chloride (99%), dimethyl sulfoxide (DMSO, 99.9%), triethylamine (99%), and ethanol (95%) were obtained purchased from Sigma-Aldrich and used as received.

C, H, and N analyses of the synthesized compounds were carried out using a FLASH 2000 CHNS/O analyzer. The 1H-NMR and 13C-NMR spectra were recorded on a DELTA2-NMR (500 MHz) in DMSO-d6 at 25 co with tetramethylsilane (TMS) as an internal standard. The FT-IR spectra were taken on an FT-IR-4100 (JASCO, Japan) spectrophotometer in the range of 4000-400 cm-1. The standard electron impact mass spectra of the ligand and metal chelates were performed at room temperature, utilizing the mass analyzer's direct inlet component in the thermal scientific GCMS model ISQ. The direct insertion probe (DIP) was gradually heated from 50 to 3000 co while the ion source was maintained at 25 co. The molar conductance in     10-3 M DMSO was calculated. The electronic absorption spectra were obtained using a Shimadzu UV-Vis 240 spectrophotometer. The X-ray diffractometer (GNR, APD 2000 PRO, Italy) was employed to have the XRD patterns of the solid compounds. The magnetic susceptibility of the chelates was carried out at 25 co using the magnetic susceptibility balance Johnson Matthey 436 Devon Park Drive by Gouy's method [31]. The Shimadzu TG-50 thermogravimetric analyzer was used to perform the thermogravimetric analysis (TGA) of the solid chelates in the range of 25–800 co, at a heating rate of 10 co /min in an N2 atmosphere. An Inductive Coupled Plasma spectrometer (Optima 7000 DV, ICP-OES) was used to measure and identify the elements within the chelate samples.

Figure S1. EI‐Mass spectrum of Co (II) complex

Figure S2.  EI‐Mass spectrum of Ni (II) complex

Figure S3. EI‐Mass spectrum of Cu (II) complex

Table S1. Bond lengths, and bond angles of Azo-dye ligand

| Bond Length (oA) |  | Bond angles (o) |  |
| --- | --- | --- | --- |
| C1-C2 | 1.396 | C4-C5-C7 | 123.5 |
| C2-C3 | 1.393 | C3-C4-C5 | 120.3 |
| C3-C4 | 1.392 | C5-C7-O9 | 121.6 |
| C4-C5 | 1.400 | C5-C7-C8 | 120.9 |
| C5-C6 | 1.402 | C1-C6-C5 | 120.5 |
| C5-C7 | 1.494 | C7-C8-C10 | 115.5 |
| C7-C8 | 1.549 | C7-C8-N23 | 111.9 |
| C7-O9 | 1.212 | C8-C10-C11 | 116.4 |
| C8-C10 | 1.549 | C8-C10-O22 | 120.4 |
| C10-O22 | 1.206 | C11-C10-O22 | 123.2 |
| C10-C11 | 1.511 | C6- C5-C7 | 117.4 |
| C8-N23 | 1.464 | C10-C8-N23 | 111.9 |
| N23-N12 | 1.248 | C8-N23-N12 | 112.4 |
| N12-C13 | 1.421 | N23-N12-C13 | 116 |
| C13-C18 | 1.392 | N12-C13-C14 | 114.5 |
| C13-C14 | 1.417 | N12-C13-C18 | 124.4 |
| C18-C17 | 1.396 | C15-C16-N19 | 132.4 |
| C14-C15 | 1.380 | C16-N19-N20 | 112.7 |
| C15-C16 | 1.403 | N19-N20-C21 | 106 |
| C16-C17 | 1.421 | N20-C21-C17 | 111.5 |
| C16-N19 | 1.421 | C21-C17-C18 | 135.8 |
| N19-N20 | 1.361 | C16-C17-C18 | 120 |
| N20-C21 | 1.315 | C16-C17-C21 | 104.2 |
| C21-C17 | 1.432 | C17-C18-C13 | 118 |

Table S2. Bond lengths, and bond angles of Co (II) complex

| Bond Length (oA) |  | Bond angles (o) |  |
| --- | --- | --- | --- |
| Co-N14 | 2.066 | O8-Co-O25 | 167.5 |
| Co-O25 | 2.290 | Cl28-Co-N14 | 168.6 |
| Co-Cl28 | 2.444 | Cl27-Co-O26 | 174.9 |
| Co-O8 | 2.137 | O8-Co-Cl28 | 91.8 |
| Co-Cl27 | 2.331 | Cl28-Co-O25 | 78.80 |
| Co-O26 | 2.071 | O25-Co-N14 | 106.18 |
| O8-C7 | 1.257 | N14-Co-O8 | 84.60 |
| C7-C3 | 1.482 | Cl28-Co-O26 | 78.20 |
| C3-C2 | 1.417 | O26-Co-O25 | 91.81 |
| C3-C4 | 1.421 | N14-Co-Cl27 | 90.52 |
| C4-C5 | 1.401 | Cl27-Co-O8 | 90.68 |
| C7-C9 | 1.563 | Co-O8-O7 | 127.39 |
| C9-C10 | 1.539 | O8-C7-C9 | 113.98 |
| C10-O11 | 1.248 | C7-C9-N13 | 109.69 |
| C10-C12 | 1.513 | C9-N13-N14 | 118.67 |
| C9-N13 | 1.496 | N13-N14-Co | 124.03 |
| N13-N14 | 1.285 | N13-N14-C15 | 113.59 |
| N14-C15 | 1.446 | N14-C15-C20 | 117.30 |
| C15-C16 | 1.403 | N14-C15-C16 | 120.77 |
| C15-C20 | 1.427 | C18-N23-N22 | 112.36 |
| C18-N23 | 1.380 | N23-N22-C21 | 105.60 |
| N23-N22 | 1.395 | O8-C7-C3 | 119.45 |
| N22-C21 | 1.342 | C7-C3-C4 | 116.12 |
| C21-C17 | 1.442 | C7-C3-C2 | 124.30 |
| C17-C16 | 1.406 | C3-C2-C1 | 119.84 |
| C20-C19 | 1.394 | C3-C4-C5 | 120.23 |
| C19-C18 | 1.413 | C15-C20-C19 | 120.82 |
| C18-C17 | 1.433 | C15-C16-C17 | 117.86 |

Table S3. Bond lengths, and bond angles of Ni (II) complex

| Bond Length (oA) |  | Bond angles (o) |  |
| --- | --- | --- | --- |
| Ni-N14 | 2.035 | N14-Ni-O25 | 168.30 |
| Ni-O25 | 1.949 | O26-Ni-Cl28 | 164.88 |
| Ni-O26 | 2.003 | O8-Ni-Cl27 | 83.22 |
| Ni-O8 | 1.947 | Cl27-Ni-O26 | 46.58 |
| Ni-Cl28 | 2.452 | O26-Ni-N14 | 93.67 |
| Ni-Cl27 | 3.932 | N14-Ni-Cl28 | 90.21 |
| O8-C7 | 1.279 | Cl28-Ni-O8 | 89.59 |
| C7-C3 | 1.514 | Cl27-Ni-O25 | 47.11 |
| C3-C2 | 1.422 | Ni-O8-C7 | 127.33 |
| C3-C4 | 1.423 | O8-C7-C9 | 124.15 |
| C4-C5 | 1.405 | C7-C9-N13 | 123.19 |
| C7-C9 | 1.569 | C9-N13-N14 | 115.53 |
| C9-C10 | 1.629 | N13-N14-Ni | 132.62 |
| C10-O11 | 1.247 | N13-N14-C15 | 111.49 |
| C10-C12 | 1.554 | N14-C15-C20 | 117.19 |
| C9-N13 | 1.537 | N14-C15-C16 | 120.84 |
| N13-N14 | 1.331 | C18-N23-N22 | 113.16 |
| N14-C15 | 1.486 | N14-N22-C21 | 102.93 |
| C15-C16 | 1.412 | O8-C7-C3 | 118.05 |
| C15-C20 | 1.440 | C7-C3-C4 | 117.29 |
| C18-N23 | 1.400 | C7-C3-C2 | 122.86 |
| N23-N22 | 1.442 | C3-C2-C1 | 119.60 |
| N22-C21 | 1.370 | C3-C4-C5 | 120.07 |
| C21-C17 | 1.451 | C15-C20-C19 | 120.96 |
| C17-C16 | 1.416 | C15-C16-C17 | 117.90 |
| C20-C19 | 1.394 | C16-C17-C18 | 119.52 |
| C19-C18 | 1.426 | C16-C17-C21 | 135.12 |
| C18-C17 | 1.441 | C20-C19-C18 | 117.21 |

Table S4. Bond lengths, and bond angles of Cu (II) complex

| Bond Length (oA) |  | Bond angles (o) |  |
| --- | --- | --- | --- |
| Cu-N12 | 2.142 | O9-Cu-Cl25 | 120.12 |
| Cu-O9 | 2.260 | Cl25-Cu-Cl26 | 94.05 |
| Cu-Cl25 | 2.359 | Cl26-Cu-N12 | 97.63 |
| Cu-Cl26 | 2.419 | N12-Cu-O9 | 85.93 |
| O9-C7 | 1.264 | Cu-O9-C7 | 118.84 |
| C7-C8 | 1.587 | O9-C7-C5 | 120.79 |
| C8-C10 | 1.576 | O9-C7-C8 | 118.84 |
| C10-C11 | 1.553 | C7-C8-C10 | 109.39 |
| C10-O22 | 1.262 | C7-C8-N23 | 110.11 |
| C8-N23 | 1.558 | N23-C8-C10 | 110.70 |
| N23-N12 | 1.336 | C8- C10-O22 | 120.97 |
| C7-C5 | 1.520 | C8-C10-C11 | 117.05 |
| C5-C4 | 1.419 | C7-C5-C6 | 116.17 |
| C5-C6 | 1.422 | C7-C5-C4 | 124.29 |
| C4-C3 | 1.407 | C8-N23-N12 | 110.46 |
| N12-C13 | 1.473 | N23-N12-C13 | 112.55 |
| C13-C18 | 1.413 | N23-N12-Cu | 127.69 |
| C18-C17 | 1.416 | N12-C13-C18 | 116.81 |
| C13-C14 | 1.444 | N12-C13-C14 | 121.28 |
| C14-C15 | 1.390 | C14-C15-C16 | 117.26 |
| C15-N16 | 1.429 | C16-N19-N20 | 113.19 |
| N19-N20 | 1.445 | N19-N20-C21 | 102.84 |
| N20-C21 | 1.370 | N20-C21-C17 | 112.99 |
| C16-N19 | 1.398 | C13-C18-C17 | 117.84 |
| C16-C17 | 1.440 | C13-C14-C15 | 120.96 |

Table S5. The Milliken charge distribution for the ligand and its metal complexes

| Ligand |  | Co (II) complex |  | Ni (II) complex |  | Cu (II) complex |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Atom | Charge | Atom | Charge | Atom | Charge | Atom | Charge |
| C1 | -0.094 | C1 | -0.241 | C1 | -0.069 | C1 | -0.069 |
| C2 | -0.059 | C2 | -0.330 | C2 | -0.070 | C2 | -0.060 |
| C3 | -0.111 | C3 | 0.278 | C3 | -0.015 | C3 | -0.072 |
| C4 | -0.02 | C4 | -0.313 | C4 | -0.049 | C4 | -0.068 |
| C5 | -0.142 | C5 | -0.226 | C5 | -0.067 | C5 | -0.018 |
| C6 | -0.017 | C6 | -0.205 | C6 | -0.056 | C6 | -0.056 |
| C7 | 0.294 | C7 | 0.251 | C7 | 0.201 | C7 | 0.177 |
| C8 | -0.156 | O8 | -0.244 | O8 | -0.103 | C8 | -0.043 |
| O9 | -0.234 | C9 | -0.297 | C9 | -0.034 | O9 | -0.103 |
| C10 | 0.214 | C10 | 0.190 | C10 | 0.181 | C10 | 0.197 |
| C11 | -0.303 | O11 | -0.237 | O11 | -0.140 | C11 | -0.235 |
| N12 | -0.175 | C12 | -0.706 | C12 | -0.241 | N12 | -0.090 |
| C13 | 0.001 | N13 | -0.072 | N13 | -0.061 | C13 | 0.074 |
| C14 | -0.061 | N14 | -0.198 | N14 | -0.091 | C14 | -0.063 |
| C15 | -0.037 | C15 | 0.429 | C15 | 0.071 | C 15 | -0.082 |
| C16 | 0.310 | C16 | -0.439 | C16 | -0.063 | C16 | 0.093 |
| C17 | -0.298 | C17 | 0.239 | C17 | -0.019 | C17 | -0.913 |
| C18 | 0.029 | C18 | 0.271 | C18 | 0.092 | C18 | -0.039 |
| N19 | -0.358 | C 19 | -0.349 | C 19 | -0.078 | N19 | -0.201 |
| N20 | -0.164 | C20 | -0.309 | C20 | -0.053 | N20 | -0.116 |
| C21 | 0.137 | C21 | -0.435 | C21 | -0.018 | C21 | -0.009 |
| O22 | -0.274 | N22 | -0.005 | N22 | -0.116 | O22 | -0.091 |
| N23 | -0.175 | N23 | -0.423 | N23 | -0.201 | N23 | -0.069 |
| H24 | 0.101 | Co24 | 0.078 | Ni24 | 0.148 | Cu24 | 0.197 |
| H25 | 0.100 | O25 | -0.693 | O25 | -0.272 | Cl25 | -0.432 |
| H26 | 0.096 | O26 | -0.684 | O26 | -0.276 | Cl26 | -0.428 |
| H27 | 0.105 | Cl27 | -0.352 | Cl27 | -0.700 | H27 | 0.098 |
| H28 | 0.113 | Cl28 | -0.402 | Cl28 | -0.562 | H28 | 0.095 |
| H29 | 0.164 | H29 | 0.235 | H29 | 0.095 | H29 | 0.092 |
| H30 | 0.134 | H30 | 0.270 | H30 | 0.098 | H30 | 0.084 |
| H31 | 0.137 | H31 | 0.287 | H31 | 0.117 | H31 | 0.115 |
| H32 | 0.137 | H32 | 0.239 | H32 | 0.100 | H32 | 0.107 |
| H33 | 0.109 | H33 | 0.235 | H33 | 0.097 | H33 | 0.106 |
| H34 | 0.100 | H34 | 0.357 | H34 | 0.127 | H34 | 0.116 |
| H35 | 0.115 | H35 | 0.237 | H35 | 0.098 | H35 | 0.107 |
| H36 | 0.243 | H36 | 0.239 | H36 | 0.108 | H36 | 0.107 |
|  |  | H37 | 0.253 | H37 | 0.109 | H37 | 0.095 |
|  |  | H38 | 0.260 | H38 | 0.109 | H38 | 0.134 |
|  |  | H39 | 0.244 | H39 | 0.104 | H39 | 0.247 |
|  |  | H40 | 0.321 | H40 | 0.103 | H40 | 0.115 |
|  |  | H41 | 0.271 | H41 | 0.105 |  |  |
|  |  | H42 | 0.334 | H42 | 0.250 |  |  |
|  |  | H43 | 0.414 | H43 | 0.254 |  |  |