Supplementary information

Decoupling the Impact of Electronic Structure and Electrode Wettability of Functionalized Iron Phthalocyanine Catalysts for Electrochemical Nitrate Reduction to Ammonia

Navid Noor,a Clara Argentino,a Ashkan Irannezhad,a, Amy Wuttke,b Mahtab Masouminia,a Anja Schouten,a Katrina Pegrum,a Madeline LeBreton,a Reza Eslami,a Shayan Angizi,a  Mohsen Shakouri,c Alexander Bagger,b* Drew Higgins,a *

a Department of Chemical Engineering, McMaster University, Hamilton, ON, Canada.

b Department of Physics, Technical University of Denmark, Copenhagen, Denmark.

c Canadian Light Source Inc., University of Saskatchewan, Saskatoon, SK, Canada.

Overview

Supplementary Note 1: Experimental procedure	3

Chemicals	3

CNT purification	3

Characterization and Quantification Methods	4

Wettability test	4

Ammonia quantification	4

15N isotope-labeling experiment	5

Faradaic Efficiency Calculation for NH3	5

Supplementary Note 2: Computational Details	7

Fe-Phthalocyanine with functional groups	7

Free energy corrections of adsorbates	7

Free energy corrections of molecular references	8

Supplementary Note 3: Calculation of free energies of adsorption	10

pH-dependent correction between HNO3 and NO3-	10

Calculation of adsorption energies	11

Reference states	13

Supplementary Note 4. Multiphysics Finite Element Method (FEM) mass-transport model	16

Supplementary Note 5: Mass transport and reaction modelling	18

Supplementary Note 6: Experimental results	19

ICP-OES	19

STEM image and the corresponding EDX elemental mapping:	20

Electrochemical performance results:	24

15N Isotope labelling:	31

In situ XAS of FePc-tBu/CNT:	32

Supplementary Note 7: HOMO/LUMO Levels	37

Supplementary Note 8: Electron Density Differences	39

Supplementary Note 9: Calculation of Formation Energies	40

References:	41

# Supplementary Note 1: Experimental procedure

## Chemicals

Potassium nitrate (≥99%, Sigma-Aldrich), potassium nitrate-15N (98 atom % 15N), Sigma Aldrich) sodium hydroxide (reagent > 98%, pellets (anhydrous) Sigma Aldrich, Nafion 117 containing solution (5%, Sigma-Aldrich), ethanol (anhydrous, Commercial Alcohols), sulfuric acid (95.0-98.0%, Sigma-Aldrich), iron (II) 2,9,16,23-tetra(amino)phthalocyanine (PorphyChem) iron (II) 2,9,16,23-tetra(carboxy)phthalocyanine (PorphyChem), iron (II) 2,9,16,23-tetra(t-butyl)phthalocyanine (PorphyChem), iron (II) 2,3,9,10,16,17,23,24-octa(cyano)phthalocyanine (PorphyChem) multi-walled carbon nanotubes (8 nm, Cheap Tubes), N,N-dimethylformamide (99.8%, Fisher Scientific), maleic acid (NMR standard, Sigma-Aldrich), deuterated dimethyl sulfoxide (99.5%, Sigma-Aldrich), ammonium chloride (≥99.5%, Sigma-Aldrich) ammonium sulfate (≥99%, Sigma-Aldrich).

## CNT purification

Commercial CNTs (≈500 mg) were dispersed in 100 mL of 10% HCl (prepared by mixing 27 mL concentrated HCl with 73 mL Milli-Q water) and bath-sonicated for 5 min. The suspension was then stirred at 300 rpm for 24 h at room temperature. The powder was collected by centrifugation and washed repeatedly with Milli-Q water (≈5 cycles) until the supernatant reached ~neutral pH. The purified CNTs were dried overnight at 60 °C.

To oxygen functionalized CNTs, a 3:1 (v/v) H₂SO₄/HNO₃ mixture was prepared by combining 60 mL concentrated H₂SO₄ and 20 mL concentrated HNO₃. The dried CNTs from the previous step were added, and the solution was bath-sonicated at ≤40 °C for 2.5 h (temperature kept ≤40 °C to avoid excessive viscosity). The reaction was quenched by dilution into ~800 mL water, then the powder was collected by vacuum filtration and rinsed with Milli-Q water until the filtrate was ~neutral pH. The functionalized CNTs were dried overnight at 60 °C.

## Characterization and Quantification Methods

Scanning transmission electron microscopy (STEM) and energy-dispersive X-ray spectroscopy (EDS) were carried out on a Thermo Scientific Spectra Ultra, a double aberration-corrected HRTEM/STEM operated at 300 kV and housed at the Canadian Centre for Electron Microscopy. HAADF-STEM images were acquired with a 50 pA probe current and a 28 mrad convergence angle, and EDS maps were collected using a Thermo Fisher Ultra X system equipped with six Super-X silicon drift detectors. In situ X-ray absorption spectroscopy (XAS) was conducted at the Canadian Light Source (SXRMB beamline) at ambient temperature using a custom electrochemical cell, and spectra were processed with the Demeter software suite.

## Wettability test

Wettability was evaluated by static contact-angle measurements using the sessile-drop method (Milli-Q water, ~7 µL). Droplet profiles were imaged with a scientific camera (Kiralux, Thorlabs) fitted with a 12 mm fine-focus zoom lens (MVL12X12Z, Thorlabs). The stage was backlit by a 470 nm LED (M470L4, Thorlabs), collimated with a lens (SM2F32-A) to provide uniform illumination and high edge contrast. Contact angles were extracted by Axisymmetric Drop Shape Analysis (ADSA).

ICP-OES sample preparation

Catalyst powders were digested in aqua regia (HCl:HNO₃ = 3:1, v/v) at 50 °C for 72 h to ensure complete dissolution of Fe. The digests were filtered to remove residual CNTs, and the clear filtrates were diluted 1:1 with Milli-Q water before analysis. Matrix blanks were prepared identically by diluting the 3:1 HCl/HNO₃ mixture 1:1 with Milli-Q water.

## Ammonia quantification

Ammonia in the catholyte and acid-trap (AT) solutions was quantified by the indophenol blue colorimetric assay with UV–vis detection. For each measurement, a chromogenic reagent was prepared by dissolving 5 wt% salicylic acid and 5 wt% citric acid in 20 mL of 1 M NaOH. An aliquot (2 mL) of this reagent was mixed with 2 mL of sample, followed by addition of 1 mL of 0.05 M NaClO and 0.2 mL of 1 wt% sodium nitroprusside (Na₂[Fe(CN)₅NO]) as catalyst. Mixtures were incubated for 40 min in the dark, then analyzed on a Cary 5000 UV–Vis–NIR spectrophotometer scanning 550–750 nm; absorbance at 650 nm was used to determine concentration. Concentrations were obtained from a calibration curve constructed with (NH₄)₂SO₄ standards (0.000, 0.005, 0.010, 0.020, 0.040, 0.060, 0.080, 0.100 mM). Samples were diluted as needed to fall within the calibration range.

Ammonia was also quantified by 1H NMR (600 MHz) using DMSO-d₆ as solvent and maleic acid (C₄H₄O₄) as an internal standard. The internal-standard stock was prepared by dissolving 20 mg maleic acid in 50 g DMSO-d₆ (0.04 wt%). Electrolyte samples were first acidified to pH ≈ 2 with 2 M H₂SO₄. For each measurement, 500 µL of the acidified sample was mixed with 50 µL of 0.5 M H₂SO₄, followed by 25 µL of the internal-standard stock. Sample preparation is illustrated in Figure S2. The NH₄⁺ resonance was integrated against the maleic-acid signal, and the NH₃ concentration was calculated from the integral ratio using the equation provided below.

IAIB=HACAHBCB                                                                       (1)

Where, IA and IB are the integral of maleic acid and NH4+, HA and HB are the number of protons in maleic acid and NH4+, and CA and CB are the concentrations of maleic acid and NH4+.

## 15N isotope-labeling experiment

15N isotope-labeling experiment was used to ensure that quantified ammonia is a product of electrochemical nitrate reduction to ammonia. In this experiment, chronoamperometry was performed using 0.1 M K15NO3 + 0.1 M NaOH at -0.6 VRHE for 30 minutes. Then, 15NH4+ was quantified using 1H NMR (600 MHz) using the same method as 14NH4+ quantification.

## Faradaic Efficiency Calculation for NH3

The NH3 Faradaic efficiency (FE) was calculated using the following formula (2):

FENH3=8×F×CNH3×VQ                                                                                   (2)

Where F is the Faraday constant (96485 C/mol), C is NH3 concentration (M), V is the volume of electrolyte (10 mL), and Q is the charge (C), t is time (s).

# Supplementary Note 2: Computational Details

The Density Functional Theory (DFT) calculations, were obtained using the GPAW calculator1  in plane-wave mode with 600 eV cutoff energy, using the RPBE exchange-correlation functional, Fermi smearing with width 0.05 eV, and 10-4 eV energy convergence threshold. Data from the electronic structure calculations were processed using the Atomic Simulation Environment (ASE).2

## Fe-Phthalocyanine with functional groups

The baseline structure is Fe-Phthalocyanine (FePc) with hydrogen termination of the benzene rings in a computational supercell with 10 Å vacuum padding in each direction, which is relaxed with a maximum force criterion of 0.05 eV/Å and a 1x1x1 k-point grid. The same parameters are used when adsorbed species are present. When introducing functional groups, one hydrogen is substituted per benzene ring by the respective functional group (-COOH, -NH2 and -tBu), while two hydrogens per benzene ring are each substituted by -CN.

To find the correct spin state, the metal center was initialized with 0, 1, 2, 3, and 4 μB, where it was found that the most stable configuration, i.e. lowest energy, was obtained when initializing the Fe center with 2 μB regardless of the functional group. This initial magnetic moment for the Fe atom was therefore used throughout all calculations with adsorbates. For some adsorbates the magnetic moment vanished after electronic convergence.

## Free energy corrections of adsorbates

Free energy corrections for adsorbates were calculated using a harmonic approximation as implemented in ASEs Harmonic Thermo class.

The vibrations of the adsorbate were calculated in ASE with 0.05 eV/Å force convergence threshold, while the atoms of the FePc were fixed. Remaining imaginary frequencies were replaced by 10 meV to obtain a harmonic approximation for the zero-point energy (ZPE), other contributions to the internal energy (heat capacitance), and entropic contributions. Then, the difference in Gibbs free energy between the bare catalyst, G*,  and the adsorbate, G*X, can be approximated using the Helmholtz free energy from an harmonic approximation, under the assumption that the change in pV is negligible (i.e. pV is constant under adsorption and cancels) and room temperature (T = 298.15 K):

G*X-G*=F*X+pV-(F*+pV)=F*X-F*=F*X-E*,

Where,

F*X=E*X+ZPE*X+0T=298.15KCv, harm dT-TS*X=E*X+G*X,corr

and E* is the potential energy of the bare catalyst since that one is fixed, and thus, unchanged in the approximation, not leading to vibrational contributions.

This expression, i.e. G*X-G*=E*X+G*X,corr-E* is applied in all the equations for adsorption energies presented in Supplementary Note 2.

## Free energy corrections of molecular references

The free energy corrections for molecular references were calculated using the free energy corrections with an ideal gas approximation using ASEs IdealGasThermo class [4], such that

Ggas=Egas+ZPEgas+0T=298.15KCp dT-TSgas,

where Egas is the potential energy from DFT, and all other contributions use vibrations calculated after relaxation up to at least 0.01 eV/Å, using a a 1x1x1 k-point grid in a computational cell with 10 Å vacuum padding along each direction. We used standard conditions (T = 298.15 K, p = 101325 Pa) and the parameters (keywords geometry, symmetry number, spin) in table S1 for the different reference molecules.

Table S2 Parameters used for the corresponding keywords in the Ideal gas approximation.

| Molecule | Geometry | Symmetry number | Spin |
| --- | --- | --- | --- |
| H2 | linear | 2 | 0 |
| H2O | nonlinear | 2 | 0 |
| HNO2 | nonlinear | 1 | 0 |
| HNO3 | nonlinear | 1 | 0 |
| NH3 | nonlinear | 3 | 0 |
| NO | linear | 1 | 0.5 |

# Supplementary Note 3: Calculation of free energies of adsorption

In order to calculate free energies of adsorption, we used tabulated free energies to determine the free energy differences of (r1), (r3), and (r4), in which HNO3g reacts respectively to NH3g, HNO2g, and NOg. Each of these species is used to reference the DFT calculated adsorption energies. We start with addressing the importance of including pH-dependence in NO3- (nitrate) reduction, while referencing to HNO3g.

## pH-dependent correction between HNO3 and NO3-

The considered reaction is

HNO3g+4H2g→NH3g+3H2Ol	(r1)

with a Gibbs’ free reaction energy of 3,4

ΔG(r1)0=ΔfG0(NH3(g))+3ΔfG0(H2O(l))-ΔfG0(HNO3(g))=-6.388 eV.	(3.1)

Since the actual reaction of interest is starting from NO3-, we consider the change from HNO3(g) to NO3-(aq) with a free energy change ΔGHNO3g→NO3-+H+0 3

HNO3g→NO3-aq+H+,

ΔGHNO3g→NO3-+H+0=ΔfG0(NO3-aq)-ΔfG0(HNO3(g))=-0.392 eV.

When considering non-standard conditions, the chemical potential of the anion shows a dependency on pKa and pH according to5

μNO3-=μNO3-0+kBTlnNO3-

NO3-=HNO31+10pKa-pH.

When using the assumptions [NO3-] = 0.1 M at pH=13 and pKa(HNO3) = -1.4, we obtain [HNO3] = 0.1 M. Thus for T=298 K,

ΔGHNO3→NO3-+H+=-0.392 eV+kBTlnHNO31+10pKa-pH=-0.451 eV,	(3.2)

which is plotted for the reduction as ΔGNO3-+H+→HNO3=-ΔGHNO3→NO3-+H+ against pH on the SHE scale in Figure SI 1b, which shows for pH>pKa, a constant value for -ΔGHNO3→NO3-+H+ with respect to SHE, corresponding to a pH-dependence on RHE scale (Figure SI 1a, red line):

ΔGNO3-+H+→HNO3,RHE=0.451 eV+0.059 eV×pH.	(3.3)

Figure SI 1. Free energy differences ΔGNO3/2-+H+→HNO3/2,RHE for different concentrations of HNO3/2 and adsorption energies of correspondingly *NO3/2 on FePc-FePc on (a) RHE scale and (b) SHE scale to illustrate the pH-dependence for pH>pKa on the RHE scale.

Therefore, the free energy change for nitrate reduction ΔGr,RHE  is pH-dependent on an RHE scale, using ΔG(r1)0 from (3.1) and ΔGHNO3→NO3-+H+ from (3.2) applied to reaction

NO3-aq+9H++8e-→NH3g+3H2Ol	(r2)

ΔGr,RHE =ΔG(r1)0+ΔGNO3-+H+→HNO3,RHE=-6.388 eV+0.451 eV+0.059 eV×pH.	(3.4)

## Calculation of adsorption energies

In the following, it is described how we determined all free energies of adsorption referenced to HNO3 via tabulated formation energies, and further include the offset -ΔG(HNO3→NO3-+H+),RHE=ΔGNO3-+H+→HNO3,RHE from (3.3) to use NO3- as the formal “zero” in the free energy diagrams

GHNO3,corr=ΔGNO3-+H+→HNO3,RHE	(3.5)

which is the reference for the adsorption energies

ΔG*NO3=G*NO3+12GH2-G*-GHNO3+GHNO3,corr-eVRHE, and

ΔG*HNO3=G*HNO3-G*-GHNO3+GHNO3,corr.

Furthermore, based on the reaction

HNO3g+H2g→HNO2g+H2Ol	(r3)

with a standard change in free energy of -2.172 eV,3 we define with respect to NO3- again using the offset ΔGNO3-+H+→HNO3,RHE

GHNO2,corr=-2.172 eV+ΔGNO3-+H+→HNO3,RHE-(-2eVRHE)	(3.6)

yielding an expression for the following adsorption energies

ΔG*NO2=G*NO2+12GH2-G*-GHNO2+GHNO2,corr-eVRHE

ΔG*HNO2=G*HNO2-G*-GHNO2+GHNO2,corr.

Similarly, we obtain for the reaction

HNO3g+32H2g→NOg+2H2Ol	(r4)

a standard change in free energy of -3.245 eV,3 resulting in

GNO,corr=-3.245 eV+ΔGNO3-+H+→HNO3,RHE-(-3eVRHE)	(3.7)

ΔG*NO=G*NO-G*-GNO+GNO,corr

ΔG*NOH=G*NOH-G*-12GH2-GNO+GNO,corr-(-eVRHE)

ΔG*NHO=G*NHO-G*-12GH2-GNO+GNO,corr-(-eVRHE)

For the remaining adsorption energies, we reference with respect to the reaction energy ΔGr,RHE from (4)

ΔG*NH2O=G*NH2O-G*-GH2O+ΔGr,RHE-GNH3+32GH2-(-5eVRHE)

ΔG*NH2OH=G*NH2OH-G*-GH2O+ΔGr,RHE-GNH3+GH2-(-6eVRHE)

ΔG*NH2=G*NH2-G*+ΔGr,RHE-GNH3+12GH2-(-7eVRHE)

ΔG*NH3=G*NH3-G*+ΔGr,RHE-GNH3-(-8eVRHE)

In the expressions above, we have furthermore used the Computational Hydrogen Electrode (CHE),6 such that on the RHE scale, the chemical potential of a proton-electron pair yields with applied potential VRHE, expressed against RHE:

μH++e-=12GH2-eVRHE

This applies for each proton-electron step in the reduction shown in Figure 4a in the main text, i.e. in each step starting from reaction coordinate 3 to 4, the energy is lowered by 0.5 eV under an applied voltage of - 0.5 V vs. RHE. However, the reaction step from reaction coordinate 0 to 1 is an oxidation and therefore the free energy for reaction coordinate 1 increases by 0.5 eV.

## Reference states

In the free energy diagrams, the references HNO3, HNO2, NO2-, NO and NH3 are included. To summarize from above, these states are purely determined from thermodynamical tables and corrections for potential and pH, i.e. from Eqs. (3.4)-(3.7)

GHNO3plot=ΔGNO3-+H+→HNO3,RHE=0.451 eV+0.059 eV×pH

GHNO2plot=-2.172 eV+0.451 eV+0.059 eV×pH+2eVRHE)

GNOplot=-3.245 eV+0.451 eV+0.059 eV×pH+3eVRHE)

GNH3plot=-6.388 eV+0.451 eV+0.059 eV×pH+8eVRHE).

For nitrite (NO2-), the derivation is equivalent to the case of nitrate above [5]:

ΔGHNO2g→NO2-+H+0=ΔfG0(NO2-aq)-ΔfG0(HNO2(g))=+0.142 eV

Assuming non-standard conditions [NO2-] = 0.1 M at pH=13 and using pKa(HNO2)=3.25 [5], we obtain [HNO2] = 0.1 M. Thus for T=298 K,

ΔGHNO2→NO2-+H+=0.142 eV+kBTlnHNO21+10pKa-pH=0.083 eV.

This is plotted as a reduction as ΔGNO2-+H+→HNO2=-ΔGHNO2→NO2-+H+ against pH on the SHE scale in Figure SI 1b as a brown line, which shows a constant value for pH>pKa(HNO2), corresponding to a pH-dependence on RHE scale (like it was also shown for nitrate):

ΔGNO2-+H+→HNO2,RHE=-0.083 eV+0.059 eV×pH.	(3.8)

Thus,

GNO2-plot=GHNO2plot+ΔGNO2-+H+→HNO2,RHE=-2.172 eV+0.451 eV+2eVRHE-0.083 eV,

which means that both on RHE and SHE scale, there is no pH dependence between NO2- and NO3- since the contributions cancel for the pH>pKa(HNO2) as expected from Figure SI 1 for the region pH>pKa(HNO2).

How the positions of the references are defined with respect to each other is also illustrated in Figure SI 2.

Figure SI 2. Overview of how the reference states are related to each other. Given that NO3- is defined to be at 0 eV, the free energy of HNO3 is fixed through equation (3.3). The levels of HNO2, NO and NH3 are set according to tabulated free energies or rather their changes following the reactions (r1), (r3), and (r4). Knowing the level of HNO2, defines the position of NO2-. All free energy levels are plotted for pH=0 and 0 V vs. SHE. The indicated values for ΔGNO2-+H+→HNO2,RHE and ΔGNO3-+H+→HNO3,RHE include pH dependence and the value for pH=0 uses the assumptions of 0.1M concentration for both ions, as explained in Supplementary Note 3.

# Supplementary Note 4. Multiphysics Finite Element Method (FEM) mass-transport model

We resolve steady-state transport and interfacial kinetics in a one-dimensional catholyte diffusion layer adjacent to a planar cathode, with x=0 at the catalyst–electrolyte interface and x=δ at the edge of the diffusion layer. The goal is to capture concentration changes, migration in the electric field, and their feedback on competing cathodic reactions. The electrolyte is isothermal, and incompressible with constant physical properties; and all potentials are reported vs RHE. The dissolved species are H+(aq), OH-(aq), and NO3-​(aq). Their molar fluxes Ni​ follow the Nernst–Planck form:

| Ni=-Di∇ci-ziDiFRTci∇ϕl+ciu | (4.1) |
| --- | --- |

with concentration ci​, diffusion coefficient Di, charge zi​, Faraday’s constant F=96485 C mol-1, gas constant R=8.314 J mol-1K-1, temperature T, and electrolyte potential ϕl​ (V). Steady species conservation is:

| ∇.Ni=Ri | (4.2) |
| --- | --- |

where Ri is volumetric reaction rate. Charge transport in the electrolyte is il=F iziNi and satisfies ∇.il=0. In the solid, is=-σs∇ϕs (Ohm’s law), and current continuity holds at the interface: is.n=-il.n. We assume a locally electroneutral electrolyte, izici=0, and enforce water self-ionization algebraically, cH.cOH=Kw(T).

Electrochemistry occurs at x=0, where two cathodic reactions compete. In alkaline media we use the balanced overall forms:

| 2 H2O+2e-→H2+2 OH- (HER, n=2) | (4.3) |
| --- | --- |
| NO3-+6 H2O+8e-→NH3+9 OH- (NO3R, n=8) | (4.4) |

The cathodic partial current density for reaction is modeled with a concentration-dependent Butler–Volmer form

| ik=-i0,kcl,kc0mk exp-αc,kF ηkRT | (4.5) |
| --- | --- |

where i0,k is the exchange current density, cl,k ​the interfacial concentration, mk an effective order, and αc,k the cathodic transfer coefficient. The overpotential is

| ηk=ϕs-ϕl-Ukeq(pH) | (4.6) |
| --- | --- |

With UHEReq=0 V vs RHE and Ukeq(pH)  found from Nernst equation. Interfacial currents map to species fluxes through Faraday’s law and stoichiometry:

| -n.Nix=0=kvi,kiknkF | (4.7) |
| --- | --- |

Where vi,k is the signed stoichiometric coefficient of species i in reaction k and nk​ the electrons per mole in the corresponding overall reaction. The total interfacial current is i=kik​, and Faradaic efficiencies are FEk=iki.

Boundary conditions are chosen to reflect a boundary-layer experiment. At the bulk side (x=δ) we impose Dirichlet concentrations cNO3-δ=CNO3-∞​ and cH+δ​, cOH-δ consistent with the specified bulk pH and set ϕlL=0 as the reference. At the electrode (x=0), species fluxes follow the interfacial stoichiometry above; the solid potential is fixed by the applied value, ϕs=Eapp​ (vs RHE).

# Supplementary Note 5: Mass transport and reaction modelling

The mechanism by which surface wettability (via contact angle, θ) and bubble formation control the diffusion‐layer thickness has been documented in the gas-evolution literature.7-9 In our model, wettability enters in two places: the bubble departure diameter db(θ) and the time-averaged bubble coverage Θ(θ). For db(θ), we use a Fritz force balance between buoyancy and capillary pinning that retains the exact contact-angle dependence of a spherical cap:

dbθ=ψ24σsinθg ρl- ρg(2+3cosθ-cos3 θ)

where σ is the surface tension, g gravity, and ρl, ρg​ are the liquid and gas densities. The factor ψ is a single calibration constant.10 The time-averaged bubble coverage, Θ(θ), was expressed as the product of two factors: the areal density of active nucleation sites (Nact), and the bubble footprint area (Afoot), following the conceptual form described by Vogt et al9. With db(θ) and Θ(θ) specified, the bubble-induced mass transfer coefficient is found from Sherwood correlations: 7

Sh1= 12π RG1/2 Sc1/2 Θ1/2

Sh2= 25 ReG1/2 Sc0.341- 83 RGR (1+Θ)

Sh= Sh12+ Sh22

kbubble= Sh Ddbθ

In these equations, Sc is Schmidt number defined as ν/D, RG is Reynolds number defined as V/Adbν in which V/A is volumetric gas flux (m S-1) obtained from Faraday’s law of electrolysis:

VA= jRTneFP

Here, j is the current density, R the gas constant, T the temperature, P the pressure, ne number of electrons, and F Faraday’s constant. Finally, the diffusion-layer thickness is calculated as: 7

δ θ= Dkbubble

# Supplementary Note 6: Experimental results

## ICP-OES

Table S1: FePc-NH2/CNT, FePc-tBu/CNT, FePc-COOH/CNT, and FePc-CN/CNT wt.% in different catalysts measured by ICP-OES.

| Sample | MPc/ MTPP (wt.%) |
| --- | --- |
| FePc-NH2/CNT | 6.7 |
| FePc-tBu/CNT | 9.2 |
| FePc-COOH/CNT | 9.7 |
| FePc-CN/CNT | 8.7 |

## STEM image and the corresponding EDX elemental mapping:

Figure S1. STEM image and the corresponding EDX elemental mapping of FePc-NH2/CNT [C(blue), O(yellow), N(orange), and Fe(cyan)].

Figure S2. STEM image and the corresponding EDX elemental mapping of FePc-tBu/CNT [C(blue), O(yellow), N(orange), and Fe(cyan)].

Figure S3. STEM image and the corresponding EDX elemental mapping of FePc-COOH/CNT [C(blue), O(yellow), N(orange), and Fe(cyan)].

Figure S4. STEM image and the corresponding EDX elemental mapping of FePc-CN/CNT [C(blue), O(yellow), N(orange), and Fe(cyan)].

## Electrochemical performance results:

Figure S5. Redox potential Fe3+/Fe2+ in FePc-R/CNT determined from CVs as a function of the Hammett constant of functional groups.

Figure S6. Linear sweep voltammetry of different FePc-R/CNT samples at 10 mV s-1 in 0.1 M KNO3 + 0.1 M NaOH.

Figure S7. NH3 partial current density of FePc-NH2/CNT, FePc-tBu/CNT, FePc-COOH/CNT, and FePc-CN/CNT in electrochemical NO3- conversion to NH3 in 0.1M KNO3 + 0.1M NaOH, 30 minutes chronoamperometry in an H-type cell.

S8. Faradaic efficiency and total current density of FePc-tBu/CNT for electrochemical NO3- conversion to NH3 in 0.1 M KNO3 + 0.1 M NaOH via 30 minutes chronoamperometry measurements in an H-type cell.

Figure S9. Faradaic efficiency and total current density of FePc in electrochemical NO3- conversion to NH3 in 0.1M KNO3 + 0.1M NaOH, 30 minutes chronoamperometry in an H-type cell.

Figure S10. Turnover frequency of FePc-NH2/CNT, FePc-tBu/CNT, FePc-COOH/CNT, and FePc-CN/CNT in electrochemical NO3- conversion to NH3 in 0.1M KNO3 + 0.1M NaOH, 30 minutes chronoamperometry in an H-type cell.

Figure S11. Faradaic efficiency and total current density of acid-washed CNTs in electrochemical NO3- conversion to NH3 in 0.1M KNO3 + 0.1M NaOH, 30 minutes chronoamperometry in an H-type cell.

## 15N Isotope labelling:

Figure S12. 1HNMR spectra of FePc-NH2/CNT, FePc-COOH/CNT, FePC-CN/CNT and FePc-tBu/CNT for 15N isotope labelling test performed in 0.1M K15NO3 and 0.1M NaOH after 30 minutes chronoamperometry at -0.8 VRHE.

## In situ XAS of FePc-tBu/CNT:

Figure S13. in situ XANES spectra of Fe K edge of a) FePc-tBu/CNT at electrode potentials ranging from OCP to -0.9 VRHE. In situ EXAFS spectra of b) FePc-tBu/CNT under reaction conditions (in 0.1 M KNO3 and 0.1 M NaOH, 30 minutes chronoamperometry in a custom designed H-type cell).

Table S2: Electronic and surface properties of different catalysts.

| Catalysts | Functional group | Hammet constant | Wettability | Contact angle | Cluster formation potential (VRHE) |
| --- | --- | --- | --- | --- | --- |
| FePc-NH2/CNT | Electron donating | -0.61 | Strongly hydrophilic | 24.4° | No cluster formation |
| FePc-COOH/CNT | Electron withdrawing | 0.45 | Strongly hydrophilic | 17.5° | -0.8 VRHE |
| FePc-CN/CNT | Electron withdrawing | 0.66 | Weakly hydrophilic | 43.8° | -0.7 VRHE |
| FePc-tBu/CNT | Electron donating | -0.2 | Weakly hydrophilic | 50.1° | -0.9 VRHE |

Table S3: Diffusion thickness layer and contact angle of FePc-R/CNT catalysts.

| Catalyst (variant) | Contact angle | Diffusion thickness (μm) |
| --- | --- | --- |
| FePc-NH2/CNT | 24.4° | 125 |
| FePc-COOH/CNT | 17.5° | 110 |
| FePc-CN/CNT | 43.8° | 170 |
| FePc-tBu/CNT | 50.1° | 210 |

Figure S14. Chemical structure of -F group functionalized FePc.

Figure S15. a) Faradaic efficiency and total current density of FePc-F/CNT, b) NH3 partial current density of FePc-F/CNT and FePc-CN/CNT in electrochemical NO3- conversion to NH3 in 0.1M KNO3 + 0.1M NaOH, 30 minutes chronoamperometry in an H-type cell.

# Supplementary Note 7: HOMO/LUMO Levels

The HOMO/LUMO levels were identified as belonging to the spin down channel, while the highest single occupied molecular orbital in the spin up channel was lower in energy than the HOMO, and equivalently, the lowest unoccupied molecular orbital in the spin up channel lies higher than the overall LUMO; for all systems regardless of the functional group. The HOMO/LUMO energies in the main text are reported with respect to the vacuum level, that was determined for each system as the average electrostatic potential in the vacuum region of the computational cell with a distance of at least 5Å away from any atom and where the electron density is smaller than 10-7 eÅ-3. This vacuum energy level (in eV for the electron energy in vacuum) is subtracted from the “raw” HOMO/LUMO energies to obtain the values in Figure 4c. The DOS for each system is plotted in Figure SI 16, while the wave functions in Figure SI 17 show that those are qualitatively very similar for the HOMO and LUMO of each system with the biggest differences in the vicinity of the functional groups.

(a)

(b)

(d)

(c)

Figure S 16. Density of states for spin up electrons in blue and spin down electrons in red for a) FePc-CN, b) FePc-COOH, c) FePc-NH2, and d) FePc-tBu.

(c)

(a)

(d)

(b)

(g)

(e)

(h)

(f)

(i)

(j)

Figure SI 17. Pseudowavefunctions belonging to the LUMO and HOMO of a,b) FePc, c,d) FePc-CN, e,f) FePc-COOH g,h) FePc-NH2, I,j) FePc-tBu.

# Supplementary Note 8: Electron Density Differences

We defined the electron density difference associated with introducing a functional group as the difference between the electron density of the catalyst ρFePc-group vs. the electron density of the same structure with removed functional groups ρFePc-removed group (i.e. without termination), and the phthalocyanine removed with only the functional groups ρgroup, such that the visualized difference is:

ΔρFePc-group=ρFePc-group-ρFePc -removed group+ρgroup.

The electron densities ρFePc-removedgroup and ρgroup are obtained as single point calculations after removing the affected atoms from the relaxed structure ρFePc-group.

The electron density difference ΔρFePc-group as seen in Figure SI 18 was visualized using VESTA 11.

(a)

(b)

(d)

(c)

Figure SI 18. Electron density differences with respect to FePc as described in Supplementary Note 4 for a) FePc-CN, b) FePc-COOH, c) FePc-NH2, and d) FePc-tBu.

# Supplementary Note 9: Calculation of Formation Energies

The formation energy of FePc with a functional group, Ef,FePc-group, to assess the stability of the Fe atom can be evaluated as

Ef,FePc-group=EFePc-group-EFe-EH2Pc-group+EH2(g),

where the reference energies are EFe for solid iron Fe; EH2Pc-group for the phthalocyanine with functional groups, but with two terminating hydrogens instead of a metal center; and EH2(g) for the hydrogen atoms after replacement by iron.

To mitigate the choice of reference e.g. Fe(bcc) or the fact if the EH2Pc-group is stable or not it is better to look at the differences in formation energy between FePc-group and FePc:

ΔEf,FePc-group=Ef,FePc-group-Ef, FePc

=EFePc-group-EFe-EH2Pc-group+EH2(g)-(EFePc-EFe-EH2Pc+EH2(g))
=EFePc-group-EFePc-(EH2Pc-group-EH2Pc)

# References:

1	Hjorth Larsen, A. et al. The atomic simulation environment—a Python library for working with atoms. Journal of Physics: Condensed Matter 29, 273002 (2017). https://doi.org/10.1088/1361-648X/aa680e

2	Larsen, A. H. et al. The atomic simulation environment—a Python library for working with atoms. Journal of Physics: Condensed Matter 29, 273002 (2017).

3	Haynes, W. M. CRC handbook of chemistry and physics.  (CRC press, 2016).

4	Calle-Vallejo, F., Huang, M., Henry, J. B., Koper, M. T. & Bandarenka, A. S. Theoretical design and experimental implementation of Ag/Au electrodes for the electrochemical reduction of nitrate. Physical chemistry chemical physics 15, 3196-3202 (2013).

5	Riyaz, M. & Bagger, A. NOX reduction mechanism: Thermal vs electrochemical step. Electrochimica Acta 513, 145429 (2025).

6	Nørskov, J. K. et al. Origin of the overpotential for oxygen reduction at a fuel-cell cathode. The Journal of Physical Chemistry B 108, 17886-17892 (2004).

7	Burdyny, T. et al. Nanomorphology-enhanced gas-evolution intensifies CO2 reduction electrochemistry. ACS Sustainable Chemistry & Engineering 5, 4031-4040 (2017).

8	Zhao, X., Ren, H. & Luo, L. Gas bubbles in electrochemical gas evolution reactions. Langmuir 35, 5392-5408 (2019).

9	Vogt, H. & Stephan, K. Local microprocesses at gas-evolving electrodes and their influence on mass transfer. Electrochimica Acta 155, 348-356 (2015).

10	Demirkır, Ç., Wood, J. A., Lohse, D. & Krug, D. Life beyond fritz: on the detachment of electrolytic bubbles. Langmuir 40, 20474-20484 (2024).

11	Momma, K. & Izumi, F. VESTA: a three-dimensional visualization system for electronic and structural analysis. Journal of Applied Crystallography 41, 653-658 (2008). https://doi.org/doi:10.1107/S0021889808012016