Vacuum Disk Filters

Iron Concentrate

Filtrate

Conditioning

Tank

Flocculant

Filter Cake

Flowsheet of concentrate filtration circuit at Sanabad iron beneficiation plant

Ceramic Vacuum Disk Filters

Filter Cake

Iron Concentrate

Input variables

Feed Particle Size

Disk Rotation Speed

Filter Tanks Pulp Level

Tank Agitator Speed Flocculant Addition

Filter Wash Cycle Time Washing Acid Concentration

Optimized variables

Feed Particle Size: 39% <38 μm

Disk Rotation Speed: 30 rpm

Filter Tanks Pulp Level: 50%

Tank Agitator Speed: 50 rpm

Flocculant Addition: 10 g/t

Filter Wash Cycle Time: 6 hours

Routine Cleaning: 1% HNO₃, 45–60 min

Output variables

Cake Moisture

Cake Thickness

Filtrate Turbidity