Study of natural aging on nanoparticles and their strengthening effect in Al-Mg-Si alloy

Zhenjie Cui 1,2,3, Haichang Jiang 1,3*, Duo Zhang 1,2,3, Yuanyuan Song 1,3, Desheng Yan 1,3, Lijian Rong 1,3*

Supplementary material

Details of the calculation of yield strength

The yield strength σy of the Al-Mg-Si alloys consists of precipitation hardening σp, solid solution strengthening σs and lattice resistance σi. The overall yield strength calculation can be achieved by adding the various contributions as equation (1) [1-4]. σi is generally assumed to be 10 MPa and σs is given by equation (2) [1, 5]:

σy=σp+σs+σi             (1)

σs=j=Mg,  Sikjωjα2/3        (2)

where kj is a constant with a specific value for element j and ωjα is the mass concentration of a specific alloying element in the solid solution.

The σp as shown in equation (7) can be explained mainly from the following aspects: (i) difference in shear modulus between precipitates and the matrix leads to modulus strengthening σmod, (ii) chemical strengthening σchem which results from the additional matrix-precipitate interface created by the dislocation when it shears through precipitates, and (iii) the lattice misfit between precipitates and the matrix products a strain field around the coherent of semi-coherent nanoparticles, and results in coherency strengthening σcoh. (iiii) The contribution from GC σGC. These four strengthening mechanisms can also be described by equations as follows [1, 4, 6, 7]:

σmod=0.0055M (ΔG)3/2 (2VfG)1/2 (rb)0.275   (3)

σchem=(6γ3bVfπΓ)1/2 r-1                  (4)

σcoh=2.6Mε3/2G2Vf rb1/2            (5)

σGC= 160(Vf)1/2                        (6)

σp=σcut=σmod+σchem+σcoh+σGC         (7)

where Vf is the volume fraction. The meanings and values of the parameters in the equations are shown in Table S1. σmod, σchem, σcoh and σGC is jointly determine the σp.

Table S1. The parameters used in the calculation

| Parameter | Unit | Value | Comments |
| --- | --- | --- | --- |
| G | N·m-2 | 2.7×1010 | The magnitude of the Shear modulus [1, 3, 7] |
| b | m | 2.84×10-10 | The magnitude of the burgers vector [1, 3, 7] |
| M | - | 3.1 | Taylor factor [1, 3, 7] |
| rc | m | 5×10-9 | From Ref. [4, 8] |
| kSi | MPa/wt%2/3 | 66.3 | From Ref. [5] |
| kMg | MPa/wt%2/3 | 29.0 | From Ref. [5] |
| γβ″ | J/m2 | 0.084 | Interfacial energy of β″/Al [4] |
| γβ′ | J/m2 | 0.18 | Interfacial energy of β′/Al [4] |
| εβ″ | - | 2.10% | The strain of β″ relative to Al matrix [4] |
| εβ′ | - | 0.99% | The strain of β′ relative to Al matrix [4] |
| ΔGβ″ | MPa | 7.7×103 | The difference of shear modulus β″ and Al matrix [9-11] |
| ΔGβ′ | MPa | 1.1×104 | The difference of shear modulus β′ and Al matrix [9-11] |
| σi | MPa | 10 | The intrinsic strength of the Al matrix [3, 4, 7] |

References

[1] S. Esmaeili, D.J. Lloyd, W.J. Poole, Modeling of precipitation hardening for the naturally aged Al-Mg-Si-Cu alloy AA6111, Acta Mater. 51(12) (2003) 3467-3481.

[2] R.K.W. Marceau, A. de Vaucorbeil, G. Sha, S.P. Ringer, W.J. Poole, Analysis of strengthening in AA6111 during the early stages of aging: Atom probe tomography and yield stress modelling, Acta Mater. 61(19) (2013) 7285-7303.

[3] M.J. Starink, L.F. Cao, P.A. Rometsch, A model for the thermodynamics of and strengthening due to co-clusters in Al–Mg–Si-based alloys, Acta Mater. 60(10) (2012) 4194-4207.

[4] M. Yang, H. Chen, A. Orekhov, Q. Lu, X. Lan, K. Li, S. Zhang, M. Song, Y. Kong, D. Schryvers, Y. Du, Quantified contribution of β″ and β′ precipitates to the strengthening of an aged Al–Mg–Si alloy, Mat. Sci. Eng A-Struct 774 (2020).

[5] O.R. Myhr, Ø. Grong, S.J. Andersen, Modelling of the age hardening behaviour of Al–Mg–Si alloys, Acta Mater. 49(1) (2001) 65-75.

[6] A.J. ARDELL, Precipitation Hardening, Metall. Trans. A 16A (1985) 1985-2131.

[7] M. Song, Modeling the hardness and yield strength evolutions of aluminum alloy with rod/needle-shaped precipitates, Mat. Sci. Eng A-Struct 443(1-2) (2007) 172-177.

[8] I.M. Robertson, H.K. Birnbaum, P. Sofronis, Dislocations in Solids, 1979.

[9] B. Zhang, L. Wu, B. Wan, J. Zhang, Z. Li, H. Gou, Structural evolution, mechanical properties, and electronic structure of Al–Mg–Si compounds from first principles, J. Mater. Sci. 50(19) (2015) 6498-6509.

[10] R. Yu, J. Zhu, H.Q. Ye, Calculations of single-crystal elastic constants made simple, Comput. Phys. Commun 181(3) (2010) 671-675.

[11] B. Bakó, E. Clouet, L.M. Dupuy, M. Blétry, Dislocation dynamics simulations with climb: kinetics of dislocation loop coarsening controlled by bulk diffusion, Philos. Mag. 91(23) (2011) 3173-3191.