Table 1S. Comprehensive summary of quercetin-loaded nanocomposite formulations with their key physicochemical attributes, formulation variables, and biological performance data, including drug loading and encapsulation efficiencies.

| Drug | Type of nanocomposite | NP Shape | Normal cell line | Cancer cell line | Size of nanocarriers(nm) | Zeta Potential (mV) | Normal cell Cytotoxicity | Loading Efficiency (%) | Encapsulation Efficiency (%) | Surface Area to Volume Ratio | Thermodynamic Stability | Biocompatibility-biodegradable | Drug Release Profile | pH/Temperature Sensitivity | Cellular Uptake and Mechanism | Selective Toxicity including ROS/Apoptosis | Ref |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Quercetin | ZnO nanoparticles loaded with quercetin, coated with chitosan-alginate | --- | HUVEC | MCF-7, MDA-MB-231 (breast cancer) | --- | --- | Reduced cytotoxicity compared to uncoated ZnO@Qc | --- | --- | --- | --- | Yes (chitosan-alginate coating) | Controlled, dose-dependent release | Yes, pH-sensitive | Enhanced uptake demonstrated; mechanism includes apoptosis induction | Selective toxicity via apoptosis induction; upregulation of CASP3, CASP8, CASP9; reduced normal cell toxicity | (1) |
| Quercetin | Gelatin-agarose-iron oxide (G-Aga-Fe₂O₃) hybrid nanocarriers loaded with quercetin | Spherical | L929 | MCF-7 | 152 | −40 | High biocompatibility (96% viability) | 43.75 | 85.25 | --- | Stable | Yes | Controlled, sustained release | pH-sensitive (95% release at pH 5.4, 60% at pH 7.4) | Enhanced uptake implied; mechanism not detailed | Selective toxicity to cancer cells (46% mortality in MCF-7), sparing normal cells | (2) |
| Quercetin | Dual-responsive disulfide-linked core–shell alginate-coated mesoporous silica nanohybrid | Monodispersed, <50 nm | --- | HT29 | <50 | −30.71 ± 0.71 | --- | 20.49 | --- | >700 m²/g (high surface area) | --- | Yes | Enhanced release in intestinal fluid | Dual-sensitive (responsive to pH and redox) | Targeted colon delivery implied; improved uptake assumed | Superior anticancer effect vs free polyphenols on HT29 cells | (3) |
| Quercetin | Magnetic iron oxide nanoparticles coated with PEG loaded with quercetin (MAG@PEG@QUE) | --- | --- | MCF-7 | --- | --- | --- | --- | --- | --- | --- | Yes (PEG coating) | Controlled, enhanced delivery | --- | Clustered uptake in vesicles; enhanced by static magnetic field | Apoptosis induction; selective cell death in targeted regions | (4) |
| Quercetin | Quercetin-conjugated nanocrystalline cellulose/cetyltrimethylammonium bromide/folic acid (NCC/CTAB/FA) nanoparticles | Rod and spherical | HDF cells | AGS, A2780 | 354.4 ± 65.37 nm | -27.05 ± 1.64 | Higher viability vs cancer cells | --- | 81.17 | --- | --- | --- | --- | --- | Cellular uptake suitable; induced apoptosis by flow cytometry | Dose-dependent apoptosis induction; antioxidant activity with free radical scavenging (ABTS and DPPH assays) | (5) |
| Quercetin | Chitosan (CS) and folate-chitosan (FA-CS)-coated magnetic nanoparticles loaded with quercetin (MNP-CS-Q, MNP-FA-CS-Q) | round nanoparticles | --- | HCT-116 | 122.32 ± 8.56 | +30.78 ± 0.8 | cell viability was lower | 80.45 (MNP-CS), 54.4 (MNP-FA-CS) |  | --- | --- | Yes | Controlled, low release (~6.4–7.7% in 24h at tumor pH) | Tumor pH-sensitive implied | Targeting via folate coating; uptake enhanced by magnetic properties | Enhanced dose-dependent antitumor effect with IC50 of 1.46 & 1.30 µg/mL vs free drug; apoptosis inferred | (6) |
| Quercetin | Chitosan, alumina (γ-Al2O3), graphene quantum dots hydrogel nanocarriers loaded with quercetin (CS/γAl2O3/GQDs/QUE) | --- | --- | Lung cancer cells | 453.23 | +11.06 | --- | --- | 87 | --- | Stable | --- | Controlled, sustained over 96 h | pH-dependent sustained release | Not explicitly detailed, assumed cellular uptake via nanocarriers | Cell death due to slow controlled release effect | (7) |
| Quercetin | PLA-PEG-FA/PLA-chitosan polymeric nanoparticles loaded with Moringa oleifera extracts and quercetin | Spherical | --- | MCF-7, BT-549 | 230 ± 0.92 | +6.4 ± 0.82 | Low toxicity (biocompatible) | --- | --- | --- | --- | Yes | Higher release at acidic pH | pH-sensitive (favors acidic tumor microenvironment) | Targeted delivery via folate receptor-mediated uptake | Increased apoptosis in BT-549 cells (31.2% pre-apoptotic; 7.15% post-apoptotic) | (8) |
| Quercetin | Branched cationic triblock micelles (PEG)13-(P4VP+140-PCL3)75% loaded with quercetin (QR) | Micellar | --- | --- | --- | Controlled by charge density | Low acute toxicity | --- | 88 | --- | Stable | Yes | Sustained release; polymer degradation in acidic conditions | Acidic pH enhances degradation | Cellular uptake supported by optimized charge balance | Genotoxicity inversely related to charge density; antioxidant activity >94% retained | (9) |
| Quercetin | Quercetin-loaded electrospun fibrous mats based on PLA and PLA/PEG | Cylindrical fibers | --- | HeLa cervical cancer cells | PLA: 768 ± 138; PLA/PEG: 671 ± 137; PLA+QUE: 807 ± 159; PLA/PEG+QUE: 713 ± 143 | --- | Lower toxicity vs cancer cells | --- | 96% | --- | --- | Yes (PLA and PEG are biodegradable) | Faster QUE release from PLA/PEG vs PLA mats | --- | Uptake via fibrous mat release mechanism | High anticancer activity with lower toxicity to normal cells | (10) |
| Quercetin | aphene oxide sol-gel (SJ-go) nanoparticles | --- | BEAS-2B human bronchial epithelial (normal) | --- | --- | --- | IC50 318.86 μg/mL; cytotoxic at higher doses | Not applicable | Not applicable | --- | --- | Likely biocompatible | --- | --- | Not detailed | Cytotoxicity linked to decreased GSH-Px activity; curcumin showed stronger antioxidant and anti-inflammatory effects compared to quercetin | (11) |
| Quercetin | Magnetic bacterial bots: Lactobacillus rhamnosus decorated with gold nanoclusters and quercetin-loaded magnetic nanoparticles | --- | --- | HeLa cervical cancer cells | --- | --- | --- | --- | --- | --- | --- | Yes (human-friendly bacteria) | Controlled via external magnetic field | Magnetically responsive | Bacteria-mediated targeted delivery, enhanced by magnetic field | High cytotoxicity (up to 91% with magnet); ROS generation increased 1.8-2.3-fold; necroptosis induction in 74% cells | (12) |
| Quercetin | pH-sensitive hydrogel nanocomposite: polyacrylamide, starch, graphene quantum dots loaded with quercetin | Semi-globular | L929 (normal) | U-87 MG (brain carcinoma) | 42.68–58 | +53.3 | 13% reduced cytotoxicity vs free QC | 48 | 89 | --- | Stable | Yes | Targeted release; 46% higher release in tumor-like pH | pH-sensitive (tumor microenvironment) | Stable dispersion; effective BBB transport assumed | Significant biocompatibility; targeted cytotoxic effects on tumor cells | (13) |
| Quercetin | Cyclodextrin-Zein-TiO2 nanoparticle-based nanoemulsion loaded with quercetin | Spherical | L929 | A549 | 80–120 | ~−50 | Biocompatible | 47.5 | 87.75 | --- | Stable | Yes | Controlled, sustained release | pH-sensitive (7.4 vs 5.4) | Uptake likely via endocytosis; stable blood circulation | Selective toxicity with higher inhibition in A549 lung cancer cells | (14) |
| Quercetin | Folic acid-functionalized oxidized carbon nanotubes (FA-OMC) loaded with curcumin and quercetin | Layered, nano-sized | NIH/3T3 (normal fibroblasts) | --- | Nano scale, low PDI | Negative | High biocompatibility | High (exact % ---) | High (exact % ---) | --- | High thermal stability | --- | Extended, controlled release | --- | Likely endocytosis-supported | Enhanced bactericidal efficacy vs MDR Gram-positive bacteria; morphological disruption confirmed | (15) |
| Quercetin | Chitosan nanoparticles from Hermetia illucens larvae (CSlarvae) and crustaceans (CScrustac) loaded with quercetin | particles are surrounded by a network of organic matter | --- | --- | 100–150 nm | +7.5 to +39.3 | --- | --- | 77 ± 7% | --- | --- | Yes | Faster release from CSlarvae than CScrustac; sustained release | --- | Likely endocytosis-mediated; antibacterial assay positive | Synergistic antimicrobial effect; superior against E. coli and M. flavus with CSlarvae NPs | (16) |
| Quercetin | MIL-100 metal-organic framework (MOF) modified with quercetin and loaded with lenalidomide derivative (MIL-100@QC@L1) | --- | --- | MDA-MB-231 (triple-negative breast cancer) | --- | --- | --- | --- | 95.18 | --- | --- | --- | Controlled | --- | --- | Reduced viability to 47.8% at 10 µg/mL after 24h, superior to free drugs | (17) |
| Quercetin | Ti3C2Tx MXene nanosheets loaded with quercetin (MX-Que) | Mono- and few-layer nanosheets | L929 (normal) | AGS, gastric cancer | ~ 40–60 | –22.14 ± 2.04 mV | 13% reduced cytotoxicity vs free QC | --- | 89 | --- | Stable | Yes | 55.22% release in 72 h under acidic pH and mild hyperthermia | pH 5.5 and 42 °C (mild hyperthermia) responsive | Uptake enhanced by nanosheet morphology; photothermal-assisted release | Induces ROS, apoptosis, ferroptosis; 55.5% cytotoxicity under NIR; tumor growth inhibited in vivo | (18) |
| Quercetin | Hyaluronic acid-coated quercetin nanoparticles (HBQ NPs) modified with phenylboric acid, integrated in multifunctional microneedle (GHCQ) patch | Nanoparticles; microneedles | --- | A375 melanoma | --- | --- (stable under physiological pH) | Excellent biocompatibility, low toxicity | --- | --- | --- | Stable | Yes | Sustained release: ~62% quercetin over 21 days at pH 5.0 | pH-sensitive (acidic tumor microenvironment) | Targeted uptake via CD44 receptor (HA ligand) on A375 cells | 83% inhibition of melanoma cells, ROS scavenging, antibacterial, promotes wound healing and angiogenesis | (19) |
| Quercetin | Beta-cyclodextrin-based inclusion complex loaded with quercetin and doxorubicin (β-CD@QD IC) | --- | MCF-7/DOX | MCF-7/DOX (multidrug-resistant breast cancer) | --- | --- | --- | --- | --- | --- | --- | Yes (cyclodextrin-based) | Sustained, controlled release per Higuchi kinetics | --- | Enhanced uptake via efflux pump inhibition | Overcomes doxorubicin resistance by inhibiting ABCG2 pump; increased ROS, apoptosis, nuclear condensation | (20) |
| Quercetin | Mesoporous silica-encapsulated cerium oxide nanozymes loaded with quercetin ((CeO2/Que)@mSiO2) | Core-shell spherical | A549 (normal lung) | Inflammatory/cancer models | Not explicitly specified (mesopores ~11 nm; CeO2 cores ~4 nm) | Not explicitly specified | Excellent biocompatibility | Enhanced Que loading due to large pore size (~11 nm) | Not explicitly specified, high implied | High surface area by BET (~1000 m²/g range) | Stable crystalline CeO2 core | Yes (mesoporous silica) | Sustained controlled release; enhanced ROS scavenging; anti-inflammatory | --- pH sensitivity; sustained drug release | Uptake via endocytosis; nanozyme catalytic activity enhances ROS modulation | Significant ROS scavenging; downregulation of inflammatory cytokines (IL-1β, IL-6, TNF-α) | (21) |
| Quercetin | MIL-101(Fe) metal-organic framework loaded with quercetin (Que@MIL-101(Fe)) | Octahedral MOF | MCF-10A (normal breast cells) | MCF-7 breast cancer | --- (typically 100–300 nm MOF size range) | --- | Low toxicity to normal cells | 54.9 | --- | High surface area typical MOF | Stable | Yes | Controlled release, 56.7% at pH 5 over 9 days | pH-sensitive (faster release at acidic pH) | Cellular uptake via endocytosis; selective cytotoxicity | Significant inhibition of MCF-7 cells with low effect on MCF-10A, enhanced anticancer effect | (22) |
| Quercetin | Thermosensitive liposomes containing IR-MnO2 (IR820 conjugated to BSA-MnO2) and quercetin (IRQL), with cell-penetrating peptide (IRQL/CPP) | Liposomal ~160-180 nm | --- | U87 glioblastoma | ~160 nm (IRQL); ~180 nm (IRQL/CPP) | --- | --- | IR-MnO2: 83.1%; Que: 65.5% | --- | --- | Stable | Yes | NIR light-triggered release | Temperature and NIR-responsive | Enhanced uptake by CPP-mediated delivery | Inhibits tumor growth under NIR irradiation; sensitizes cells via HSP70 downregulation; enhanced photothermal and chemo effects | (23) |
| Quercetin | Polylactic acid microspheres surface-modified with carboxymethyl cellulose (PPC microspheres) loaded with alendronate-hydroxyapatite-quercetin nanoparticles (AHQ) | Microspheres | --- | Relevant to osteoarthritis | 5.5–10 µm | −12.47 ± 3.24 mV to −49.53 ± 4.85 mV | >98% biocompatibility | 2.90 ± 0.54 % to 7.12 ± 0.58 %. | 98.51 ± 1.03 % to 59.37 ± 0.62 % | --- | Stable | Yes | Sustained, controlled release; designed for intra-articular injection | pH-sensitive (acidic microenvironment) | Cell adhesion enhanced by CMC surface modification; retention in joint cavity | Antioxidant activity (DPPH 87.36%; ABTS 90.7%); reduces ROS overproduction in OA | (24) |
| Quercetin | Dy3+-doped Fe3O4 nanoparticles encapsulated in multilamellar liposomes co-loaded with quercetin and functionalized with cell-penetrating peptide (IRQL/CPP) | Small multilamellar vesicles (~160-180 nm) | HEK293 (normal human embryonic kidney cells) | U87 glioblastoma cells | ~160 nm (IRQL); ~180 nm (IRQL/CPP) | --- | Negligible cytotoxicity | IR-MnO2: 83.1; Quercetin: 65.5 | --- | --- | Stable | Yes | NIR-triggered release of IR-MnO2 and quercetin | Temperature and NIR light-responsive | Enhanced intracellular uptake via CPP-mediated endocytosis | Enhanced photothermal therapy; HSP70 downregulation sensitizes cancer cells; tumor growth prevented in vivo | (25) |
| Quercetin | Quercetin-loaded nanostructured lipid carriers (QUE-NLCs) incorporated into Carbopol 934 gel (QUE-NLC-GEL) | Spherical | --- | AGA mice model | 335 | −24 | Non-irritant skin profile | --- | ~94.56 | --- | Stable | Yes | Sustained release ~76.75% in 72 h | --- | Superior skin penetrability shown by CLSM | Comparable efficacy to marketed 2% Minoxidil in AGA mice | (26) |
| Quercetin | Lignin/chitosan conjugated nanoparticles (LCNPs) prepared by green interfacial co-assembly loaded with quercetin (Q-LCNPs) | Spherical, polymeric with 60-200 nm size by TEM | --- | --- | 60-200 | Approximately +30 mV (positive surface charge) | High biocompatibility in initial tests | --- | 95.75 | --- | Stable polymeric network | Yes (biopolymers) | pH-responsive release: 21.9% at pH 1.2, 68.5% at 7.4, 99.8% at 6.8 | pH-sensitive (gastric to intestinal pH) | Uptake likely via endocytosis; controlled release via diffusion and polymer relaxation | High encapsulation efficiency; sustained release; anticipated antioxidant activity | (27) |
| Quercetin | Sodium alginate microspheres loaded with quercetin/magnesium nanoparticles for osteoarthritis therapy (Que/Mg-SA microspheres) | Microspheres | --- | Chondrocytes or OA cells likely | --- | --- | --- | --- | --- | --- | Stable | Yes | Sustained release; kinetics follow Weibull model | --- | Cellular uptake likely via endocytosis; mucoadhesion enhances retention | Anti-inflammatory; promotes osteogenesis via macrophage immunomodulation; ROS scavenging | (28) |
| Quercetin | Stem cell-derived exosome co-loaded with hydroxyl-terminated phosphorus dendrimers (AK76) and quercetin (QAE NPs) for Parkinson’s disease treatment | Spherical | --- | Neurodegeneration model (PD mice) | ~269.7 | --- | Favorable cytocompatibility | --- | --- | --- | Stable | Yes | Controlled drug release; pharmacokinetics suited for nasal delivery | --- | Nasal mucosa penetration; accumulates in brain without BBB crossing | Scavenges ROS, promotes M2 microglial polarization, reduces inflammation, induces autophagy; improves motor and non-motor symptoms in PD mice | (29) |
| Quercetin | BSA-coated MnFe2O4 nanoparticles loaded with quercetin (Qu-BSA@MnFe2O4 NPs) | Spherical, ~7 nm core size; 85 nm hydrodynamic size | --- | 4T1 murine breast cancer | 85.27 ± 0.26 | Not explicitly detailed | High biocompatibility (minimal hemolysis <5%) | 27.5 | Not specifically stated | --- | Stable | Yes | 62% release at pH 5.7 after 120h; 41% at pH 7.4 | pH-sensitive (acidic favors release) | Favorable binding with BSA and MnFe2O4 surface; endocytosis-mediated uptake | Dose-dependent cytotoxicity on 4T1 tumor cells; improves quercetin stability and bioavailability | (30) |
| Quercetin | Quercetin-loaded ginkgo-derived starch nanoparticles (SNPs/Qc) | Spherical | --- | 3LL murine lung cancer | 166.25 nm | --- | Excellent biocompatibility | 26.62% | --- | --- | Stable | Yes | Significant early apoptosis (33% at 25 µg/mL); dose-dependent inhibition; tumor volume reduced by 49.4% in mice after 15 days | --- | Tumor-targeted penetration enhanced over free quercetin | Antitumor efficacy: induced apoptosis, cell cycle arrest, improved survival by 20% in mice | (31) |
| Quercetin | Cationic polymer micelles carrying bioactive sesquiterpene lactones (e.g., alantolactone, isoalantolactone) from Inula helenium L. for antibacterial biofilm treatment | Micelles | --- | Bacterial biofilms (e.g., Staphylococcus aureus) | 83 ± 6 nm | 21.2 mV | --- | --- | 72% | --- | Stable | Yes | Controlled release sustained over time | --- | Enhanced penetration of biofilms via cationic charge and nanosize | Potent anti-biofilm and antibacterial properties, including MRSA strains inhibition | (32) |
| Quercetin | Supramolecular co-assembled Fmoc-FRGDF peptide and hyaluronic acid hydrogel loaded with quercetin (Que) | Hydrogel network | --- | --- | 12-31 nm | --- | High biocompatibility | 15.5% to 16.8% | 85.8% to 90.3% | Not applicable | Physically stable | Yes | Sustained release; modulated by hydrogel network | pH-responsive; sustained over days | Cellular uptake modulated by HA-CD44 receptor targeting and peptide interactions | Antioxidant, anti-inflammatory effects; supports tissue regeneration | (33) |
| Quercetin | Supramolecular co-assembled Fmoc-FRGDF peptide and hyaluronic acid hydrogel loaded with quercetin (Que) | Hydrogel matrix | normal oral epithelial cells | --- | Hydrogel form ( 12.8 to 20.1 nm) | --- | High biocompatibility | 16.8% | 90.3% | Not applicable | Physically stable with enhanced modulus upon Que loading | Yes | Controlled, sustained release following Korsmeyer-Peppas kinetics | pH-responsive; sustained over days | Uptake likely by HA receptor-mediated endocytosis and peptide affinity | Antioxidant and anti-inflammatory activity; potential for tissue regeneration and bioactive delivery | (33) |
| Quercetin | Pluronic® F127/chitosan-myristic acid copolymer mixed micelles (QTN MM) loaded with quercetin | Spherical | Albino rats (in vivo) | --- | ~34.08 | +36.24 | Demonstrated safety | ~95.10 | ~12.28 | --- | Physically stable | Yes | Enhanced dissolution, ex vivo permeation; improved bioavailability | Not explicitly pH sensitive | Improved permeation shown ex vivo; likely endocytosis | Improved antioxidant and hepatoprotective activity vs. free quercetin in CCL4 rat liver injury model | (34) |
| Quercetin | Glycethosomes and Allanthosomes loaded with Rosa canina extract, incorporated into Spanish broom wound dressings | Spherical vesicles | Human fibroblasts | Not applicable | Allanthosomes: 237.3 ± 14.9; Glycethosomes: 146.6 ± 3.2 | Allanthosomes: −37.21 ± 2.62; Glycethosomes: −33.40 ± 2.74 | Non-cytotoxic |  | >70 (Allanthosomes: 72.9 ± 4.8) | --- | Stable | Yes | Sustained release consistent with wound healing requirements | pH 4.18–4.9 (optimal for wound environment) | Facilitates bioadhesion and local delivery | Promotes fibroblast proliferation and migration; complete scratch closure ~30 h | (35) |
| Quercetin | Biodegradable nanoemulsion-based edible film containing vitamin D3 and Cordia myxa mucilage | Film with dispersed nanoparticles | --- | Not applicable | 3231.7 ± 0.10 nm | − 75.50 ± 0.10 mV | Yes (biocompatible) |  | 91.5% | --- | Improved thermal stability | Yes | Sustained vitamin D3 retention over 14 days | --- | Mucoadhesion and antimicrobial effects enhance function | Antimicrobial activity against Gram-positive bacteria; 67.4% antioxidant activity; flavonoid content 218.2 µg/g | (36) |
| Quercetin | pH-responsive chitosan/halloysite nanotubes/graphene quantum dots nanocomposite loaded with quercetin (CS/HNTs/GQDs@QC) | Nanotube/nanoparticle hybrid | L929 fibroblast cells | A549 lung carcinoma cells | --- | --- | Low toxicity on L929 | 44.25 | 85.5 | --- | Stable | Yes | Higher release with GQDs: 97.5% at pH 5.4, 67% at pH 7.4 | pH-sensitive release, first-order kinetics | Endocytosis likely; enhanced uptake with GQDs and HNTs | Highest cytotoxicity on A549 cells; apoptosis induction early (74.4%) and late (5.15%) stages | (37) |
| Quercetin | Corn starch-coated quercetin nanoliposomes (QT-NLs) optimized by central composite design | Spherical | VERO cells | MCF-7 breast cancer | 39.5 | -41.2 | Demonstrated safety | >80 | >80 | --- | Stable | Yes | Sustained and controlled release | --- | Enhanced uptake demonstrated | IC50 5.8 μM vs 7.9 μM for free QT; induces apoptosis and necrosis; causes cell cycle arrest | (38) |
| Quercetin | pH-responsive starch/polyvinyl alcohol/halloysite nanotube double nanoemulsion loaded with quercetin (S/PVA/HNT/QUE) | Semi-spherical | --- | MCF-7 breast cancer | 171.25 | --- | --- | 46.25 | 87 | --- | Stable | Yes | Sustained release, control by pH; release models indicate diffusion/dissolution mechanisms | pH-sensitive release, higher at acidic pH (5.4) than neutral pH (7.4) | Likely endocytosis; enhanced intracellular delivery | Significant cytotoxicity; increased apoptosis in MCF-7 cells compared to free drug | (39) |
| Quercetin | Quercetin-loaded nickel ferrite (NiFe2O4) magnetoliposomes (QC-MLs) | Spherical | --- | MCF-7 breast cancer | ~329.5 | --- | --- | 7.3 ± 0.1 | 83.5 ± 1.4 | --- | Stable | Yes | 62.3% release at pH 5.1; 44% at pH 7.4 after 24 h | pH-sensitive release | Magnetic field-assisted targeting and cellular internalization | Enhanced cytotoxicity vs free QC; tested via MTT on MCF-7 cells | (40) |
| Quercetin | Alginate-modified quercetin-loaded ZIF-8 (Alg@Qc@ZIF-8) | Spherical | --- | 4T1 breast cancer | ~50 (SEM), 154.9 ± 7.25 (DLS) | −23.8 ± 5.33 | Not separately detailed | 10.40 ± 0.02 | --- | --- | Stable | Yes | pH-sensitive release; ~3.6 times more Qc released at pH 5.4 than pH 7.4 after 24 h | pH-responsive release | Likely endocytosis and intracellular release | IC50 2.16 times lower than free Qc; enhanced tumor growth inhibition and metastasis reduction in vivo | (41) |
| Quercetin | Chitosan/starch/graphene quantum dots/titanium dioxide nanocomposite loaded with quercetin (CS/Starch/GQDs/TiO2@QC) | Mixed nanoparticle/hydrogel | --- | A549 lung carcinoma | --- | --- | Biocompatible | --- | --- | Porous structure | Stable | Yes | Fickian diffusion-controlled release; stimuli-responsive to pH and temperature | Responsive to pH 5.4/7.4, 37 °C/42 °C | Endocytosis likely facilitated by GQDs and polymer matrix | Enhanced cytotoxicity vs free QC; MTT assay results against A549 model | (42) |
| Quercetin | Agarose-Graphene Quantum Dots-α-Fe2O3 hydrogel nanocomposite loaded with quercetin | Spherical | L929 (normal fibroblasts) | HepG2 liver carcinoma | ~279.04 | +52.8 | Non-toxic | 47 | 86.25 | --- | Stable | Yes | Sustained and enhanced QC retention and release | pH-responsive; enhanced with Span 80 surfactant | Likely endocytosis; enhanced delivery with magnetic component | Enhanced anticancer activity on HepG2 cells; potential safety toward normal cells | (43) |
| Quercetin | Quercetin-loaded mesoporous silica SBA-15 modified with APTES, carbon quantum dots, PVP, folic acid | Porous nanoparticles | MCF-10A (normal breast epithelial) | MCF-7 breast cancer | --- | --- | Less toxic on MCF-10A | --- | --- | High surface area (mesoporous) | Stable | Yes | pH 5.3 optimal release; controlled and sustained release | pH-sensitive release | Folate receptor-mediated targeting likely | Higher toxicity on cancer cells (IC50 13.4 μM) vs normal cells (IC50 53.6 μM) | (44) |
| Quercetin | Hydrogel nanocomposite composed of gelatin/polyvinyl alcohol/titanium dioxide loaded with quercetin (G/PVA/TiO2/QC) | Porous network | --- | MCF-7 breast cancer | --- | +23.6 | Biocompatible | 45.7 | 88.25 | Porous | Stable | Yes | pH-responsive release with higher QC release at acidic pH | pH-sensitive (higher release at tumor pH) | Endocytosis and cellular uptake likely | Higher apoptosis and cytotoxicity vs free quercetin indicated by MTT and flow cytometry | (45) |
| Quercetin | Hydrogel nanocomposite of polyvinylpyrrolidone (PVP), agarose, and hydroxyapatite (HAp) loaded with quercetin | Spherical | --- | --- | 440-536 | --- | --- | --- | --- | High (due to HAp nanoparticles) | Stable | Yes | Controlled, pH-responsive release; less burst effect | Acidic pH enhances release | Likely endocytosis | Enhanced apoptotic induction due to sustained release of QC | (46) |
| Quercetin | Quercetin-conjugated magnetite nanoparticles (QMNPs) | Spherical | --- | MCF-7 breast cancer | ~40 | --- | Non-toxic in vivo | --- | --- | --- | Stable | Yes | pH-sensitive controlled release; enhances radiosensitivity and apoptosis induction | pH-sensitive | Endocytosis; magnetic field enhances targeting | Significant inhibition of cancer proliferation; radiosensitization benefits | (47) |
| Quercetin | Polyethylene imine (PEI)-coated Fe3O4 nanoparticles with quercetin | Spherical | --- | MCF-7 breast cancer | 91.2 | +65.1 | Biocompatible | 74 | --- | --- | Stable | Yes | Controlled release at 37°C and 42°C | Temperature and pH sensitive | Endocytosis | Enhanced cytotoxicity and morphological alterations in MCF-7 cells | (48) |
| Quercetin | Carboxymethyl cellulose (CMC), agarose (AG), carbon quantum dots (CQDs) nanocarrier loaded with quercetin (CMC/AG/CQDs@QC) | Spherical | --- | A549 lung cancer | --- | --- | --- | Enhanced (vs CMC/AG) | Enhanced (vs CMC/AG) | --- | Stable | Yes | Controlled and sustained release; pH-sensitive increase at pH 5.4 | pH-responsive, higher release at acidic pH 5.4 | Endocytosis likely | Highest apoptosis in A549 cells; superior antitumor efficacy | (49) |
| Quercetin | Chitosan nanoparticles loaded with Quercetin (Que) and Valproic Acid (VPA) | Spherical | SH-SY5Y human neuroblastoma | SH-SY5Y human neuroblastoma | 180.5 ± 8.23 nm | 27.2 ± 3.67 | Sustained cell viability protection against oxidative stress (H2O2-induced) | 62.22% | >95% | --- | Stable | Yes | --- | --- | Endocytosis likely | Enhanced antioxidant activity; cytoprotective effects against oxidative stress in SH-SY5Y cells | (50) |
| Quercetin | Starch/zein/montmorillonite (MMT) nanocomposite loaded with quercetin | Spherical | L929 (normal) | A549 lung cancer | 50–100 | --- | Biocompatible | --- | --- | --- | Stable | Yes | pH-dependent, 29% release in first 12h, sustained release | pH-sensitive (pH 5.4 and 7.4 studied) | Endocytosis likely | Enhanced cytotoxicity on A549; minimal toxicity on L929 cells | (51) |
| Quercetin | Alginate-Chitosan nanocomposite with eugenol-loaded silver nanoparticles | Varied morphology | Mouse fibroblast | --- | ~30 (Ag NPs) | −25 (Ag NPs eugenol) | High biocompatibility, low cytotoxicity | --- | Not applicable | --- | Stable | Yes | Sustained release with prevented burst effect | pH-responsive | Endocytosis and gradual release | High antimicrobial and antioxidant effects; enhanced wound healing; reduced toxicity | (52) |
| Quercetin | Polyacrylic acid (PAA)-agarose/Fe3O4@SiO2 hydrogel nanocomposite loaded with quercetin | Spherical | --- | U-87 MG glioma cancer | ~193 | +38 | --- | 86 | 48 | --- | Stable | Yes | Controlled, pH-responsive release best fit Korsmeyer-Peppas model | pH 5.4 and 7.4 | Endocytosis and magnetic interaction likely | Enhanced apoptosis compared to free QC; elevated ROS generation | (53) |
| Quercetin | Fe3O4 nanoparticles coated with PEI and loaded with quercetin | Spherical | --- | MCF-7 breast cancer | 90-100 | --- | Biocompatible | Enhanced drug loading | --- | --- | Stable | Yes | Increased drug release in cancer microenvironment | Acidic pH and temperature sensitive | Receptor-mediated endocytosis | Higher cytotoxic impact on cancer cells vs free quercetin | (53) |
| Quercetin | Gelatin-oxidized alginate hydrogel with chitosan-coated zein nanoparticles (quercetin) and doxorubicin loaded hydrogel | Porous, flexible | --- | MCF-7 breast cancer | 218.8 ± 2.77 | 52.5 ± 3.80 | safe | 2.22 to 5.89% | 67.32 ± 0.06% | High porosity | Stable | Yes | Distinct release for DOX (81.2%), QC (9.7%) at pH 6.8 | pH 6.8 | Endocytosis likely | 20.7 fold enhanced cytotoxicity for DOX+QC hydrogel over DOX alone; increased apoptosis confirmed | (54) |
| Quercetin | Cu-based metal-organic frameworks (MOFs): Cu2(BDC)2(DABCO) and Cu2(F4BDC)2(DABCO) loaded with quercetin | Spherical | HEK-293 human embryonic kidney | HeLa cervical cancer | --- | --- | Low cytotoxicity | 49.5 (Cu2(BDC)2(DABCO)), 41.3 (Cu2(F4BDC)2(DABCO)) | --- | High surface area | Stable | Yes | Sustained release up to 15 days; pH-controlled release | pH-sensitive | Endocytosis likely | Induced apoptosis; excellent anticancer efficacy against HeLa cells | (55) |
| Quercetin | Carboxymethyl cellulose (CMC) and starch-based hydrogel nanocomposite with copper-carbon quantum dots (Cu-CQDs) loaded with quercetin | Spherical | L929 (normal) | U87-MG glioma | 151.57 ± 37 | +38.8 | High viability (92%) | 47.00 ± 0.45 | 86.25 ± 0.75 | High surface area (due to hydrogel matrix) | High | Yes | Sustained, pH-sensitive release; enhanced solubility/stability | pH-sensitive (acidic pH favored) | Endocytosis likely | Significant selective cytotoxicity; reduced cancer cell viability (48%); ROS induction noted | (56) |
| Quercetin | Carboxymethyl cellulose/polyvinyl pyrrolidone/graphitic carbon nitride (g-C3N4) nanocomposite loaded with quercetin | Spherical | --- | MCF-7 breast cancer | 160 | −38.7 | --- | 95 | --- | High surface area | Stable | Yes | Controlled, pH-sensitive release; 97% release at pH 5.4, 54% at pH 7.4 | pH-sensitive | Endocytosis likely | Significant cytotoxicity and apoptosis enhanced by g-C3N4 presence | (57) |
| Quercetin | Polyacrylic acid (PAA), polyethylene glycol (PEG), carbon quantum dots (CQDs) nanocomposite loaded with quercetin | Spherical | --- | MCF-7 breast cancer | --- | --- | --- | 47 | 89 | High | Stable | Yes | Sustained acidic pH release; selective drug release | pH-sensitive with tumor acidity | Endocytosis likely | Higher cytotoxicity and apoptotic death vs free drug; synergistic with CQDs | (58) |
| Quercetin | Quercetin fullerene conjugate (QFC), chitosan-coated QFC | Spherical | SH-SY5Y neuroblastoma | SH-SY5Y neuroblastoma | QFC: 179.2 ± 1.10, CC-QFC: 293.4 ± 2.757 | QFC: -5.28 ± 1.43, CC-QFC: +11.6 ± 0.4 | High viability (80.69% at 50 μg/ml) | 42.77 (loading) | 85.55 (entrapment) | --- | Stable | Yes | Controlled release due to ester bond degradation | --- | Mucoadhesive properties enhanced by chitosan coating | Low ciliotoxicity; promising nose-to-brain delivery for Alzheimer's | (59) |
| Quercetin | Agarose (AGA) modified with polyethylene glycol (PEG) hydrogel coated with ferric oxide (Fe2O3) loaded with 5-fluorouracil (5-Fu) | Spherical | --- | Breast cancer | 223 | −47.6 | Biocompatible | --- | --- | --- | Stable | Yes | pH-sensitive controlled release; sustained release at pH 5.4 and 7.4 | Responsive to pH (tumor acidic environment) | Endocytosis and magnetic targeting likely | No deleterious effects observed on normal cells; targeted toxicity on tumor cells | (60) |
| Quercetin | Carboxymethyl cellulose/agarose/cerium oxide (CMC/Aga/CeO2) nanocomposite loaded with quercetin | Spherical | L929 (normal) | HepG2 hepatocellular carcinoma | 193.48 | −61.6 | High viability (94%) | 51 | 88.25 | High | High | Yes | Sustained, tumor pH-selective release (98% at pH 5.4, 64% at pH 7.4) | pH-sensitive | Endocytosis likely | Selective cytotoxicity in HepG2; reduced normal cell toxicity; ROS induction noted | (61) |
| Quercetin | Polyacrylic acid (PAA), polyvinyl pyrrolidone (PVP), MoS2 nanocomposite loaded with 5-Fluorouracil (5-FU) | Spherical | L929 (normal) | A549 lung cancer | ~315 | −33.5 | Low toxicity | 46 | 87.25 | High due to microemulsion | Stable | Yes | Controlled, sustained release | pH-sensitive | Endocytosis; sustained retention by niosomal microemulsion | Enhanced anticancer activity in A549 cells; biocompatible to normal cells | (62) |

References

1.	Khalighi N, Reiisi S, Mokhtari A, Heidari R, Ghorbanpoor M. Quercetin-loaded zinc oxide nanoparticles encapsulated in chitosan-alginate: a synergistic approach to cancer and bacterial therapy. Naunyn-Schmiedeberg's Archives of Pharmacology. 2025:1-17.

2.	Khoz R, Pourmadadi M, Yazdian F, Rahdar A, Razzaq S, Fathi-karkan S, et al. Quercetin-loaded gelatin/agarose/Fe2O3 hybrid nanocarriers in a microemulsion matrix: synthesis, characterization, and cancer therapeutic potential. Materials Today Communications. 2025:112597.

3.	Alallam B, Abdkadir E, Hayati A, Keong YY, Lim V. Alginate coated mesoporous silica nanoparticles as oral delivery carrier of curcumin and quercetin to colon cancer: preparation, optimization, characterization, and anticancer activity. Drug Delivery and Translational Research. 2025:1-42.

4.	Tiburzi S, Lezcano V, Principe G, Montiel Schneider MG, Miravalles AB, Lassalle V, et al. Quercetin-loaded magnetic nanoparticles: a promising tool for antitumor treatment in human breast cancer cells. Journal of Drug Targeting. 2025:1-16.

5.	Soltani M, Ahmadzadeh N, Nasiraei Haghighi H, Khatamian N, Homayouni Tabrizi M. Targeted cancer therapy potential of quercetin-conjugated with folic acid-modified nanocrystalline cellulose nanoparticles: a study on AGS and A2780 cell lines. BMC biotechnology. 2025;25(1):29.

6.	Macedo JBd, Bueno JNS, Kanunfre CC, Miranda JRdA, Bakuzis AF, Ferrari PC. Polymer-Functionalized Magnetic Nanoparticles for Targeted Quercetin Delivery: A Potential Strategy for Colon Cancer Treatment. Pharmaceutics. 2025;17(4):467.

7.	Karami M, Pourmadadi M, Abdouss M, Kalaee M. Synthesis, characterization, and in vitro analysis of a chitosan/gamma alumina/graphene quantum dots/bio-hydrogel for quercetin delivery to lung cancer cells. Bionanoscience. 2025;15(1):62.

8.	Noruzpour M, Zakaria RA, Zare N, Bourang S, Ebrahimi HA, Granados-Principal S. Delivery of Moringa oleifera extract via PLA-PEG-FA/chitosan-PLA NPs into breast cancer cell lines. BioNanoScience. 2025;15(2):287.

9.	Yousfi RE, Atanase LI, Makaoui A, Achalhi N, Belkadi MC, Dalli M, et al. Enhanced Quercetin Encapsulation through Charge Density and Amphiphilicity Tuning in Cationic Triblock Micelles. ACS Applied Polymer Materials. 2025;7(10):6365-83.

10.	Stoyanova N, Nachev N, Georgieva A, Toshkova R, Spasova M. Electrospun Quercetin-Loaded PLA and PLA/Polyethylene Glycol Fibers: Preparation, Characterization, and In Vitro Evaluation. Pharmaceutics. 2025;17(5):577.

11.	Cagil EM, Ozcan F, Korucu EN, Kuvvet KY, Menevse E. Curcumin and quercetin modulate oxidative stress and inflammation of healthy lung cells treated with sol-gel graphene oxide nanoparticles. Biochemical and Biophysical Research Communications. 2025:152584.

12.	Roy S, Debasmita D, Dey U, Ghosh SS, Chattopadhyay A. Unveiling the cytotoxic potential of quercetin-loaded magnetic bacterial bots against cervical cancer. ACS Applied Materials & Interfaces. 2025;17(4):5799-812.

13.	Ordoukhani P, Pourmadadi M, Abdouss M. Development and Assessment of Polyacrylamide-Starch Hydrogel Nanocomposites with Graphene Quantum Dots for Targeted Quercetin Delivery to Brain Tumors. Carbohydrate Polymer Technologies and Applications. 2025:100848.

14.	Bahadori M, Pourmadadi M, Abdouss M, Jafari SH. Novel Carbohydrate-Based Nanomedicine: A pH-Responsive Cyclodextrin/Zein/TiO₂ Nanoemulsion for Sustained Release and Enhanced Anti-cancer Effects of Quercetin. Carbohydrate Polymer Technologies and Applications. 2025:100874.

15.	Gul J, Jabbar A, Perveen S, Awan AN, Shah MR. Development of Folic Acid Functionalized Carbon Nanotubes for Efficient Delivery of Curcumin and Quercetin Against Pathogenic Bacteria. Journal of Cluster Science. 2025;36(1):10.

16.	Guarnieri A, Mallamaci R, Trapani G, Ianniciello D, Scieuzo C, Iannielli F, et al. Physicochemical and Biological Properties of Quercetin-Loaded Low-Molecular-Weight Chitosan Nanoparticles Derived from Hermetia illucens Larvae and Crustacean Sources: A Comparative Study. Pharmaceutics. 2025;17(8):1016.

17.	Özsoy M, Tok YP, Eskiler GG, Tok F, Karakus S, Ozsoy Y, et al. The lenalidomide derivative loaded and quercetin modified MIL-100 based novel drug delivery system for breast cancer treatment. Journal of Drug Delivery Science and Technology. 2025;108:106923.

18.	Liu J, Niu S, Sheng Y, Zhou X, Zhang K, Hu X, et al. Quercetin-loaded Ti3C2Tx MXene nanosheets enhance chemo-photothermal therapy in gastric cancer. Materials & Design. 2025:114392.

19.	Fang H, Xu J, Zhu J, Ma H, Feng Z, Du J, et al. A Multifunctional Microneedle Patch Combined with Quercetin Nanoparticles for Local Drug Release Therapy and Wound Healing after Skin Tumor Surgery. ACS Applied Materials & Interfaces. 2025.

20.	Pawar CS, Balamurugan K, Baskar S, Prasad NR, Khan HA. Enhancing chemosensitivity in drug-resistant breast cancer cells using β-cyclodextrin-loaded quercetin and doxorubicin inclusion complex via modulating SRC/PI3K/akt pathway. Applied Biochemistry and Biotechnology. 2025;197(6):4068-95.

21.	Zhou S, Zhang Y, Casals E, Zeng M, Morales-Ruiz M, Liu Q, et al. Mesoporous Silica-Encapsulated Cerium Oxide Nanozymes and Quercetin for Synergistic ROS-Modulated Downregulation of Inflammatory Cytokines. International Journal of Nanomedicine. 2025:8191-207.

22.	Majidinia M, Mirhosseyni M, Abdollahzadeh N, Ghareghomi S, Khatibi A. MIL-101 (Fe) Nanoplatform for pH-Triggered Quercetin Release: Unlocking Potent Pro-oxidant and Anticancer Synergy in Breast Cancer Therapy. Journal of Molecular Structure. 2025:142966.

23.	Das S, Dash BS, Lu Y-J, Tg D, Chen J-P. Photo-Enhanced Chemotherapy with NIR-Triggered Co-Delivery of IR820-MnO2 and Quercetin from Targeted Thermosensitive Liposomes for Photo–Chemo Combination Cancer Therapy. ACS Applied Materials & Interfaces. 2025;17(28):40303-25.

24.	Yang L, Yao J, Shi D, Wang F, Zheng X, Huang Z, et al. Controllable preparation of hydrophilic alendronate hydroxyapatite quercetin multifunctional polylactic acid microspheres for treating osteoarthritis. International Journal of Biological Macromolecules. 2025;310:143071.

25.	Govindharaj P, Murugan D, Gupta S, Dhayalan A, Lahiri BB, Dasgupta A, et al. Design of Green-Synthesized Dy3+-Doped Iron Oxide Nanoparticle-Entrapped Liposomes for Synergistic Modulation of MRI Contrast, Magnetic Hyperthermia, and Combined Anticancer Efficacy. ACS Applied Bio Materials. 2025.

26.	Sayyed MM, Patil TS, Khairnar TD, Gujarathi NA, Aher A, Agrawal YO. QbD-Enabled Development of Quercetin Dihydrate-Loaded Nanostructured Lipid Carriers: In Vitro Characterization, Safety and Efficacy Assessment in Androgenetic Alopecia Mice Model. BioNanoScience. 2025;15(2):216.

27.	Yanev Z, Georgieva D, Hristova S, Tzanova M, Nicheva D, Andonova-Lilova B, et al. Innovative in situ interfacial Co-Assembled lignin/chitosan Nanoparticles—Green synthesis, physicochemical characterization, in vitro release, and intermolecular interactions. International Journal of Molecular Sciences. 2025;26(14):6883.

28.	Chen J, Wu G, Wu J, Jiao Z. Sodium alginate microspheres loaded with Quercetin/Mg nanoparticles as novel drug delivery systems for osteoarthritis therapy. Journal of Orthopaedic Surgery and Research. 2025;20(1):300.

29.	Zhang L, Zhan M, Sun H, Zou Y, Laurent R, Mignani S, et al. Mesenchymal Stem-Cell-Derived Exosomes Loaded with Phosphorus Dendrimers and Quercetin Treat Parkinson’s Disease by Modulating Inflammatory Immune Microenvironment. ACS Applied Materials & Interfaces. 2025;17(22):32013-27.

30.	Hashemi N, Naderlou S, Mohammadi A, Danafar H. An integrated computational and experimental study of BSA-coated MnFe 2 O 4 nanoparticles as a drug delivery platform for quercetin. Materials Advances. 2025;6(9):2925-41.

31.	Sun Y, Cong K, Wang T, Li X, Li T, Fan G, et al. Quercetin-Loaded Ginkgo Starch Nanoparticles: A Promising Strategy to Improve Bioactive Delivery and Cellular Homeostasis in Functional Foods. Foods. 2025;14(11):1890.

32.	Stancheva R, Damyanova T, Paunova-Krasteva T, Veleva R, Topouzova-Hristova T, Ivanova V, et al. Cationic Polymer Micelles as Carriers of Bioactive Sesquiterpene Lactones from Inula Helenium L. for Effective Treatment of Bacterial Biofilms. Pharmaceutics. 2025;17(6):800.

33.	Su X-N, Wang Y-Y, Khan MF, Zhu L-N, Chen Z-L, Wang Z, et al. Supramolecular Co-Assembled Fmoc-FRGDF/Hyaluronic Acid Hydrogel for Quercetin Delivery: Multifunctional Bioactive Platform. Foods. 2025;14(15):2629.

34.	Telange DR, Kamdi S, Hemke AT, Pethe AM, Lambole VB, Telrandhe UB. Preparation, Characterization, and Hepatoprotective Activity Evaluation of Quercetin-loaded Pluronic® F127/Chitosan-Myristic Acid Mixed Micelles. Current Drug Delivery. 2025;22(6):761-83.

35.	Rossi M, Rossello S, Sallustio V, Mandrone M, Cerchiara T, Chiocchio I, et al. GinExtraMed: Focus on Rosa canina L. Extract Encapsulated into Glycethosomes and Allanthosomes for Accelerating Skin Wound Healing. Pharmaceutics. 2025;17(5):632.

36.	Rousta P, Yazdanpanah S, Shahamirian M, Shirazinejad A. Fabrication and analysis of nanoemulsion-based edible films loaded with vitamin D3 and Cordia myxa mucilage. Scientific Reports. 2025;15(1):33040.

37.	Abad FRA, Pourmadadi M, Abdouss M. Development and characterization of a novel pH-Responsive nanocarrier for enhanced quercetin delivery and cytotoxicity in lung cancer. Inorganic Chemistry Communications. 2024;170:113175.

38.	Bhargav E, Mohammed N, Singh UN, Ramalingam P, Challa RR, Vallamkonda B, et al. A central composite design-based targeted quercetin nanoliposomal formulation: Optimization and cytotoxic studies on MCF-7 breast cancer cell lines. Heliyon. 2024;10(17).

39.	Badrloo MA, Pourmadadi M, Abdouss M, Rahdar A, Pandey S, Fathi-Karkan S. Ameliorating quercetin delivery in cancer therapy with polyvinyl alcohol/halloysite/starch nanocomposite. Industrial Crops and Products. 2024;218:118939.

40.	Elbeltagi S, Alfassam HE, Saeedi AM, Eldin ZE, Ibrahim E, Abd El-Aal M. A novel quercetin-loaded NiFe2O4@ Liposomes hybrid biocompatible as a potential chemotherapy/hyperthermia agent and cytotoxic effects on breast cancer cells. Journal of Drug Delivery Science and Technology. 2024;91:105203.

41.	Rostamkhani N, Salimi M, Adibifar A, Karami Z, Agh-Atabay A-H, Rostamizadeh K, et al. Enhanced anti-tumor and anti-metastatic activity of quercetin using ph-sensitive alginate@ zif-8 nanocomposites: in vitro and in vivo study. Nanotechnology. 2024;35(47):475102.

42.	Tahamtan S, Shamsabadipour A, Pourmadadi M, Khodabandehloo AH, Ghadami A, Fathi-karkan S, et al. Biocompatible chitosan/starch/graphene quantum dots/titanium dioxide nanocomposite: A stimuli-responsive, porous nanocarrier for prolonged quercetin delivery in lung cancer treatment. BioNanoScience. 2024;14(3):2491-508.

43.	Najafi M, Khoddam Z, Masnavi M, Pourmadadi M, Abdouss M. Physicochemical and in vitro characterization of Agarose based nanocarriers incorporated with Graphene Quantum Dots/α-Fe2O3 for targeted drug delivery of Quercetin to liver cancer treatment. Materials Chemistry and Physics. 2024;320:129333.

44.	Mirzaei M, Ebrahimipour SY, Mohamadi M, Shamspur T. Targeted drug delivery of quercetin to breast cancer cells using a modified SBA-15 mesoporous nanostructure. Journal of Cluster Science. 2024;35(5):1345-58.

45.	Rahmani M, Pourmadadi M, Shakouri S, Rahdar A, Díez-Pascual AM. Novel hydrogel-based gelatin/polyvinyl alcohol/titanium dioxide nanocomposite as a pH-responsive nanocarrier for the controlled release of quercetin in cancer therapy. BioNanoScience. 2024;14(5):5286-96.

46.	Seddighi Y, Pourmadadi M, Abdouss M, Mazinani S, Rahdar A, Ghotekar S. In vitro evaluation and characterization of double emulsion based on polyvinylpyrrolidone/agarose/ZIF-8 hydrogel nanocomposite platform for quercetin delivery to breast cancer cells. BioNanoScience. 2024;14(3):3153-67.

47.	Askar MA, El-Nashar HA, Al-Azzawi MA, Rahman SSA, Elshawi OE. Synergistic effect of quercetin magnetite nanoparticles and targeted radiotherapy in treatment of breast cancer. Breast cancer: basic and clinical research. 2022;16:11782234221086728.

48.	Sadeghi Nodoushan F, Hakimian F, Haghiralsadat BF, Taghiyar S. The Effect of Superparamagnetic Fe3O4 Nanoparticles Combined with Quercetin on Breast Cancer Cell Line (MCF-7). Journal of Nutrition and Food Security. 2023;8(4):565-76.

49.	Pourmadadi M, Shabestari SM, Abdouss H, Amiri Z, Abdouss M, Rahdar A, et al. Green synthesis of pH-sensitive carboxymethyl cellulose/agarose/carbon quantum dots nanocarriers for quercetin delivery to A549 lung cancer using an emulsification method. BioNanoScience. 2024;14(4):4570-84.

50.	Canbolat F, Demir N, Yayıntas OT, Pehlivan M, Eldem A, Ayna TK, et al. Chitosan nanoparticles loaded with quercetin and valproic acid: a novel approach for enhancing antioxidant activity against oxidative stress in the SH-SY5Y human neuroblastoma cell line. Biomedicines. 2024;12(2):287.

51.	Pourmadadi M, Ajalli N, Sadeghi M, Poorkhalili P, Mehrabi MG, Cheraghi A, et al. Co-biopolymer of zein/starch hydrogel incorporated montmorillonite for efficient quercetin delivery in lung cancer treatment. Inorganic Chemistry Communications. 2024;170:113300.

52.	Arghand N, Reiisi S, Karimi B, Khorasgani EM, Heidari R. Biosynthesis of nanocomposite alginate-chitosan loaded with silver nanoparticles coated with eugenol/quercetin to enhance wound healing. Bionanoscience. 2024;14(5):5149-66.

53.	Mohammadi ZS, Pourmadadi M, Abdouss M, Jafari SH, Rahdar A, Diez-Pascual AM. pH-sensitive polyacrylic acid/Fe3O4@ SiO2 hydrogel nanocomposite modified with agarose for controlled release of quercetin. Inorganic Chemistry Communications. 2024;163:112338.

54.	Nascimento SdPD, de Souza RRM, Sobral MV, Xavier-Junior FH, da Silva MVS, Viana MM, et al. Gelatin-Oxidized Alginate and Chitosan-Coated Zein Nanoparticle Hydrogel Composite to Enhance Breast Cancer Cytotoxicity in Dual-Drug Delivery. ACS omega. 2024;9(45):45190-202.

55.	Parsaei M, Akhbari K, Tylianakis E, Froudakis GE. Effects of Fluorinated Functionalization of Linker on Quercetin Encapsulation, Release and Hela Cell Cytotoxicity of Cu‐Based MOFs as Smart pH‐Stimuli Nanocarriers. Chemistry–A European Journal. 2024;30(1):e202301630.

56.	Najafi M, Pourmadadi M, Abdous M, Rahdar A, Pandey S. Formulation of double nanoemulsions based on pH-sensitive carboxymethyl cellulose/Starch copper doped carbon quantum dots for quercetin controlled release. Journal of Molecular Liquids. 2024;400:124543.

57.	Salehi M, Pourmadadi M, Abdouss M, Rahdar A, Díez-Pascual AM. Novel carboxymethyl cellulose/polyvinyl pyrrolidone hydrogel incorporating graphitic carbon nitride for quercetin delivery. Inorganic Chemistry Communications. 2024;160:111932.

58.	Pourmadadi M, Tajiki A, Abdouss M, Mohammadi AB, Kharaba Z, Rahdar A, et al. Novel carbon quantum dots incorporated polyacrylic acid/polyethylene glycol pH-sensitive nanoplatform for drug delivery. Inorganic Chemistry Communications. 2024;159:111814.

59.	Palai AK, Kumar A, Mazahir F, Sharma A, Yadav AK. Synthesis and characterization of fullerene-based nanocarrier for targeted delivery of quercetin to the brain. Therapeutic Delivery. 2024;15(7):545-59.

60.	Pourmadadi M, Garousi NA, Abdouss M, Rahdar A, Fathi-Karkan S, Pandey S. PEG-modified Fe2O3 coated agarose hydrogel: A synthesized nanocomposite for regulated 5-fluorouracil delivery. International Journal of Biological Macromolecules. 2024;276:133900.

61.	Pourmadadi M, Omrani Z, Doustgani A, Yazdian F, Nourhashemi M, Ahmadi T, et al. Liver-Targeted Antioxidant Strike: Machine Learning Models Predict pH-Responsive Drug Release from Liver-Targeted Agarose-CMC-CeO2 Nanocomposites. Journal of Drug Delivery Science and Technology. 2025:107555.

62.	Pourmadadi M, Abdouss M, Mazinani S, Behzadmehr R, Rahdar A, Aboudzadeh MA. Hybrid nanocarriers based on polyacrylic acid, polyvinyl pyrrolidone, and molybdenum disulfide for enhanced 5-fluorouracil delivery in lung cancer therapy. Inorganic Chemistry Communications. 2024;159:111749.