| Device Name | Purpose of usage |
| --- | --- |
| CNC lathe machine | For turning operation |
| Sono bright Ultrasonic vibration machine | To mix an avocado oil and water |
| Round bottom flask | To contain the mixed oil and distilled water |
| Portable grinder | For grinding |
| Surface roughness tester | To measure the surface roughness |

Table 1. Machines and equipment used in the experiments.

| Machining parameters |  |  | Levels |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Input parameter | Unit | L1 |  | L2 | L3 | L4 |
| Cutting speed | rpm | 900 |  | 1000 | 1100 | 1200 |
| Feed rate | mm/min | 85 |  | 90 | 95 | 100 |
| Depth of cut | mm | 0.5 |  | 1 | 1.5 | 2 |
| Avocado oil fluids | mm2/s | 0 |  | 3 | 6 | 9 |

Table 2. Machining parameters and their level

| S/N | Fluid: AO | Exp.No | Input parameters |  |  | Output parameters |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Cutting speed | Feed rate | Depth of cut | Ra (μm) |
| 1 | 0% AO with 100% DW | E1 | 900 | 85 | 0.1 | 1.87 |
|  |  | E2 | 900 | 90 | 1 | 0.95 |
|  |  | E3 | 900 | 95 | 1.5 | 2.05 |
|  |  | E4 | 900 | 100 | 2 | 2.1 |
| 2 | 3% AO with 97% DW | E5 | 1000 | 85 | 1 | 1.56 |
|  |  | E6 | 1000 | 90 | 0.1 | 1.72 |
|  |  | E7 | 1000 | 95 | 2 | 0.98 |
|  |  | E8 | 1000 | 100 | 1.5 | 0.93 |
| 3 | 6% AO with 94% DW | E9 | 1100 | 85 | 1.5 | 1.07 |
|  |  | E10 | 1100 | 90 | 2 | 0.67 |
|  |  | E11 | 1100 | 95 | 0.1 | 0.89 |
|  |  | E12 | 1100 | 100 | 1 | 0.56 |
| 4 | 9% AO with 91% DW | E13 | 1200 | 85 | 2 | 0.14 |
|  |  | E14 | 1200 | 90 | 1.5 | 0.22 |
|  |  | E15 | 1200 | 95 | 1 | 0.39 |
|  |  | E16 | 1200 | 100 | 0.1 | 0.12 |

Table 3. Experimental result for Ra.

| Source | DF | Adj SS | Adj MS | F-Value | P-Value | % of C | Hypothesis |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Cutting Speed | 3 | 5.16 | 1.72 | 12.96 | 0.032 | 76.78 | Significant |
| Feed Rate | 3 | 0.19 | 0.06 | 0.48 | 0.031 | 2.82 | Significant |
| Depth of Cut | 3 | 0.18 | 0.06 | 0.45 | 0.043 | 2.67 | Significant |
| Avocado oil fluid | 3 | 0.77 | 0.25 | 1.95 | 0.019 | 11.45 | Significant |
| Error | 3 | 0.39 | 0.13 |  |  | 5.8 |  |
| Total | 15 | 6.72 |  |  |  |  |  |

Table 4. ANOVA for Ra versus Oil, Speed, Feed and Doc

| Factors | A | B | C | D | Grey relational grade | Grey relational Rank |
| --- | --- | --- | --- | --- | --- | --- |
| Trail no | Column |  |  |  |  |  |
|  | 1 | 2 | 3 | 4 |  |  |
| 1 | 1 | 1 | 1 | 1 | 0.361 | 14 |
| 2 | 1 | 2 | 2 | 2 | 0.543 | 9 |
| 3 | 1 | 3 | 3 | 3 | 0.339 | 15 |
| 4 | 1 | 4 | 4 | 4 | 0.333 | 16 |
| 5 | 2 | 1 | 2 | 3 | 0.407 | 12 |
| 6 | 2 | 2 | 1 | 4 | 0.382 | 13 |
| 7 | 2 | 3 | 4 | 1 | 0.535 | 10 |
| 8 | 2 | 4 | 3 | 2 | 0.55 | 8 |
| 9 | 3 | 1 | 3 | 4 | 0.51 | 11 |
| 10 | 3 | 2 | 4 | 3 | 0.642 | 6 |
| 11 | 3 | 3 | 1 | 2 | 0.562 | 7 |
| 12 | 3 | 4 | 2 | 1 | 0.692 | 5 |
| 13 | 4 | 1 | 4 | 2 | 0.98 | 2 |
| 14 | 4 | 2 | 3 | 1 | 0.908 | 3 |
| 15 | 4 | 3 | 2 | 4 | 0.785 | 4 |
| 16 | 4 | 4 | 1 | 3 | 1 | 1 |

Table 5. Response table for mean Grey relational grade (GRG)

| Level | Input parameters |  |  |  |
| --- | --- | --- | --- | --- |
|  | Avocado oil | Cutting speed | Feed rate | Depth of cut |
| Level 1 | 0.394 | 0.564 | 0.576 | 0.624 |
| Level 2 | 0.468 | 0.618 | 0.606 | 0.658 |
| Level 3 | 0.601 | 0.555 | 0.576 | 0.597 |
| Level 4 | 0.918 | 0.643 | 0.622 | 0.502 |
| Max. | 0.918 | 0.643 | 0.622 | 0.658 |
| Min. | 0.394 | 0.555 | 0.576 | 0.502 |
| Max.- Min. | 0.524 | 0.088 | 0.046 | 0.156 |
| Rank | 1 | 3 | 4 | 2 |

Table 6. Average GRG

| S/N | Response | Calculated value | Experimental value | (%) Error |
| --- | --- | --- | --- | --- |
| 1 | Surface roughness (μm) | 0.11 | 0.12 | 9.09 |

Table 7.  Confirmation test for Ra