# Supplementary Material

Figure S1. Illustration of the re-lithiation reaction mechanism.

Figure S2. (A) LG Chem E63B cell; (B) Cathode and anode foils after manual disassembling. Source: Photo by the author.

Table S1. Experimental conditions for the hydrothermal tests.

| Test | LiOH Concentration (M) | Temperature (°C) | Time (h) |
| --- | --- | --- | --- |
| 1 | 4.0 | 160 | 2 |
| 2 | 4.0 | 160 | 1 |
| 3 | 4.0 | 220 | 2 |
| 4 | 4.0 | 220 | 1 |
| 5 | 2.0 | 160 | 2 |
| 6 | 2.0 | 160 | 1 |
| 7 | 2.0 | 220 | 2 |
| 8 | 2.0 | 220 | 1 |
| 9 | 0.5 | 160 | 2 |
| 10 | 0.5 | 160 | 1 |
| 11 | 0.5 | 220 | 2 |
| 12 | 0.5 | 220 | 1 |

Figure S3. XRD results of the spent CAM and (simulated) diffraction pattern of the α-NaFeO2 structure.

Figure S4. Composition of the regenerated cathode material.

Figure S5. Interaction effect between concentration - temperature and time