Table 1 Elemental analysis of the NPs

Sample Fe (%) Cu (%) Zn (%) Mn (%) O (%) Molecular structure

FexCuyZnzOk 34 18 10 --- 38 Fe4Cu1.86Zn1O15.8 FexCuyMnzOk 35 12 --- 13 40 Fe3.4Cu1Mn1.05O13.8

| Table 2 Optimization of reaction condition for the synthesis of pyrrole using FexCuyZnzOk |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Entry | Catalyst | Solvent | Time(min) | Temp.(⁰C) | Yield (%) |
| 1 | no catalyst | no salvent | 60 | r.t | trace |
| 2 | no catalyst | no salvent | 120 | r.t | 30 |
| 3 | FexCuyZnzOk (5) | EtOH | 90 | r.t | 60 |
| 4 | FexCuyZnzOk (8) | EtOH | 90 | r.t | 73 |
| 5 | FexCuyZnzOk (10) | EtOH | 90 | r.t | 77 |
| 6 | FexCuyZnzOk (15) | EtOH | 90 | r.t | 77 |
| 7 | FexCuyZnzOk (20) | EtOH | 90 | r.t | 79 |
| 8 | FexCuyZnzOk (25) | EtOH | 90 | r.t | 79 |
| 9 | FexCuyZnzOk (10) | H2O | 90 | r.t | 36 |
| 10 | FexCuyZnzOk (10) | EtOH | 90 | r.t | 47 |
| 11 | FexCuyZnzOk (10) | MeOH | 90 | r.t | 40 |
| 12 | FexCuyZnzOk (10) | CH3CN | 90 | r.t | 75 |
| 13 | FexCuyZnzOk (10) | DCM | 90 | r.t | 56 |
| 14 | FexCuyZnzOk (10) | CH2Cl2 | 90 | r.t | 43 |
| 15 | FexCuyZnzOk (10) | H2O/EtOH | 90 | r.t | 55 |
| 16 | FexCuyZnzOk (10) | H2O/CH3CN | 90 | r.t | 84 |

Reaction conditions: 4-cyanobenzaldehyde (1 mmol), 4-bromoaniline (2 mmol), ethyl pyruvate (1 mmol),

in the presence of the catalyst in a 5 ml solvent.

| Table 3 Synthesis of pyrrole derivatives using FexCuyZnzOk as a catalyst |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Entry Product Ar2 m.p (◦C) lit m.p (◦C) Yield (%) |  |  |  |  |  |
| 1 | 1,5-diphenyl-3-(phenylamino)-1,5-dihydro-2H-pyrrol-2-one (1a) |  | Ref [66] | 219-220 White solid | 84 |
| 2 | 5-(pyridin-3-yl)-1-(p-tolyl)-3-(p-tolylamino)-1,5-dihydro-2H-pyrrol-2-one (1b) |  | Ref [66] | 188-189 Cream powder | 80 |
| 3 | 1-(4-bromophenyl)-3-((4-bromophenyl) amino)-5-(2-chlorophenyl)-1,5-dihydro-2H-pyrrol-2-one (1c) |  | Ref [67] | 240-242 White powder | 72 |
| 4 | 1-(4-bromophenyl)-3-((4-bromophenyl) amino)-5-(4-chlorophenyl)-1,5-dihydro-2H-pyrrol-2-one (1d) |  | Ref [67] | 191-193 White cream powder | 88 |
| 5 | 1-(4-bromophenyl)-3-((4-bromophenyl) amino)-5-(4-methoxyphenyl)-1,5-dihydro-2H-pyrrol-2-one (1e) |  | Ref [66] | 198-200 Cream powder | 79 |
| 6 | 1-(3-chlorophenyl)-3-((3-chlorophenyl) amino)-5-(2,4-dimethylphenyl)-1,5-dihydro-2H-pyrrol-2-one (1f) |  | Ref [68] | 168-170 Cream powder | 78 |
| 7 | 4-(1-(4-bromophenyl)-4-((4-bromophenyl) amino)-5-oxo-2,5-dihydro-1H-pyrrol-2yl) benzonitrile (1g) |  | Ref [69] | 234-236 Cream powder | 93 |
| 8 | 4-(1-(4-chlorophenyl)-4-((4-chlorophenyl) amino)-5-oxo-2,5-dihydro-1H-pyrrol-2yl) benzonitrile (1h) |  | Ref [69] | 232-234 White powder | 91 |
| 9 | 5-(3-nitrophenyl)-1-phenyl-3-(phenylamino)-1,5-dihydro-2H-pyrrol-2-one (1k) |  | Ref [66] | 213-214 Yellow powder | 81 |

Reaction conditions: aldehyde (1 mmol), aniline (2 mmol), ethyl pyruvate (1 mmol), in the presence of the      
   FexCuyZnzOk in a 5 ml solvent.

| Table 4 Comparison of the efficiency of catalysts |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Entry | Catalyst | Solvent | Tem (⁰C) | Time (h) | ref | Yield (%) |
| 1 | Thiourea | Toluene | r.t | 18 | [70] | 48-85 |
| 2 | Fluorous imine-1,10-bis (carbothioate) | CH3CN | r.t | 12 | [71] | 41-93 |
| 3 | PS-DETSO3H | n-Hexane | r.t | 2 | [72] | 80-96 |
| 4 | FexCuyZnzOk | H2O/CH3CN | r.t | 1.5 | This work | 78-93 |