Stirring at (25± 3 ◦C)

Graphical Abstract

pH = 8–9

NS was obtained

+

Na2SiO3

HCl conc.

Cross linker (0.1 %)

+

NS (10%)

+

AM (10%)

+

AN (10%)

Stirring for 2h

{P(AN-AM)-NS} nano-composite was obtained

Hydrogel yield was cut into minor fragments

Then subject to γ-radiation at 50 kGy

Washed with distilled water, dried at 60 oC, and grained

Soaking in acetone for the elimination of unreacted monomers fragments