Supplementary Table captions

Supplementary Table S1. Atomic coordinate, isotropic thermal parameter, and occupancy of Ca2.82(PO4)2:0.09Eu3+, 0.09Li+ phosphor.

Supplementary Table S2. Atomic coordinate, isotropic thermal parameter, and occupancy of Ca2.82(PO4)2:0.09Eu3+, 0.09Na+ phosphor.

Supplementary Table S3. Atomic coordinate, isotropic thermal parameter, and occupancy of Ca2.82(PO4)2:0.09Eu3+, 0.09K+ phosphor.

Supplementary Table S4. Ca−O and P−O lengths in Ca2.82(PO4)2:0.09Eu3+, 0.09Li+ phosphor.

Supplementary Table S5. Ca−O and P−O lengths in Ca2.82(PO4)2:0.09Eu3+, 0.09Na+ phosphor.

Supplementary Table S6. Ca−O and P−O lengths in Ca2.82(PO4)2:0.09Eu3+, 0.09K+ phosphor.

Supplementary Table S1. Atomic coordinate, isotropic thermal parameter, and occupancy of Ca2.82(PO4)2:0.09Eu3+, 0.09Li+ phosphor.

|  | Atomic coordinates |  |  |  | Isotropic thermal parameter Biso (Å2) | Occupancy |
| --- | --- | --- | --- | --- | --- | --- |
| Atom | Site | x | y | z |  |  |
| Ca(1) | 18b | 0.7260 | 0.8588 | 0.1671 | 0.4374 | 0.9776 |
| Eu(1) | 18b | 0.7260 | 0.8588 | 0.1671 | 0.4374 | 0.0224 |
| Ca(2) | 18b | 0.6215 | 0.8227 | −0.0337 | 0.3332 | 0.9632 |
| Eu(2) | 18b | 0.6215 | 0.8227 | −0.0337 | 0.3332 | 0.0368 |
| Ca(3) | 18b | 0.7259 | 0.8510 | 0.0613 | 0.5677 | 0.9758 |
| Eu(3) | 18b | 0.7259 | 0.8510 | 0.0613 | 0.5677 | 0.0242 |
| Ca(4) | 6a | 0.0000 | 0.0000 | −0.0870 | 1.7402 | 0.2905 |
| Li | 6a | 0.0000 | 0.0000 | −0.0870 | 1.7402 | 0.2095 |
| Ca(5) | 6a | 0.0000 | 0.0000 | 0.7364 | 0.9759 | 1.0000 |
| P(1) | 6a | 0.0000 | 0.0000 | 0.0000 | 0.3814 | 1.0000 |
| P(2) | 18b | 0.6904 | 0.8661 | 0.8682 | 2.1176 | 1.0000 |
| P(3) | 18b | 0.6531 | 0.8470 | 0.7669 | 0.2029 | 1.0000 |
| O(1) | 18b | 0.7316 | −0.0885 | −0.0909 | 2.1318 | 1.0000 |
| O(2) | 18b | 0.7490 | 0.7655 | 0.8543 | 0.5653 | 1.0000 |
| O(3) | 18b | 0.7336 | 0.0088 | 0.8479 | 0.2637 | 1.0000 |
| O(4) | 18b | 0.5172 | 0.7657 | 0.8634 | 0.3174 | 1.0000 |
| O(5) | 18b | 0.6023 | −0.0499 | 0.7785 | 0.4358 | 1.0000 |
| O(6) | 18b | 0.5677 | 0.6916 | 0.7836 | 0.4572 | 1.0000 |
| O(7) | 18b | 0.0939 | 0.9045 | 0.7801 | 0.0956 | 1.0000 |
| O(8) | 18b | 0.6300 | 0.8271 | 0.7275 | 0.7406 | 1.0000 |
| O(9) | 18b | 0.0134 | 0.8640 | −0.0087 | 0.7817 | 1.0000 |
| O(10) | 6a | 0.0000 | 0.0000 | 0.0406 | 1.6234 | 1.0000 |

Supplementary Table S2. Atomic coordinate, isotropic thermal parameter, and occupancy of Ca2.82(PO4)2:0.09Eu3+, 0.09Na+ phosphor.

|  | Atomic coordinates |  |  |  | Isotropic thermal parameter Biso (Å2) | Occupancy |
| --- | --- | --- | --- | --- | --- | --- |
| Atom | Site | x | y | z |  |  |
| Ca(1) | 18b | 0.7250 | 0.8576 | 0.1635 | 0.4722 | 0.9754 |
| Eu(1) | 18b | 0.7250 | 0.8576 | 0.1635 | 0.4722 | 0.0246 |
| Ca(2) | 18b | 0.6199 | 0.8212 | −0.0344 | 0.2661 | 0.9597 |
| Eu(2) | 18b | 0.6199 | 0.8212 | −0.0344 | 0.2661 | 0.0403 |
| Ca(3) | 18b | 0.7291 | 0.8516 | 0.0600 | 0.9577 | 0.9763 |
| Eu(3) | 18b | 0.7291 | 0.8516 | 0.0600 | 0.9577 | 0.0237 |
| Ca(4) | 6a | 0.0000 | 0.0000 | −0.0866 | 2.6293 | 0.3546 |
| Na | 6a | 0.0000 | 0.0000 | −0.0866 | 2.6293 | 0.1454 |
| Ca(5) | 6a | 0.0000 | 0.0000 | 0.7338 | 0.8030 | 1.0000 |
| P(1) | 6a | 0.0000 | 0.0000 | 0.0000 | 1.2783 | 1.0000 |
| P(2) | 18b | 0.6874 | 0.8608 | 0.8634 | 1.3596 | 1.0000 |
| P(3) | 18b | 0.6522 | 0.8467 | 0.7658 | 0.2171 | 1.0000 |
| O(1) | 18b | 0.7318 | −0.0890 | −0.0932 | 1.9463 | 1.0000 |
| O(2) | 18b | 0.7659 | 0.7798 | 0.8543 | 0.8614 | 1.0000 |
| O(3) | 18b | 0.7299 | 0.0058 | 0.8467 | 0.3395 | 1.0000 |
| O(4) | 18b | 0.5167 | 0.7620 | 0.8606 | 0.7730 | 1.0000 |
| O(5) | 18b | 0.5996 | −0.0490 | 0.7794 | 0.3900 | 1.0000 |
| O(6) | 18b | 0.5735 | 0.6900 | 0.7841 | 0.1319 | 1.0000 |
| O(7) | 18b | 0.0888 | 0.9064 | 0.7786 | 0.2456 | 1.0000 |
| O(8) | 18b | 0.6301 | 0.8291 | 0.7264 | 0.7754 | 1.0000 |
| O(9) | 18b | 0.0085 | 0.8639 | −0.0118 | 1.7284 | 1.0000 |
| O(10) | 6a | 0.0000 | 0.0000 | 0.0405 | 0.8314 | 1.0000 |

Supplementary Table S3. Atomic coordinate, isotropic thermal parameter, and occupancy of Ca2.82(PO4)2:0.09Eu3+, 0.09K+ phosphor.

|  | Atomic coordinates |  |  |  | Isotropic thermal parameter Biso (Å2) | Occupancy |
| --- | --- | --- | --- | --- | --- | --- |
| Atom | Site | x | y | z |  |  |
| Ca(1) | 18b | 0.7231 | 0.8572 | 0.1656 | 0.3000 | 0.9791 |
| Eu(1) | 18b | 0.7231 | 0.8572 | 0.1656 | 0.3000 | 0.0209 |
| Ca(2) | 18b | 0.6178 | 0.8229 | −0.0337 | 0.4193 | 0.9666 |
| Eu(2) | 18b | 0.6178 | 0.8229 | −0.0337 | 0.4193 | 0.0334 |
| Ca(3) | 18b | 0.7291 | 0.8516 | 0.0604 | 0.6996 | 0.9776 |
| Eu(3) | 18b | 0.7291 | 0.8516 | 0.0604 | 0.6996 | 0.0224 |
| Ca(4) | 6a | 0.0000 | 0.0000 | −0.0851 | 3.0462 | 0.3610 |
| K | 6a | 0.0000 | 0.0000 | −0.0851 | 3.0462 | 0.1390 |
| Ca(5) | 6a | 0.0000 | 0.0000 | 0.7332 | 0.8985 | 1.0000 |
| P(1) | 6a | 0.0000 | 0.0000 | 0.0000 | 1.1528 | 1.0000 |
| P(2) | 18b | 0.6855 | 0.8590 | 0.8697 | 1.3000 | 1.0000 |
| P(3) | 18b | 0.6515 | 0.8465 | 0.7670 | 0.2061 | 1.0000 |
| O(1) | 18b | 0.7287 | −0.0941 | −0.0927 | 1.6415 | 1.0000 |
| O(2) | 18b | 0.7608 | 0.7721 | 0.8545 | 0.6230 | 1.0000 |
| O(3) | 18b | 0.7335 | 0.0057 | 0.8470 | 0.1287 | 1.0000 |
| O(4) | 18b | 0.5146 | 0.7647 | 0.8608 | 0.8914 | 1.0000 |
| O(5) | 18b | 0.5993 | −0.0484 | 0.7795 | 0.3766 | 1.0000 |
| O(6) | 18b | 0.5693 | 0.6801 | 0.7833 | 0.5314 | 1.0000 |
| O(7) | 18b | 0.0842 | 0.9008 | 0.7781 | 0.2195 | 1.0000 |
| O(8) | 18b | 0.6326 | 0.8261 | 0.7254 | 0.4003 | 1.0000 |
| O(9) | 18b | 0.0085 | 0.8643 | −0.0121 | 1.4173 | 1.0000 |
| O(10) | 6a | 0.0000 | 0.0000 | 0.0399 | 0.6735 | 1.0000 |

Supplementary Table S4. Ca−O and P−O lengths in Ca2.82(PO4)2:0.09Eu3+, 0.09Li+ phosphor.

|  | Ca−O and P−O bonds |  | Bond length (Å) |
| --- | --- | --- | --- |
| Ca−O† | Ca(1)−O | Ca(1)−O(3) | 2.5670 |
|  |  | Ca(1)−O(4) | 2.4117 |
|  |  | Ca(1)−O(4) | 2.4904 |
|  |  | Ca(1)−O(5) | 2.4839 |
|  |  | Ca(1)−O(6) | 2.3630 |
|  |  | Ca(1)−O(8) | 2.4195 |
|  |  | Ca(1)−O(9) | 2.4794 |
|  | Ca(2)−O | Ca(2)−O(1) | 2.3864 |
|  |  | Ca(2)−O(2) | 2.4567 |
|  |  | Ca(2)−O(3) | 2.3308 |
|  |  | Ca(2)−O(5) | 2.6399 |
|  |  | Ca(2)−O(6) | 2.8473 |
|  |  | Ca(2)−O(7) | 2.4771 |
|  |  | Ca(2)−O(7) | 2.3389 |
|  |  | Ca(2)−O(9) | 2.3298 |
|  | Ca(3)−O | Ca(3)−O(1) | 2.6470 |
|  |  | Ca(3)−O(2) | 2.5742 |
|  |  | Ca(3)−O(3) | 2.3808 |
|  |  | Ca(3)−O(5) | 2.3869 |
|  |  | Ca(3)−O(6) | 2.4871 |
|  |  | Ca(3)−O(8) | 2.5965 |
|  |  | Ca(3)−O(8) | 2.5807 |
|  |  | Ca(3)−O(10) | 2.5988 |
|  | Ca(4)−O | Ca(4)−O(1) | 2.4771 |
|  | Ca(5)−O | Ca(5)−O(4) | 2.2292 |
|  |  | Ca(5)−O(7) | 2.3666 |
| P−O | P(1)−O | P(1)−O(9) | 1.5297 |
|  |  | P(1)−O(10) | 1.5172 |
|  | P(2)−O | P(2)−O(1) | 1.5953 |
|  |  | P(2)−O(2) | 1.5468 |
|  |  | P(2)−O(3) | 1.5254 |
|  |  | P(2)−O(4) | 1.5823 |
|  | P(3)−O | P(3)−O(5) | 1.4832 |
|  |  | P(3)−O(6) | 1.5392 |
|  |  | P(3)−O(7) | 1.5207 |
|  |  | P(3)−O(8) | 1.4921 |

†The distances of Eu(1)−O, Eu(2)−O, Eu(3)−O, and Li−O equal to those of Ca(1)−O, Ca(2)−O, Ca(3)−O, and Ca(4)−O, respectively.

Supplementary Table S5. Ca−O and P−O lengths in Ca2.82(PO4)2:0.09Eu3+, 0.09Na+ phosphor.

|  | Ca−O and P−O bonds |  | Bond length (Å) |
| --- | --- | --- | --- |
| Ca−O† | Ca(1)−O | Ca(1)−O(3) | 2.5519 |
|  |  | Ca(1)−O(4) | 2.4390 |
|  |  | Ca(1)−O(4) | 2.4458 |
|  |  | Ca(1)−O(5) | 2.3878 |
|  |  | Ca(1)−O(6) | 2.2900 |
|  |  | Ca(1)−O(8) | 2.4420 |
|  |  | Ca(1)−O(9) | 2.4627 |
|  | Ca(2)−O | Ca(2)−O(1) | 2.4472 |
|  |  | Ca(2)−O(2) | 2.4572 |
|  |  | Ca(2)−O(3) | 2.3338 |
|  |  | Ca(2)−O(5) | 2.6385 |
|  |  | Ca(2)−O(6) | 2.7842 |
|  |  | Ca(2)−O(7) | 2.4471 |
|  |  | Ca(2)−O(7) | 2.3541 |
|  |  | Ca(2)−O(9) | 2.3574 |
|  | Ca(3)−O | Ca(3)−O(1) | 2.6639 |
|  |  | Ca(3)−O(2) | 2.5889 |
|  |  | Ca(3)−O(3) | 2.4027 |
|  |  | Ca(3)−O(5) | 2.4410 |
|  |  | Ca(3)−O(6) | 2.5312 |
|  |  | Ca(3)−O(8) | 2.5818 |
|  |  | Ca(3)−O(8) | 2.5797 |
|  |  | Ca(3)−O(10) | 2.5616 |
|  | Ca(4)−O | Ca(4)−O(1) | 2.4855 |
|  | Ca(5)−O | Ca(5)−O(4) | 2.2321 |
|  |  | Ca(5)−O(7) | 2.3518 |
| P−O | P(1)−O | P(1)−O(9) | 1.5342 |
|  |  | P(1)−O(10) | 1.5147 |
|  | P(2)−O | P(2)−O(1) | 1.5223 |
|  |  | P(2)−O(2) | 1.5372 |
|  |  | P(2)−O(3) | 1.5737 |
|  |  | P(2)−O(4) | 1.5779 |
|  | P(3)−O | P(3)−O(5) | 1.5320 |
|  |  | P(3)−O(6) | 1.5752 |
|  |  | P(3)−O(7) | 1.4719 |
|  |  | P(3)−O(8) | 1.4906 |

†The distances of Eu(1)−O, Eu(2)−O, Eu(3)−O, and Na−O equal to those of Ca(1)−O, Ca(2)−O, Ca(3)−O, and Ca(4)−O, respectively.

Supplementary Table S6. Ca−O and P−O lengths in Ca2.82(PO4)2:0.09Eu3+, 0.09K+ phosphor.

|  | Ca−O and P−O bonds |  | Bond length (Å) |
| --- | --- | --- | --- |
| Ca−O† | Ca(1)−O | Ca(1)−O(3) | 2.5810 |
|  |  | Ca(1)−O(4) | 2.4088 |
|  |  | Ca(1)−O(4) | 2.4943 |
|  |  | Ca(1)−O(5) | 2.3831 |
|  |  | Ca(1)−O(6) | 2.3025 |
|  |  | Ca(1)−O(8) | 2.3846 |
|  |  | Ca(1)−O(9) | 2.4555 |
|  | Ca(2)−O | Ca(2)−O(1) | 2.4411 |
|  |  | Ca(2)−O(2) | 2.4121 |
|  |  | Ca(2)−O(3) | 2.3295 |
|  |  | Ca(2)−O(5) | 2.6767 |
|  |  | Ca(2)−O(6) | 2.7964 |
|  |  | Ca(2)−O(7) | 2.4194 |
|  |  | Ca(2)−O(7) | 2.3896 |
|  |  | Ca(2)−O(9) | 2.3590 |
|  | Ca(3)−O | Ca(3)−O(1) | 2.7063 |
|  |  | Ca(3)−O(2) | 2.5613 |
|  |  | Ca(3)−O(3) | 2.4131 |
|  |  | Ca(3)−O(5) | 2.4272 |
|  |  | Ca(3)−O(6) | 2.4697 |
|  |  | Ca(3)−O(8) | 2.6336 |
|  |  | Ca(3)−O(8) | 2.5557 |
|  |  | Ca(3)−O(10) | 2.5741 |
|  | Ca(4)−O | Ca(4)−O(1) | 2.5107 |
|  | Ca(5)−O | Ca(5)−O(4) | 2.1978 |
|  |  | Ca(5)−O(7) | 2.3629 |
| P−O | P(1)−O | P(1)−O(9) | 1.5338 |
|  |  | P(1)−O(10) | 1.4920 |
|  | P(2)−O | P(2)−O(1) | 1.4832 |
|  |  | P(2)−O(2) | 1.5770 |
|  |  | P(2)−O(3) | 1.5986 |
|  |  | P(2)−O(4) | 1.5858 |
|  | P(3)−O | P(3)−O(5) | 1.5244 |
|  |  | P(3)−O(6) | 1.5774 |
|  |  | P(3)−O(7) | 1.5587 |
|  |  | P(3)−O(8) | 1.5665 |

†The distances of Eu(1)−O, Eu(2)−O, Eu(3)−O, and K−O equal to those of Ca(1)−O, Ca(2)−O, Ca(3)−O, and Ca(4)−O, respectively.

Supplementary Figure captions

Supplementary Fig. S1. XRD Rietveld refined profiles of Ca2.82(PO4)2:0.09Eu3+, 0.09Li+ phosphor.

Supplementary Fig. S2. XRD Rietveld refined profiles of Ca2.82(PO4)2:0.09Eu3+, 0.09Na+ phosphor.

Supplementary Fig. S3. XRD Rietveld refined profiles of Ca2.82(PO4)2:0.09Eu3+, 0.09K+ phosphor.

Supplementary Fig. S4. Crystal structure of Ca2.93(PO4)2:0.07Eu3+ phosphor drawn by the VESTA program and XRD Rietveld refinement data.

Supplementary Fig. S5. Crystal structure of Ca2.92(PO4)2:0.08Eu3+ phosphor drawn by the VESTA program and XRD Rietveld refinement data.

Supplementary Fig. S6. Crystal structure of Ca2.91(PO4)2:0.09Eu3+ phosphor drawn by the VESTA program and XRD Rietveld refinement data.

Supplementary Fig. S7. Crystal structure of Ca2.82(PO4)2:0.09Eu3+, 0.09Li+ phosphor drawn by the VESTA program and XRD Rietveld refinement data.

Supplementary Fig. S8. Crystal structure of Ca2.82(PO4)2:0.09Eu3+, 0.09Na+ phosphor drawn by the VESTA program and XRD Rietveld refinement data.

Supplementary Fig. S9. Crystal structure of Ca2.82(PO4)2:0.09Eu3+, 0.09K+ phosphor drawn by the VESTA program and XRD Rietveld refinement data.

Supplementary Fig. S1. XRD Rietveld refined profiles of Ca2.82(PO4)2:0.09Eu3+, 0.09Li+ phosphor.

Supplementary Fig. S2. XRD Rietveld refined profiles of Ca2.82(PO4)2:0.09Eu3+, 0.09Na+ phosphor.

Supplementary Fig. S3. XRD Rietveld refined profiles of Ca2.82(PO4)2:0.09Eu3+, 0.09K+ phosphor.

Supplementary Fig. S4. Crystal structure of Ca2.93(PO4)2:0.07Eu3+ phosphor drawn by the VESTA program and XRD Rietveld refinement data.

Supplementary Fig. S5. Crystal structure of Ca2.92(PO4)2:0.08Eu3+ phosphor drawn by the VESTA program and XRD Rietveld refinement data.

Supplementary Fig. S6. Crystal structure of Ca2.91(PO4)2:0.09Eu3+ phosphor drawn by the VESTA program and XRD Rietveld refinement data.

Supplementary Fig. S7. Crystal structure of Ca2.82(PO4)2:0.09Eu3+, 0.09Li+ phosphor drawn by the VESTA program and XRD Rietveld refinement data.

Supplementary Fig. S8. Crystal structure of Ca2.82(PO4)2:0.09Eu3+, 0.09Na+ phosphor drawn by the VESTA program and XRD Rietveld refinement data.

Supplementary Fig. S9. Crystal structure of Ca2.82(PO4)2:0.09Eu3+, 0.09K+ phosphor drawn by the VESTA program and XRD Rietveld refinement data.