Supporting Information for

Thiosemicarbazide-linked covalent organic framework: preparation, properties and applications

Heping Wang a,*, Tengteng He a, Dandan Quan a, Tong Wang a, Cong Li b,*, Yehua Shen b

a Research Centre of New Materials, Ankang Research Centre of Zn Based Materials Science and Technology, School of Chemistry and Chemical Engineering, Ankang University, Ankang, Shaanxi 725000, China

b Key Laboratory of Synthetic and Natural Function Molecule Chemistry of Ministry of Education, College of Chemistry and Materials Science, Northwest University, Xi'an, Shaanxi 710069, China

*Corresponding Author:

Heping Wang

Research Centre of New Materials

Ankang Research Centre of Zn Based Materials Science and Technology

School of Chemistry and Chemical Engineering,

Ankang University

Ankang, Shaanxi 725000, China

Email: hepingwang1982@163.com

Phone: +86-0915-3261415

Cong Li

Key Laboratory of Synthetic and Natural Function Molecule Chemistry of Ministry of Education

College of Chemistry and Materials Science,

Northwest University

Xi'an, Shaanxi 710069, China

Email: licong@nwu.edu.cn

Phone: +86-029-81535025

EXPERIMENTAL SECTION

The thermodynamic parameters are calculated by the following equations:

Kc=QeCe               (S1)

∆Go=-RTlnKc               (S2)

lnKc=-∆HoRT+∆SoR               (S3)

∆Go=∆Ho-T∆So               (S4)

where Qe (mg g-1) is the equilibrium adsorption capacity, Ce (mg g-1) is the equilibrium ion concentration, Go (kJ mol-1) is the standard Gibbs free energy change, Ho (kJ mol-1) is the standard enthalpy change, So (J mol-1 K-1) is the standard entropy change. The Ho and So for the adsorption process were obtained from the slope (-Ho/R) and intercept (So/R) of the plot of lnKc versus 1/T (Fig. S1).

Fig. S1. Plot of lnKc vs. 1/T

Table S1 Kinetic models

| Model | Equation | Parameters |
| --- | --- | --- |
| Pseudo-first-order | lnQe-Qt=lnQe-k1t | k1 (min-1): the pseudo-first-order rate constant |
| Pseudo-second-order | tQt=1Qet+1k2Qe2 | k2 (g mg-1 min-1): the pseudo-first-order rate constant |
| Intraparticle diffusion | Qt=Kidt1/2+C | Kid (mg g-1 min-1/2): the intraparticle diffusion rate constant C (mg g-1): a constant proportional to the thickness of the boundary layer |
| Qe (mg g-1): the equilibrium adsorption capacity of metal ions; Qt (mg g-1): the adsorption capacity of metal ions at time t (min) |  |  |

Table S2 Adsorption isotherm models

| Model | Equation | Parameters |
| --- | --- | --- |
| Langmuir | 1Qe=1Qm+1KLQmCe | Qm (mg g-1): the maximum monolayer coverage capacities KL (L mg-1): the Langmuir isotherm constant |
| Freundlich | lnQe=lnKF+1nlnCe | KF (mg g-1): the Freundlich isotherm constant n: the adsorption intensity |
| Temkin | Qe=RTKTlnAT+RTKTlnCe | KT (mg g-1): the Temkin isotherm constant AT (L g-1): the Temkin isotherm equilibrium binding constant |
| Dubinin-Radushkevich | lnQe=lnQDR-βRTln1+1Ce2 | R (8.314 J mol-1 K-1): the universal gas constant T (K): the absolute temperature QDR (mg g-1): the maximum adsorption capacity of D-R model β (mol2 Kj-2): the D-R constant |
| Qe (mg/g-1): the adsorption capacity of metal ions at equilibrium; Ce (mg g-1): the equilibrium concentration of heavy metal ions |  |  |

Table S3 Parameters for kinetic models

| Ion | Qe exp (mg g-1) | pseudo-first-order |  |  | pseudo-second-order |  |  | intraparticle diffusion |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | K1 (min-1) | Qe cal (mg g-1) | R2 | K2 (g mg-1 min-1) | Qe cal (mg g-1) | R2 |  | Kid (mg g-1 min-1/2) | C (mg g-1) | R2 |
| Cu | 34.75 | 3.40×10-2 | 30.46 | 0.7018 | 8.06×10-4 | 36.76 | 0.9918 | Part I Part II | 1.7208 0.9587 | 9.94 16.14 | 0.8651 0.8497 |
| Pb | 48.25 | 7.68×10-2 | 39.99 | 0.3048 | 8.40×10-4 | 48.08 | 0.9880 | Part I Part II | 1.1556 0.9959 | 25.74 26.48 | 0.8819 0.8976 |
| Cd | 17.27 | 1.06×10-1 | 15.10 | 0.3109 | 3.87×10-3 | 16.92 | 0.9857 | Part I Part II | 0.4852 0.2998 | 10.66 10.67 | 0.6298 0.5940 |

Table S4 Parameters for adsorption isotherm models

| Ion | Qe exp (mg g-1) | Langmuir |  |  | Freundlich |  |  | Temkin |  |  | D-R |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | KL (L mg-1) | Qm (mg g-1) | R2 | KF (mg g-1) | n | R2 | KT (mg g-1) | AT (L g-1) | R2 | QDR (mg g-1) | β (mol2 Kj-2) | R2 |
| Cu | 73.50 | 0.0551 | 40.98 | 0.7341 | 6.75 | 2.97 | 0.9527 | 200.99 | 0.178 | 0.8064 | 37.70 | 210-5 | 0.3712 |
| Pb | 56.53 | 0.0891 | 43.67 | 0.8986 | 14.15 | 4.99 | 0.9528 | 350.63 | 1.892 | 0.9221 | 39.96 | 110-5 | 0.6120 |
| Cd | 94.13 | 0.0121 | 34.36 | 0.8370 | 0.61 | 1.36 | 0.9285 | 115.67 | 0.037 | 0.7445 | 28.34 | 910-5 | 0.3796 |

Table S5 Thermodynamic parameters

| Ion | T(K) | Go(kJ mol-1) | Ho(kJ mol-1) | So(J mol-1 K-1) |
| --- | --- | --- | --- | --- |
| Cu | 298 | 3.99 | 41.90 | 127.22 |
|  | 308 | 2.72 |  |  |
|  | 318 | 1.45 |  |  |
|  | 328 | 0.17 |  |  |
| Pb | 298 | 1.71 | 14.19 | 41.86 |
|  | 308 | 1.29 |  |  |
|  | 318 | 0.87 |  |  |
|  | 328 | 0.45 |  |  |
| Cd | 298 | 4.98 | 37.91 | 110.52 |
|  | 308 | 3.87 |  |  |
|  | 318 | 2.77 |  |  |
|  | 328 | 1.66 |  |  |