Supporting Information

Synthesis, characterization and evaluation of 169Yb-labeled tailored hydroxyapatite nanospheres for potential application in nanobrachytherapy

Sourav Patra1, 7, Khajan Singh1, Partha Sarathi Ghosh2, K V Vimalnath1, Priya Banerjee3, Ravi Kumar4,7, Chandan Kumar1,7, Avik Chakraborty5, Santosh Gupta 6,7, D. Bhattacharyya4,7, Rubel Chakravarty1,7, Sudipta Chakraborty1, 7*

1Radiopharmaceuticals Division, Bhabha Atomic Research Centre, Trombay, Mumbai 400085, India.

Glass and Advanced Materials Division, Bhabha Atomic Research Centre, Trombay, Mumbai 400085, India.

3Post Irradiation Examination Division, Bhabha Atomic Research Centre, Trombay, Mumbai 400085, India.

4Atomic & Molecular Physics Division, Bhabha Atomic Research Centre, Trombay, Mumbai 400085, India.

5Radiation Medicine Centre, Bhabha Atomic Research Centre, Parel, Mumbai 400012, India.

6Radiochemistry Division, Bhabha Atomic Research Centre, Trombay, Mumbai 400085, India.

7Homi Bhabha National Institute, Anushaktinagar, Mumbai 400094, India.

*To whom all correspondences must be addressed:

E-mail: sudipta@barc.gov.in

Fig. S1 (A) Variation of hydrodynamic diameter of GAHAnp with amount of GA and (B) XRD of GAHAnp after removing GA from the surface

Fig. S2 Variation of (A) hydrodynamic diameter and (B) zeta potential of GAHAnp with time. (C) Representative T2 relaxation plot of GAHAnp dispersed in aqueous medium at 25 oC. (D) Colloidal stability plot of GAHAnp over a period of 15 days

Fig. S3 (A) Size distribution of bare HAnp obtained from DLS (B) Variation of particle size of bare HAnp with time

Fig. S4 Visual inspection of (A) GAHAnp and (B) bare HAnp at different time points over a period of 14 days

Production of 169Yb

Ytterbium-169 was produced via 168Yb(n,)169Yb [ = 2300 b] route in Dhruva research reactor at Bhabha Atomic Research Centre having moderate thermal neutron flux (~ 1.0 × 1014 n/cm2/s). The isotopic composition of the enriched ytterbium target used along with the thermal neutron activation products and their decay characteristics are listed in Table S1. Theoretical calculations were carried out to estimate the activity of 169Yb using Equation 1 employing Westcott convention (Chakravarty and Chakraborty, 2021; Dvorakova, 2007)

A = [exp{-1kt} – exp{-(+2)t}]					(1)

where, A is the activity produced, No is the number of 168Yb atoms in the target before irradiation,  is decay constant of 169Yb (s-1), 1 the thermal neutron capture cross section of 168Yb at the neutron velocity of 2,200 ms-1 (2300 b), 2 is the thermal neutron capture cross section of 169Yb at the neutron velocity of 2,200 ms-1 (3600 b),  the thermal neutron flux of the reactor (n.cm-2 s-1), t is the time of irradiation and ‘k’ is so called k-factor which can be expressed as:

k = [Gth.g(Tn) + Gr.r() . so ()]

where, Gth is the thermal neutron self-shielding factor, Gr is the epithermal neutron self-shielding factor, g(Tn) is the Westcott factor with thermal neutron temperature Tn, r() . is the Westcott spectral index, so () is the so (Er)-, where so and Er are constants. The k-factor depends on various parameters such as, thermal energy cross-section at a reference temperature, epithermal index, epithermal flux shape factor, resonance integral, Westcott g-factor, temperature, Cadmium cut-off energy, effective resonance energy and flux attenuation factor for thermal and epithermal neutrons.(Dvorakova, 2007) Generally, the value of ‘k’ is reported to be between 1.5 and 2.5. For the Dhruva reactor, ‘k’ value was 1.75.

Theoretical yields of 169Yb at different irradiation time when 35.8% enriched 168Yb target is irradiated at 1×1014 n/cm2/s thermal neutron flux is shown in Fig. S5. It was observed that with increasing irradiation time, activity yield of 169Yb increases and became maximum after a 21 d of irradiation of the targets and then activity yield of 169Yb declined. This could be attributed to high thermal cross section of 169Yb ( = 3600 b) which absorbs neutron to produce 170Yb. In our study, 100 µg of (35.8% enriched168Yb) Yb target in the form of [168Yb]Yb(NO3)3 was irradiated for 21 d at thermal neutron flux of 1.0 × 1014 n/cm2/s in Dhruva research reactor. In the isotopic composition of the enriched 168Yb target (Table S1), in addition to the predominant 168Yb isotope (35.8%), substantial amounts of 174Yb (11%) and 176Yb (3.4%) are also present. Therefore, it is evident that upon thermal neutron irradiation of enriched Yb target, 175Yb, and 177Lu radionuclides will be co-produced along with 169Yb. Theoretical activities 169Yb and the radionuclidic impurities at different time after end of irradiation is listed in Table S2. It is evident from the data that a minimum cooling period of 25 days post-irradiation is required to achieve radionuclidic purity of > 99.9% for 169Yb.

Table S1 Isotopic composition of the enriched ytterbium and thermal neutron activation products formed by direct activation route

| Ytterbium isotopes | % Abundance | Cross section (b) | Product isotopes and their characteristics |
| --- | --- | --- | --- |
| 168Yb | 35.8 | 2300 | 169Yb (EC, 32d) 169Tm (stable) |
| 169Yb | - | 3600 | 170Yb (stable) |
| 170Yb | 4.5 | 11.4 | 171Yb (stable) |
| 171Yb | 25.50 | 48.6 | 172Yb (stable) |
| 172Yb | 12.6 | 0.80 | 173Yb (stable) |
| 173Yb | 7.2 | 17.1 | 174Yb (stable) |
| 174Yb | 11 | 69.4 | 175Yb (-, 4.2 d) 175Lu (stable) |
| 176Yb | 3.4 | 2.85 | 177Yb (-, 1.9 h)177Lu (-, 6.65 d) |

Table S2 Theoretical activities 169Yb and the radionuclidic impurities at different time after end of irradiation of 35.8% enriched 168Yb target at a flux of 1.0 × 1014 n cm-2 s-1 for 21 d irradiation

| Time after end of irradiation (d) | Activity of 169Yb (GBq/mg) | Activity of 175Yb (GBq/mg) | Activity of 177Lu (GBq/mg) | Radionuclidic purity (%) |
| --- | --- | --- | --- | --- |
| 0 | 91.39 | 2.85 | 0.025 | 96.95 |
| 5 | 82.01 | 1.25 | 0.018 | 98.47 |
| 10 | 73.59 | 0.55 | 0.012 | 99.24 |
| 15 | 66.04 | 0.24 | 0.008 | 99.62 |
| 20 | 59.26 | 0.11 | 0.006 | 99.81 |
| 25 | 91.40 | 0.05 | 0.004 | 99.94 |

Fig. S5 Theoretical yields of 169Yb at different irradiation time when 35.8% enriched 168Yb target is irradiated at 1×1014 n/cm2/s thermal neutron flux (at the end of irradiation)

Labeling study of 45Ca labeled GAHAnp with inactive Yb3+

Radioactive GAHAnp was synthesized by adopting the same method as described section 2.2 except using [45Ca]Ca(NO3)2 as a precursor of Ca. The production and radiochemical separation of 45Ca was carried out by adopting the same method reported earlier by our group (Chakravarty et al., 2022). Using the synthezied 45Ca-labeled GAHAnp, Yb-[45Ca]GAHAnp formulation was prepared by adsorption of cold Yb3+. For this first, 1 mg/mL of Yb solution was prepared by dissolving Yb2O3 in 0.1 M HCl. Subsequently, 5 mL of this solution was incubated with 50 mg of 45Ca-labeled GAHAnp at room temperature for 1 h at pH~ 6 under constant stirring. Subsequently, the solution was centrifuged at 5000 rpm for 20 min and the supernatant was withdrawn carefully and the activity (As) was measured. The activity (AT) of 50 mg of 45Ca-labeled GAHAnp was measured before incubation with Yb. Then, the fraction of Ca replaced by Yb was calculated using given formula:

% of Ca replacement = (As/AT) × 100						(3)

X-ray Absorption Spectroscopy (XAS) study

XAS measurements, which comprises of both X-ray Near Edge Structure (XANES) and Extended X-ray Absorption Fine Structure (EXAFS)techniques, have been carried out to probe the local structure of Yb adsorbed GAHAn along with YbCl3 and Yb2O3. The XAS measurements was conducted at the Energy-Scanning EXAFS beamline (BL-9) at the Indus-2 Synchrotron Source (2.5 GeV, 100 mA) at Raja Ramanna Centre for Advanced Technology (RRCAT), Indore, India (Basu et al., 2014; Poswal et al., 2014). This beamline operates in the energy range of 4 KeV to 25 KeV. The beamline optics consists of a Rh/Pt coated collimating meridional cylindrical mirror and the collimated beam reflected by the mirror is monochromatized by a Si (111) (2d=6.2709 Å) based double crystal monochromator (DCM). The second crystal of DCM is a sagittal cylinder used for horizontal focusing while a Rh/Pt coated bendable post mirror facing down is used for vertical focusing of the beam at the sample position. Rejection of the higher harmonics content in the X-ray beam is performed by detuning the second crystal of DCM. In the present case, XAS measurements have been performed in the transmission mode at Yb L3 edge. For the transmission mode measurement, three ionization chambers (300 mm length each) have been used for data collection, one ionization chamber for measuring incident flux (I0), second one for measuring transmitted flux (It) and the third ionization chamber for measuring XAS spectrum of a reference metal foil for energy calibration. Appropriate gas pressure and gas mixtures have been chosen to achieve 10-20% absorption in first ionization chamber and 70-90% absorption in second ionization chamber to improve the signal to noise ratio. The absorption coefficient µ is obtained using the relation:

(1)

# where, x is the thickness of the absorber.

To obtain the qualitative information about the local structure, oscillations in the absorption spectra  have been converted to absorption function  defined as follows:

(2)

Where, E0 is absorption edge energy,  is the bare atom background and  is the step in  value at the absorption edge. The energy dependent absorption coefficient  has been converted to the wave number dependent absorption coefficient using the relation,

(3)

where, m is the electron mass.  is weighted by k2 to amplify the oscillation at high and the χ(k)k2 functions are fourier transformed in R space to generate the  versus R spectra in terms of the real distances from the center of the absorbing atom. The set of EXAFS data analysis programme available within Demeter software package which was used for EXAFS data analysis (Newville et al., 1995). This includes background reduction and Fourier transform to derive the versus R spectra from the absorption spectra using ATHENA software (Newville et al., 1995), generation of the theoretical EXAFS spectra starting from an assumed crystallographic structure and finally fitting of experimental data with the theoretical spectra using ARTEMIS  software (Newville et al., 1995).

Table S3: Linear fitting formula of different isotherm and kinetics model

| Model name | General formula | Linear formula | Terms involved |
| --- | --- | --- | --- |
| Langmuir isotherm | qe=Q0 bCe1+bCe | 1qe=1Q0+ 1Q0bCe | Q0-monolayer sorption capacity, b- constant and Ce-concentration of Lu3+ at equilibrium. |
| Freundlich isotherm | qe=KFCe1n | ln(qe) = lnKF + ln(Ce) | KF and n are Freundlich constant. |
| Langmuir-Freundlich (L-F) isotherm | qe= QmaxKLFCe1nLF1+ KLFCe1nLF | ln(1qe) = ln(1Qmax2KLF) + 1nLFln(1/Ce) | Qmax is maximum sorption capacity, KLF is L-F constant and nLF is an exponent. |
| Pseudo-first order kinetic | qt= qe (1-e-k1t) | log (qe – qt) = log qe - k1t2.303 | qt is sorption capacity at time ‘t’ and k1 is pseudo first order rate constant. |
| Pseudo-second order kinetic | dqdt=k2 (qe-qt)2 | tqt= 1k2qe2+ tqe | k2 is pseudo second order rate constant. |

Fig. S6 (A) Variation of equilibrium sorption capacity with the initial concentration of Yb3+. (B) Variation of sorption capacity with time.

Fig. S7 Linear fitting of the sorption of Yb3+ on GAHAnp in (A) Langmuir Isotherm (B) Freundlich isotherm and (C) pseudo- first order kinetics

Fig S8 Radiochemical stability of [169Yb]Yb-GAHAnp in PBS and mouse serum

References

Basu, S., Nayak, C., Yadav, A.K., Agrawal, A., Poswal, A.K., Bhattacharyya, D., Jha, S.N., Sahoo, N.K., 2014. A comprehensive facility for EXAFS measurements at the INDUS-2 synchrotron source at RRCAT, Indore, India. J Phy: Conference Series 493, 012032.

Chakravarty, R., Chakraborty, S., 2021. A review of advances in the last decade on targeted cancer therapy using 177Lu: focusing on 177Lu produced by the direct neutron activation route. Am J Nucl Med Mol Imaging 11, 443-475.

Chakravarty, R., Ram, R., Patra, S., Sarma, H.D., Chakraborty, S., 2022. A solvent extraction-based procedure for removal of 46Sc impurity from reactor produced [45Ca]CaCl2 for its potential use in bone pain palliation. Appl Radiat Isot 188, 110352.

Dvorakova, Z., 2007. Production and chemical processing of Lu-177 for nuclear medicine at the Munich research reactor FRM-II. Technische Universität München.

Newville, M., Ravel, B., Haskel, D., Rehr, J.J., Stern, E.A., Yacoby, Y., 1995. Analysis of multiple-scattering XAFS data using theoretical standards. Physica B: Condensed Matter 208-209, 154-156.

Poswal, A.K., Agrawal, A., Yadav, A.K., Nayak, C., Basu, S., Kane, S.R., Garg, C.K., Bhattachryya, D., Jha, S.N., Sahoo, N.K., 2014. Commissioning and first results of scanning type EXAFS beamline (BL-09) at INDUS-2 synchrotron source. AIP Conference Proceedings 1591, 649-651.