Nanosized octahedral LiNi0.5Mn1.5O4 with predominant (111) facet as high performance cathode for Lithium-ion batteries

Haibo Rong a*, Binglu Deng a, Dongchu Chen a,b,* Min Chen a

a College of Materials Science and Energy Engineering, Foshan University, Foshan, 528000, Guangdong, China

b Guangdong Key Laboratory for Hydrogen Energy Technologies，Foshan University, Foshan, 528000, Guangdong, China

Fig.S1 SEM image of the B-LNMO

|  | Ni / mg L-1 | Mn / mg L-1 |
| --- | --- | --- |
| B-LNMO | 0.465 | 1.84 |
| O-LNMO | 0.056 | 0.025 |

Table.S1. Concentration of Ni and Mn that deposited on the lithium anode extracted from the cells with B-LNMO and O-LNMO cathodes, respectively.