Supplementary Information

Kinetic Modeling and Optical Property Evolution of Silver Nanoparticles from Water Hyacinth: A Simulation Approach Using Mie-Drude and Quantum Confinement Theories

John Onyango Agumba¹*, Godfrey Okumu Barasa², Clovis Ntahkie Takembo³, Philip Amuyunzu⁴, Joseph Owino⁵

S1. Computational Setup

S1.1 Software Environment

All simulations were performed in Python 3.12 using the following libraries:

- NumPy 1.26.4 - for numerical computation

- SciPy 1.12 - for integration and optimization

- Matplotlib 3.9 - for data visualization

- Pandas 2.2 - for data handling

- SymPy - for symbolic derivations and kinetic fitting

Simulations were executed on a Dell Inspiron system (Intel Core i9, 64 GB RAM, 2 TB SSD) running Windows 11. Each computational run involved 10⁵ particles or 1200 time steps depending on the simulation type.

S2. Supplementary Figures and Descriptions

Figure S1: Lognormal Size Distribution Simulation

Simulated nanoparticle size distributions for mean diameters between 40-100 nm using 100,000 virtual particles.

Distributions are right-skewed and nearly monodisperse (DI = 0.04-0.12).
This supports the use of the lognormal model for experimental DLS data interpretation.

Figure S2: Validation of Lognormal Distribution

Comparison of simulated and experimentally reported AgNP size distributions shows close agreement (R² = 0.98) when using lognormal parameters (μ, σ) derived from Equation 10 of the manuscript.

Figure S3: Temperature-Dependent Reduction Kinetics

Plots of simulated Ag⁺ depletion and Ag⁰ formation at 25-125 °C.
Higher temperatures accelerate Ag⁺ reduction and nanoparticle growth.
Rate constants follow the Arrhenius trend with activation energy ≈ 45 kJ/mol.

Figure S4: Sensitivity of Reduction Rate Constant (k)

Simulated concentration–time profiles at k = 0.01-0.10 min⁻¹.
Higher rate constants yield faster reduction, shorter induction periods, and earlier absorbance saturation at 420 nm.

Figure S5: Optical Absorbance Evolution

Time-resolved UV-Vis spectra (300-600 nm) showing growth of the surface plasmon resonance (SPR) peak near 420 nm.
Absorbance increases with Ag⁰ formation and stabilizes after 120 minutes.

Figure S6: Size-Dependent SPR Shift

Simulated SPR peaks for particle radii of 10, 20, 30, 40, and 50 nm using the quasi-static Mie–Drude model.
Peak red-shifts from 392 nm (10 nm) to 421 nm (50 nm) due to enhanced electron oscillation damping.

Figure S7: Bandgap Energy vs Particle Size

Plot of bandgap energy (E₉) vs particle diameter.
E₉ decreases from 3.12 eV (15 nm) to 3.07 eV (21 nm), illustrating the quantum confinement relaxation with increasing nanoparticle size.

S3. Supplementary Tables

| Table S1. Simulation Parameters Used in Each Module |  |
| --- | --- |
| Reaction order | Pseudo-first order |
| Pre-exponential factor (K₀) | 1 × 10⁵ L·mol⁻¹·min⁻¹ |
| Activation energy (Eₐ) | 45 kJ mol⁻¹ |
| Simulation temperature range | 25–125 °C |
| Wavelength range | 180–800 nm |
| Particle concentration (N) | 2 × 10⁻⁷ mol L⁻¹ |
| Cuvette path length (l) | 1 cm |
| Plasma frequency (ℏωₚ) | 9.0 eV |
| High-frequency dielectric constant (ε∞) | 5.0 |
| Bulk damping (γ₀) | 0.07 eV |
| Refractive index of medium (nₘ) | 1.33 (water) |

S4. Model Validation

The pseudo-first-order kinetic model was validated by nonlinear regression of the simulated Ag⁰ concentration data to Equation (3) in the main text.
The best-fit correlation coefficient was R² = 0.995, confirming excellent agreement with theoretical kinetics.

Similarly, the simulated UV–Vis spectra were compared with experimental AgNP spectra from cellulose- and plant-extract-mediated syntheses in literature.
The simulated SPR peak positions deviated by less than ±5 nm from reported experimental values, verifying the predictive accuracy of the Mie–Drude implementation.

S5. Code Availability

Representative Python scripts for each simulation (size distribution, kinetics, optical spectra, and bandgap) are available upon request from the corresponding author:
Dr. John O. Agumba (agumba.john@gmail.com).

S6. Additional Notes

- All figures were generated using Matplotlib with consistent UV-Vis plotting convention (UV on the left, visible on the right).

- All units conform to SI conventions.

- The reported kinetic and optical values were averaged over five simulation runs to ensure reproducibility.

- The model can be extended to gold or copper nanoparticles by substituting the corresponding Drude parameters.