Eco-friendly Al-Bi2WO6 nanosheets for effective elimination of crystal violet and methylene blue dyes

Diwakar Malla1,4, Bishal Hamal1,4, Rakshya Mulmi2, Neel Kamal Koju3, Rishi Ram Ghimire4, and Deependra Das Mulmi1*

1Nanomaterials Research Laboratory, Nepal Academy of Science and Technology (NAST), Lalitpur, 44700, Nepal

2KIST Medical College and Teaching Hospital, Lalitpur, 44705, Nepal

3Goldengate International College, Trikuti Colony, Kathmandu, 44600, Nepal

4 Racah Institute of Physics and the Harvey M. Kruger Family Center for Nanoscience and Nanotechnology, the Hebrew University of Jerusalem, Jerusalem 919040, Israel.

*Corresponding author: dmulmi@gmail.com

S1. Schematic diagram of synthesis

S2. FE-SEM analysis

S2 (a-c) depict FE-SEM images of Al-Bi2WO6 at different magnification scales. S2 (d-f) illustrate histograms of the dimension of nanosheets following the Gaussian distribution.

S2 (a-c) FE-SEM images of Al-Bi2WO6 at different magnification scales. S2 (d-f) are histograms of the count of the width, length, and thickness of Al-Bi2WO6, respectively.

S3. Schematic diagram of Adsorption experiment