| Dye | λ max (nm) | Time for Complete Degradation | Degradation Efficiency (%) | Pseudo-First-Order Rate Constant (k, min⁻¹) |
| --- | --- | --- | --- | --- |
| Methylene Blue (MB) | ~664 | 100 min | 99% | 0.05147 |
| Rhodamine B (RhB) | ~550 | 140 min | 98% | 0.02743 |
| Crystal Violet (CV) | ~590-600 | 160 min | 98% | 0.02409 |

Table 1: Photocatalytic degradation of MB, RhB, and CV using TiO₂ nanoparticles under sunlight