Supporting information for

Reversible formation of coordination bonds in Sn-based metal-organic frameworks for high-performance lithium storage

Jingwei Liu,1 Daixi Xie,1 Xiufang Xu,1 Luozhen Jiang,2 Rui Si,2 Wei Shi,1 and Peng Cheng1

1Key Laboratory of Advanced Energy Materials Chemistry (MOE), Renewable Energy Conversion and Storage Center, College of Chemistry, Nankai University, Tianjin 300071, China

2Shanghai Synchrotron Radiation Facility, Shanghai Institute of Applied Physics, Chinese Academy of Sciences, Shanghai 201204, China

Correspondence: shiwei@nankai.edu.cn (W.S.) and sirui@sinap.ac.cn (R.S.).

| Table of Contents |  |
| --- | --- |
| Supplementary Figure 1. (a) Coordination environment of Sn2+ ion in Sn2(dobpdc). (b) 3D structure of Sn2(dobpdc) along the b axis. (c) The 1D chain linked by hydroxyl groups along the c axis. | 4 |
| Supplementary Figure 2. Simplified topological structure of Sn2(dobdc) and Sn2(dobpdc). | 4 |
| Supplementary Figure 3. PXRD patterns. Simulated and experimental PXRD patterns of Sn2(dobdc) (a) and Sn2(dobpdc) (b). Insert: the optical photographs of the crystals for electrolyte stability tests. | 5 |
| Supplementary Figure 4. TGA patterns. | 5 |
| Supplementary Figure 5. The in situ variable-temperature PXRD patterns for Sn2(dobdc) and Sn2(dobpdc). | 6 |
| Supplementary Figure 6. Cycling performances of Sn2(dobdc) (a) and Sn2(dobpdc) (b) electrodes at 500 mA g-1. | 6 |
| Supplementary Figure 7. Calculated lithium storage sites of the organic ligands of Sn2(dobdc) (a) and Sn2(dobpdc) (b). | 7 |
| Supplementary Figure 8. Kinetics and quantitative analysis of Li+ storage mechanism. | 8 |
| Supplementary Figure 9. The GITT results. (a, b) GITT curves for Sn2(dobdc) and Sn2(dobpdc). (c) The values of (∆Es/∆Eτ)2. (d) Diffusion coefficients calculated from GITT versus state of discharge of Sn2(dobdc) and Sn2(dobpdc). | 9 |
| Supplementary Figure 10. Schematic diagrams of the pore surfaces of Sn2(dobdc) (a) and Sn2(dobpdc) (b) calculated by Material Studio. | 10 |
| Supplementary Figure 11. In situ PXRD and ex situ FTIR analysis of Sn2(dobdc) electrode. | 11 |
| Supplementary Figure 12. Selected in situ PXRD patterns at the different states of Sn2(dobdc) (a) and Sn2(dobpdc) (b) electrodes during the first two cycles. | 12 |
| Supplementary Figure 13. XAFS results. (a) Synchrotron Sn K-edge XANES spectra of pristine Sn2(dobpdc), Sn foil, standard SnO and SnO2. Inset: enlarged spectra at Sn K-edge. (b) Sn K-edge k3-weighted FT-EXAFS spectra of pristine Sn2(dobpdc), Sn metal, SnO and SnO2. | 13 |
| Supplementary Figure 14. (a) Synchrotron Sn K-edge XANES spectra of pristine Sn2(dobpdc), after the fifth fully discharged, and after the fifth fully charged. (b) Sn K-edge k3-weighted FT-EXAFS spectra of pristine Sn2(dobpdc), after the fifth fully discharged, and after the fifth fully charged. (c) Corresponding EXAFS fitting results of (b). | 14 |
| Supplementary Figure 15. Ex situ HRTEM images at different states during the second lithiation-delithiation cycle of Sn2(dobpdc). | 15 |
| Supplementary Figure 16. HRTEM images of pristine Sn2(dobdc) (a) and Sn2(dobpdc) (b) powders. | 15 |
| Supplementary Figure 17. FTIR spectra. | 16 |
| Supplementary Figure 18. Morphology characterizations. | 16 |
| Supplementary Table 1. Comparison of recent MOFs as anodes for LIBs | 17 |
| Supplementary Table 2. Crystal data and structural refinement parameters for Sn2(dobdc) and Sn2(dobpdc). | 18 |
| Supplementary Table 3. Selected bond lengths (Å) and angles (º) for Sn2(dobdc) and Sn2(dobpdc). | 19 |
| Supplementary Table 4. Cartesian coordinates of Li8dobdc and Li12dobpdc for DFT calculation. | 20, 21 |
| Supplementary Table 5. Calculated capacities and utilization efficiencies of Sn2(dobdc) and Sn2(dobpdc). | 22 |
| Supplementary Table 6. Sn K-edge EXAFS fitting results. | 23 |
| Supplementary Table 7. Selected Sn-based anodes and other typical anode materials for LIBs | 24 |
| Supplementary References. | 25-27 |

Supplementary Figure 1. (a) Coordination environment of Sn2+ ion in Sn2(dobpdc). (b) 3D structure of Sn2(dobpdc) along the b axis. (c) The 1D chain linked by hydroxyl groups along the c axis. The yellow, gray and red balls represent Sn, C and O atoms, respectively.

Supplementary Figure 2. Simplified topological structure of Sn2(dobdc) and Sn2(dobpdc). The framework can be viewed as a (3,6)-connected rtl net with the short (Schläﬂi) vertex symbol of {4·6^2}2{4^2·6^10·8^3}.

Supplementary Figure 3. PXRD patterns. Simulated and experimental PXRD patterns of Sn2(dobdc) (a) and Sn2(dobpdc) (b). Insert: the optical photographs of the crystals for electrolyte stability tests.

Supplementary Figure 4. TGA patterns. TGA curves of Sn2(dobdc) (a) and Sn2(dobpdc) (b).

Supplementary Figure 5. PXRD patterns. The in situ variable-temperature PXRD patterns for Sn2(dobdc) (a) and Sn2(dobpdc) (b) measured on a Pt sample platform under N2 atmosphere in the temperature ranges of 50-600 °C. The peaks observed at ca. 46.3 degree is from the Pt sample platform.

Supplementary Figure 6. Cycling performances of Sn2(dobdc) (a) and Sn2(dobpdc) (b) electrodes at 500 mA g-1. The reversible capacities of Sn2(dobdc) and Sn2(dobpdc) electrodes can maintain at 400 and 650 mAh g-1 after 600 cycles, respectively.

Supplementary Figure 7. Calculated lithium storage sites of the organic ligands of Sn2(dobdc) (a) and Sn2(dobpdc) (b).

Theoretical capacity calculation: take the case of Sn2(dobdc), the structure unit of Sn2(dobdc) can reversibly alloy 8.8 Li+ ions with 2.0 Sn and insert 8.0 Li+ ions with one organic ligand including the insertion to functional groups and the superlithiation of the aromatic ligand. Theoretical capacity is calculated by the equation: Ctheo = nF/3.6M, where n is the number of electrons transferred, F is the Faraday constant, M is the relative molecular mass (g/mol).

Supplementary Figure 8. Kinetics and quantitative analysis of Li+ storage mechanism. CV curves of Sn2(dobdc) (a) and Sn2(dobpdc) (b) electrodes at different scan rates. The corresponding plots of log (peak current) vs. log (scan rate) at each peak of Sn2(dobdc) (c) and Sn2(dobpdc) (d). The capacitive contributions of Sn2(dobdc) (e) and Sn2(dobpdc) (f) at different scan rates.

Supplementary Figure 9. The GITT results. (a, b) GITT curves for Sn2(dobdc) and Sn2(dobpdc). (c) The values of (∆Es/∆Eτ)2. (d) Diffusion coefficients calculated from GITT versus state of discharge of Sn2(dobdc) and Sn2(dobpdc).

Supplementary Figure 10. Schematic diagrams of the pore surfaces of Sn2(dobdc) (a) and Sn2(dobpdc) (b) calculated by Material Studio. It is noteworthy that the void space (13.6%) for Sn2(dobpdc) is significantly larger than that (5.2%) of Sn2(dobdc), which is attributed to the expanded organic linker. Thus, the calculated surface area (89.75 m2/g) of Sn2(dobpdc) is higher than that (51.56 m2/g) of Sn2(dobdc), which is beneficial for facilitating mass/charge transport and interface interaction. For these two Sn-MOFs, the shortest distances of the slits are less than 2 Å, which are both inaccessible for the gases including N2, CO2, Ar for the experimental surface area measurement.

Supplementary Figure 11. In situ PXRD and ex situ FTIR analysis of Sn2(dobdc) electrode. (a) Discharge-charge profile of Sn2(dobdc) at 50 mA g-1 in the first cycle. (b) In situ PXRD of Sn2(dobdc) collected at different discharge-charge states corresponding to the process in S11a. (c) Discharge-charge profile of Sn2(dobdc) at 100 mA g-1 in the first cycle. (d) Ex situ FTIR spectra at selected states. (e) Magnification of FTIR spectra at the range from 600 to 1800 cm-1.

Supplementary Figure 12. Selected in situ PXRD patterns at the different states of Sn2(dobdc) (a) and Sn2(dobpdc) (b) electrodes during the first two cycles.

Supplementary Figure 13. XAFS results. (a) Synchrotron Sn K-edge XANES spectra of pristine Sn2(dobpdc), Sn foil, standard SnO and SnO2. Inset: enlarged spectra at Sn K-edge. (b) Sn K-edge k3-weighted FT-EXAFS spectra of pristine Sn2(dobpdc), Sn metal, SnO and SnO2 (the EXAFS intensity of SnO2 is shown at half value).

As shown in Supplementary Figure13a, the XANES spectra of Sn foil, standard SnO and SnO2 are much different from that of the pristine Sn2(dobpdc), probably because of the formation of SnO4 coordination environment in the Sn2(dobpdc). However, the Sn2+ state in pristine Sn2(dobpdc) can be clearly identified because the intensity of white line in Sn2(dobpdc) is very close to that of main peak in SnO. The Fourier transformations (FT) of k3-weighted for EXAFS oscillations for the radial structure functions of pristine Sn2(dobpdc), Sn foil, standard SnO and SnO2 are demonstrated in Supplementary Figure 13b. The pristine Sn2(dobpdc) exhibits the characteristic Sn-O coordination with intensive peak at around 2.13 Å, which coincides well with the lengths of Sn-O bonds obtained from the single crystal X-ray diffraction data (Supplementary Table 3). The absence of Sn-Sn bonds suggests that there were no metal Sn in pristine Sn2(dobpdc) sample.

Supplementary Figure 14. (a) Synchrotron Sn K-edge XANES spectra of pristine Sn2(dobpdc), after the fifth fully discharged, and after the fifth fully charged. (b) Sn K-edge k3-weighted FT-EXAFS spectra of pristine Sn2(dobpdc), after the fifth fully discharged, and after the fifth fully charged. (c) Corresponding EXAFS fitting results of (b).

Supplementary Figure 15. Ex situ HRTEM images at different states during the second lithiation-delithiation cycle of Sn2(dobpdc). (a) HRTEM images of Sn2(dobpdc) in a pristine state, discharged to 0.7 V and discharged to 0.01 V. (b) HRTEM images of Sn2(dobpdc) after being charged to 0.3 V, charged to 1.0 V and charged to 3.0 V.

Supplementary Figure 16. HRTEM images of pristine Sn2(dobdc) (a) and Sn2(dobpdc) (b) powders.

Supplementary Figure 17. FTIR spectra. Ex situ FTIR spectra of Sn2(dobdc) at different states before (a) and after cycling (b). Ex situ FTIR spectra of Sn2(dobpdc) before (c) and after cycling (d).

Supplementary Figure 18. Morphology characterizations. SEM images of Sn2(dobdc) (a-c) and Sn2(dobpdc) (d-f) collected at different states.

Supplementary Table 1. Comparison of recent MOFs as anodes for LIBs.

| MOFs | RC (mAh g-1) / CR (mA g-1) | Cycle number | Refs. |
| --- | --- | --- | --- |
| Sn2(dobdc) | 731 / 200 | 200 | This work |
| Sn2(dopbdc) | 1018 / 200 | 200 | This work |
| Mn-UMOFNs | 1187 / 100 | 100 | S1 |
| Mn-BDC | 974 / 100 | 100 | S2 |
| CoBTC-EtOH | 856 / 100 | 100 | S3 |
| Mn-BTC | 694 / 100 | 100 | S4 |
| NENU-507 | 640 / 100 | 100 | S5 |
| [Co3(L1)(N3)4] | 580 / 100 | 200 | S6 |
| [Co4L2(N3)(H2O)2] | 595 / 100 | 200 | S6 |
| [Mn4L2(N3)6(H2O)2] | 595 / 100 | 200 | S6 |
| Ni-UMOFNs | 546 / 100 | 100 | S1 |
| [Mn2(L1)(N3)2(H2O)2]·3H2O | 358 / 100 | 200 | S6 |
| [Cd(HTCPPA)·2H2O]n | 302 / 100 | 100 | S7 |
| Cu3(BTC)2 | 474 / 383 | 50 | S8 |
| Co2(OH)2BDC | 650 / 50 | 100 | S9 |
| Ni-MOF | 620 / 100 | 100 | S10 |
| Mn(3,5-PDC) 2H2O | 554 / 100 | 240 | S11 |
| Mn(2,5-FDC) 3H2O | 436 / 100 | 206 | S11 |
| [Co(C8H4O4)4]n | 700 / 60 | 100 | S12 |
| Zn3(HCOO)6 | 560 / 60 | 60 | S13 |
| Co3(HCOO)6 | 410 / 60 | 60 | S13 |
| NNU-11 | 750 / 50 | 200 | S14 |
| Co-LCP | 545 / 50 | 50 | S15 |
| Mn-LCP | 390 / 50 | 50 | S16 |
| Ni-Me4bpz | 120 / 50 | 100 | S17 |

RC: Reversible capacity. CR: Current Rate.

Supplementary Table 2. Crystal data and structural refinement parameters for Sn2(dobdc) and Sn2(dobpdc).

|  | [Sn2(dobdc)]n | [Sn2(dobpdc)]n |
| --- | --- | --- |
| Formula | C4HO3Sn | C7H3O3Sn |
| Fw | 215.76 | 253.78 |
| Temp, K | 120.00(10) | 120.00(10) |
| Crystal syst | Monoclinic | Monoclinic |
| Space group | P21/c | P21/c |
| a, Å | 7.4141(3) | 10.8951(3) |
| b, Å | 7.5679(2) | 7.5313(2) |
| c, Å | 9.1100(3) | 8.8733(3) |
| α, deg | 90 | 90 |
| ß, deg | 106.603 | 92.329(3) |
| , deg | 90 | 90 |
| V, Å3 | 489.84 | 727.49(4) |
| Z | 4 | 4 |
| Dc, g/cm3 | 2.925 | 2.317 |
| μ, mm-1 | 5.107 | 3.458 |
| Data/ parameter | 857 / 73 | 1277 / 100 |
| obs reflns | 2814 | 4619 |
| range, | 7.126 - 50.002 | 6.578 - 49.992 |
| Rint/GOF on F2 | 0.0418 / 1.021 | 0.0468 / 1.063 |
| R1, wR2[I>2 (I)] | 0.0232, 0.0407 | 0.0253, 0.0417 |
| R1, wR2(all data) | 0.0329, 0.0447 | 0.0340, 0.0463 |
| max/min, e Å-3 | 0.58 / -0.68 | 0.64 / -0.65 |

Supplementary Table 3. Selected bond lengths (Å) and angles (º) for Sn2(dobdc) and Sn2(dobpdc).

| Sn2(dobdc) |  |  |  |
| --- | --- | --- | --- |
| Sn1-O31 | 2.195(3) | O31-Sn1-O1 | 80.18(12) |
| Sn1-O2 | 2.183(3) | O31-Sn1-O12 | 78.00(12) |
| Sn1-O12 | 2.382(3) | O2-Sn1-O31 | 85.59(13) |
| Sn1-O1 | 2.222(3) | O2-Sn1-O12 | 72.67(12) |
|  |  | O2-Sn1-O1 | 77.00(12) |
|  |  | O1-Sn1-O12 | 143.65(7) |
| Symmetry transformations used to generate equivalent atoms: 1+X, 3/2-Y, -1/2+Z; 21-X, 1/2+Y, 1/2-Z; 3+X, 3/2-Y, 1/2+Z; 41-X, -1/2+Y, 1/2-Z; 52-X, 1-Y, 1-Z. |  |  |  |

| Sn2(dobpdc) |  |  |  |
| --- | --- | --- | --- |
| Sn1-O31 | 2.181(3) | O31-Sn1-O1 | 81.59(11) |
| Sn1-O2 | 2.116(8) | O31-Sn1-O12 | 79.55(10) |
| Sn1-O12 | 2.104(6) | O2-Sn1-O31 | 83.28(10) |
| Sn1-O1 | 2.065(6) | O2-Sn1-O12 | 71.45(9) |
|  |  | O2-Sn1-O1 | 77.56(10) |
|  |  | O1-Sn1-O12 | 145.23(6) |
| Symmetry transformations used to generate equivalent atoms: 1+X, 3/2-Y, -1/2+Z; 21-X, 1/2+Y, 1/2-Z; 3+X, 3/2-Y, 1/2+Z; 41-X, -1/2+Y, 1/2-Z; 5-X,1-Y,1-Z. |  |  |  |

Supplementary Table 4. Cartesian coordinates of Li8dobdc and Li12dobpdc for DFT calculation.

| Cartesian coordinates for Li8dobdc |  |  |  |
| --- | --- | --- | --- |
| Element | Coordinates |  |  |
|  | X | Y | Z |
| O | 3.726424 | 0.642739 | -0.275760 |
| O | 3.221470 | -1.498581 | -0.535850 |
| O | 1.553859 | 2.322339 | 0.518391 |
| C | 2.801745 | -0.279485 | -0.226161 |
| C | 0.572344 | -1.289576 | 0.365570 |
| H | 0.986574 | -2.141050 | 0.917040 |
| C | 0.854192 | 1.262153 | 0.343834 |
| C | 1.450358 | -0.072227 | 0.132073 |
| O | -3.726232 | -0.642573 | -0.275118 |
| O | -3.221079 | 1.498458 | -0.536083 |
| O | -1.553319 | -2.322564 | 0.516312 |
| C | -2.801689 | 0.279541 | -0.225703 |
| C | -0.571766 | 1.290659 | 0.363537 |
| H | -0.986094 | 2.142178 | 0.914961 |
| C | -0.853179 | -1.262169 | 0.342710 |
| C | -1.449865 | 0.072574 | 0.132276 |
| Li | -0.012742 | -0.000714 | 2.057254 |
| Li | 0.001254 | 0.000401 | -1.458559 |
| Li | 1.979344 | -2.798545 | -0.592796 |
| Li | 4.939017 | -0.725681 | -0.724666 |
| Li | 3.318525 | 2.345750 | 0.273871 |
| Li | -3.317545 | -2.346947 | 0.270346 |
| Li | -4.938512 | 0.726246 | -0.726475 |
| Li | -1.976776 | 2.796661 | -0.597628 |

| Cartesian coordinates for Li12dobpdc |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Element | Coordinates |  |  | Element | Coordinates |  |  |
|  | X | Y | Z |  | X | Y | Z |
| O | -4.03291 | -2.31359 | 0.23475 | H | 0.13111 | -2.38594 | 0.0588 |
| O | -5.55591 | -0.76408 | -0.2938 | C | 0.70888 | -0.27231 | -0.01423 |
| O | -4.64352 | 1.96555 | 0.17109 | Li | -5.16576 | 3.83152 | 0.20041 |
| C | -4.32359 | -1.10101 | 0.00652 | Li | -6.83905 | -1.8848 | -1.166 |
| C | -3.25277 | -0.07899 | 0.04194 | Li | -4.25966 | -3.99602 | 0.89521 |
| C | -3.45999 | 1.38327 | 0.07717 | Li | 4.25864 | 3.99389 | -0.90035 |
| C | -2.29117 | 2.18649 | 0.03403 | Li | 6.83421 | 1.89492 | 1.17198 |
| H | -2.40942 | 3.26436 | 0.05628 | Li | 5.16276 | -3.83246 | -0.22732 |
| C | -1.8479 | -0.56388 | 0.08046 | Li | -6.16543 | 0.87377 | 0.28646 |
| H | -1.7434 | -1.63788 | 0.10716 | Li | -1.97473 | 0.94335 | 1.93406 |
| C | -0.93925 | 1.6708 | -0.02928 | Li | 6.169 | -0.87739 | -0.25511 |
| H | -0.13137 | 2.3859 | -0.06896 | Li | 1.9815 | -0.93278 | -1.93685 |
| C | -0.70876 | 0.27233 | 0.01154 | Li | -2.17049 | 0.90793 | -1.86423 |
| O | 4.03437 | 2.31286 | -0.2354 | Li | 2.16796 | -0.92024 | 1.86355 |
| O | 5.55426 | 0.76479 | 0.30524 |  |  |  |  |
| O | 4.64368 | -1.96578 | -0.17212 |  |  |  |  |
| C | 4.32378 | 1.10082 | -0.00262 |  |  |  |  |
| C | 3.25285 | 0.07874 | -0.04077 |  |  |  |  |
| C | 3.46008 | -1.38331 | -0.07897 |  |  |  |  |
| C | 2.29104 | -2.18655 | -0.04033 |  |  |  |  |
| H | 2.40921 | -3.26437 | -0.06519 |  |  |  |  |
| C | 1.84816 | 0.56395 | -0.07986 |  |  |  |  |
| H | 1.74371 | 1.63803 | -0.10351 |  |  |  |  |
| C | 0.93919 | -1.67086 | 0.02306 |  |  |  |  |

Supplementary Table 5. Calculated capacities and utilization efficiencies of Sn2(dobdc) and Sn2(dobpdc).

| MOFs | Sn2(dobdc) | Sn2(dobpdc) |
| --- | --- | --- |
| Theoretical number of Li uptake in organic ligand | 8 | 12 |
| Theoretical number of Li uptake in metal center | 8.8 | 8.8 |
| Theoretical Capacity (mAh g-1) | 1044 | 1099 |
| Reversible Capacity at 200 mA g-1 (mAh g-1) | 731 | 1018 |
| Utilization Efficiency (%) | 70.0 | 92.6 |

Supplementary Table 6. Sn K-edge EXAFS fitting results (R: distance; CN: coordination number; 2: Debye-Waller factor; E0: inner potential correction; D: discharge; C: charge) for Sn2(dobpdc) electrode.

| Sample | Sn-O |  | Sn-Sn |  | 2 (Å2) | E0 (eV) |
| --- | --- | --- | --- | --- | --- | --- |
|  | R (Å) | CN | R (Å) | CN |  |  |
| Pristine | 2.130.02 | 3.70.7 |  |  | 0.01(Sn-O) 0.015(Sn-Sn) | 111(Sn-O) 31(Sn-Sn) |
| D 1.5 V | 2.140.02 | 2.80.5 |  |  |  |  |
| D 0.01 V |  |  | 2.920.03 | 6.31.2 |  |  |
| C 0.6 V |  |  | 2.930.03 | 2.50.6 |  |  |
| C 3.0 V | 2.140.02 | 2.70.4 |  |  |  |  |
| 5th full discharge | 2.150.02 | 1.80.3 | 2.950.02 | 3.10.8 |  |  |
| 5th full charge | 2.150.02 | 3.50.6 |  |  |  |  |

Supplementary Table 7. Selected Sn-based anodes and other typical anode materials for LIBs

| Active materials | Structure or type | Preparation method | RC / CR | Cycle number | Refs. |
| --- | --- | --- | --- | --- | --- |
| Sn2(dobdc) | Sn atoms anchored on organic ligands | One-step hydrothermal method | 731 / 200 | 200 | This work |
| Sn2(dopbdc) | Sn atoms anchored on organic ligands | One-step hydrothermal method | 1018 / 200 | 200 | This work |
| 3D Sn scaffold | Sn hollow spheres | Multistep templating | 885 / 200 | 200 | S18 |
| TiO2-Sn@CNFs | Nano-Sn dispersed in carbon nanofibers and TiO2 pipes | Electrospinning and atomic layer deposition | 831 / 100 | 200 | S19 |
| Co–Sn intermetallic electrodes | Highly ordered mesoporous CoxSny framework | Nanoreplication method | 530 / 50 | 50 | S20 |
| SnO2-Fe-G nanocomposites | SnO2-Fe aggregates binding on graphite nanosheets | Two-step ball milling | 1338 / 200 | 400 | S21 |
| Sn@C nanoboxes | Sn nanoparticles encapsulated in hollow carbon nanobox | Sacrificial template method | 810 / 200 | 500 | S22 |
| Polydopamine -coated SnO2 | SnO2 nanocrystals coated with polydopamine | Sacrificial template method | 921 /200 | 300 | S23 |
| SnO2@MOF/graphene composite. | SnO2 nanoparticles packed into Al-MOF wrapped by graphene | Wet impregnation method and assembly process | 450 / 1000 | 1000 | S24 |
| Porous hard carbons | Insertion type | Thermal annealing method | 310 / 5000 | 10000 | S25 |
| Fe2O3 microboxes | Conversion type | Thermal annealing method | 950 / 200 | 30 | S26 |
| Co3O4 | Conversion type | Hybrid assembly and chemical reduction approaches | 1000 / 74 | 130 | S27 |

RC: Reversible capacity (mAh g-1). CR: Current Rate (mA g-1)

Supplementary References:

S1 Li, C. et al. Ultrathin Manganese-Based Metal-Organic Framework Nanosheets: Low-Cost and Energy-Dense Lithium Storage Anodes with the Coexistence of Metal and Ligand Redox Activities. ACS Appl. Mater. Interfaces 9, 29829–29838 (2017).

S2 Hu, H. P. et al. A thermally activated manganese 1,4-benzenedicarboxylate metal organic framework with high anodic capability for Li-ion batteries. New J. Chem. 40, 9746–9752 (2016).

S3 Li, C. et al. High anodic performance of Co 1, 3, 5-benzenetricarboxylate coordination polymers for Li-ion battery. ACS Appl. Mater. Interfaces 8, 15352–15360 (2016).

S4 Maiti, S., Pramanik, A., Manju U., Mahanty, S. Reversible lithium ltorage in manganese 1,3,5-benzenetricarboxylate metal-organic gamework with high capacity and rate performance. ACS Appl. Mater. Interfaces 7, 16357–16363 (2016).

S5 Wang, Y. Y. et al. Diamondoid-structured polymolybdate-based metal–organic frameworks as high-capacity anodes for lithium-ion batteries. Chem. Commun. 53, 5204–5207 (2017).

S6 Gong, T., Lou, X., Gao, E., Hu, B. Pillared-layer metal–organic frameworks for improved lithium-ion dtorage performance. ACS Appl. Mater. Interfaces 9, 21839–21847 (2017).

S7 Lin, X. M. et al. Lithium-ion-battery anode materials with improved capacity from a metal-organic framework. Inorg. Chem. 55, 8244–8247 (2016).

S8 Maiti, S., Pramanik, A., Manju, U., Mahanty, S. Cu3(1,3,5-benzenetricarboxylate)2 metal-organic framework: a promising anode material for lithium-ioMn battery. Microporous Mesoporous Mater. 226, 353–359 (2016).

S9 Gou, L. et al. One-pot synthesis of a metal–organic framework as an anode for Li-ion batteries with improved capacity and cycling stability. J. Solid State Chem. 210, 121–124 (2014).

S10 Zhang, Y. et al. A nickel-based metal-organic framework: a novel optimized anode material for Li-ion batteries. Mater. Lett. 161, 712–715 (2015).

S11 Fei, H. L., Liu, X., Li, Z. W., Feng, W. J. Metal dicarboxylates: new anode materials for lithium-ion batteries with good cycling performance. Dalton Trans. 44, 9909-9914 (2015).

S12 Wang, L. P. et al. Metal organic framework derived cobalt dicarboxylate as a high capacity anode material for lithium-ion batteries. Energy Technol. 5, 634–642 (2017).

S13 Saravanan, K., Nagarathinam, M., Balaya P., Vittal, J. J. Lithium storage in a metal organic framework with diamondoid topology–a case study on metal formats. J. Mater. Chem. 20, 8329–8335 (2010).

S14 Huang, Q. et al. A highly stable polyoxometalate-based metal-organic framework with π-π stacking for enhancing lithium ion battery performance. J. Mater. Chem. A 5, 8477–8483 (2017).

S15 Shi, C. D. et al. Synthesis of cobalt-based layered coordination polymer nanosheets and their application in lithium-ion batteries as anode materials. RSC Adv. 6, 4442–4447 (2016).

S16 Liu, Q. et al. Manganese-based layered coordination polymer: synthesis, structural characterization, magnetic property, and electrochemical performance in lithium-ion batteries. Inorg. Chem. 52, 2817–2822 (2013).

S17 An, T. et al. A flexible ligand-based wavy layered metal–organic framework for lithium-ion storage. J. Colloid Interf. Sci. 445, 320–325 (2015).

S18 Liu, J. et al. High volumetric capacity three-dimensionally sphere-caged secondary battery anodes. Nano Lett. 16, 4501–4507 (2016).

S19 Mao, M. et al. Pipe-wire TiO2-Sn@carbon nanofibers paper anodes for lithium and sodium ion batteries. Nano Lett. 17, 3830–3836 (2017).

S20 Park, G. O. et al. Discovering a dual-buffer effect for lithium storage: durable nanostructured ordered mesoporous Co-Sn intermetallic electrodes. Adv. Funct. Mater. 26, 2800–2808 (2016).

S21 Hu, R. et al. Stabilizing the nanostructure of SnO2 anodes by transition metals: a route to achieve high initial coulombic efficiency and stable capacities for lithium storage. Adv. Mater. 29, 1605006 (2017).

S22 Zhang, H. et al. Tailored yolk-shell Sn@C nanoboxes for high-performance lithium storage. Adv. Funct. Mater. 27, 1606023 (2017).

S23 Jiang, B. et al. Polymer-templated formation of polydopamine-coated SnO2 nanocrystals: anodes for cyclable lithium-ion batteries. Angew. Chem. Int. Ed. 56, 1869–1872 (2017).

S24 Gao, C. et al. Optimized assembling of MOF/SnO2/Graphene leads to superior anode for lithium ion batteries. Nano Energy 74, 104868 (2020).

S25 Lv, W. et al. Peanut shell derived hard carbon as ultralong cycling anodes for lithium and sodium batteries. Electrochim. Acta 176, 533–541 (2015).

S26 Zhang, L. et al. Formation of Fe2O3 microboxes with hierarchical shell structures from metal-organic frameworks and their lithium storage properties. J. Am. Chem. Soc. 134, 17388–17391 (2012).

S27 Yang, S., Feng, X., Ivanovici, S., Mullen, K. Fabrication of graphene-encapsulated oxide nanoparticles: towards high-performance anode materials for lithium storage. Angew. Chem. Int. Ed. 49, 8408–8411 (2010).