Supplementary Information

Regulating Surface and Local Chemistry in High Na-content P2-type Cathode to Achieve Ultrahigh Power and Low Temperature Sodium Storage

Supplementary Fig. 1 The P2-and O3-type crystal structures. a, The hexagonal structure of P2-type oxide with the space group of P63/mmc (194). b, The Rhombohedral structure O3-type oxide with the space group of R-3m (166). The TM stand for transition metal.

Supplementary Fig. 2 Shift of the (002) and (004) diffraction peak of P2-NaMN and P2-NaMNNb compounds.

Supplementary Fig. 3 a, Field-emission scanning electron microscope (SEM) image of P2-NaMNNb compound. b, HADDF-STEM image that illustrates the surface reconstruction layer of P2-NaMNNb only exists along [100] direction.

Supplementary Fig. 4 Fast Fourier Transform (FFT) diffraction of P2-NaMNNb and P2-NaMN.

Supplementary Fig. 5 Schematic diagram of spinel-like-atomic structure projected along [110] crystallographic direction.

Supplementary Fig. 6 a, STEM-HAADF image showing Energy Spectrum Line Scan position. B, Corresponding EDS line profiles of (a) O (orange), Na (green), Mn (red), Ni (blue) and Nb (cyan-blue).

Supplementary Fig. 7 a-c, HAADF images of the Na0.78Ni0.3Mn0.67O2 particles projected along [010] zone axes taken after different electron beam irradiation times (0 min, 1 min and 3 min) with a dose rate of ~1.12 × 104 electrons Å-2 s-1, at a dwell time of ~1μs/pixel.

Supplementary Fig. 8 a, HRTEM image of the Na0.78Ni0.3Mn0.67O2 projected along [010] zone axis, and taken after different electron beam irradiation times (0 min, 1 min and 3 min corresponding to b, c, d.

Supplementary Fig. 9 Charge–discharge curves of a, P2-NaMNNb and b, P2-NaMN cathode at 25 °C and -40 °C.

Supplementary Fig. 10 Ex-situ XPS analysis of a Ni 2p and Mn 2p for P2-NaMN at pristine state, charge to 4.15 V. b, Ni 2p, c, Mn 2p and d, Nb 3d for P2-NaMNNb at pristine state, charge to 4.15 V and discharge to 2.4 V, respectively.

The valance states of the elements at different charge/discharge voltages of P2-NaMN and P2-NaMNNb were investigated by ex-situ X-ray photoelectron spectroscopy (XPS). For P2-NaMNNb, the high-resolution spectrum of Ni 2p reveals that the 2p3/2 and 2p1/2 peaks of Ni are 854.2 and 871.6 eV, respectively. When charged to 4.15 V, the spectrum of Ni2+ 2p shifts to the direction of high binding energy (Supplementary Fig. 10b). It shifts to Ni3+ and a tiny valence state of Ni4+, indicating oxidation of Ni2+/Ni3+/Ni4+1,2, which means more electrons participate in the redox reaction to contribute more capacity than that of P2-NaMN (Supplementary Fig. 10a). This consequence fits well with the circumstance of CV (Fig. 3a) and charging/discharging curves (Supplementary Fig. 9). After discharged to 2.4 V, the valence of Ni close to +2 with trivial trivalent nickel, this is because the valance of Ni is not completely reduced to +2 at 2.4 V. The XPS Mn 2p spectrum of P2-NaMNNb (Supplementary Fig. 10c) depicts that co-existence of Mn3+ and Mn4+ with the ratio of 0.27 : 0.73 owing to the Nb doping. During the charging process, the valence of Mn gradually increases, and only Mn4+ exists when reaching 4.15 V. Moreover, the valence of Mn remains +4 after discharged to 2.4 V, indicating that the presence of Mn4+ is steady upon cycling. The valence of Nb is +5 during the entire charge and discharge process, which proving that Nb does not participate in charge compensation (Supplementary Fig. 10d).

Supplementary Fig. 11 Calculated Na+ diffusion coefficients of P2-NaMN electrodes from GITT at 25 and -40 °C.

Supplementary Fig. 12 Long-term cycling stability at a high rate of 5 C at 25 °C.

Supplementary Fig. 13 a, The average working voltage (> 3.3 V) in the rate of 0.5 C at -40 °C. b, Corresponding charging and discharging curves of various cycle numbers at -40 °C.

Supplementary Fig. 14 Structure evolution of P2-NaMNNb upon Na+ extraction/insertion. a, The typical intensity contour maps of in-situ XRD patterns corresponding to the charge and discharge curves between 2.4-4.15 V. b, The variation of cell parameters a/b (green lines), c (blue lines), and V (gray lines).

Supplementary Fig. 15 Comparison of X-ray diffraction patterns of P2-NaMNNb and P2-NaMN after 30 cycles.

Supplementary Fig. 16 EDX spectra of a, P2-NaMN, b, P2-NaMNNb of Na anodes after 30 cycles.

Supplementary Fig. 17 The total density of state of Na24Ni10Mn22O64.

Supplementary Fig. 18 Galvanostatic charge/discharge curves of the hard carbon electrode.

Supplementary Fig. 19 a Galvanostatic charge/discharge curves of various rate of the full-cell at 25 °C. b Galvanostatic charge/discharge curves of various cycles numbers at 25 °C.

Supplementary Fig. 20 Galvanostatic charge/discharge curves of various rate of the full-cell at -40 °C.

Supplementary Fig. 21 The image of the low temperature electrochemical test for half and full cell at -40 °C.

Supplementary Table 1. Stoichiometry from the inductively coupled plasma atomic emission spectrometry (ICP-AES) analysis.

|  | Na | Mn | Ni | Nb |
| --- | --- | --- | --- | --- |
| Na0.78Mn0.67Ni0.31Nb0.02O2 | 0.78 | 0.67 | 0.31 | 0.02 |

Supplementary Table 2. Crystallographic parameters of P2-NaMNNb refined by the Rietveld method.

| site | x | y | z | Occ. |
| --- | --- | --- | --- | --- |
| Naf | 0 | 0 | 1/4 | 0.237 |
| Nae | 2/3 | 1/3 | 3/4 | 0.543 |
| Mn | 0 | 0 | 0 | 0.670 |
| Ni | 0 | 0 | 0 | 0.310 |
| Nb | 0 | 0 | 0 | 0.02 |
| O | 2/3 | 1/3 | 0.07520 | 1 |
| a= 2.888(2)Å | c= 11.155(4)Å | V=80.56(2)Å3 | Rp= 2.36% | Rwp= 4.19% |

Supplementary Table 3. Crystallographic parameters of P2-NaMN refined by the Rietveld method.

| site | x | y | z | Occ. |
| --- | --- | --- | --- | --- |
| Naf | 0 | 0 | 1/4 | 0.303 |
| Nae | 2/3 | 1/3 | 3/4 | 0.477 |
| Mn | 0 | 0 | 0 | 0.68 |
| Ni | 0 | 0 | 0 | 0.32 |
| O | 2/3 | 1/3 | 0.07239 | 1 |
| a= 2.887(1)Å | c= 11.148(2)Å | V=80.46(1)Å3 | Rp= 3.17% | Rwp= 5.61% |

Supplementary Table 4. Comparison of low-temperature performance of various cathode materials for sodium ion batteries.

|  | Cathode | Electrolyte | Anode | Operating temperature | Capacity retention (vs.25 °C) |  | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | NVP-CNTs | NaPF6/G2 | Bi | -15 °C | 84.3% | 3 |  |
|  | NVPOF | NaClO4 in EC/PC+5% FEC | 3DSG | -25 °C | 60.7% | 4 |  |
|  | NVPF-NTP | NaClO4 in EC/PC+5% FEC | Na | -25 °C | 76.4% | 5 |  |
|  | NVPC | Na[FSA]-[C2C1im][FSA] +0.2Na[FSA] | Na | -20 °C | 57.1% | 6 |  |
| polyanion materials | NGO@ Na3V(PO3)3N | NaClO4 in EC/PC+5% FEC | Na | -15 °C | 75% | 7 |  |
|  | Na4Fe3(PO4)2(P2O7) | NaClO4 in EC/PC+5% FEC | Na | -20 °C | 87.7% | 8 |  |
|  | Na4MnCr(PO4)3 | NaClO4 in PC with 5 % and 10 % FEC | Hard carbon | -10 °C | 79% | 9 |  |
|  | NVP@3D hierarchical porous architectures | NaClO4 in EC/PC (1:1) +5% FEC | Na | -20 °C | 93% | 10 |  |
|  | Na3Fe2(PO4)3@flake-porous | NaClO4 in EC/DMC | Hard carbon | -20 °C | 48.3% | 11 |  |
|  | Mo-doped Na3V2(PO4)3 nanowires | NaClO4 in EC/DMC+5% FEC | Hard carbon | -15 °C | 95.9% | 12 |  |
|  | NVP@C | NaClO4 in EC/PC | Na | -30 °C | 88% | 13 |  |
| Prussian blue material | PB/CNT | NaClO4 in EC/PC | Na | -25 °C | 85% | 14 |  |
| Layered oxide material | RAHC Na[Ni0.60Co0.05Mn0.35]O2 | NaPF6 in EMS (98%) and FEC (2%) | Hard carbon | -20 °C | 79.7% (vs 30°C) | 15 |  |
|  | Na2/3Ni1/3Mn7/12Fe1/12O2 | NaClO4 in PC+5% FEC | Na | -25 °C | 63% | 16 |  |
|  | NCM@NTP7 | NaPF6 in a EC/DEC(11 v/v) | Na | -20 °C | 80.5% | 17 |  |
|  | Na0.67Ni0.2Co0.2Mn0.6O2 | NaPF6 in diglyme | Na | -40 °C | 78.8% | 18 |  |
|  | P2-NaMNNb | NaPF6 in diglyme | Na | -40 °C | 98% | Our work |  |
|  |  |  | Hard carbon |  | 97.2% |  |  |

Reference

1.	Liu, Z., et al. Ultralow Volume Change of P2-type Layered Oxide Cathode with Controlled Phase Transition by Regulating Distribution of Na+. Angew. Chem. Int. Ed. n/a,

2.	Ma, C., et al. Exploring Oxygen Activity in the High Energy P2-Type Na0.78Ni0.23Mn0.69O2 Cathode Material for Na-Ion Batteries. J. Am. Chem. Soc. 139, 4835-4845 (2017).

3.	Wang, C., Du, D., Song, M., Wang, Y. &Li, F. A High-Power Na3V2(PO4)3-Bi Sodium-Ion Full Battery in a Wide Temperature Range. Adv. Energy Mater. 9, 1900022 (2019).

4.	Wang, Y.-Y., et al. An Ultralong Lifespan and Low-Temperature Workable Sodium-Ion Full Battery for Stationary Energy Storage. Adv. Energy Mater. 8, 1703252 (2018).

5.	Guo, J.-Z., et al. High-Energy/Power and Low-Temperature Cathode for Sodium-Ion Batteries: In Situ XRD Study and Superior Full-Cell Performance. Adv. Mater. 29, 1701968 (2017).

6.	Hwang, J., Matsumoto, K. &Hagiwara, R. Na3V2(PO4)3/C Positive Electrodes with High Energy and Power Densities for Sodium Secondary Batteries with Ionic Liquid Electrolytes That Operate across Wide Temperature Ranges. Advanced Sustainable Systems 2, 1700171 (2018).

7.	Chen, M., et al. Development and Investigation of a NASICON-Type High-Voltage Cathode Material for High-Power Sodium-Ion Batteries. Angew. Chem. Int. Ed. 59, 2449-2456 (2020).

8.	Chen, M., et al. NASICON-type air-stable and all-climate cathode for sodium-ion batteries with low cost and high-power density. Nat. Commun. 10, 1480 (2019).

9.	Zhang, J., et al. A Novel NASICON-Type Na4MnCr(PO4)3 Demonstrating the Energy Density Record of Phosphate Cathodes for Sodium-Ion Batteries. Adv. Mater. 32, 1906348 (2020).

10.	Rui, X., et al. A Low-Temperature Sodium-Ion Full Battery: Superb Kinetics and Cycling Stability. Adv. Funct. Mater. 31, 2009458 (2021).

11.	Cao, Y., et al. Highly Stable Na3Fe2(PO4)3@Hard Carbon Sodium-Ion Full Cell for Low-Cost Energy Storage. ACS Sustainable Chemistry & Engineering 8, 1380-1387 (2020).

12.	Liang, L., et al. Construction and Operating Mechanism of High-Rate Mo-Doped Na3V2(PO4)3@C Nanowires toward Practicable Wide-Temperature-Tolerance Na-Ion and Hybrid Li/Na-Ion Batteries. Adv. Energy Mater. n/a, 2100287

13.	Liu, T., et al. All-climate sodium ion batteries based on the NASICON electrode materials. Nano Energy 30, 756-761 (2016).

14.	You, Y., et al. Subzero-Temperature Cathode for a Sodium-Ion Battery. Adv. Mater. 28, 7243-7248 (2016).

15.	Hwang, J.-Y., et al. Radially aligned hierarchical columnar structure as a cathode material for high energy density sodium-ion batteries. Nat. Commun. 6, 6865 (2015).

16.	Yang, Q., et al. Advanced P2-Na2/3Ni1/3Mn7/12Fe1/12O2 Cathode Material with Suppressed P2–O2 Phase Transition toward High-Performance Sodium-Ion Battery. Acs Appl. Mater. Inter 10, 34272-34282 (2018).

17.	Li, Y., et al. Construction nasicon-type NaTi2(PO4)3 nanoshell on the surface of P2-type Na0.67Co0.2Mn0.8O2 cathode for superior room/low-temperature sodium storage. Chem. Eng. J. 402, 126181 (2020).

18.	Wang, X., et al. Rational design of Na0.67Ni0.2Co0.2Mn0.6O2 microsphere cathode material for stable and low temperature sodium ion storage. Chem. Eng. J. 428, 130990 (2022).