Supporting Information

7-O-(o-CF3-benzyl)-fangchinoline-loaded solid lipid nanoparticles with improved anti-lung cancer activity in vivo and in vitro

Xu-tao Lv1,2, Yu-kai Zhang1, Mu-xuan Wang2, Jia-shu Chen1, Xu Guo2, Qing Wang2, Ying-ying Chen2, Jin-yue Sun2*, Ning-yang Li3*, Yu-fa Liu1*and Chao Liu2*

1College of Chemistry, Chemical Engineering and Materials Science, Collaborative Innovation Center of Functionalized Probes for Chemical Imaging in Universities of Shandong, Key Laboratory of Molecular and Nano Probes, Ministry of Education, Shandong Provincial Key Laboratory of Clean Production of Fine Chemicals, Shandong Normal University, 88 East Wenhua Road, Jinan 250014, PR China;

2Key Laboratory of Novel Food Resources Processing, Ministry of Agriculture and Rural Affairs/Key Laboratory of Agro-Products Processing Technology of Shandong Province/Institute of Agro-Food Science and Technology, Shandong Academy of Agricultural Sciences, 202 Gongye North Road, Jinan 250100, PR China;

3College of Food Science and Engineering, Shandong Agricultural University, Tai'an, 271018, PR China

*Co-authors E-mail: liuchao555@126.com (Chao Liu), moon_s731@hotmail.com (Jin-yue Sun), liuyufa@sdnu.edu.cn (Yu-fa Liu), liny@sdau.edu.cn (Ning-yang Li)

Supporting document 1

Fig. S1 (a) Synthesis of 7-O-(o-CF3-benzyl)-Fan, reagent condition a: 2-CF3-benzyl bromide, NaH, DMF, low temperature magnetic stirring.

(b) 1H-NMR of 7-O-(o-CF3-benzyl)-Fan

(c) 13C-NMR of 7-O-(o-CF3-benzyl)-Fan

(d) HR-MS of 7-O-(o-CF3-benzyl)-Fan

Supporting document 2

Table S1. Single factor optimization process

| Solution type | stearic acid (mg) | soyabean lecithin (mg) | Drug (mg) | tween-80 (mL) | particle size (nm) | Zeta (-mV) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 80 | 10 | 10 | 0.16 | 156.1 | 8.19 |
| 2 | 80 | 10 | 15 | 0.16 | 151.4 | 8.61 |
| 3 | 80 | 10 | 50 | 0.16 | 736.8 | 6.90 |
| 4 | 80 | 10 | 10 | 0.08 | 142.2 | 6.39 |
| 5 | 80 | 10 | 15 | 0.08 | 207.2 | 8.74 |
| 6 | 100 | 10 | 10 | 0.08 | 132.6 | 6.45 |
| 7 | 100 | 10 | 15 | 0.08 | 238.3 | 0.39 |
| 8 | 150 | 10 | 10 | 0.16 | 37.7 | 16.8 |
| 9a | 150 | 10 | 10 | 0.08 | 45.3 ± 4.8 | 21.6 ± 2.4 |

a Under this condition, the experiment was repeated three times independently, and the results showed that the particle size of 7-O-(o-CF3-benzyl)-Fan-SLN was stable at 45.3 nm and the Zeta potential was stable at -21.6 mV.

Supporting document 3

Table S2-1. Standard curve of 7-O-(o-CF3-Benzyl)-Fan

| concentration（µg/mL） | 10 | 20 | 50 | 80 | 100 |
| --- | --- | --- | --- | --- | --- |
| peak area | 686.9 | 1628.3 | 4894.2 | 7826.8 | 9666.4 |

Standard curve of 7-O-(o-CF3-Benzyl)-Fan

Table S2-2. Standard curve precision test result

| Number of parallel | Peak area | RSD（%） |
| --- | --- | --- |
| 1 | 668.3 | 1.7 a |
| 2 | 676.5 |  |
| 3 | 695.7 |  |
| 4 | 688.4 |  |
| 5 | 696.1 |  |
| 6 | 676.3 |  |

a The relative standard deviation (RSD) of precision is less than 2%, indicating that the precision of the experiment meets the requirements.