Supporting Information

Scalable Synthesis of Iron Oxide–Based Composite Films as Freestanding Negative Electrodes with Ultra-High Areal Capacitances for High-Performance Asymmetric Supercapacitors

Jincy Parayangattil Jyothibasua, Ruei-Hong Wanga, Kenneth Ongb, Juping Hillary Lin Ongb, and Rong-Ho Lee*a

a Department of Chemical Engineering, National Chung Hsing University, Taichung 402, Taiwan

b WALT Taiwan Co., Ltd., Changhua County 51244, Taiwan.

* To whom all correspondence should be addressed.

Tel.: 886-4-22854308; Fax: 886-4-22854734

E-mail: rhl@nchu.edu.tw

(a)

C

O

Fe

(b)

(c)

(d)

Fig. S1 (a) Low-magnification SEM image of the CCF-a composite and (b–d) corresponding EDX mapping patterns for (b) C, (c) O, and (d) Fe elements.

Fig. S2 CV curves, recorded at scan rates from 1 to 30 mV s–1, of the (a) CC, (b) CCF-b, and (c) CF freestanding electrodes.

Fig. S3 (a, b) GCD curves, recorded at current densities from 2 to 6 mA cm–2, of the (a) CC and (b) CCF-b freestanding electrodes. (c) GCD curves, recorded at current densities from 0.4 to 0.8 mA cm–2, of the CF freestanding electrode.

Table S1 Capacitive performances of iron oxide–based negative electrodes reported previously in the literature and in this present study

| Electrode materials | Preparation method | Electrolyte | Mass loading of active materials (mg cm–2) | Specific capacitance of electrode (Cs) | Cycle life (%) | Reference |
| --- | --- | --- | --- | --- | --- | --- |
| CCF-b freestanding electrode | One-step chemical co-precipitation (room temperature, 1 h) | 1 M Na2SO4 | 69.5 (Fe2O3) 77.3 (CNT + Fe2O3) | 9107.16 mF cm–2 (314 mF cm-3) at a current density of 2 mA cm–2 | 90.32% after 10,000 cycles | This study |
| Fe2O3 nanoplates coated on CC | Molten salt method (380 °C) | 6 M KOH | 3.33 | 4175.7 mF cm–2 | 95% after 10,000 cycles | 1 |
| α-Fe2O3/PANi/CNT hydrogel | Hydrothermal method (95 °C, 4 h) and post-sintering (550 °C, 2 h) for the preparation of α-Fe2O3 | 1 M Na2SO4 | 9.3 | 2434.7 mF cm–2 (261.8 F g–1) | 96.3% after 10,000 cycles | 2 |
| FNCs/CNTs-C | In situ growth technique (80 °C), followed by a post-heat treatment process (800 °C, 2 h) | 6 M KOH | 5 | 1687 mF cm–2 at 2 mA cm–2 | 95.8% after 20,000 cycles | 3 |
| Fe2O3/graphene oxide paper | Hydrothermal method (120 °C, 6 h) and post-annealing (300 °C) | – | 1.2 | 3.08 F cm–2 at 5 mA cm–2 | 95% after 5000 cycles | 4 |
| Fe2O3 nanospheres anchored on activated carbon cloth | One-step hydrothermal method (190 °C, 48 h) | 3M LiNO3 | 1.87 | 2775 mF cm–2 | 92% after 10,000 cycles | 5 |
| α-Fe2O3@MnCo2O4 composite | Hydrothermal method (200 °C, 6 h) and post-annealing (400 °C, 2 h) | 1 M KOH | – | 1073 mF cm–2 at 1 mA cm–2 | 77.8% after 6000 cycles | 6 |
| α-Fe2O3@Co3O4 composite | Hydrothermal method (200 °C, 6 h) and post-annealing (400 °C, 2 h) | 1 M KOH | – | 490 mF cm–2 at 1 mA cm–2 | 74.6% after 6000 cycles | 6 |
| Tetsubo-like α-Fe2O3/C nanoarrays | Sacrificial template-accelerated hydrolysis method to grow α‐Fe2O3 and post-annealing (400 °C, 30 min) | 1 M Na2SO4 | 1.1 | 430.8 mF cm–2 (391.8 F g–1) at 1 mA cm–2 | 91.8% after 4000 cycles | 7 |
| Oxygen-deficient α-Fe2O3 nanorods | Hydrothermal method (95 °C, 6 h) followed by thermal annealing (400 °C, 1 h) | 3 M LiCl | 4.3 | 382.7 mF cm–2 (equal to 89 F g–1 and 9.5 F cm–3) at 0.5 mA cm–2 | 95.2% after 10,000 cycles | 8 |
| Hierarchical Tectorum-like α-Fe2O3/PPy nanoarrays | ZnO nanoarrays obtained via a hydrothermal method (85 °C, 24 h) used as sacrificial templates for α-Fe2O3 followed by thermal annealing (550 °C, 5 h) | 1 M Na2SO4 | 0.81 | 382.4 mF cm–2 at 0.5 mA cm–2 | 97.2% after 5000 cycles | 9 |
| Fe2O3/ RGO/Fe3O4 nanocomposite | One-step hydrothermal growth (150 °C, 12 h) | 2 M KOH | 4.3 | 337.5 mF cm–2, 78.49 F g–1 at 20 mA cm–2 | 95% after 5000 cycles | 10 |
| CNT film/double-sided carbon tape/CNT film@Fe2O3 | Hydrothermal method (150 °C, 6 h) | 0.1 M Na2SO4 | 5.0 | 339.1 mF cm–2 at 1 mA cm–2 | – | 11 |
| Hematite nanocrystal–carbon cloth composite | Hydrothermal method | 1 M Na2SO4 | 0.9–1.0 | 1.66 F cm–2 at a current density of 2 mA cm–2 | 88.6% retention after 5000 cycles | 12 |
| Ti-doped Fe2O3@PEDOT core/shell | Hydrothermal treatment (120 °C, 1 h) and sintering (300 °C, 1 h) | 5 M LiCl | – | 1.15 F cm–2 (311.6 F g–1, 28.8 F cm–3) at 1 mA cm–2 | 96.1% after 30,000 cycles | 13 |
| Fe2O3 nanoparticle clusters/rGO paper | Hydrothermal synthesis (195 °C, 12 h) and thermal treatment (150 °C, 30 min) | 3 M KOH | 1.2 g cm–3 | 178.3 F cm–3 at 1 mV s–1 | – | 14 |
| Metal-like fluorine-doped β-FeOOH nanorods | Hydrothermal synthesis (120 °C, 5 h) and post-annealing treatment (400 °C, 2 h) | 6 M KOH | 0.90–1.00 | 1.12 F cm–2 at a current density of 1 mA cm–2 | – | 15 |
| SiC NWs@Fe2O3 NNAs) | Hydrothermal route (120 °C, 8 h) followed by annealing treatment (450 °C, 2 h) | 2 M KOH | 1.4 | 1 F cm–2 at 2.8 mA cm–2 | – | 16 |
| Plasma activated Fe2O3 nanorods on CC | Hydrothermal reaction (120 °C, 6 h), post thermal annealing (450 °C, 3 h), and plasma activation (300 °C, 1 h) | 1 M Na2SO4 | - | 340 mF cm−2(369 F g−1) at 1 mA cm−2 | 83% after 5000 cycles | 17 |
| GF-CNT@ Fe2O3 electrode | CVD method (750 °C) to construct GF-CNT and anatomic layer deposition (165 °C) to coat crystalline Fe2O3 | 2 M KOH | – | 470.5 mF cm–2 at 20 mA cm–2 | 111.2% after 50,000 cycles | 18 |
| Fe2O3 nanotubes grown on carbon fabric | Sacrificial template-accelerated hydrolysis and post-annealing (400 °C, 2 h) | 5 M LiCl | 0.71 | 180.4 mF cm–2 at 1 mA cm–2 | – | 19 |
| Binder-free hematite NF electrode | Hydrothermal method (95 °C, 6 h) followed by annealing (550 °C, 1 h) | 3 M LiCl | 1.5 | 145.9 mF cm–2 (100.6 F g–1) at 1 mA cm–2 | 87.2% after 5000 cycles | 20 |
| α-Fe2O3@PANI core–shell nanowire arrays | Electrodeposition (40 min) and calcination (500 °C, 2 h) | 1 M Na2SO4 | – | 103 mF cm–2 at 0.86 mA cm–2 | 100% after 2500 cycles | 21 |
| Ni/GF/Fe2O3 | Hydrothermal synthesis (120 °C, 6 h) and post-annealing treatment (400 °C, 1 h) | 3 M KOH | – | 572 mF cm–2 at 1 mA cm–2 | 94.1% after 3000 cycles | 22 |
| Fe2O3-δ crystalline core/amorphous shell heterostructure | Hydrothermal synthesis (120 °C, 6 h) and post-annealing treatment (400 °C, 1 h) | 1 M LiOH | 1.3 | 701 F g–1 (701 mF cm–2) at 1 A g–1 | 90% after 5000 cycles | 23 |

Table S2 Capacitive performances of asymmetric supercapacitor devices reported previously in the literature and in this present study

| Material | Electrolyte | Voltage window | Areal (volumetric)capacitance | Energy density | Power density | Reference |
| --- | --- | --- | --- | --- | --- | --- |
| CCM//CCF-b | 1 M Na2SO4 | 1.8 V | 2907.1 mF cm–2 (26.4 F cm–3) | 1.31 mW h cm–2 (11.9 mW h cm–3) | 274.4 mW cm–2 (2.5 W h cm–3) | This work |
| Mn3O4@CC//Fe2O3@CC | 6 M KOH | 2.0 V | 1047.9 mF cm–2 | 2.91 mW h cm–3 | 278 mW cm–3 | 1 |
| ## RuO2//Fe2O3 | CMC/Na2SO4 | 1.5 V | 4.9 F cm–3 | 1.5 mW h cm–3 | 9.1 mW h cm–3 | 24 |
| TNT@α-Fe2O3//AC | 1 M KCl | 1.4 V | 142.86 mF cm–2 | 38.88 µW h cm–2 | 1.9 mW h cm–2 | 25 |
| CDC@MnO2//CDC@ Fe2O3 | PVA/LiClO4 | 2.1 V | 6.8 F cm–3 | 4.1 mW h cm–3 | 22.3 mW cm–3 | 11 |
| MnO2//Fe2O3 | PVA/LiCl | 1.6 V | – | 0.55 mW h cm–3 | 139.1 mW cm–3 | 19 |
| Fe2O3-P//MnO2 | 1 M Na2SO4 | 1.6 V | - | 0.42 mWh/cm3 | 258.1 W cm−3 | 17 |
| MnO2// Fe2O3/PPy- | PVA/LiCl | 1.6 V | 835.5 mF cm–3 | 0.22 mW h cm–2 | 165.6 mW cm–3 | 9 |
| Fe3O4@Fe2O 3//Fe3O4 @MnO2 | 1 M Na2SO4 | 2 V | 1.49 F cm–3 | 0.83 mW h cm–3 | 500 mW cm–3 | 26 |
| ASC MG/FG-t2 | 3 M KOH | 1.8 V | – | 0.056 W h cm–3 | 6.21 W cm–3 | 14 |
| α-Fe2O3 @PANI//PANI | 1 M Na2SO4 | 1.5 V | 2.02 mF cm–3 | 0.35 mW h cm–3 | 120.51 mW cm–3 | 21 |
| α-Fe2O3/C//α - Fe2O3/MnOx | 1 M Na2SO4 | 2.0 V | 1.28 F cm–3 | 0.64 mW h cm–3 | 155 mW cm–3 | 27 |
| Co3O4/GN/BC// r‐Bi2O3/GN/BC | 6 M KOH | 1.6 V | – | 0.449 mW h cm–2 (7.74 mW h cm–3) | 40 mW cm–2 (690 mW cm–3) | 28 |
| PANi gel//α- Fe2O3/PANi | PVA/LiCl | 1.8 V | 1.5 C cm–3 | 0.31 mW h cm–3 | 67.1 mW cm–3 | 29 |
| MnO2//Fe2O3 | PVA/LiCl | 1.6 V | 1.21 F cm–3 | 0.41 mW h cm–3 | 0.1 W cm–3 at 6 mA cm–2 | 8 |
| MnO2//α- Fe2O3/C | 1 M Na2SO4 | 2.0 V | 78.2 mF cm–2 (1.15 F cm–3) | 0.64 mW h cm–3 | 248.4 mW cm–3 | 7 |
| MnO2 //MXene@ Fe2O3 | PVA/LiCl | 1.8 V | 143.4 mF cm–2 | 1.61 mW h cm–3 | 495.6 mW cm –3 | 30 |
| MnO2//Ti-Fe2O3@PEDOT | PVA/LiCl | 1.6 V | 2.40 F cm–3 | 0.89 mW h cm–3 | 0.44 W cm–3 | 13 |
| Ni/GF/H-CoMoO4//Ni/GF/H-Fe2O3 | PVA/KOH | 1.5 | 3.6 F cm–3 | 1.13 mW h cm–3 | 150 mW cm–3 | 22 |

References

1.	Y. J. Gu, W. Wen, S. Zheng and J.-M. Wu, Mater. Chem. Front. 2020, 4, 2744-2753.

2.	Z. Yang, A. Qiu, J. Ma and M. Chen, Compos Sci Technol. 2018, 156, 231-237.

3.	R. Wang, S. Cai, Y. Yan, W. M. Yourey, W. Tong and H. Tang, J. Mater. Chem. A 2017, 5, 22648-22653.

4.	S. Xie, M. Zhang, P. Liu, S. Wang, S. Liu, H. Feng, H. Zheng and F. Cheng, Mater. Res. Bull. 2017, 96, 413-418.

5.	J. Li, Y. Wang, W. Xu, Y. Wang, B. Zhang, S. Luo, X. Zhou, C. Zhang, X. Gu and C. Hu, Nano Energy 2019, 57, 379-387.

6.	X. Zheng, Z. Han, F. Chai, F. Qu, H. Xia and X. Wu, Dalton Trans. 2016, 45, 12862-12870.

7.	D. Chen, S. Zhou, H. Quan, R. Zou, W. Gao, X. Luo and L. Guo, Chem. Eng. J. 2018, 341, 102-111.

8.	X. Lu, Y. Zeng, M. Yu, T. Zhai, C. Liang, S. Xie, M. S. Balogun and Y. Tong, Adv. Mater. 2014, 26, 3148-3155.

9.	L. Wang, H. Yang, X. Liu, R. Zeng, M. Li, Y. Huang and X. Hu, Angew. Chem. Int. Ed. 2017, 56, 1105-1110.

10.	C. Zhao, X. Shao, Y. Zhang and X. Qian, ACS Appl. Mater. Interfaces 2016, 8, 30133-30142.

11.	Y. Zhang, X. Yuan, W. Lu, Y. Yan, J. Zhu and T. W. Chou, Chem. Eng. J. 2019, 368, 525-532.

12.	S. Peng, L. Yu, B. Lan, M. Sun, G. Cheng, S. Liao, H. Cao and Y. Deng, Nanotechnology 2016, 27, 505404.

13.	Y. Zeng, Y. Han, Y. Zhao, Y. Zeng, M. Yu, Y. Liu, H. Tang, Y. Tong and X. Lu, Adv. Energy Mater. 2015, 5, 1402176.

14.	Y. Hu, C. Guan, Q. Ke, Z. F. Yow, C. Cheng and J. Wang, Chem. Mater. 2016, 28, 7296-7303.

15.	L. F. Chen, Z. Y. Yu, J. J. Wang, Q. X. Li, Z. Q. Tan, Y. W. Zhu and S. H. Yu, Nano Energy, 2015, 11, 119-128.

16.	J. Zhao, Z. Li, X. Yuan, Z. Yang, M. Zhang, A. Meng and Q. Li, Adv. Energy Mater. 2018, 8, 1702787.

17.	H. Liang, C. Xia, A.-H. Emwas, D. H. Anjum, X. Miao and H. N. Alshareef, Nano Energy 2018, 49, 155-162.

18.	C. Guan, J. Liu, Y. Wang, L. Mao, Z. Fan, Z. Shen, H. Zhang and J. Wang, ACS Nano 2015, 9, 5198-5207.

19.	P. Yang, Y. Ding, Z. Lin, Z. Chen, Y. Li, P. Qiang, M. Ebrahimi, W. Mai, C. P. Wong and Z. L. Wang, Nano Lett., 2014, 14, 731-736.

20.	T. Liu, Y. Ling, Y. Yang, L. Finn, E. Collazo, T. Zhai, Y. Tong and Y. Li, Nano Energy 2015, 12, 169-177.

21.	X. F. Lu, X. Y. Chen, W. Zhou, Y. X. Tong and G. R. Li, ACS Appl. Mater. Interfaces, 2015, 7, 14843-14850.

22.	K. Chi, Z. Zhang, Q. Lv, C. Xie, J. Xiao, F. Xiao and S. Wang, ACS Appl. Mater. Interfaces 2017, 9, 6044-6053.

23.	S. Sun, T. Zhai, C. Liang, S. V. Savilov and H. Xia, Nano Energy 2018, 45, 390-397.

24.	Q. Wang, X. Liang, Y. Ma and D. Zhang, Dalton Trans. 2018, 47, 7747-7753.

25.	S. T. Manikkoth, K. M. Thulasi, A. Paravannoor, S. Palantavida, M. Bhagiyalakshmi and B. K. Vijayan, Nano-Struct. Nano-Objects 2020, 24, 100543.

26.	X. Tang, R. Jia, T. Zhai and H. Xia, ACS Appl. Mater. Interfaces 2015, 7, 27518-27525.

27.	D. Sarkar, S. Pal, S. Mandal, A. Shukla and D. D. Sarma, J. Electrochem. Soc. 2017, 164, A2707-A2715.

28.	R. Liu, L. Ma, G. Niu, X. Li, E. Li, Y. Bai and G. Yuan, Adv. Funct. Mater. 2017, 27, 1701635.

29.	Z. Yang, L. Tang, J. Ye, D. Shi, S. Liu and M. Chen, Electrochim. Acta 2018, 269, 21-29.

30.	F. Li, Y. L. Liu, G. G. Wang, H. Y. Zhang, B. Zhang, G. Z. Li, Z. P. Wu, L. Y. Dang and J. C. Han, J. Mater. Chem. A 2019, 7, 22631-22641.