Supporting information

Study on the synergistic effect of TPF phenolic curing agent and OMMT on the cured multifunctional epoxy grafted by SAP

Zhuhuan Chen  Shijie Zhang  Ruobing Yu

a School of Materials Science and Engineering, East China University of Science and Technology, Meilong Road 130#, Xuhui District, Shanghai 200237, China

* Email address: rbyu@ecust.edu.cn

Content

Table S1.  Formulation for preparation of TASx and TAS10My

Figure S1.  SEM image of impact fracture surface of the cured (a) TAS10M5, (b) TAS10M10 and (c) TAS10M15

Figure S2.  Spline and solution changes of composite materials soaked in 98% H2SO4 and 25% NaOH for 7 days

Table S1  Formulation for preparation of TASx and TAS10My

| Systems | SAP/g | AFG-90H/g | TPF/g | 2,4-EMI/g | OMMT/g |
| --- | --- | --- | --- | --- | --- |
| TAS0 | 0 | 100 | 27.2 | 0.5 | / |
| TAS5 | 5 | 95 | 25.8 | 0.5 | / |
| TAS10 | 10 | 90 | 24.5 | 0.5 | / |
| TAS15 | 15 | 85 | 23.1 | 0.5 | / |
| TAS20 | 20 | 80 | 21.7 | 0.5 | / |
| TAS10M5 | 10 | 90 | 24.5 | 0.5 | 5 |
| TAS10M10 | 10 | 90 | 24.5 | 0.5 | 10 |
| TAS10M15 | 10 | 90 | 24.5 | 0.5 | 15 |

Figure S1.  SEM image of impact fracture surface of the cured (a) TAS10M5, (b) TAS10M10 and (c) TAS10M15

Figure S2.  Spline and solution changes of composite materials soaked in 98% H2SO4 and 25% NaOH for 7 days