Achieving ultrahigh power factor in n-type Ag2Se thin films by carrier engineering

Zhuang-hao ZHENG1, Jun-yu NIU1, Tian-bao CHEN1, 2, Yue-Xing CHEN1, *, Fu LI1, Jing-ting LUO1, Guang-xing LIANG1, Shuo CHEN1, Hong-li MA2, Xiang-hua ZHANG2, Ping FAN1

1Shenzhen Key Laboratory of Advanced Thin Films and Applications, Key Laboratory of Optoelectronic Devices and Systems of Ministry of Education and Guangdong Province, College of Physics and Optoelectronic Engineering, Shenzhen University, Shenzhen 518060, P. R. China.

2 Univ Rennes, CNRS, ISCR (Institut des Sciences Chimiques de Rennes) UMR6226, Rennes F-35000, France.

* Corresponding Author, Email: chenyx@szu.edu.cn

Supporting information

Fig. S1. Surface morphology of the Ag2Se based thin films with different Ag to Se atomic ratio

Fig. S2. SEM shows morphology of Ag2.05Se with different annealing temperature (a-f: 393K,423K,453K,483K,513K,543K) contains the chemical deviation due to heat treatment at high temperature.

Fig. S3. Section morphology and element distribution of Ag2.05Se after annealed at 493 K.

Fig. S5. The temperature dependence of X-ray peaks corresponding to Ag2Se thin film

Fig. S5. plot of ln[(Rmax-Rmin)/(R-Rmin)] versus energy used to obtain direct band gap. This shows the heat treatment reduces Ag vacancies.

Table S1. Compositions of the Ag2.05Se thin films with different annealing temperature.

| Annealing temperature (K) | 303 | 393 | 423 | 453 | 483 | 513 | 543 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Ag（at%) | 67.2 | 67.3 | 67.6 | 67.6 | 68.1 | 68.8 | 69.1 |
| Se（at%) | 32.8 | 32.7 | 32.4 | 32.4 | 31.9 | 31.2 | 30.9 |